Malaysian Journal of Analytical Sciences Vol 19 No 4 (2015): 649 - 657

PHOTODEGRADATION OF REACTIVE GOLDEN YELLOW R DYE CATALYZED BY EFFECTIVE TITANIA (TiO2)

(Fotodegradasi Pewarna Reactive Golden Yellow R Dimangkinkan oleh Titania (TiO2) yang Efektif )

Edmand Andrew Bedurus1*, Marinah Mohd Ariffin1, Mohd Hasmizam Razali2

1School of Marine and Environmental Sciences,

2School of Fundamental Sciences,

Universiti Malaysia Terengganu, 21030 Kuala Terengganu, Terengganu

*Corresponding author: edmand_andrew@yahoo.com

Received: 8 February 2015; Accepted: 11 June 2015

Abstract

In the present research, Microwave Assisted Synthesis (MAS) method was applied to synthesize titania (TiO2) at 150 oC in a range of 2-6 hours heating time. Each prepared TiO2 were characterized by scanning electron microscopy (SEM), X-ray diffraction (XRD) and nitrogen gas (N2) sorption analysis (Brunaeur-Emmett-Teller (BET) and Barrett-Joyner-Halenda (BJH) calculation) techniques. The TiO2 prepared by MAS 150 oC (4 hours) has emerged with the highest photocatalytic activity. Within 4 hours, the TiO2 managed to catalyze the degradation of Reactive Golden Yellow R dye up to 98.51 %. This is because of the TiO2 possessed high crystallinity of anatase phase, small crystallite size and high pore volume compared to other prepared TiO2.

Keywords: Titania (TiO2), Microwave Assisted Synthesis (MAS), Reactive Golden Yellow R dye, photo-degradation

Abstrak

Dalam kajian ini, kaedah Sintesis Bantuan Gelombang Mikro (MAS) telah digunakan untuk mensintesis titania (TiO2) pada suhu 150 oC dalam tempoh masa pemanasan 2 ke 6 jam. Setiap TiO2 yang disintesis telah dicirikan menggunakan teknik Mikroskopi Imbasan Elektron (SEM), Pembelauan Sinar-X (XRD), dan analisis serapan gas nitrogen (pengiraan menggunakan formula Brunaeur-Emmett-Teller (BET) dan Barrett-Joyner-Halenda (BJH)). TiO2 yang disintesis dengan kaedah MAS pada suhu 150 oC (4 jam) mempunyai aktiviti fotokatalitik yang tertinggi. Dalam masa 4 jam, TiO2 tersebut telah berjaya memangkinkan degradasi pewarna Reactive Golden Yellow R sebanyak 98.51 %. Hal ini adalah disebabkan oleh TiO2 tersebut mempunyai fasa hablur anatase yang tinggi, saiz hablur yang kecil dan isipadu liang yang tinggi berbanding dengan TiO2 yang lain.

Kata kunci: Titania (TiO2), Sintesis Bantuan Gelombang Mikro (MAS), Pewarna Reactive Golden Yellow R, fotodegradasi

References

- Boulamanti, A. K. & Philippopoulos, C. J. 2008. Photocatalytic degradation of methyl tert-butyl ether in the gas-phase: A kinetic study. Journal of Hazardous Materials 160: 83-87.

- Sharma, S. D., Saini, K. K., Kant, C., Sharma, C. P. & Jain, S. C. 2008. Photodegradation of dye pollutant under UV light by nano-catalyst doped titania thin films. Applied Catalysis B: Environmental 84: 233-240.

- Kim, S. & Ehrman, S. H. 2009. Photocatalytic activity of a surface-modified anatase and rutile titania nanoparticle mixture. Journal of Colloid and Interface Science 338(1): 304-307.

- Hao, H. & Zhang, J. 2009. Low temperature synthesis of crystalline mesoporoustitania with high photocatalytic activity by post-treatment in nitric acid ethanol solution. Material Letters 63: 106-108.

- Moctezuma, E., Leyva, E., Monreal, E., Villegas, N. & Infante, D. 1999. Photocatalytic degradation of the herbicide “Paraquat”.Chemosphere 39 (3): 511-517.

- Jang, S.-J., Kim, M.-S. & Kim, B.-W. 2005. Photodegradation of DDT with the photodeposited ferric ion on the TiO2 film. Water Research 39: 2178-2188.

- Parra, S., Stanca, S. E., Guasaquillo, I. & Thampi, K. R. 2004. Photocatalytic degradation of atrazine using suspended and supported TiO2. Applied Catalysis B: Environmental 51: 107-116.

- Chen, C. C., Lu, C. S., Chung, Y. C. & Jan, J. L. 2007. UV light induced photodegradation of malachite green on TiO2 nanoparticles. Journal of Hazardous Materials 141: 520-528.

- Wu, J.-M. & Zhang, T.-W. 2004. Photodegradation of rhodamine B in water assisted by titania films prepared through a novel procedure. Journal of Photochemistry and Photobiology A: Chemistry 162: 171-177.

- Wilhelm, P. & Stephan, D. 2006. Photodegradation of Rhodamine B in aqueous solution via SiO2@TiO2 nano-spheres. Journal of Photochemistry and Photobiology A: Chemistry 185(1): 19-25.

- Zhang, G., Wu, J., Liu, S. & Yan, M. 2008. Fabrication of titania thin film with composite nanostructure and its ability to photodegrade Rhodamine B in water. Frontier Chemical Engineering China. 2 (1): 44-48.

- Oh, H.-J., Lee, J.-H., Kim, Y.-J., Suh, S.-J., Lee, J.-H. & Chi, C.-S. 2008. Synthesis of effective titania nanotubes for wastewater purification. Applied Catalysis B: Environmental. 84: 142-147.

- Yi, X., Liqin, D., Lizhen, A., Shiying, B. & Zhibin, L. 2008. Photocatalytic degradation of Rhodamine B and phenol by TiO2 loaded on mesoporous graphitic carbon. Chinese Journal of Catalysis. 29 (1): 31-36.

- Tsui, K. C. K., 2007. Dye coated titania photocatalysts operating in the visible. MSc. thesis.The University of Calgary.

- Zhang, F., Yediler, A., Liang, X. & Kettrup, A. 2004. Effects of dye additives on the ozonation process and oxidation by-products: a comparative study using hydrolyzed C.I. Reactive Red 120. Dyes and Pigments 60: 1-7.

- Ribbens, S., Meynen, V., Tendeloo, G. V., Ke, X., Mertens, M., Maes, B. U. W., Cool, P. & Vansant, E. F. 2008. Development of photocatalytic efficient Ti-based nanotubes and nanoribbons by conventional and microwave assisted synthesis strategies. Microporous and Mesoporous Materials. 114: 401-409.

- Rao, C. N. R., Müller, A. & Cheetam, A. K. 2004. Microwave heating. In The Chemistry of Nanomaterials: Synthesis, Properties and Applications, Vol. 1, pp 152-155. Weinheim: WILEY-VCH Verlag GmbH & Co. KGaA.

- Wu, X., Jiang, Q.-Z., Ma, Z.-F., Fu, M. & Shangguan W.-F. 2005. Synthesis of titania nanotubes by microwave irradiation. Solid State Communications. 136: 513-517.

- Asiltürk, M., Sayılkan, F., Erdemoğlu, S., Akarsu, M., Sayılkan, H., Erdemoğlu, M. & Arpaç, E. 2006. Characterization of the hydrothermally synthesized nano-TiO2 crystallite and the photocatalytic degradation of Rhodamine B. Journal of Hazardous Materials. B129: 164-170.

- Sing, K.S.W., Everett, D.H., Haul, R.A.W., Moscou, L., Pierotti, R.A., Rouquérol, J. and Siemieniewska, T. (1985). Reporting physisorption data for gas/solid systems with special reference to the determination of surface area and porosity (Recommendations 1984). Pure and Applied Chemistry 57: 603-619.