Malaysian Journal of Analytical Sciences Vol 19 No 4 (2015): 760 - 765

OPTICAL BEHAVIOR OF NH4I DOPED CELLULOSE ACETATE MEMBRANE FOR DYE SENSITIZED SOLAR CELL

# (Pelakuan Optikal Selulosa Asetat Membran yang Didopkan NH4I untuk

# Pewarna Sensitif Solar Sel)

Noor Syafiqah Samsi1, Rosnah Zakaria1, Oskar Hasdinor Hassan2, Muhd Zu Azhan Yahya3,

Ab Malik Marwan Ali1,2*

1Faculty of Applied Sciences,

2 iMADE, Institute of Science,

Universiti Teknologi MARA, 40450 Shah Alam, Selangor, Malaysia

3Universiti Pertahanan Nasional Malaysia, Kem Sungai Besi, 57000 Kuala Lumpur, Malaysia

*Corresponding author: ammali@salam.uitm.edu.my

Received: 23 November 2014; Accepted: 27 June 2015

Abstract

The effect of ammonium iodide (NH4I) on cellulose acetate (CA) membrane based on solid polymer electrolyte was investigated. FTIR analysis showed that the complaxation was taken placed between polymer and salt to form CA-NH4I complexes. Alternating current impedance measurement was carried out in the frequency range between 50 Hz and 1MHz at room at elevated temperature with an applied voltage of 1V. The ionic conductivity increased up to 10-04 Scm-1 with increasing NH4I contents for the CA-NH4I at room temperature. As NH4+ ion concentration increase, the optical band gaps decreased. This suggests that NH4I, as a dopant, is a good choice to improve the electrical properties of cellulose acetate polymer electrolytes.

# Keywords: polymer electrolyte, Dye Sensitized Solar Cell, UV-Vis Spectroscopy

Abstrak

# Kesan ammonium iodida (NH4I) pada selulosa asetat (CA) membran berdasarkan elektrolit polimer pepejal telah disiasat. Analisis FTIR menunjukkan complaxation itu diambil diletakkan di antara polimer dan garam untuk membentuk kompleks CA-NH4I. Seli pengukuran galangan semasa telah dijalankan dalam julat frekuensi di antara 50 Hz dan 1MHz di bilik pada suhu tinggi dengan voltan kenaan 1V. Kekonduksian ionik meningkat sehingga 10-04 SCM-1 dengan meningkatkan kandungan NH4I untuk CA-NH4I pada suhu bilik. Sebagai NH4 + kepekatan ion peningkatan, jurang jalur optik menurun. Ini menunjukkan bahawa NH4I, sebagai pendopan yang, adalah pilihan yang baik untuk meningkatkan ciri-ciri elektrik elektrolit polimer selulosa asetat.

# Kata kunci: polimer elektrolit, Dye sensitif Sel Solar, UV-Vis Spektroskopi

References

- Chaurasia, S. K., Singh, R. K. and S. Chandra, S. (2013) Ion–polymer complexation and ion-pair formation in a polymer electrolyte PEO:LiPF6 containing an ionic liquid having same anion: A Raman study. Vibrational Spectroscopy 68: 190–195.

- Kumar,K. Kiran., Ravi, M., Pavani, Y., Bhavani, S., Sharma, A. K. and Narasimha Rao, V. V. R (2011). Investigations on the effect of complexation of NaF salt with polymer blend (PEO/PVP) electrolytes on ionic conductivity and optical energy band gaps. Physica B: Condensed Matter 406 (9): 1706–1712.

- Kim M., Park S., Kim J. and J. Lee, Dye-Sensitized Solar Cells Based on Polymer Electrolytes. Chapter 10, "Solar Cells - Dye-Sensitized Devices", book edited by Leonid A. Kosyachenko" Intech Publisher.

- Ibrahim, S., Ahmad, R. and Johan, M. R. (2012) Conductivity and optical studies of plasticized solid polymer electrolytes doped with carbon nanotube. Journal of Luminescence 132 (1): 147–152.

- Mahmud, Z. S., Adam, N. I., Zaki, N. H. M., Ali, A. M. M. and Yahya, M. Z. A. (2012).Conductivity and optical studies of plasticized polymer electrolytes based on 49% PMMA-grafted natural rubber,” 2012 IEEE Symposium on Business, Engineering and Industrial Applications 504–508.

- Su’ait,M. S.,  Ahmad, A.,  Hamzah, H. and Rahman,M. Y. A. (2011). Effect of lithium salt concentrations on blended 49% poly(methyl methacrylate) grafted natural rubber and poly(methyl methacrylate) based solid polymer electrolyte. Electrochimica Acta,  57: 123–131

- Harun, N.I., Ali, R. M.,  Ali, A. M. M. and Yahya, M. Z. A. (2013). Effects of Ammonium Tetrafluoroborate on Conductivity and Thermal Studies on Cellulose Acetate Based Polymer Electrolytes.  Advanced Materials Research, 667: 150–154.

- Ali, R. M.,  Harun, N. I.,  Ali, A. M. M. and Yahya, M. Z. A. (2012). Effect of ZnS Dispersoid in Structural and Electrical Properties of Plasticized CA-NH4I. Physics Procedia 25: 293–298.