Malaysian Journal of Analytical Sciences Vol 19 No 6 (2015): 1284 - 1289

ANALYSIS OF THERMOGRAVIMETRIC (TG) AND INFRA-RED (FTIR) ON Dy SUBSTITUTION IN Bi(Pb)-2223 SUPERCONDUCTOR

(Analisis Termogravimetri (TG) dan Infra-Merah (FTIR) ke atas pemasukan Dy dalam Superkonduktor Bi(Pb)-2223)

Siti Hawa Jamil1, Azhan Hashim2*, Syed Yusainee Syed Yahya1, Azman Kasim2, Nurul Hidayah Hasan1,

Norazidah Abdul Wahab1

1Faculty of Applied Sciences,

Universiti Teknologi MARA, 40450 Shah Alam, Selangor, Malaysia

2Faculty of Applied Sciences,

Universiti Teknologi MARA Pahang, 26400 Jengka, Pahang, Malaysia

*Corresponding author: dazhan@pahang.uitm.edu.my

Received: 23 November 2014; Accepted: 3 September 2015

Abstract

In this paper, the results of the thermal and infra-red analysis of Dy substituted in Bi (Pb)-2223 superconductor have been studied by thermogravimetric (TG) and Fourier transform infrared (FTIR). The samples with nominal composition of Bi1.6Pb0.4Sr2Ca2-xDyxCu3Oy where x = 0.000, 0.025, 0.050, 0.100, and 0.200 were prepared by co-precipitation (COP) method using metal acetate as the starting salts. The mechanism of thermal analysis of the precursor powder for each stage (drying, precalcine, and calcine) were studied from 20 °C to 920 °C by 5 °C/min of heating rate. Interestingly, the thermal decomposition proceeds in the almost similar way regardless of the Dy substitution level with five major drops at the drying stage. Based on TG curves results, the temperature range from 840 °C to 850 C can be suggested as an optimum calcination and sintering temperature. The majority of decomposition step which related to the loss of water from oxalate was in the range of 100 °C to 200 C while the formation of precipitation into Bi2O3, PbO, SrCO3, CaCO3, CuO, and Dy2O3 were in the range of 210 °C to 360 C. From the FTIR result, all the precursor powders qualitatively showed four main regions and the existence of –OH group can increase the diffusion rate between metals during the synthesis process.

Keywords: dy-substitution, BSCCO, superconductor, FTIR, thermogravimetric analysis

Abstrak

Dalam laporan ini, keputusan analisa terma dan infra-merah terhadap pemasukan Dy di dalam superkonduktor Bi (Pb)-2223 telah dikaji melalui termogravimetri dan transformasi fourier infra-merah (FTIR). Semua sampel dengan komposisi nominal Bi1.6Pb0.4Sr2Ca2-xDyxCu3Oy dimana x = 0.000, 0.025, 0.050, 0.100 dan 0.200 telah disediakan melalui kaedah ko-pemendakan (COP) dengan menggunakan logam asetat sebagai garam pemula. Mekanisma analis terma terhadap serbuk pelopor untuk setiap peringkat (pengeringan, pra-pengkalsinan dan pengkalsinan) telah dikaji dari suhu 20 C hingga 920 C dengan kadar pemanasan 5C/min. Menariknya, penguraian terma berlaku agak sama tanpa menghiraukan aras pemasukan Dy iaitu dengan lima jatuhan pada peringkat pengeringan. Berdasarkan kepada keputusan keluk TG, dicadangkan bahawa julat suhu dari 840 °C hingga 850 C  merupakan suhu pengkalsinan dan suhu sinteran optimum. Majoriti langkah penguraian yang berhubungkait dengan kehilangan air dari oksalat, berlaku dalam julat 210 °C hingga 360 C manakala pembentukan pemendakan dalam Bi2O3, PbO, SrCO3, CaCO3, CuO, dan Dy2O3 adalah dalam julat 210 °C hingga 360 C. Dari keputusan FTIR, semua serbuk pelopor secara kualitatifnya menunjukkan empat daerah utama dan keujudan kumpulan –OH boleh meningkatkan kadar peresapan antara logam semasa proses sintesis.

Kata kunci: pemasukan Dy, BSCCO, superkonduktor, FTIR, analisis termogravimetri

References

- Hamadneh, I., Halim, S. A. and Lee, C. K.  (2006). Characterization of Bi1.6Pb0.4Sr2Ca2Cu3Oy ceramic superconductor prepared via coprecipitation method at different sintering time. Journal of Materials Science 41:  5526 – 5530.

- Hawa, J. S., Azhan, H., Yahya, S.Y., Azman, K., Hidayah, H. N. and Norazidah, A. W. (2012). Influence of Na, Mg and Yb Substitution for Ca in Bi (Pb)-2223 Superconductor. Advanced Materials Research. 501:  289 – 293.

- Bahmani, A., Sellami, M. and Betthahar, N. (2012). Synthesis of bismuth mixed oxide by thermal decomposition of a coprecipitate precursor. Journal of Thermal Analysis and Calorimetry 107: 955 – 962.

- Wahid, M. H., Zainal, Z., Hamadneh, I., Tan, K. B., Halim, S. A., Rosli, A. M., Alaghbari, E. S., Nazarudin, M. F. and Kadri, E. F. (2012). Phase formation of REBa2Cu3O7−δ (RE: Y0.5Gd0.5, Y0.5Nd0.5, Nd0.5Gd0.5) superconductors from nanopowders synthesised via co-precipitation. Ceramic International 38: 1187 – 1193.

- Popa, M., Calderon-Moreno, J., Crisan, D. and Zaharescu, M. (2000). Study of Fe addition on the thermal decomposition of coprecipitated oxalates for the Bi-based superconductor synthesis. Journal of Thermal Analysis and Calorimetry 62: 633 – 645.

- Nenartaviciene, G., Tõnsuaadu, K., Jasaitis, D., Beganskiene, A. and Kareiva, A. (2007). Preparation and characterization of superconducting YBa2(Cu1−xCrx)4O8 oxides by thermal analysis. Journal of Thermal Analysis and Calorimetry 90: 173 –178.

- Arshad, M., Qureshi, A. H., Masud, K. and Qazi, N. K. (2007). Production of BSCCO bulk high TC superconductors by sol-gel method and their characterization by FTIR and XRD techniques. Journal of Thermal Analysis and Calorimetry 89: 595 – 600.

- Tran T. T., Hoste, S., Herman, G. G., De Buysser, K., Lommens, P., Feys, J. and Vandeput, D.  (2009). Van Driessche, I. Sol–gel chemistry of an aqueous precursor solution for YBCO thin films. Journal of Sol-Gel Science and Technology 52: 124 – 133.