Malaysian Journal of Analytical Sciences Vol 19 No 6 (2015): 1297 - 1302

FABRICATION AND OPTICAL CHARACTERISATION OF RARE EARTH ACTIVE IONS DOPED TELLURITE GLASS SYSTEM

(Fabrikasi dan Pencirian Optik Sistem Kaca Telurit Didopkan Ion–Ion Aktif Nadir Bumi)

Azman Kasim1*, Azhan Hashim1, Syamsyir Akmal Senawi1, Mardhiah Andullah1, Noranizah Awang2,

Nurbaisyatul Ermiza Suhaimi2, Siti Nasuha Mohd Rafien2

1Faculty of Applied Sciences,

Universiti Teknologi MARA Pahang, 26400 Jengka, Pahang, Malaysia

2Faculty of Applied Sciences,

UniverstitiTeknologi MARA, 40540 Shah Alam, Selangor, Malaysia

*Corresponding author: azman615@pahang.uitm.edu.my

Received: 23 November 2014; Accepted: 3 September 2015

Abstract

Five samples of tellurite glasses with the system of (78-x) TeO2-10PbO- 10Li2O-2Nd2O3-xEr2O3 where x = 0.0, 0.5, 1.0, 1.5, 2.0 mol % have been prepared by using the conventional melt-quenching method. In this work, the optical properties by mean of their up-conversion luminescence as well as the optical parameters related to Judd-Ofelt theory were measured. The result reveals that six distinctive up-converted bands contributed from Nd3+ ions are observed to be centered at 485 nm, 605 nm, 665 nm, 880 nm, 1062 nm and 1340 nm attributed from 4G11/2 → 4I11/2, 4G11/2 → 4I15/2 , 4G7/2 → 4I13/2 , 4F3/2 → 4I13/2 , 4F3/2 → 4I11/2 and 4F3/2 → 4I9/2 transitions whereas, three upconverted bands contributed from Er3+ ions to be centered at 493 nm, 524 nm and 550 nm are found originating from 4F7/2 → 4I15/2, 2H11/2 → 4I15/2 and 4S3/2 → 4I15/2 transitions under the excitation at 585 nm. Meanwhile, the optical parameters according to Judd-Ofelt theory such as the radiative lifetime, , stimulated emission cross-section and the non-radiative relaxation,of the glass were found ranging from 0.812ms to 1.248ms, 0.812 x 1020 cm2 to 1.248 x 1020 cm2 and from 0.144 ms-1 to 0.180 ms-1 respectively with respect to mol% of composition . Further analysis and discussion will be elaborated in brief.

Keywords: up-conversion, excitation, Judd-Ofelt, radiative, relaxation

Abstrak

Lima sampel kaca tellurite dengan sistem (78-x) TeO2-10PbO- 10Li2O-2Nd2O3-xEr2O3 dimana x = 0.0, 0.5, 1.0, 1.5, 2.0 mol % telah disedia menggunakan kaedah sepuh-lindap konvensional. Dalam kerja ini, sifat-sifat optikal seperti pendarkilau pertukaran atas serta parameter optikal yang berkaitan dengan teori Judd-Ofelt telah diukur. Keputusan menunjukkan bahawa enam jalur pertukaran atas tersendiri sumbangan dari ion-ion Nd3+ telah dicerap berpusat di   485 nm, 605 nm, 665 nm, 880 nm, 1062 nm dan 1340 nm ditentukan dari transisi 4G11/2 → 4I11/2, 4G11/2 → 4I15/2 , 4G7/2 → 4I13/2 , 4F3/2 → 4I13/2 , 4F3/2 → 4I11/2 and 4F3/2 → 4I9/2 manakala, tiga jalur pertukaran atas adalah sumbangan dari ion-ion Er3+ dijumpai berpusat di 493 nm, 524 nm and 550 nm hasil dari transisi  4F7/2 → 4I15/2, 2H11/2 → 4I15/2 dan 4S3/2 → 4I15/2 di bawah pengujaan 585nm. Sementara itu, parameter optikal merujuk kepada teori Judd-Ofelt seperti jangkahayat radiasi, , keratan rentas penyinaran terangsang,   dan relaksasi tak bersinar, bagi kaca didapati dalam julat masing-masing dari 0.812ms hingga 1.248ms, 0.812 x 1020 cm2 hingga 1.248 x 1020 cm2 dan dari 0.144 ms-1 hingga 0.180 ms-1 terhadap mol% komposisi. Analisa lanjut dan perbincangan akan dihurai dengan lebih lanjut.

Kata kunci: pertukaran-atas, pengujaan, Judd-Ofelt, penyinaran, relaksasi

References

- Kumar, K.U., Prahyusha,V.A., Babu, P., Jayashankar, C.K., Joshi, A.S., Spehgini, A. and Bettinelli, M. (2007). Fluorescence Properties of Nd3+ doped Tellurite Glasses,  Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy  67(3-4): 702 –708.

- Sahar, M. R., Yusoff, N. M., Ghoshal, S. K., Rohani, M. S., Hamzah, K. and Arifin, R. (2012), Luminescence Properties of Magnesium Phosphate Glass Doped samarium,  Advanced Materials Research 501: 111 – 115.

- Azman, K., Razali, W. A. W., Azhan, H. and Sahar, M. R. (2012). Luminescence Spectra of TeO2-PbO-Li2O Doped Nd2O3 Glass, Advanced Materials Research 501: 121 – 125.

- Jalasi, I., Elhouichet, H., Ferid M. (2011). Thermal and Optical Properties of Tellurite Glasses doped Erbium, Journal of Materials Science 46: 806 – 812.

- Ramos, F., Jaque, D., Romero,J., Garcia, S.J., Caldino, U.G. (1999). Optical Spectroscopy of Nd3+ in the Bi12SiO20 Piezoelectric Crystal Journal of Phyics: Condensed Matter  11: 3201 – 3207.

- Wade,S.A., Collins, S.F., Baxter, G.W., (2003), Fluorescence intensity ratio technique for optical fiber point temperature sensing, Jounal of Applied Physics 94: 4743

- Koepke, Cz., Wisniewski, K., Sikorski, L., Piatkowski, D., Kowalska, K. and Naftaly, M. (2006). Upconverted luminescence Under 800nm Laser Diode Excitation in Nd3+-activated Fluoroaluminate Glass, Journal of Optical Materials 28: 129 –136.

- Halimah, M. K., Daud, W. M. and Sidek, H. A. A. (2010). Elastic properties of TeO2-B2O3-Ag2O Glasses, Ionics 16:  807 – 813.

- Rao, T. V. R., Reddy, R. R., Nazeer Ahamad, Y., Parandamiah, M., Sooraj Hussain, N., Buddhudu, S. And Purandar, K. (2000). Luminescence Properties of Nd3+: TeO2-B2O3- P2O5-Li2O Glass Infrared Physics and Technology 41(4): 247 – 258.

- Nazabal V., Todoroki S., Nukui A., Matsumoto T., Suehara S., Hondo T., Araki T., Inuoe S., Rivero C. and Cardinal T., (2003). Oxyfluoride Tellurite Glasses Doped by Erbium: Thermal Analysis, Structural Organization and Spectral Properties, Journal of Non-Crystalline Solids 325: 85 –102.

- Kumar, K., Rai, S. B. and Anita Rai, (2008). Strong Blue Emission from Pr3+ Ions Through Energy Transfer Process from Nd3+ to Pr3+ via Yb3+ in Tellurite Glass.  Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy 71: 508 – 512.

- Lakshminarayan, G., Yang,H. and Qiu, J. (2009). Photoluminescence of Pr3+, Nd3+ and Ni3+ doped TeO2-ZnO-WO3-TiO2-Na2O Glasses, Journal of Alloys and Compound 475(1-2): 569 – 576.

- Jayasimhadri, M., Rama Moorthy, L. and Ravikumar, R. V. S. S. N. (2007). An investigation of the optical properties of Nd3+ ions in alkali tellurofluorophosphate glasses, Optical Materials 29(11): 1321 –1326.

- Reza Dousti, M., Sahar, M. R., Ghoshal, S. K., Amjad, R. J. and Arifin, R. (2013). Plasmonic enhanced luminescence in Er3+: Ag co-doped tellurite glass, Journal of Molecular Structure 1033: 79 – 83.

- Azman, K., Razali, W. A. W., Azhan, H. and Sahar, M. R. (2012). Luminescence Spectra of TeO2-PbO-Li2O Doped Nd2O3 Glass, Advanced Materials Research 501: 121 – 125.

- Sudhakar Reddy, B., Vemasevana Raju, K., Sailaja, S., Nageswara Raju, C. and Sreekantha Reddy, D. (2010). Optical Characterization of Eu3+ and Tb3+ Ions Doped Zinc Lithium Borotellurite Glasses. Advanced Materials Research, 123-125: 1283 –1286.

- Ajith Kumar, G., Biju, P.R., Venugopal, C. and Unnikrishnan, N. V. (1997). Spectroscopic Parameters of  Nd3+ Ion in Phosphate Glasses . Journal of Non-Crystalline Solids 221: 47 – 58.

- Ryba-Romanowski, W. (1990). Effect of Temperature and Activator Concentration on Luminescence Decay of Erbium Doped Tellurite Glass. Journal of Luminescence 46: 163 – 172.

- Meisong, L., Tatsuya, Y., Lihui, H., Yusuke, A., Takenobu, S. and Yasutake, O. (2009) Relaxation Process of the 4I13/2 level of Er3+ in Borosilicate Glass,  Journal of Non-Crystalline Solids 355(2): 96 – 100.