PERFORMANCE OF ORGANIC THIN FILM TRANSISTORS (OTFTs) AT VARIOUS TEMPERATURES ON POLYETHYLENE TEREPHTHALATE (PET) SUBSTRATE
(Prestasi Transistor Organik Filem Nipis (OTFTs) pada Suhu yang Berbeza di atas Substrat Polietilena Tereftalat (PET)
Nurhazwani Musa1*, Mohd Noor Ahmad1, Nurul Farhanah Abd Halim1, Uda Hashim2, A. K. M. Shafiqul Islam3

1School of Material Engineering, 
Kompleks Pusat Pengajian Jejawi 2, Taman Muhibbah, 
Universiti Malaysia Perlis, 02600 Jejawi, Arau, Perlis
2 Institute of Nano Electronic Engineering, 
Universiti Malaysia Perlis, Lot 106, 108 & 110, Blok A, Taman Pertiwi Indah, 
Jalan Kangar-Alor Setar, Seriab 01000 Kangar, Perlis
3Faculty of Engineering Technology, 
Universiti Malaysia Perlis, 02100 Sungai Chuchuh, Padang Besar, Perlis
*Corresponding author: nurhazwani9389@yahoo.com

Abstract
Fabrication of organic thin film transistors (OTFTs) on a flexible substrate has been the subject of much attention in the sensor research community as its cost effective, low temperature processing, ease of fabrication, disposability and delivery of accurate result. The OTFTs with pentacene as active layer and polymethyl methacrylate (PMMA) as gate insulator was fabricated and its performance was investigated. The PMMA and pentacene thin films were coated on indium tin oxide coated polyethylene terephthalate (PET) substrate by a spin coating method. The substrates temperature were varied at 40, 60, 80 and 100 oC prior to the deposition of aluminum onto the interdigitated electrodes (IDE) structure via physical vapour deposition (PVD) method. The atomic force microscopy (AFM) images and current-voltage (I-V) relationship indicated that the variation of substrate temperature has an impact on both physical and electrical properties of pentacene thin film transistors. The AFM images show that the morphological grain size increased as the substrate temperature was increased.  In addition, the I-V measurement using SPA shown that the source-drain current of OTFTs was highest at temperature 100 oC.
Keywords: Organic thin film transistors (OTFTs), Pentacene, Polyethylene terephthalate (PET) substrate, Polymethyl methacrylate (PMMA)
Abstrak
Fabrikasi transistor organik filem nipis (OTFTs) di atas substrat fleksibel telah menjadi perhatian dalam komuniti penyelidikan sensor kerana berkos sederhana, suhu pemprosesan rendah, mudah difabrikasi, pakai buang dan memberikan keputusan yang tepat. OTFTs dengan mnggunakan pentasina sebagai lapisan aktif dan polimetil metakrilat (PMMA) sebagai pintu penebat telah difabrikasi dan prestasinya dikaji. PMMA dan filem nipis pentasina disediakan di atas substrat indium timah oksida bersalut polietilena tereftalat (PET) melalui kaedah salutan putaran dan suhu permukaan dipelbagaikan pada 40, 60, 80 dan 100 oC sebelum elektod interdigitated (IDE) aluminium dihasilkan melalui kaedah pemendapan wap fizikal (PVD) pada substrat. Gambar daya mikroskop daya atom (AFM) dan hubungan voltan semasa (I-V) telah menunjukkan bahawa suhu teleh memberi impak terhadap sifat fizikal dan elektrik transistor filem nipis pentasina tersebut.  Gambar AFM menunjukkan bahawa saiz butiran morfologi bertambah apabila suhu permukaan meningkat. Di samping itu, ukuran I-V menggunakan SPA menunjukkan bahawa arus punca-saliran OTFTs adalah tinggi pada suhu 100 oC.
Kata kunci: Organik filem nipis (OTFTs), Pentasina, Substrat polietilena tereftalat (PET), Polymetil metakrilat (PMMA)
Introduction
Organic thin film transistors (OTFTs) have been popular in the research community due to its potential to be cost effective [1], low temperature processing [2], ease of fabrication, disposability and delivery of accurate results. The OTFTs consist of three terminals that are the source, drain and gate that allows controlling current flow between the two electrodes through the modulation of the voltage at the third electrode [3]. Most of OTFTs prepared by vacuum deposition technique showed better electrical performances on the silicon-based thin film transistors (TFTs). However, this technique has limitation for the large area application, so a new technique has been proposed using solution process [4]. 
Among the various organic semiconductors that are being considered as the active materials in OTFTs, pentacene is one of the most promising and widely used due to its outstanding performance in terms of electrical performance such as mobility, threshold voltage and on-off ratio [5]. Therefore, pentacene is the best candidate for the p-type semiconductor OTFT. Its advantages also include air stability and good solubility. The face-to-face stacking in crystalline form is very beneficial for Π-orbital overlap [6].
In this research, pentacene, used as the active material for OTFTs was deposited at 40, 60, 80 and 100 oC and the electrical performance was investigated by I-V measurement using semiconductor parameter analyzer (SPA). The morphology of pentacene on polyethylene terephthalate (PET) substrate at various temperatures was investigated using an atomic force microscope (AFM). 
Materials and Methods
Materials and Chemicals

Anisole, Decane, Polymethyl methacrylate (PMMA), 6, 13- Bis(triisopropylsilylethynl) pentacene,  aluminum wire and indium tin oxide coated polyethylene terephthalate (PET) substrate were purchased from Sigma Aldrich.  
Organic Thin Film Transistors (OTFTs) Fabrication 
The TIPS-pentacene based OTFTs were fabricated in a top contact and bottom gate structure, as shown in Figure 1. The Indium tin oxide (ITO) layer on the PET substrate was patterned for a gate electrode.
[image: image1.png]Aluminium source Aluminium drain
contact contact

I I

Pentacene semiconductor

PMMA gate dielectric

PET





Figure 1. Schematic Structure of OTFT Device on PET Substrate
The thin films of pentacene were deposited on the PET substrates having the dimension of 2” x 2”. Before fabrication process, the substrate was cleaned and kept at ambient temperature. The Polymethyl methacrylate (PMMA) was spin coated on the cleaned substrates at 600 rpm for 60 s to form a gate insulator. The PMMA, molecular weight of 120 K was diluted in anisole (4 wt %). The spin coated PMMA was baked at 40, 60, 80 and 100 oC for 60s. For an organic semiconductor, TIPS-pentacene which is dissolved in 91 % anisole and 9 % decane by weight, was spin coated onto the PMMA gate insulator at 600 rpm for 60 s and baked at 40, 60, 80 and 100 oC for 60 s on a hot plate. The source and drain electrodes, aluminium layer were deposited through the shadow mask by using physical vapour deposition (PVD). The pentacene TFTs have a device length (L) and width (W) dimensions of 5.0 mm and 10.0 mm, respectively. Figure 2 shows an OTFT fabricated on Indium tin oxide coated PET substrate.
The surface morphology of pentacene thin film was obtained using atomic force microscopy (AFM) with contact mode and 5 x 5 µm2 were scanned. The electrical measurements were performed using semiconductor parameter analyzer (Keithley 4200).
[image: image2.png]



Figure 2. OTFT Fabricated On Indium Tin Oxide Coated PET Substrate
Result and Discussion
The surface morphology of pentacene thin film deposited at temperatures of 40, 60, 80 and 100 oC were obtained using AFM. The information about the effect of varying substrate temperatures can be gained by looking at the AFM images of pentacene layer of different samples in Fig. 3(a – d) which are for to 40, 60, 80 and 100 oC, respectively.  Figure 3 shows AFM images of the pentacene thin films on PET substrates with an area of 5 × 5 μm2. According to Figure 3, the morphological grain size increased as the substrate temperature was increasing. The grain size obtained at 100 oC film is larger than that at 40 oC. This is because by increasing substrate temperatures, the mobility of the molecule to arrive at the surface increases. Thus, produce a better alignment of the molecules and lower nucleation density [1]. 
[image: image3.png][pm]

()

[uml(d)




Figure 3. Pentacene OTFTs deposited at Tsub of (a) 40 oC, (b) 60 oC, (c) 80 oC and (d) 100 oC

The surface roughness of pentacene thin films increased from 0.84 to 10.60 nm as the temperature increased from 40 to 100 oC.  As the surface roughness increased, the root mean square (RMS) roughness also increased as shown in Figure 4. This is because the nucleation and grain structure of pentacene are very sensitive to the changes in substrate temperature. According to Chanhom and Nukeaw [7], the higher temperature would cause increasing of the grain size by restructuring of pentacene molecule as seen in the AFM results (Figure 3). The modification in the pentacene molecule structure gives effect towards the surface grain morphology of pentacene.  This is due to the weaker interaction between impinging molecules and the surface [8].

[image: image4.png]oo
—

O =t u o [=#] p=} -t [} (=]

Lo Ll

() ssouydnoy (SINY) arenbg uea] 100y

Lol

100

20

80

70

60

50

40

Substrate Temperature ("C)




Figure 4. The Root Mean Square (RMS) Roughness of Pentacene Thin Film Proportion to Substrate Temperature

The surface roughness and RMS roughness of pentacene thin film has a significant influence on the device performance. Thus, measuring the surface roughness and RMS roughness are important before manufacturing the device. Current-Voltage (I-V) for OTFTs is shown in Figure 5. The I-V plots display the drain-source current (IDS) versus drain-source voltage (VDS) at fixed gate-source voltage (VGS) values. Usually, OTFTs characteristic followed the traditional behavior of FET and showed typical p-type semiconductor. The I-V characters indicate comparable values of drain -source current at various temperature for OTFTs on PET substrate. From this research, it shows that VGS strongly affected the current flow through the OTFTs. 
[image: image5.png]0.003

—m—40 °C
RLIS ~® 60 ‘C v
A 80 °C /v/
0.001 —w—100°C Pl
v/v At
~2_A-A"o-@
iX/X/A ././
< 0.000 Iflflflfl7.7‘71;.;‘;‘2.4/¥7.7'7:\Iflflfl
@ - ;" S
-0.001 - v’ Ves =TV
2 v
/V/
v
e
-0.002 - P
v
-0.003 : : : : : : : : ,
-10 -5 0 5 10





Figure 5. Output Characteristics of Pentacene OTFTs Using PMMA as Gate Insulator at Various Temperatures

IDS was measured by VDS sweeping from -10V to 10V with the swept of 1.0 V step at constant VGS. IDS is higher when a negative voltage is applied at VGS= -7V. For negative gate-source voltage, pentacene OTFTs operate in the accumulation mode and the accumulated charge are holes [9]. During forward biased, electrons are repelled by the external voltage (Vgs) applied to the gate transistor and some of the charges are repelled from the area of the gate called depletion region. The highest value 0.00185 A of drain current, IDS of pentacene-OTFTs obtained from pentacene-OTFTs with thin films deposited at Tsub = 100oC. Furthermore, the effective carrier mobility when Tsub = 100 oC is larger compared to other OTFTs pentacene with different Tsub. It is because when the temperature increase; the grain size increased, thus reducing the grain boundaries. An electron carrier that traps at the grain boundaries decreased by reducing the grain boundaries. This situation will increase the number of effective carriers that leads to higher drain current.
Conclusion
OTFTs based on pentacene active layer and PMMA as dielectric have been fabricated. The temperature dependence of the pentacene OTFTs distinguishes different physical and electrical properties of them. It is found that increasing substrate temperature resulted in the increased grain size and surface roughness. The result also shows that PMMA and pentacene can be easily deposited by spin coating method. From this experiment, the average grain size and RMS roughness of pentacene thin film are largest at Tsub = 100oC and its show the highest value of I-V measurement 0.00185 A at Tsub = 100oC.  This study can be extended to further OTFTs research and useful for chemical and bio sensing materials.

Acknowledgements
This work has been carried out with financial support from Malaysian Ministry of Higher Education (MOHE) under the research funding FRGS grants (9003-00419). The authors would like to thank Mubaraq Hans Von Schleusingen for his contribution to this work.
References
1. Stadlober, B., Satzinger, V., Maresch,H., Somitsch,D.,  Haase, A., Pichler, H., Rom, W.  and Jakopic, G. (2003). Structural and Electrical Properties of Polymorphic Pentacene Thin Films. Proceedings of 
SPIE Organic Field Effect Transistors II, 5217: 112 – 123.
2. Hsiao-W.Z. and Cheng-W.C. (2009). Effect of surface energy on pentacene thin-film growth and organic thin film transistor characteristics. Japanese Journal of Applied Physics, 48 (031501): 1 – 6.
3. Daniel, E., Nathan, C.,Warwick, B., Paul, C. D., and Xiaojing, Z. (2014). Organic Thin Film Transistor (OTFT) Based Sensor. Electronics, 3: 234 – 254.
4. Chang, M. K., Jin, H. K., Sin,D. L, and Jin,H. B. (2013). Control of the molecular order and cracks of the 6,13-bis(triisopropylsilylethynyl)-pentacene on a polymeric insulator by anisotropic solvent drying. Solid-State Electronics, 89: 189 –193.
5. Kim J. K., Kim J. M., Yoon T. S., Lee H. H., Jeon D. and Kim Y. S. (2009). Pentacene Thin Film Transistors with Various Polymer Gate Insulators. Journal of Electrical Engineering & Technology, 4 (1): 118 – 122.
6. Basu, S., Adriyanto, F. and Wang, Y. H. (2014). Blending effect of 6,13 bis(triisopropylsilylethynyl) pentacene–graphene composite layers for flexible thin film transistors with a polymer gate dielectric. Nanotechnology , 25: 1 – 11.
7. Chanhom, A. and Nukeaw, J. (2007). The Effect of Substrates Temperature on Pentacene Thin Films prepared by Organic Thermal Evaporator. Proceedings of the 7th IEEE International Conference on Nanotechnology, Hong  Kong August: 2 – 5.
8. Chaeho, K., Kyoungyoon, B., Ilsin, A., Kang, C. J., Kim, Y. S. and Jeon, D. (2006). Morphology and ellipsometry study of pentacene films grown on native SiO2 and glass substrates. Current Applied Physics, 6: 925 – 930.
9. Puigdollers, J., Voz, C., Orpella, A., Quidant, R., Martin, I., Vetter, M. and Alcubilla, R. (2004). Pentacene thin-film transistors with polymeric gate dielectric. Organic Electronics, 5: 67 –71.

