Malaysian Journal of Analytical Sciences Vol 20 No 1 (2016): 64 - 72

EFFECT OF SILVER NANOPARTICLE ADDITION ON THE STRUCTURE AND CHARACTERISTICS OF RADIO-PHOTOLUMINESCENCE GLASS DOSIMETER

(Kesan Penambahan Nanozarah Argentum Terhadap Struktur dan Sifat – Sifat Dosimeter Kaca Radio – Pendarcahaya)

Irman Abdul Rahman1*, Muhammad Taqiyuddin Mawardi Ayob1,2, Hur Munawar Kabir Mohd1,

Ainee Fatimah Ahmad1, Shamellia Sharin1, Faizal Mohamed1, Sidek Ab Aziz2, Shahidan Radiman1

1School of Applied Physics, Faculty of Science and Technology,

Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor Darul Ehsan, Malaysia

2Department of Physics, Faculty of Science,

Universiti Putra Malaysia, 43400 Serdang, Selangor Darul Ehsan, Malaysia

*Corresponding author: irman@ukm.edu.my

Received: 9 December 2014; Accepted: 16 October 2015

Abstract

A series of silver-activated phosphate glass was prepared by melt quenching method. The effect of silver nanoparticle addition on the phosphate glass microstructure, composition and chemical characteristics was investigated using x-ray diffraction, fourier transform infrared and photoluminescence spectroscopy. Other physical property such as density was also evaluated. The density increased when the amount of silver ions were increased, due to the enhanced formation of non-bridging oxygen. In this study, we discuss the emission mechanism of two radio-photoluminescence peaks at 460 nm and 620 nm, where the electrons and holes produced by γ-irradiation a re-trapped by Ag+ ions to produce Ag0 and Ag2+ ions respectively, when the Ag+-doped phosphate glass is exposed to γ-ray. We proposed that an emission mechanism of 460 and 620 nm radio-photoluminescence peaks with these Ag2+ and Ag0 ions. Furthermore, a correlation between the investigated properties and glass composition is discussed.

Keywords: silver nanoparticle, optical and physical properties, radio-photoluminescence glass dosimeter

Abstrak

Satu siri gelas argentum-aktif fosfat telah dihasilkan menerusi kaedah peleburan. Kesan penambahan nanobahan argentum ke dalam mikrostruktur gelas fosfat, komposisi dan sifat-sifat kimia dikaji dengan menggunakan pembelauan sinar-X, penjelmaan inframerah Fourier dan spektroskopi pendarcahaya. Sifat fizikal yang lain seperti ketumpatan kacaturut dikaji. Ketumpatan kaca bertambah apabila jumlah ion-ion argentum ditingkatkan, disebabkan oleh peningkatan pembentukan oksigen tanpa-hubung. Dalam kajian ini, kami membincangkan mekanisme pemancaran oleh dua puncak radio-pendarcahaya pada jalur 460 nm dan 620 nm, di mana elektron dan lohong yang terhasil daripada sinar-γ diperangkap oleh ion – ion Ag+ seterusnya menghasilkan ion – ion Ag0 dan Ag2+, apabila kaca Ag+-aktif fosfat didedahkan kepada sinar-γ. Kami turut membincangkan mekanisme pemancaran bagi setiap puncak radio-pendarcahaya pada jalur 460 dan 620 nm berdasarkan ion – ion Ag2+ dan Ag0 berkenaan. Tambahan lagi, hubung kait antara komposisi kaca dan sifat-sifat kaca yang terhasil turut dibincangkan.

Kata kunci: nanobahan argentum, sifat fizikal and optik, dosimeter kaca radio-pendarcahaya

References

- Andreeva, N. Z., Vil’chinskaya, N. N., Dmitryuk, A.V., Perminov, A. S., Petrovskii, G. T. and Savvina, O. C. (1985). Influence of activator concentration on the dosimetric properties of radio photoluminescent glasses. Atom. Énergiya. 58(2): 132 – 135.

- Beekenkamp, P. (1965). Colorcenters in borate, phosphate and borophosphate glasses. Thesis, Technical University, Eindhoven, Philips Res., Suppl. 4.

- Bishay, A. (1961). Gamma-ray induced coloring of some phosphate glasses. J. Am. Ceram. Soc. 44(11): 545-552.

- Bishay, A. (1970). Radiation induced colorcenters in multicomponent glasses. J. Non-Cryst. Solids. 3: 54 –114.

- Bocharova, T. V., Karapetan, G. O., Mironov, A. M., Khalilev, V. D. and Tagil’tseva, N. O. (2006). Gamma-induced absorption spectra as a new method for RE-ion environment study in a fluorophosphates glasses. Opt. Mater. 28: 1296 –1300.

- Dmitryuk, A. V., Paramzina, S. E., Savvina, O. C. and Yashchurzhinskaya, O. A. (1989). Nature of radiophotoluminescent centers in silver-activated phosphate glasses. Opt. Spectrosc. 66: 1070 – 1075.

- Hsu, S. M., Yang, H. W., Huang, D. Y. C., Hsu, W. L., Lu, C. C. and Chen, W. L. (2008). Development and physical characteristics of a novel compound radiophotoluminescent glass dosimeter. Radiat. Meas. 43: 538 –541.

- Takeda, Y., Plaksin, O. A. and Kishimoto, N. (2007). Dispersion of nonlinear dielectric function of Au nanoparticles in silica glass. Opt. Express. 15: 6010 – 6018.

- Dmitryuk, A. V., Paramzina, S. E., Solov’eva, N. D. and Timofeev, N.T. (1996). The influence of glass composition on the properties of silver-doped radiophotoluminescent phosphate glasses. J. Non-Cryst. Solids. 202: 173 – 177.

- Kurobori, T., Zheng, W., Miyamoto, Y., Nanto, H. and Yamamoto, T. (2010). The role of silver in the radio-photoluminescent properties in silver-activated phosphate glass and sodium chloride crystal. Opt. Mater. 32: 1231 –1236.

- Yokota, R. and Imagawa, H. (1965). ESR studies of radiophotoluminescent centers in silver-activated phosphate glass. J. Phys. Soc. Jpn. 20: 1537 –1538.

- Ahmed, I., Abou Neel, Valappil, S. P., Nazhat, S. N., Pickup, D. M., Carta, D., Carroll, D. L., Smith, M. E. and Knowles, J. C. (2007). The structure and properties of silver-doped phosphate-based glasses. J. Mater. Sci. Mater. Med. 42:9827 – 9835.

- Birkin, P. R., Offin, D. G., Joseph, P. F. and Leighton, T.G. (2005). Cavitation, shock waves and the invasive nature of sonoelectrochemistry. J. Phys. Chem. B.109: 16997 –17005.

- ElBatal, F. H., Ouis, M. A., Morsi, R. M. M. and Marzouk, S. Y. (2010).Interaction of gamma rays with some sodium phosphate glasses containing cobalt.J. Non.-Cryst. Solids. 356(1): 46-55.

- Piao, F., Oldham, W. G. and Haller, E. E. (2000). The mechanism of radiation-induced compaction in vitreous silica. J. Non-Cryst. Solids. 276: 61 –71.

- Maurel, C., Cardinal, T., Bellec, M., Canioni, L., Bousquet, B., Treguer, M., Videau, J. J. and Richardson, M. (2009). Luminescence properties of silver zinc phosphate glasses following different irradiations. J. Lumin. 129(12): 1514 –1518.

- Zhao, Quan, Z., Qiu, J. R., Jiang, X. W., Zhao, C. J. and Zhu, C. S. (2004). Controllable precipitation and dissolution of silver nanoparticles in ultrafast laser pulses irradiated Ag+-doped phosphate glass. Opt. Exp. 12(17): 4035 – 4040.

- Yokota R. and Muto Y. (1971). Silver-activated phosphate dosimeter glasses with low energy dependence and higher sensitivity. Health Phys. 20: 662 – 663.