# Malaysian Journal of Analytical Sciences Vol 20 No 2 (2016): 296 - 302

# OXIDATION OF COMMERCIAL PETRONAS DIESEL WITH TERT-BUTYL HYDROPEROXIDE OVER POLYMOLYBDATE ALUMINA SUPPORTED CATALYST MODIFIED WITH ALKALINE EARTH METALS

(Pengoksidaan Diesel Komersial Petronas dengan Tert-Butil Hidroperoksida bersama Pemangkin Polimolibdenum Diubahsuai dengan Logam Alkali)

# Wan Nazwanie Wan Abdullah, Rusmidah Ali*, Wan Azlee Wan Abu Bakar

# Department of Chemistry, Faculty of Science,

# Universiti Teknologi Malaysia, 81310 UTM Johor Bahru, Johor, Malaysia

*Corresponding author: rusmidah@kimia.fs.utm.my

Received: 9 December 2014; Accepted: 9 October 2015

Abstract

# Due to strict environmental legislation for ultra-low sulfur diesel fuels, increasing technical and operational challenges are imposed to conventional hydrodesulfurization (HDS) technology. Therefore, catalytic oxidative desulfurization (Cat-ODS) has been suggested to be an alternative method to replace a conventional method which is hydrodesulfurization. In this study, catalytic oxidation of commercial diesel was performed using an oil-soluble oxidant, tert-butyl hydroperoxide (TBHP), over polymolybdate supported on alumina MoO3-PO4/Al2O3 catalyst. A commercial Petronas diesel with 440 ppmw of total sulfur was employed to evaluate the elimination of sulfur compounds. Besides, the percentage of sulfur removal was measured by (GC-FPD). Alkaline earth metals, such as Calcium (Ca), Barium (Ba) and Strontium (Sr) were introduced on the surface of MoO3-PO4/Al2O3. The results showed that the catalytic activity decreased in the order, Ca/MoO3-PO4/Al2O3>Sr/MoO3-PO4/Al2O3> Ba/MoO3-PO4/Al2O3. The Ca/MoO3-PO4/Al2O3 catalyst was characterized by XRD and FESEM. XRD results showed that the best catalyst was highly amorphous while FESEM micrograph illustrated an aggregation and agglomeration of various particle sizes. The catalytic activity of Ca/MoO3-PO4/Al2O3 catalyst with various Ca/Mo ratios were also studied. When the Ca/Mo ratio was 15:85, the sulfur removal  was the highest (79%) at 45ºC, 30 min and O/S molar ratio 3.0 with solvent = dimetylformamide (DMF), diesel/solvent ratio = 1.0.

# Keywords: 	Oxidative desulfurization, commercial diesel, tert-butyl hydroperoxide, alkaline earth metals, polymolybdate, dimetylformamide

Abstrak

Disebabkan undang-undang alam sekitar yang ketat untuk bahan api sulfur diesel ultra-rendah, peningkatan cabaran teknikal dan operasi dikenakan kepada hydropenyahsulfuran konvensional teknologi (HDS). Oleh itu, penyahsulfuran oksidatif mengunakan pemangkin (Cat-ODS) telah dicadangkan untuk menjadi satu kaedah alternatif untuk menggantikan kaedah konvensional iaitu hydopenyahsulfuran. Dalam kajian ini, pengoksidaan diesel komersial telah dijalankan menggunakan oksida larut minyak, tert-butil hidroperoksida (TBHP) dan  mangkin molibdena berpenyokong alumina, MoO3-PO4/Al2O3. Diesel komersial Petronas yang mengandungi sulfur 440 ppmw telah digunakan untuk menilai penyahsulfuran. Selain itu, peratusan penyingkiran sulfur telah diukur menggunakan (GC-FPD). Logam alkali, seperti Kalsium (Ca), Barium (Ba) dan Strontium (Sr) telah dicelup pada permukaan MoO3-PO4/Al2O3 pemangkin. Hasil kajian menunjukkan bahawa aktiviti pemangkin menurun mengikut susunan, Ca/MoO3-PO4/Al2O3 > Sr/MoO3-PO4/Al2O3 > Ba/MoO3-PO4/Al2O3. Pemangkin Ca/MoO3-PO4/Al2O3 telah dicirikan menggunakan XRD dan FESEM. Keputusan XRD menunjukkan pemangkin yang terbaik adalah sangat amorfus manakala FESEM mikrograf menggambarkan satu aglomerasi dalam pelbagai saiz zarah. Aktiviti pemangkin Ca/MoO3-PO4/Al2O3 dengan pelbagai nisbah Ca/Mo telah juga dikaji. Apabila nisbah Ca/Mo adalah 15:85, penyingkiran sulfur adalah tertinggi (79%) pada keadaan optimum: 45ºC, 30 min dan nisbah O/S molar = 3.0 dengan pelarut = dimetilformamida (DMF), nisbah diesel/pelarut = 1.0.

# Kata kunci: 	penyahsulfuran oksidatif, diesel komersial, tert-butil hidroperoksida, logam alkali, polimolibdena, dimetil-formamida

References

- Chica, A., Corma, A. and Dómine M. E. (2006). Catalytic oxidative desulfurization (ODS) of diesel fuel on a continuous fixed-bed reactor. Journal of Catalysis, 242: 299 – 308.

- Abdullah, W. N. W., Bakar, W. A. W. A. and Ali, R. (2014). Catalytic oxidative desulfurization of diesel fuel utilizing a polymolybdate alumina supported catalyst: Characterization, catalytic activity and mechanistic study. Reaction Kinetic Mechanism and Catalyst, 114:547 – 560.

- Lifeng, W., Baode, S., Frances, H. Y. and Ralph, T. Y. (2012). Effects of aromatics on desulfurization of liquid fuel by p-complexation and carbon adsorbents. Chemical Engineering Society, 73:208 – 217.

- Tam, P. S., Kittrell, J. R. and Eldridge J. W. (1990). Desulfurization of fuel oil by oxidation and extraction. 1. Enhancement of extraction oil yield. Industrial & Engineering Chemistry Research, 29(3): 321 – 324.

- Wan Abu Bakar, W. A., Ali, R., Abdul Kadir, A. A. and Wan Mokhtar, W. A. (2012). Effect of transition metal oxides catalyst on oxidative desulfurization of model diesel. Fuel Processing Technology, 101: 78 – 84.

- Malka, K. and Tatiboue, J. M. (1998). A two-step preparation of silica-supported calcium-molybdenum catalysts. Journal of Catalysis, 175: 204 – 212.

- Chang, J., Wang, A., Liu, J., Li, X. and Hu, Y. (2010). Oxidation of dibenzothiophene with cumene hydroperoxide on MoO3/SiO2 modified with alkaline earth metals. Catalysis Today, 149: 122 – 126.

- Wan Abdullah, W. N., Wan Abu Bakar W. A., Ali R. and Embong Z. (2015). Oxidative desulfurization of commercial diesel catalyzed by tert-butyl hydroperoxide polymolybdate on alumina: Optimization of Box-Behnken design. Clean Technologies and Environment Policy, 17: 433 – 441.

- Jones, C., Cole, K. J., Taylor, S. H., Crudace, M. J. and Hutchings, G. J. (2009). Copper manganese oxide catalysts for ambient temperature carbon monoxide oxidation: Effect of calcination on activity. Journal of Molecular Catalysis A: Chemical, 305:121 – 124.