Malaysian Journal of Analytical Sciences Vol 20 No 2 (2016): 329 - 334

FRACTIONATION OF HEMICELLULOSE FROM RICE STRAW BY ALKALINE EXTRACTION AND ETHANOL PRECIPITATION

(Pemisahan Hemiselulosa daripada Hampas Batang Padi melalui Pengekstrakan Beralkali dan Pemendakan Etanol)

Nur Hazlilla Zulyadi, Sabiha Hanim Saleh*, Siti Halimah Sarijo

School of Chemistry and Environment, Faculty of Applied Sciences,

Universiti Teknologi MARA, 40450 Shah Alam, Selangor, Malaysia

*Corresponding author: sabihahanim@salam.uitm.edu.my

Received: 24 February 2015; Accepted: 27 October 2015

Abstract

Hemicelluloses were extracted from rice straw using alkaline extraction and ethanol precipitation. The effects of different extraction conditions; temperature (45 – 65 °C), pH (4.5 – 6.5), and concentrations of NaOH (0.25 – 1 M) on the hemicellulose yield were investigated. Two hemicelllulosic fractions namely Ha1 and Ha2 were obtained by precipitation of alkaline soluble hemicellulose in 0.2 volumes and 4 volumes ethanol, respectively. The Ha1 and Ha2 were further characterized to obtain total sugar, monosaccharides and Klason Lignin content. The highest hemicellulose yield for Ha1 was 4.00 % obtained at 55 °C and pH 5.5 with 0.25 M of NaOH, whereas the highest hemicellulose yield for Ha2 was 19.88 % obtained at 55 °C and pH 5.5 with 0.5 M of NaOH. This study revealed that hemicellulose yield is dependent on the pH, temperature and concentration of NaOH in the alkaline extraction.

Keywords: hemicelluloses, rice straw, alkaline extraction, ethanol precipitation

Abstrak

Hemiselulosa daripada hampas batang padi telah diekstrak melalui pengekstrakan beralkali dan pemendakan etanol. Kesan perbezaan kondisi pengekstrakan; suhu (45 – 65 °C), pH (4.5 – 6.5), dan kepekatan NaOH (0.25 – 1 M) ke atas hasil hemiselulosa dikaji. Dua pecahan hemiselulosa,  Ha1 and Ha2 telah diperolehi melalui pemendakan hemisellulosa larut alkali dalam isipadu etanol 0.2 dan 4 masing-masing. Ha1 and Ha2 dicirikan oleh jumlah gula, kandungan monosakarida dan Klason Lignin. Hasil hemiselulosa tertinggi untuk Ha1 adalah 4.00 % yang diperolehi pada suhu 55 °C, pH 5.5 and 0.25 M NaOH, manakala untuk Ha2 adalah 19.88 % diperolehi pada suhu 55 °C, pH 5.5 and kepekatan 0.5 M NaOH. Kajian ini membuktikan hasil hemisellulosa bergantung kepada pH, suhu dan kepekatan NaOH dalam pengekstrakan beralkali.

Kata kunci: hemiselulosa, hampas batang padi, pengekstrakan beralkali, pemendakan etanol

References

- Sharma, R. K. and Arora, D. S. (2010). Biodegradation of paddy straw obtained from different geographic locations by means of Phlebia spp. for animal feed. Biodegradation, 22: 143 – 152.

- Lim, J. S., Abdul Manan, Z., Wan Alwi, S. R. and Hashim, H. (2012). A review on utilisation of biomass from rice industry as a source of renewable energy. Renewable and Sustainable Energy Reviews, 16(5): 3084 – 3094.

- Ebringerová, A., Hromádková, Z., Híbalová, V., Xu, C., Holmbom, B., Sundberg, A., and Willför, S. (2007). Norway spruce galactoglucomannans exhibiting immunomodulating and radical-scavenging activities. International  Journal of Biology Macromolecule, 42: 1 – 5.

- Sabiha-Hanim, S. and Siti-Norsafurah, A. M. (2012). Physical properties of hemicellulose films from sugarcane bagasse. Procedia Engineering, 42: 1390 – 1395.

- Peng, P., Peng, F., Bian, J., Xu, F., Sun, R.-C. and Kennedy, J. F. (2011).Isolation and structural characterization of hemicelluloses from the bamboo species Phyllostachysincarnata Wen. Carbohydrate Polymers, 86(2): 883 – 890.

- Bian, J., Peng, F., Peng, X.-P., Xu, F., Sun, R.-C. and Kennedy, J. F. (2012). Isolation of hemicelluloses from sugarcane bagasse at different temperatures: Structure and properties. Carbohydrate Polymers, 88(2): 638 – 645.

- Yang, D., Zhong, L-X., Yuan, T-Q., Peng, X-W. and Sun, R-C. (2013). Studies on the structural characterization of lignin, hemicelluloses and cellulose fractionated by ionic liquid followed by alkaline extraction from bamboo. Industrial Crops and Products, 43: 141 – 149.

- Xiao, B., Sun, X. and Sun, R. (2001). Chemical, structural, and thermal characterizations of alkali-soluble lignins and hemicelluloses, and cellulose from maize stems, rye straw, and rice straw. Polymer Degradation and Stability, 74(2): 307 – 319.

- Egüés, I., Eceiza, A. and Labidi, J. (2013). Effect of different hemicelluloses characteristics on film forming properties. Industrial Crops and Products, 47: 331 – 338.

- Rabetafika, H. N., Bchir, B., Blecker, C., Paquot, M. and Wathelet, B. (2014). Comparative study of alkaline extraction process of hemicelluloses from pear pomace. Biomass and Bioenergy, 61: 254 – 264.

- Kacurakova, M., Belton, P. S., Wilson, R. H. and Hirsch, J. (1998). Hydration properties of xylan-type structure: an FTIR study of xylooligosaccharides. Journal Science of  Food and Agriculture, 77(1): 38 – 48.

- Cai, Y., Li, G., Nie, J., Lin, Y., Nie F. and Zhang, J. (2010). Study of the structure and biosynthetic pathway of lignin in stone cells of pear. Science Horticulturae, 125()3: 374 – 379.

- Sun, R. C., Tomkinson, J., Ma, P. L. and Liang, S. F. (2000). Comparative study of hemicelluloses from rice straw by alkali and hydrogen peroxide treatments. Carbohydrate Polymers, 42(2): 111 – 122.

- Kacuráková, M., Ebringerova, A., Hirsch, J. and Horomadkova, Z. (1994). Infrared study of arabinoxylans. Journal Science of Food Agriculture, 66 (3): 423 – 427.