# Malaysian Journal of Analytical Sciences Vol 20 No 2 (2016): 335 - 341

# PREPARATION, CHARACTERIZATION AND PERFORMANCE STUDIES OF ACTIVE PVDF ULTRAFILTRATION-SURFACTANTS MEMBRANES CONTAINING PVP AS ADDITIVE

(Penyediaan, Pencirian dan Kajian Prestasi PVDF Aktif  Ultraturasan-Surfaktan Membran mengandungi PVP sebagai Bahan Tambahan)

# Nur Izzah Md Fadilah and Abdul Rahman Hassan*

# Industrial Membrane Technology Laboratory,

# Department of Industrial Chemical Technology,

# Faculty of Science and Technology,

# Universiti Sains Islam Malaysia, 71800 Nilai, Negeri Sembilan, Malaysia

*Corresponding author: abdrahman@usim.edu.my

Received: 24 February 2015; Accepted: 27 October 2015

# The role of surfactants in the formation of active Poly(vinylidene fluoride) (PVDF) ultrafiltration (AUF) membranes was studied. The effect combination of surfactants that are Sodium dodecyl sulfate (SDS)/Tween 80 and Tween 80/Triton X-100 formulations on performance and morphological structures were investigated for the first time. The influence of surfactants blends on the membrane pores was also examined. Experimental data showed that combination of Tween 80/Triton X-100 give the highest BSA permeation flux with a value of 285.51 Lm-2h-1. With combination of SDS/Tween 80, the AUF membrane showed the highest protein rejection up to 93 % and 79 % for Bovine Serum Albumin (BSA) and Egg Albumin (EA), respectively. Moreover, membranes characterization demonstrated that the addition of SDS/Tween 80 and Tween 80/Triton X-100 were found to affect the performance, surface morphologies and membrane pores of AUF PVDF membranes.

# Keywords: poly(vinylidene fluoride), ultrafiltration, surfactant, protein rejection, morphology

Abstrak

# Peranan surfaktan dalam pembentukan ultraturasan PVDF aktif (AUF) membran telah dikaji. Gabungan kesan surfaktan iaitu SDS/Tween 80 dan Tween 80/Triton X-100 formulasi terhadap prestasi dan struktur morfologi telah dikaji buat pertama kali. Pengaruh adunan surfaktan pada liang membran juga diperiksa. Data ujikaji menunjukkan bahawa gabungan Tween 80/Triton X-100 memberikan bacaan penyerapan fluks tertinggi iaitu 285.51 Lm-2h-1. Dengan kombinasi SDS/Tween 80, membran AUF menunjukkan protein penolakan tertinggi sehingga 93 % dan 79 % masing – masing untuk Albumin Serum Bovine (BSA) dan Albumin Telur (EA). Selain itu, membran pencirian menunjukkan bahawa penambahan SDS/Tween 80 dan Tween 80/Triton X-100 didapati memberi kesan kepada prestasi, morfologi permukaan dan liang membran AUF PVDF.

# Kata kunci: poli(vinylidene fluorida), ultraturasan, surfaktan, penolakan protein, morfologi

References

- Idris, A., Zain, N. M. and Yusof, N. M. (2007). Synthesis, characterization and performance of asymmetric Polyethersulfone (PES) ultrafiltration membranes with polyethylene glycol of different molecular weights as additives. Desalination, 207:324 – 339.

- Zuo, D. Y., Xu, Y. Y., Xu, W. L. and Zou, H. T. (2008). The influence of PEG molecular weight on morphologies and properties of PVDF asymmetric membranes. Chinese Journal of Polymer Science, 26: 405 – 414.

- Zhao, S., Wang, Z., Wei, X., Tian, X., Wang, J., Yang, S. and Wang, S. (2011). Comparison study of the effect of PVP and PANI nanofibers additives on membrane formation mechanism, structure and performance. Journal of Membrane Science, 385: 110 – 122.

- Ismail, A. F. and Hassan, A. R. (2007). Effect of additive contents on the performances and structural properties of asymmetric Polyethersulfone (PES) nanofiltration membranes. Separation and Purification Technology, 55: 98 – 109.

- Jung, B., Yoon, J. K., Kim, B. and Rhee, H. W. (2004). Effect of molecular weight of polymeric additives on formation, permeation properties and hypochlorite treatment of asymmetric polyacrylonitrile membranes. Journal of Membrane Science, 243: 45 – 57.

- Xu, Z. L., Chung, T. S. and Huang, Y. (1999). Effect of polyvinylpyrroli-done molecular weights on morphology, oil/water separation, mechanical and thermal properties of polyetherimide/ polyvinylpyrrolidone hollow fiber membranes.  Journal of Applied Polymer Science, 74: 2220 – 2233.

- Wang, D., Li, K. and Teo, W. K. (1999). Preparation and characterization of polyvinylidene fluoride (PVDF) hollow fiber membranes. Journal of Membrane Science, 163: 211 – 220.

- Fernandez, E., Benito, J. M., Pazos, C. and Coca, J. (2005). Ceramic membrane ultrafiltration of anionic and non-ionic surfactant solutions. Journal of Membrane Science, 246:1 – 6.

- Sun, C. (2009). Poly(vinylidene fluoride) membranes: preparation, modification, characterization and applications. University of Waterloo, Waterloo, Ontario, Canada.

- Arthanareeswaran, G., Thanikaivelan, P., Srinivasn, S., Mohan, D. and Rajendran, M. (2004). Synthesis, characterization and thermal studies on cellulose acetate membranes with additive. Journal of European Polymer, 40: 2153 – 2159.

- Rahimpour, A., Madaeni, S. and Mehdipour-Atei, S. (2008). Synthesis of a novel poly(Amide-Imide) and preparation and characterization of PAI blended Polyethersulfone (PES) membrane. Journal of Membrane Science, 311: 349 – 359.

- Ghasem, N., Al-Marzouqi, M. and Duidar, A. (2012). Effect of PVDF concentration on the morphology and performance of hollow fiber membrane employed as gas-liquid membrane contactor for CO2 absorption. Separation and Purification Technology, 98: 174 – 185.

- Amirilargani, M., Saljoughi, E. and Mohammadi, T. (2009). Effects of Tween 80 concentration as a surfactant additive on morphology and permeability of flat sheet Polyethersulfone (PES) membranes. Desalination, 249: 837 – 842.