Malaysian Journal of Analytical Sciences Vol 20 No 2 (2016): 393 – 400

EFFECT OF SUPPORT MATERIALS ON CATALYTIC ACTIVITY OF NANO RUTHENIUM CATALYST IN HYDROGENOLYSIS OF GLYCEROL

# (Kesan Bahan Penyokong Terhadap Aktiviti Pemangkin Nano Ruthenium dalam Hidrogenolisis Gliserol)

Noraini Hamzah1* and Mohd Ambar Yarmo2

# 1School of Chemistry and Environmental, Faculty of Science and Technology

# Universiti Teknologi MARA, 40450 Shah Alam, Selangor, Malaysia

2School of Chemical Sciences and Food Technology, Faculty of Science and Technology,

Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor, Malaysia

*Corresponding author: pnoraini@salam.uitm.edu.my

Received: 24 February 2015; Accepted: 27 October 2015

Abstract

A series of heterogenous catalysts based on supported ruthenium were prepared from RuCl3 precusor by impregnation method. The effect of support materials (bentonite, TiO2, Al2O3 and SiO2) on catalytic activity of Ru catalyst for hydrogenolysis of glycerol were investigated under mild reaction condition of 150C and 20 bar initial hydrogen pressure for 7 hours reaction time and glycerol concentration was 20%(wt). It was found that the type of support material have significant effects on the activity and selectivity of glycerol hydrogenolysis. The order of Ru catalyst activity was Ru/bentonite > Ru/Al2O3  Ru/TiO2 > Ru/SiO2. This study showed that bentonite supported Ru catalyst was the most active with glycerol conversion reaching 62.5% compared to other supports. All the tested catalyst exhibited high selectivity to 1,2-propanediol with more than 80%. Characterization of the catalysts was carried out using BET, XPS, FESEM-EDX and TEM to obtain the physicochemical properties of the catalysts.

# Keywords: hydrogenolysis, ruthenium, bentonite, 1,2-propanediol, glycerol

Abstrak

# Satu siri pemangkin heterogen berasaskan logam ruthenium berpenyokong disediakan daripada prekusor garam RuCl3 menggunakan teknik impregnasi. Kesan bahan penyokong (bentonit, TiO2, Al2O3 dan SiO2) terhadap aktiviti pemangkin Ru dalam hidrogenolisis gliserol dilakukan pada keadaan tindak balas yang sederhana dengan suhu 150C, tekanan awal hydrogen 20 bar, masa tindak balas 7 jam dan kepekatan gliserol 20%(wt). Keputusan yang diperolehi menunjukkan jenis bahan penyokong mempunyai kesan signifikan terhadap aktiviti dan pemilihan dalam hidrogenolisi gliserol. Turutan aktiviti pemangkin Ru adalah Ru/bentonit > Ru/Al2O3  Ru/TiO2 > Ru/SiO2. Kajian ini menunjukkan pemangkin Ru yang disokong atas bentonit adalah pemangkin yang paling aktif dengan peratus penukaran mencapai 62.5% berbanding dengan penyokong lain. Semua pemangkin yang diuji menunjukkan peratus pemilihan terhadap produk 1,2-propandiol yang tinggi iaitu melebihi 80%. Pencirian pemangkin dilakukan menggunakan alat BET, XPS, FESEM-EDX dan TEM bagi mendapatkan sifat-sifat fizikokimia pemangkin.

# Kata kunci: hidrogenolisis, ruthenium, bentonit, 1,2-propanediol, gliserol

References

- Maris, E. P. and Davis, R. J. (2007). Hydrogenolysis of glycerol over carbon-supported Ru and Pt catalysts. Journal of Catalysis, 249(2): 328 - 337.

- Bolado, S., Treviño, R. E., García-Cubero, M. T., and Benito, G. G. (2010). Glycerol hydrogenolysis to 1, 2 propanediol over Ru/C catalyst. Catalysis Communications, 12(2): 122 - 126.

- Balaraju, M., Rekha, V., Prasad, P. S. S., Devi, B. L. A. P., Prasad R. B. N. and Lingaiah N. (2009). Influence of solid acids as co-catalysts on glycerol hydrogenolysis to propylene glycol over Ru/C catalysts. Applied Catalysis A: General, 354(1-2): 82 - 87.

- Balaraju, M., Rekha, V., Sai Prasad P. S., Prasad R. B. N. and Lingaiah N. (2008). Selective hydrogenolysis of glycerol to 1, 2 propanediol over Cu–ZnO catalysts. Catalysis Letters, 126(1): 119 - 124.

- Vasiliadou, E. S., Heracleous, E., Vasalos I. A., and Lemonidou A. A. (2009). Ru-based catalysts for glycerol hydrogenolysis - effect of support and metal precursor. Applied Catalysis B: Environmental, 92(1-2): 90-99.

- Maris, E. P., Ketchie, W. C., Murayama M. and Davis R. J. (2007). Glycerol hydrogenolysis on carbon-supported Pt/Ru and Au/Ru bimetallic catalysts. Journal of Catalysis, 251(2): 281- 294.

- Nakagawa, Y., Shinmi, Y., Koso S. and Tomishige K. (2010). Direct hydrogenolysis of glycerol into 1,3-propanediol over rhenium-modified iridium catalyst. Journal of Catalysis, 272(2):191 – 194

- Huang, L., Zhu, Y., Zheng, H., Ding, G. and Yongwang, Li. (2009). Direct conversion of glycerol into 1,3-propanediol over Cu-H4SiW12O40/SiO2 in Vapor Phase. Chemistry Letters, 131(1):312 – 320.

- Feng, J., Fu. H., Wang, J., Li, R., Chen, H. and Li, X. (2008). Hydrogenolysis of glycerol to glycols over ruthenium catalysts: Effect of support and catalyst reduction temperature. Catalysis Communications,  9(6): 1458 - 1464.

- Zhou, Z., Li, X. Zeng, T., Hong, W., Cheng Z. and Yuan, W. (2010). Kinetics of Hydrogenolysis of Glycerol to Propylene Glycol over Cu-ZnO-Al2O3 Catalysts. Chinese Journal of Chemical Engineering,  18(3): 384 - 390.

- Shinmi, Y., Koso, S., Kubota, T., Nakagawa. Y. and Tomishige, K. (2010). Modification of Rh/SiO2 catalyst for the hydrogenolysis of glycerol in water. Applied Catalysis B: Environmental, 94(3-4): 318 - 326.

- Miyazawa, T., Koso, S., Kunimori, K. and Tomishige, K. (2007). Glycerol hydrogenolysis to 1,2-propanediol catalyzed by a heat-resistant ion-exchange resin combined with Ru/C. Applied Catalysis A: General, 329: 30 – 35.

- Jiang, T., Zhou, Y., Liang, S., Liu H. and Han B. (2009) Improved utilisation of renewable resources: New important derivatives of glycerol. Green Chemistry, 7: 1000 - 1006.

- Yuan, Z. Wang, J., Wang, L., Xie, W., Chen, P., Hou Z. and Zheng. X., (2010). Biodiesel derived glycerol hydrogenolysis to 1,2-propanediol on Cu/MgO catalysts. Bioresource Technology, 101: 7088 – 7092.

- Balaraju, M., Rekha, V., Devi, B. L. A. P., Prasad, R. B. N., Prasad P. S. S. and Lingaiah N. (2010). Surface and structural properties of titania-supported Ru catalysts for hydrogenolysis of glycerol. Applied Catalysis A: General   384: 107 - 114.