Temperature Programmed Reduction and X-Ray Diffractometry Studies of MoO3 Reduction by Different ConcentrationS of Carbon Monoxide 

(Kajian Penurunan Suhu Berprogram dan Pembelauan Sinar-X 
Terhadap Penurunan MoO3 Menggunakan Kepekatan 
Karbon Monoksida Berbeza)
Alinda Samsuri1, 2*, Tengku Shafazila Tengku Saharuddin1, Fairous Salleh1, Rizafizah Othaman1, 
Mohamed Wahab Mohamed Hisham1, Mohd. Ambar Yarmo1
1Catalysis Research Group, 
School of Chemical Science and Food Technology, 
Faculty of Science and Technology, 
Universiti Kebangsaan Malaysia, 
43600 UKM Bangi, Selangor Darul Ehsan, Malaysia. 
2Centre for Defence Foundation Studies, 
Universiti Pertahanan Nasional Malaysia, 
Kem Sungai Besi, 57000 Kuala Lumpur, Malaysia
*Corresponding author: alindasamsuri@gmail.com
Abstract

Reduction of molybdenum trioxide, MoO3 to molybdenum dioxide, MoO2 by using carbon monoxide, CO has been studied by temperature programmed reduction (TPR) and X-ray diffraction spectroscopy (XRD). The influence of carbon monoxide concentration on the reduction of MoO3 have been investigated by comparing the reduction behaviour of MoO3 to MoO2 with 20 vol.% and 40 vol.% of CO concentration. The XRD results show that by using  20% of CO, reduction to MoO2 takes place at 700°C in 60 minutes. However, by using 40% of CO, complete reduction to MoO2 takes place at 700°C in only 30 minutes. Moreover, excess of CO results in the formation of molybdenum carbide, Mo2C. It is suggested that by using CO, complete reduction from MoO3 to MoO2 gives two-steps reduction (MoO3 → Mo4O11 → MoO2) with Mo4O11 as an intermediate product. It can be concluded that the reducing behavior of MoO3 is strongly dependent on the concentration of CO and reaction time.
Keyword: molybdenum trioxide, molybdenum dioxide, molybdenum carbide, carbon monoxide
Abstrak

Penurunan molibdenum trioksida, MoO3 kepada molibdenum dioksida, MoO2 dengan menggunakan karbon monoksida, CO telah dikaji menggunakan suhu penurunan berprogram (TPR) dan spektroskopi pembelauan sinar-X (XRD). Kesan kepekatan karbon monoksida terhadap penurunan MoO3 telah dikaji dengan membandingkan kesan penurunan MoO3 kepada MoO2 menggunakan kepekatan karbon monoksida di antara 20 % dan 40 %. Keputusan XRD menunjukkan bahawa dengan menggunakan 20 % kepekatan CO, penurunan kepada MoO2 berlaku pada suhu 700 °C dalam masa 60 minit. Walau bagaimanapun, dengan menggunakan 40 % kepekatan CO, penurunan lengkap kepada MoO2 berlaku pada suhu 700 °C dalam masa hanya 30 minit. Selain itu, pendedahan kepada CO berlebihan akan menyebabkan pembentukan molibdenum karbida, Mo2C. Adalah dicadangkan bahawa dengan menggunakan CO, penurunan lengkap daripada MoO3 kepada MoO2 terdiri daripada dua peringkat penurunan (MoO3 → Mo4O11 → MoO2) dengan menghasilkan Mo4O11 sebagai produk perantara. Ini boleh disimpulkan bahawa kelakuan penurunan MoO3 adalah amat bergantung kepada kepekatan CO dan tempoh masa tindak balas.
Kata kunci: molibdenum trioksida, molibdenum dioksida, molibdenum karbida, karbon monoksida
Introduction
Metallic molybdenum offers excellent mechanical, thermal and electric properties and good corrosion resistance and is widely used as an alloying agent for manufacturing steels, cast irons and super-alloys to increase their mechanical strength, hardness, swiftness and resistance to corrosion and wearing [1]. Molybdenum powder is manufactured in two-step process starting from MoO3. The first step reduction is exothermic in nature that is carried out at lower temperatures and involves transformation of MoO3 to MoO2. The second step reduction is endothermic in nature where MoO2 is further reduced to Mo [2]. The reduction of MoO3 to MoO2 is a crucial stage in the production of metallic molybdenum. The reduction of MoO3 to MoO2 by using hydrogen consists of two reduction stages, namely Mo6+ → Mo5+ and Mo5+ → Mo4+ [3]. It seems that during the reduction of MoO3, MoO3 is first reduced to Mo4O11, then to MoO2. Generally, pure molybdenum powders are produced using the well known two-step hydrogen reduction process [4]. The first step occurs in the temperature range of 450 - 650 °C and reduces the input material to MoO2. The second step reduction is performed in the 1000 - 1100 °C range and this process results the formation of molybdenum metal. Nevertheless, usage of hydrogen as a reducing agent of MoO3 reduction is expensive. Carbon is also used to reduce MoO3 at elevated temperature (600 - 1200 °C) [5]. When metal oxides react with carbon, one of the reaction products would be gaseous and could be readily separated from the solid reaction products [6]. Therefore, it would be highly desirable to develop an alternative process to manufacture molybdenum. Reduction of MoO3 by using CO as reductant was suggested as an alternative process for producing molybdenum. However, currently there are limited number of studies using CO for reduction of MoO3 to MoO2. In this study, we report the influence of CO content on the reduction behaviour of MoO3. The isothermal and non-isothermal temperature programmed reduction (TPR) was performed to investigate the reduction behaviour of MoO3 to MoO2 by using CO as a reducing agent and later characterizing by XRD. Reduction of MoO3 to MoO2 by CO was suggested to follow two reduction stages which are shown as Equation 1 and Equation 2.
4MoO3  +  CO  →  Mo4O11  +  CO2




   


   (1)

Mo4O11  +  3CO  →  4MoO2  +  3CO2




  

   (2)

Materials and Methods
Chemicals and raw materials 

Commercial molybdenum trioxide, MoO3 (AnalaR) powder was obtained from BDH Chemicals Ltd.. The gas mixture of carbon monoxide (CO) in nitrogen (20 and 40 vol % of CO) from Linde Malaysia was used.
Reduction of molybdenum trioxide 
The commercially bought MoO3 powder was calcined to remove impurities at 400 °C for 4 hours in air and then cooled to room temperature before undergo the reduction process by using a Micromeritic Autochem 2920 Chemisorption Analyzer apparatus. The completeness of the reduction of the powder was analysed using a temperature programmed reduction (TPR) method. In this experiment, a mixed gas of 20 % CO in 80 % nitrogen and 40 % CO in 60 % nitrogen was introduced into the apparatus at an effective flow rate of 20 mL/min. Then, temperature was increased from 40 to 700 °C with a heating rate of 10 °C/min and continued with isothermal reduction for 30 and 60 minutes at 700 °C.

Characterization method
The crystal structures of the MoO3 powder before and after reactions were determined by XRD's Bruker AXS D8 Advance type. The radiation source used was Cu Kα (40 kV, 40 mA) to record the 2θ diffraction angles from 10° to 80° at wavelength (λ = 0.154 nm). For identification purposes of crystalline phase composition, diffraction patterns obtained were matched with standard diffraction data (JCPDS) file. 
Results and Discussion
Thermodynamic Consideration Data

According to the thermodynamic analysis for the reduction of MoO3 by using CO as a reducing agent to the reaction in Equation 3 and Equation 4, the Gibbs free energy changes due to reaction and the equilibrium composition of the oxides was calculated. 

MoO3 +  CO  →  MoO2  +  CO2                    





               
    (3)                                                            

2MoO2 +  6CO →  Mo2C + 5CO2 






         
   (4)                                                                                                 
From the calculation, the Gibbs free energy for formation of MoO2 for reaction Equation 3 is ∆G(298 K) = -29.8 kcal/mol which clearly indicates that the reaction is favorable. However, if excess CO is introduced to the reduction system, the formation of Mo2C will take place according to reaction Equation 4 with the ∆G(298 K) = -34.9 kcal/mol which means the reaction is very spontaneous. 
Characterization by TPR

The reduction behaviour of MoO3 to MoO2 was studied using TPR. Figure 1 shows the TPR profile of non-isothermal reduction of MoO3 until 700 °C continued with isothermal reduction at 700 °C for 60 minutes by using 20% and 40% of CO in nitrogen. Complete reduction to MoO2 needs to complete at temperature lower than its melting point (795 °C) since MoO3 will end up as an alloy fused mass when it is taken to its melting point [5].

[image: image1.png]0.523

0.518

TCD Singnal (a.u.)
(e}
W
2

— TCD Signal

_____ Temperature

40% CO in N,

111

20% CO in N,

60
Time (min)

80

100

120

850

750

650

550

450

350

250

150

- 50

Temperature (°C)




Figure 1. TPR profile of non-isothermal reduction of MoO3 with 20% and 40% of CO in nitrogen at 40-700 °C and continued with isothermal reduction at 700 °C for 60 minutes.
The TPR profile of MoO3 represents two reduction events (denoted I and II) which event I owing to peak displayed at early reaction time may regard to the reduction of MoO3 to Mo4O11, while event II is subsequent to reduction steps of Mo4O11 to MoO2. However, with excess of CO supply to the reduction system, it brings to the formation of Mo2C. The profile monitor CO consumption peaks by using 20 % of CO in nitrogen which started at about 530 °C was pointed to the first stage of reduction (event I) in agreement with Dang et al. [7], as mentioned that the MoO3 is firstly reduced to Mo4O11, then to MoO2. After continuing the reaction with isothermal reduction at 700 °C for 40 minutes, new broad peak is observed due to sample changes that occurred, reflecting to second stage reduction of Mo4O11 to MoO2. 

Then, for the reduction of MoO3 in 40 % of CO atmosphere, the TPR profile shows two peaks that reflect the two stages of reduction. By increasing concentration of CO to 40 % CO, the reduction peaks are leading to a low temperature to 420 °C, while the second peak can be monitored after 10 minutes, starting off with isothermal reduction at 700 °C. It seems that, the reduction of MoO3 is observed to occur with a slight shift to lower temperature by increasing the concentration of CO. In addition, it shows that the reducing behaviour of MoO3 is strongly dependent on the concentration of CO. The phases formed after the reduction by TPR were analysed by recording XRD pattern of the residual obtained after selected reduction condition.

Characterization by XRD

To investigate the reduction behaviour of MoO3 by using different concentration of CO, the samples were collected and XRD patterns were measured. The XRD profile obtained in Figure 2 revealed the MoO3 (JCPDS 74-7383) was not yet reduced to MoO2 even after flowing with 20 % of CO until 700 °C. It is due to insufficient of CO and heat supply to the reaction. However, by flowing with 40% of CO the XRD patterns showed peaks that identified with MoO2 phases (JCPDS 76-1807). From the results, the reduction of MoO3 by using 20% and 40% of CO concentration shows two stages process (MoO3 → Mo4O11 → MoO2) in respect to a trace of intermediate Mo4O11 (JCPDS 89-0687) which presence is identified at 700 °C. It is comparable with literature reported by Lalik [8] that suggested formation of Mo4O11 as the earliest product in the reduction of MoO3. 

[image: image2.png]Intensity (a.u.)

a = MoO;
o 0 Mo,Oy,
® MoO,

40% CO in N,

2 Theta (deg)




Figure 2. XRD patterns of non-isothermal reduction of MoO3 with 20 % and 40 % of CO in nitrogen until       700 °C
Since MoO3 is not completely reduced to MoO2, isothermal reduction with 20 % and 40 % of CO in nitrogen was conducted at 700 °C for 30 minutes to complete reduction to MoO2. From the XRD profile obtained in Figure 3, it is seen that by using 20% of CO, the MoO2 peaks start to appear and MoO3 peaks nearly disappear. Most of the peaks are intermediate phases of Mo4O11. However, by using 40 % of CO, the intensity of MoO2 peaks sharply increase and intermediate phases of Mo4O11 completely disappear. It shows that, reduction to MoO2 in 20 % of CO concentration required higher heat supply to be accomplished compared by using 40 % of CO. It is seen that the higher concentration of CO will give the higher reduction to MoO3. 

[image: image3.png]Intensity (a.u.)

= MoO;

o Mo,Oyy

® MoO,

40% CO in N,

10

2 Theta (deg)

80




Figure 3. XRD patterns of non-isothermal reduction of MoO3 with 20 % and 40 % of CO in nitrogen until 700 °C and continued with isothermal reduction at 700 °C for 30 minutes
Isothermal reduction at 700 °C was increased to 60 minutes to study the reduction behaviour by excessing the CO supplied. Figure 4 shows the XRD patterns of isothermal reduction for 60 minutes by using 20 % and 40 % of CO. As it is shown, MoO3 was completely reduced to MoO2 after isothermal reduction using 20 % of CO at 700 °C for 60 minutes. Figure 4 show the formation of carbide will take place in excess of CO. This was confirmed by the XRD profile of 40 % of CO displayed a decrease in the intensity of the MoO2 peaks and new formation peaks of Mo2C (JCPDS 65-8766) when the isothermal reduction prolongs until 60 minutes. This XRD patterns match well to previously reported pattern for processing of Mo2C [9].
[image: image4.png]Intensity (a.u.)

® MoO,
o Mo,C 40% CO in N,
[ 3]
bt R R
.
°
°
20% CO in N,
°
°
oo
| JL | -\ : M
10 20 30 40

2 Theta (deg)





Figure 4. XRD patterns of non-isothermal reduction of MoO3 with 20% and 40% of CO in nitrogen until 700 °C and continued with isothermal reduction at 700 °C for 60 minutes
Conclusion
In conclusion, the reduction behaviour of MoO3 by TPR technique and XRD characterization shows that the reduction reaction of MoO3 is strongly dependent on the concentration of CO and reaction time. The reduction reaction follows the consecutive two-steps mechanism, namely, MoO3 is firstly reduced to Mo4O11 and then Mo4O11 is reduced to MoO2. However, if excess of CO is introduced to the system, the formation of Mo2C will take place.

Acknowledgement
The authors wish to thank the Ministry of Higher Education (MOHE) and Universiti Pertahanan Nasional Malaysia for funding staff’s scholarships and also Universiti Kebangsaan Malaysia (UKM) for funding this project under research grant number LRGS/BU/2011/USM-UKM/PG/02, BKBP-FST-K003323-2014, FRGS/2/2013/TK06/UKM/02/3, ETP-2013-066 as well as the Centre of Research and Innovation Management (CRIM) for the instruments facilities.
References
1. Manukyan, K., Davtyan, D., Bossert, J. and Kharatyan, S. (2011). Direct reduction of ammonium molybdate to elemental molybdenum by combustion reaction. Chemical Engineering Journal, 168 (2): 925 – 930.
2. Enneti, R. K. and Wolfe, T. A. (2012). Agglomeration during reduction of MoO3. International Journal of Refractory Metals and Hard Materials, 31: 47 – 50.
3. Wang, J., Ren, Z., Liu, W., Gao, F. and Zhou, M. (2009). Effects of RE2O3 doping on the reduction behavior of molybdenum oxide and properties of molybdenum powder. International Journal of Refractory Metals and Hard Materials, 27 (1): 155 – 158.
4. Saghafi, M., Heshmati-Manesh, S., Ataie, A. and Khodadadi, A. A. (2012). Synthesis of nanocrystalline molybdenum by hydrogen reduction of mechanically activated MoO3. International Journal of Refractory Metals and Hard Materials, 30 (1): 128 – 132.
5. Saghafi, M., Ataie, A. and Heshmati-Manesh, S. (2011). Effects of mechanical activation of MoO3/C powder mixture in the processing of nano-crystalline molybdenum. International Journal of Refractory Metals and Hard Materials, 29 (4): 419 – 423.
6. Satyajeet Chaudhury, V. V., Mukerjee, S. K. and Vaidya, V. N. (1997). Kinetics and mechanism of carbothermic reduction of MoO3 to Mo2C. Journal Alloys Compounds, 261: 105 – 113.
7. Dang, J., Zhang, G.-H., Chou, K. C., Reddy, R. G., He, Y. and Sun Y. (2013). Kinetics and mechanism of hydrogen reduction of MoO3 to MoO2. International Journal of Refractory Metals and Hard Materials, 41: 216 – 223.
8. Lalik, E. (2011). Kinetic analysis of reduction of MoO3 to MoO2. Catalysis Today, 169: 85 – 92.
9. Claridge, J. B., York, A. P. E., Brungs, A. J., Marquez-Alvarez, C., Sloan, J., Tsang, S. C.  and Green, M. L. H. (1998). New Catalysts for the Conversion of Methane to Synthesis Gas : Molybdenum and Tungsten Carbide. Journal of Catalysis, 180: 85 – 100. 



