Fatin et al:  
IMMOBILISED METAL AFFINITY CHROMATOGRAPHY (IMAC) BEADS FOR LYSOZYME SEPARATION: SYNTHESIS AND CHARACTERIZATION STUDY
Malaysian Journal of Analytical Sciences, Vol 20 No 3 (2016): 577 – 583
DOI: http://dx.doi.org/10.17576/mjas-2016-2003-17

[image: image1.png]¥,

2BKU  XS,BB8  Sem INOS, UMT
& 8



[image: image7.png]ANALIS




MALAYSIAN JOURNAL OF ANALYTICAL SCIENCES
Published by The Malaysian Analytical Sciences Society
IMMOBILISED METAL AFFINITY CHROMATOGRAPHY (IMAC) BEADS FOR LYSOZYME SEPARATION: SYNTHESIS AND CHARACTERIZATION STUDY

(Kromatografi Afiniti Logam Dipegun (IMAC) untuk Pemisahan Lysozim: Sintesis dan Kajian Pencirian)

Fatin Mohd Nasir1, Sofiah Hamzah1*, Amirah Hamzah1, Nora’aini Ali1, Marinah Mohd Ariffin2
1School of Ocean Engineering

2School of Marine Science and Environment
Universiti Malaysia Terengganu, 21030 Kuala Terengganu, Terengganu, Malaysia
*Corresponding author: sofiah@umt.edu.my
Received: 24 February 2015; Accepted: 27 October 2015
Abstract

Immobilized metal affinity chromatography (IMAC) has been established as a highly specific chromatographic technique for the production of enzymes and proteins including lysozyme. This study aimed to prepare and characterize the IMAC beads for lysozyme separation. Silica gel served as chromatographic matrix which has been coated with chitosan layer and crosslinked with glutaraldehyde (GTA-CTS-SiO2) since it is very convenient to promote fixation. Various IMAC ligands were immobilized by chelating 1500 mg/l Cu2+, Zn2+, Fe2+, Fe3+ and Al3+ ions, respectively on GTA-CTS-SiO2. IMAC which was immobilized with 1200mg/l Cu2+ exhibited the maximal immobilization capacity (27.08mg/g) of within 30 minutes incubation time. This fundamental study can be a momentous pathway to develop an efficient chromatographic system for lysozyme separation in the future. 

Keywords: silica gel, chitosan, glutaraldehyde, metal ions, copper (II) ion

Abstrak

Kromatografi afiniti logam dipegun (IMAC) telah diperlihatkan sebagai satu teknik kromatografi yang sangat spesifik untuk pengeluaran enzim dan protein termasuk lysozim. Kajian ini bertujuan untuk menyediakan dan mencirikan manik IMAC bagi tujuan pemisahan lysozim. Gel silika berperanan sebagai sokongan kepada kromatografi yang telah dilapisi dengan lapisan kitosan dan diaktifkan dengan glutaraldehid (GTA-CTS-SiO2) kerana kesesuaiannya yang berupaya menggalakkan lekatan. Beberapa ligan IMAC dengan kepekatan 1500mg/l (Cu2+, Zn2+, Fe2+, Fe3+ dan Al3+ ion) telah dipegunkan pada GTA-CTS-SiO2. IMAC yang dipegunkan dengan kepekatan 1200mg/l Cu2+ menunjukkan penjerapan  kapasiti yang maksimum (27.08 mg) dalam tempoh 30 minit masa pengeraman. Kajian asas ini boleh menjadi satu anjakan dalam langkah membangunkan sistem kromatografi yang berkesan untuk pengasingan lysozim pada masa akan datang.

Kata kunci: gel silika, kitosan, glutaraldehid, ion logam, ion kuprum (II) 
Introduction

Currently lysozyme has been commercially become as an important enzyme used due to the high specificity, selectivity and efficiency function in the industries. Potent bacteriostatic and bactericidal properties of lysozyme give a huge impact as an antimicrobial agent [1] for the human body and as the food preservative especially in extension shelf life in food industries. Small amount of lysozyme makes the process of purification becomes challenge and intricate especially for the large scale production. Conventionally, separation of lysozyme has been obtained by several techniques such as ion exchange chromatography, ultrafiltration and affinity chromatography. However rigorous limitations occur including lengthy steps, complicated and expensive for large scale production has hampered the applications. Separation technique for protein by Immobilized Metal Affinity Chromatograph (IMAC) has established [2] due to the ligand stability, high adsorption capacity, mild elution condition, simple regeneration and low cost [3]. Selection of IMAC solid chromatographic matrix to entrap metal ions for the best serve as affinity ligands for various proteins such a critical attention in order to meet the requirement of high efficiency and fast flow operation. Conventional supports for IMAC are based on soft gel that coating with dextran and agarose give the compressible and restricted low flow rate in chromatography operations [4]. Upgrading matrix with porous silica as an ideal IMAC support which has high mechanical resistance, insolubility and available for long shelf life inorganic materials. To achieve the maximum protein adsorption, surface of silica beads are modified by coating with a hydrophilic and functional natural polymer. According to Wu et al, silica beads cross-linked with chitosan indicate convenient matches for metal ion adsorption [5]. 
Chitosan (CTS) is widely used for the hydrophilic modification due to its biocompatibility, biodegradability, chemical innertness, high mechanical strength and non-toxic material [6]. Besides, amino and hydroxyl groups in chitosan molecules supplied active reaction sites for the various functional ligands, therefore it considered as an excellent matrix for IMAC. However, chitosan required a cross-linker to modify chemical structure and textural properties by linking at the amine or the hydroxyl sites. Glutaraldehyde (GTA) is the best chosen cross-linker for chitosan which has a porous network that could improve adsorption properties and helped to form quaternary structure on the surface of the materials, thus increase the content of protonated amino groups [7] as well as improved the chemical stability of chitosan in acidic solution [8]. Practically, IMAC is depend on the formation of coordinate bonds between immobilized metal ions such as Cu2+, Zn2+, Ni2+, and Fe2+ with the functional groups of exposed amino acids on the surface of the target protein [9].
Inspired by previous researches, we have prepared IMAC beads with porous silica based characterized by chitosan-glutaraldehyde modified polymer. ATR-FTIR was analysed to determine the binding of chitosan and crosslinking agent onto the silica beads. Then, modificated silica beads were studied the immobilized various metal ions sorption and the evaluation of optimum metal ion in different concentration by ICP-OES.
Materials and Methods

Chemicals and materials 

Silica gels (70-230 mesh size) were obtained by Merck Millipore. Chitosan as a modified polymer and glutaraldehyde were purchased by Sigma Aldrich. Glacial acetic acid, sodium hydroxide, hydrochloric acid, dimethylsulphoxide (DMSO), copper (II) sulfate, calcium sulfate, iron (II) sulfate, iron (III) sulfate and zinc sulfate were analytical grade reagents commercially available and used without further purification. 
Preparation of chitosan coated silica beads

Preparation of Chitosan-coated silica beads (CTS-SiO2) was according to Shi et al. [8] with some modification. Chitosan powder (5 g) was added into 250 ml of 1M acetic acid and dissolved by magnetic stirring for several minutes at room temperature and finally, the prepared chitosan solution was stored in a Schott bottle at room temperature. Initiate with treated 50 g of silica beads with 20 % of hydrochloric acid for 8 hours in incubator shaker at room temperature to obtain high adsorptive property of porous silica beads. The beads were rinsed with distilled water to remove the residual of hydrochloride inside silica beads and dried at 40 oC in oven. Prior to the surface coating, treated silica beads were immersed again into distilled water for 2 hours in order to wet the pore surface. An amount 10 g of silica beads were immersed into the chitosan solution and the flask containing the mixture was placed in the incubator shaker for the process of surface coating reaction at room temperature with 100 rpm for 72 hours. Subsequently, immersed chitosan coated silica beads with dimethylsulphoxide (DMSO) for one hour to enhance polarity of the surface. Coated beads were then added into sodium hydroxide (NaOH) solution (pH 8) for 2 hours to ensure solidify and fix the coating layer in the incubator shaker at 25 oC.

Beads activation and ligand immobilization
CTS-SiO2 beads were cross-linking with glutaraldehyde which can be form a Schiff’s base for chitosan. CTS-SiO2 beads were incubated in incubator shaker for 30 minutes in reacting solution containing 50 v/v % (25 % glutaraldehyde in 0.1M NaCl and 0.1M sodium acetate-acetic acid buffer pH 7.4) at room temperature. After adjusting pH to 6.0 by adding acetic acid, the flask was sealed and reaction was allowed to continue for 16 hours in the incubator at 25 oC. When the reaction achieved, the excess GTA was removed by washing the beads with distilled water.
Activated silica beads (GTA-CTS-SiO2) were reacted with 0.1M of five metal ions; CuSO4, FeSO4, Al2 (SO4)3, Fe(SO4)3 and ZnSO4 respectively for 20 hours in incubator shaker (100 rpm) at room temperature. The adsorbent were then rinsed with distilled water before storage or usage for the lysozyme adsorption. Prepared beads hereafter are called immobilized metal affinity chromatography (IMAC) beads. IMAC is operated based on the affinity adsorption between the metal-binding amino acids in the side chains of the proteins such as histidine, lysine, glutamic acid and etc as well as the metal ions including Cu2+, Fe3+, Fe2+, Al3+ and Zn2+ chelated by chelating ligand immobilized on the solid supports. The optimum metal ion immobilization has been chosen and verified the best concentration of metal ion before further studies with the evaluation performance of lysozyme adsorption.

IMAC characterization 

Prepared IMAC beads were characterized in terms of morphology and the structure were observed using Scanning Electron Microscope (SEM), while the presence of elements has been analyzed by inductively coupled plasma optical emission spectrometry (ICP-OES) and the determination of functional groups for modified beads by using Attenuated Total Reflectance Fourier Transform Infra-Red Spectroscopy (ATR-FTIR). 
Adsorption studies

After the metals concentration analysis using the ICP-OES, the amount of elements (Cu2+,Fe3+,Fe2+,Al3+ and Zn2+ ) immobilized on the beads, P(mg/g), were approximately calculated using the following equation 1: 
P (mg/g) = V (Co – Ce) / WD 







         (1)

where Co (mg/l) is the initial elements concentration; Ce (mg/l) is the final elements concentration after adsorption; V is the volume of the elements solution used; and WD (g) is the weight of beads.
Results and Discussion

IMAC characterization 
IMAC beads were achieved in several stages including treating silica beads with hydrochloric acid, chitosan coating, cross-linking with glutaraldehyde and metal chelating. Chitosan mechanism interaction with silica beads been established [10] and the glutaraldehyde cross-linking could exhibit high operational stability of chitosan beads was coated [11]. Amination of the residue epoxy groups of could recover the loss of primary amino group during cross-linking with glutaraldehyde [12]. Hydrophilic characteristics of activated beads were improved the tendency of matrix for metal ion immobilization in the final stage of IMAC preparation. The surface morphologies of silica bead treated with hydrochloric acid is shown in Figure 1(a). The treated silica beads displayed smooth and channel like surface. The surface morphologies of silica beads modified with chitosan-glutaraldehyde represented in Figure 1(b) covered with a layer of rough surface as well as Figure 1(c) presented the rough and highly porous surface structure which can exhibit surface area and reducing the mass transfer resistance and facilitated the diffusion of protein molecules.

The ATR-FTIR spectra of native and modified silica beads are represented in Figure 2. The large broad stretching band around 3400 cm-1 corresponds to the associated O-H stretching vibration of the hydroxyl groups and adsorbed water which means the hydrophilic character of the porous silica shown in Figure 2(a). The peaks at around 800 and 566 cm-1 are attributed to the typical symmetric and bending vibration of Si-O-Si in support framework of silica beads, respectively [13].

[image: image8.png]


        [image: image2.jpg]: <.
IMOS, UMT




[image: image3.png]0
18kU XS BEE.  Swam




Figure 1.  
SEM micrograph of (a) silica bead treated with hydrochloric acid (b) modified silica beads with chitosan glutaraldehyde (c) IMAC absorbent
[image: image4.emf]4000.0


3600


3200


2800


2400


2000


1800


1600


1400


1200


1000


800


600


400.0


0.0


5


10


15


20


25


30


35


40


45


50


55


60


65


70


75


80


85


90


95


100.0


cm-1


%T 


3403.77


1641.56


1209.60


975.24


799.19


566.06


3351.91


2120.08


1642.53


1437.86


1245.03


799.99


710.91


611.83


3339.97


1646.61


1228.89


968.35


798.33


679.78




4000.0 3600 3200 2800 2400 2000 1800 1600 1400 1200 1000 800 600 400.0

0.0

5

10

15

20

25

30

35

40

45

50

55

60

65

70

75

80

85

90

95

100.0

cm-1

%T 

3403.77

1641.56

1209.60

975.24

799.19

566.06

3351.91

2120.08

1642.53

1437.86

1245.03

799.99

710.91

611.83

3339.97

1646.61

1228.89

968.35

798.33

679.78


Figure 2.  ATR-FTIR spectra (a) silica beads (b) chitosan coated beads (c) GTA-CTS-SiO2
The band around 975 cm-1 from free silanol groups of silica disappeared or weakened after the modification (Figure 2(b)). The stretching vibration around 1640 cm-1 represent the C=N in amine reaction between amino groups in silica and chitosan and aldehyde groups in glutaraldehyde [14]. The chitosan cross-linked with glutaraldehyde (Figure 2(c)) illustrated peaks at 968 and 1200 cm-1 assigned to saccharide structure. Hence, all peaks summarized the characterization of chitosan and glutaraldehyde for IMAC support.

Immobilization capacity of metal ion onto IMAC matrix

According to the IMAC separation concept, the use of metal ions that covalently bound chelating compound on a solid chromatographic matrix serves as affinity ligands that were vital to entrap optimum target proteins. Immobilization capacities studies of several kinds of metal ions were investigated in order to choose the most excellent metal ion among them. The chosen of metal ions; Cu2+, Fe2+, Fe3+, Al3+ and Zn2+ ions rather than Ni2+ which is usually used in IMAC technique and has higher binding affinity for protein because of the leaking Ni2+ ions could cause human carcinogenic even in trace amount [15]. In this study, the GTA-CTS-SiO2 beads were used as IMAC supports and immobilization of ligand (metal ion) displayed in Figure 3.

[image: image5.png]35 4

30 A

25

20

15

10

Immobilization Capacity(ml/g)

60 90 120 150
Time(min)

—a—Al(ml/g)
—e—Fe2+(mli/g)
—=—Fe3+(mli/g)
—>—Cu(mg/1)

—&—7Zn(mg/l)




Figure 3.  Immobilization capacity of metal ions

The capacity of Fe3+, Fe2+ and Al3+ ions adsorption is the lower than surfactant modified chitosan beads. Those metal ions might not suitable for the chitosan coated beads adsorption. Fe3+ and Al3+ have been used for Ortho-phosphoserine (OPS) chelating compounds for immobilization in IMAC [16]. The adsorption capacities for Zn2+ is lower than Cu2+ otherwise still give high adsorbent amount. The maximal adsorption achieved at 30 minutes of incubation time. Obviously, Cu2+ is the high immobilized metal ion towards the GTA-CTS-SiO2 with the maximal capacity 28.07 mg/g within the optimum time incubation, 30 minutes. The apparent affinity of a protein for a metal chelate depends strongly on metal ions involved in coordination. To fulfil the requirement of high protein adsorption onto the IMAC beads, the particular concentration of metal ion need to be obtained.
The principle of IMAC towards the immobilization of protein on IMAC beads were mainly through the coordination between metal ions with electron donating side chain of residues such as histidine and crysteine hence known as important factors in determining the absolute concentration of immobilized metal ion [17].
Based on the calculated values which is analysed by ICP-OES, the optimum concentration amount that ideal to the IMAC beads is 1200 mg/l with maximal adsorption amount 286.11 mg/g (Figure 4). It shown that efficient ligand immobilization could be achieved when 1200 mg/l ligand were utilized. An increased of ligand concentration up to 1500 mg/l tend to the formation of precipitation due to the excess of Cu(II) and also effected the adsorption of further protein. This optimum concentration of ligand provided higher surface area and accessible for lysozyme to bind. The lower concentration of glutaraldehyde was maintained to give the sufficient amount of free amino groups of Cu2+ interaction on the chitosan beads as well as yielded better adsorption capacity. The glutaraldehyde method was served high endurance for the ligand immobilization [18]. Furthermore, Cu2+ adsorption was performed excellent at neutral pH to avoid the formation of Cu2+ hydroxide which could affect the adsorption capacity for the further protein recovery.


[image: image6.emf]0

50

100

150

200

250

300

350

300 600 900 1200 1500

immobilization capacity(mg/g)

Conc of Copper (mg/l)


Figure 4.  Immobilization capacity on different concentration of copper (II) ion

Conclusion

Preparation and characterization of IMAC beads were successfully performed by modification of silica beads with chitosan and glutaraldehyde as activated cross-linked. The morphology of modified polymer and IMAC absorbent was visualized by SEM and followed with the ATR-FTIR analysis, which was verified the presence of chitosan, glutaraldehyde and Cu2+ onto the IMAC surface. Maximum immobilization capacity of metal ion obtained using Cu2+ at 1200 mg/l and this finding could be used for further application of lysozyme adsorption. 
Acknowledgement
The authors would like to express a high gratitude to Ministry of Higher Education Malaysia for the funding of this research (ERGS 55097) and University Malaysia Terengganu (UMT) for all supports and contribution.
References

1. Evrim, B. A., Nalan, T., Candan, N. and Adil, D. (2007). Use of magnetic poly(glycidyl methacrylate)        monosize beads for the purification of lysozyme in batch system. Journal of Chromatography, 853(1-2): 105 – 113.
2. Mooney, J. T., Fredericks, D. P., Hearn and Milton T. W. (2013). Application of an IMAC cassette for the purification of N-terminally tagged proteins. Separation and Purification Technology, 120: 265 –274.
3. Arnold F. H. (1991). Metal affinity separations: a new dimension in protein processing. Biotechnology, 9 (2): 151– 156.
4. Gaberc-Porekar, V. and Menart, V. (2001). Perspectives of immobilized-metal affinity chromatography. Journal Biochemical and Biophysical Methods, 49 (1-3): 335 – 360.
5. Wu, F., Zhu, Y. and Jia Z. (2006). Preparation of dye–ligand affinity chromatographic packing’s based on monodisperse poly (glycidylmethacrylate-coethylenedimethacrylate) beads and their chromatographic properties. Journal Chromatography A, 1134(1–2): 45 – 50. 
6. Tan, T. W., Xu, W. J. and Zhang, S. R. (1997). The synthesis of chitosan coated affinity chromatography absorbent. Ion Exchange Adsorption. 13: 141 – 146.
7. Rose, D., Jöris, J., Hackermüller, J., Reiche, K., Li, Q. and Stadler, P. F.(2008). Duplicated RNA genes in teleost fish genomes. Journal of Bioinformatics and Computational Biology, 6(6): 1157 – 1175.
8. Shi, Q-H, Tian, Y, Dong, X-Y, Bai, S. and Sun. Y. (2003). Chitosan-coated silica beads as immobilized metal affinity support for protein adsorption. Biochemical Engineering Journal, 16: 317 – 322.

9. Xi, F. N. and Wu, J. M. (2004). Macroporous chitosan layer coated on non-porous silica gel as a support for metal chelate affinity chromatographic adsorbent. Journal Chromatography A, 1057: 41 – 47.

10. Singla, A. K. and Chawla, M. (2001). Chitosan: some pharmaceutical and biological aspects – an update. Journal of Pharmacy and Pharmacology, 53: 1047 – 1067.
11. Lee, Y. M., Nam, S. Y. and Woo, D. J. (1998). PV performance of β–chitosan membrane for water/alcohol mixtures. Journal of Polymer Engineering, 18(12): 131 – 146.
12. Altun, G. D and Cetinus, S. A. (2007). Immobilization of pepsin on chitosan beads. Food Chemistry 100:  964 – 971.
13. Qu, R., Zhang,Y., Qu, W., Sun, C., Chen, J., Ping, Y., Chen, H. and Niu, Y. (2013). Mercury adsorption by sulfur- and amidoxime-containing bifunctional silica gel based hybrid materials. Chemical Engineering Journal, 219: 51 – 61.
14. Cetinus, S. A., Sßahin, E. and Saraydin, D., (2009). Preparation of Cu(II) adsorbed chitosan beads for catalase immobilization. Food Chemistry, 114: 962 – 969.                 
15. Bal, W., Liang, R., Lukszo, J., Lee, S. H., Dizdaroglu, M. and Kasprzak, K. S. (2000). Ni(II) specifically cleaves the C-Terminal tail of the major variant of histone H2A and forms an oxidative damage-mediating complex with the cleaved-off octapeptide. Chemistry Research Toxicology, 13(7): 616 – 624.
16. Zachariou, M, Traverso, I. and Hearn, M. T. (1993). High-performance liquid chromatography of amino acids, peptides and proteins. CXXXI. O-phosphoserine as a new chelating ligand for use with hard Lewis metal ions in the immobilized-metal affinity chromatography of proteins. Journal of Chromatography, 646(1): 107 – 120.
17. Sun, J., H. Ma, Y. Liu, Y. Su, W. Xia and Yang, Y. (2012). Improved preparation of immobilized trypsin on superparamagnetic nanoparticles decorated with metal ions. Colloids Surfaces A: Physicochemical Engineering Aspects, 414: 190 – 197.
18. Guo, W. and Ruckenstein, E. (2003). Crosslinked glass fiber affinity membrane chromatography and its application to fibronectin separation. Journal Chromatography B,795: 61 – 72
     ISSN 1394 - 2506








b





a





c





(b)





(c)





(a)








582
577

_1524490953.xls
Chart1

		300		0.3243489167		0.3243489167

		600		3.8382333525		3.8382333525

		900		5.2213833501		5.2213833501

		1200		21.5035044457		21.5035044457

		1500		11.6		11.6



Adsorption capacity (mg/g)

Conc of Copper (mg/l)

immobilization capacity(mg/g)

156.0250941029

201.1307482424

223.8707852861

286.1081436339

293.0588118141



Sheet1

		

				Std conc		Reading1		Reading 2		Reading3		Average		STDEV

				0		13		21		25		19.67		6.11

				0.2		3048		2990		3032		3023.33		29.96

				0.4		6398		6454		6387		6413.00		35.93

				0.6		9309		9214		9434		9319.00		110.34

				0.8		13641		13595		13593		13609.67		27.15

				1		16554		16560		16441		16518.33		67.04





Sheet1

		0		6.1101009266		6.1101009266

		0.2		29.9555225849		29.9555225849

		0.4		35.9304884464		35.9304884464

		0.6		110.3403824536		110.3403824536

		0.8		27.1538824722		27.1538824722

		1		67.0397891801		67.0397891801



Concentration(mg/l)

Intensity(mg/l)

Std Curve Cu

19.6666666667

3023.3333333333

6413

9319

13609.6666666667

16518.3333333333



Sheet2

		

						ADSORPTION STUDY- DIFFERENT CONCENTRATIONS OF METAL ION

												Metal Ion Cu

						stdrd lama

						concentration		Initial intensity		Final intensity		Initial concentration		Final concentration		Adsorption capacity

						(mg/l)		(mg/l)		(mg/l)		(mg/l)		(mg/l)		(mg/g)

						30		2.20E+05		41871		1.31E+01		2.49E+00		2.66E+02

						30		2.20E+05		45709		1.31E+01		2.72E+00		2.60E+02

						30		2.20E+05		5.50E+04		1.31E+01		3.27E+00		2.47E+02

						Average										2.58E+02

						Std Dev										1.00E+01

						60		5.09E+05		3.66E+05		3.04E+01		2.18E+01		2.15E+02

						60		5.09E+05		3.64E+05		3.04E+01		2.17E+01		2.18E+02

						60		5.09E+05		3.38E+05		3.04E+01		2.02E+01		2.56E+02

						Average										2.30E+02

						Std Dev										2.27E+01

						90		7.52E+05		5.38E+05		4.50E+01		3.21E+01		3.21E+02

						90		7.52E+05		5.44E+05		4.50E+01		3.25E+01		3.13E+02

						90		7.52E+05		5.37E+05		4.50E+01		3.21E+01		3.23E+02

						Average										3.19E+02

						Std Dev										5.40E+00

						120		1.00E+06		8.00E+05		6.00E+01		4.78E+01		3.05E+02

						120		1.00E+06		8.11E+05		6.00E+01		4.84E+01		2.88E+02

						120		1.00E+06		8.62E+05		6.00E+01		5.15E+01		2.11E+02

						Average										2.68E+02

						Std Dev										4.99E+01

						150		1.27E+06		1.06E+06		7.61E+01		6.35E+01		3.16E+02

						150		1.27E+06		1.06E+06		7.61E+01		6.33E+01		3.21E+02

						150		1.27E+06		1.04E+06		7.61E+01		6.24E+01		3.43E+02

						Average										3.27E+02

						Std Dev										1.44E+01





Sheet3

		

						std lama

						Concentration		Adsorption capacity

						(mg/l)		(mg/g)

						30.0		2.58E+02

						60.0		2.30E+02

						90.0		3.19E+02

						120.0		2.68E+02

						150.0		3.27E+02

						Concentration		Stdev

						(mg/l)

						30.0		1.00E+01

						60.0		2.27E+01

						90.0		5.40E+00

						120.0		4.99E+01

						150.0		1.44E+01





Sheet3

		30		10.0436677372		10.0436677372

		60		22.7446409648		22.7446409648

		90		5.3950024645		5.3950024645

		120		49.9397847635		49.9397847635

		150		14.4286761973		14.4286761973



concentration(ppm)

adsorption capacuty(ppm)

Effect of Different Cu Concentration towards the Adsorption Capacity

257.7601322419

229.6746529645

318.6690964131

268.0576766047

327.0238393977



Sheet4

		

								NEW STANDARD

								concentration		Initial intensity		Final intensity		Initial concentration		Final concentration		Adsorption capacity

								(mg/l)		(mg/l)		(mg/l)		(mg/l)		(mg/l)		(mg/g)

								30		2.20E+05		41871		9.86E+00		1.88E+00		2.00E+02

								30		2.20E+05		45709		9.86E+00		2.05E+00		1.95E+02

								30		2.20E+05		5.50E+04		9.86E+00		2.46E+00		1.85E+02

								Average										1.93E+02

								Std Dev										7.55E+00

								60		5.09E+05		3.66E+05		2.29E+01		1.64E+01		1.61E+02

								60		5.09E+05		3.64E+05		2.29E+01		1.63E+01		1.63E+02

								60		5.09E+05		3.38E+05		2.29E+01		1.52E+01		1.92E+02

								Average										1.72E+02

								Std Dev										1.71E+01

								90		7.52E+05		5.38E+05		3.38E+01		2.42E+01		2.41E+02

								90		7.52E+05		5.44E+05		3.38E+01		2.44E+01		2.34E+02

								90		7.52E+05		5.37E+05		3.38E+01		2.41E+01		2.42E+02

								Average										2.39E+02

								Std Dev										4.06E+00

								120		1.00E+06		8.00E+05		4.51E+01		3.59E+01		2.29E+02

								120		1.00E+06		8.11E+05		4.51E+01		3.64E+01		2.16E+02

								120		1.00E+06		8.62E+05		4.51E+01		3.87E+01		1.58E+02

								Average										2.01E+02

								Std Dev										3.75E+01

								150		1.27E+06		1.06E+06		5.72E+01		4.77E+01		2.37E+02

								150		1.27E+06		1.06E+06		5.72E+01		4.76E+01		2.41E+02

								150		1.27E+06		1.04E+06		5.72E+01		4.69E+01		2.58E+02

								Average										2.45E+02

								Std Dev										1.08E+01





Sheet5

		

				standard baru

						Concentration		Adsorption capacity

						(mg/l)		(mg/g)

						30.0		1.93E+02

						60.0		1.72E+02

						90.0		2.39E+02

						120.0		2.01E+02

						150.0		2.45E+02

						Concentration		Stdev

						(mg/l)

						30.0		7.55E+00

						60.0		1.71E+01

						90.0		4.06E+00

						120.0		3.75E+01

						150.0		1.08E+01





Sheet5

				7.5500052512		7.5500052512

				17.0975547194		17.0975547194

				4.0555201549		4.0555201549

				37.5406322743		37.5406322743

				10.8462947907		10.8462947907



concentartion(ppm)

adsortion capacity(ppm)

effect of different cu concentration towards adsorption capacity



Sheet6

		

						SELECT THE BEST REPLICATION IN THREE READING

						concentration		Initial intensity		Final intensity		Initial concentration		Final concentration		Adsorption capacity

						(mg/l)		(mg/l)		(mg/l)		(mg/l)		(mg/l)		(mg/g)

						30		2.20E+05		54916		1.31E+01		3.27E+00		2.47E+02

						30		2.20E+05		54852		1.31E+01		3.26E+00		2.47E+02

						30		2.20E+05		5.51E+04		1.31E+01		3.28E+00		2.46E+02

						Average										2.47E+02

						Std Dev										1.82E-01

						60		5.09E+05		3.64E+05		3.04E+01		2.17E+01		2.18E+02

						60		5.09E+05		3.63E+05		3.04E+01		2.17E+01		2.19E+02

						60		5.09E+05		3.65E+05		3.04E+01		2.18E+01		2.17E+02

						Average										2.18E+02

						Std Dev										1.32E+00

						90		7.52E+05		5.38E+05		4.50E+01		3.21E+01		3.21E+02

						90		7.52E+05		5.35E+05		4.50E+01		3.20E+01		3.25E+02

						90		7.52E+05		5.37E+05		4.50E+01		3.21E+01		3.22E+02

						Average										3.23E+02

						Std Dev										2.07E+00

						120		1.00E+06		7.99E+05		6.00E+01		4.77E+01		3.06E+02

						120		1.00E+06		8.00E+05		6.00E+01		4.78E+01		3.05E+02

						120		1.00E+06		8.01E+05		6.00E+01		4.78E+01		3.03E+02

						Average										3.05E+02

						Std Dev										1.67E+00

						150		1.27E+06		1.04E+06		7.61E+01		6.20E+01		3.53E+02

						150		1.27E+06		1.05E+06		7.61E+01		6.27E+01		3.36E+02

						150		1.27E+06		1.05E+06		7.61E+01		6.25E+01		3.41E+02

						Average										3.43E+02

						Std Dev										8.66E+00





Sheet7

		

						Concentration		Adsorption Capacity

						(mg/l)		(mg/g)

						30.0		2.47E+02

						60.0		2.18E+02

						90.0		3.23E+02

						120.0		3.05E+02

						150.0		3.43E+02

						Concentration		Stdev

						(mg/l)

						30.0		1.82E-01

						60.0		1.32E+00

						90.0		2.07E+00

						120.0		1.67E+00

						150.0		8.66E+00





Sheet7

				0.1823044309		0.1823044309

				1.3182995896		1.3182995896

				2.0733543685		2.0733543685

				1.6654797472		1.6654797472

				8.6614180186		8.6614180186



Concentration(ppm)

Adsorption Capacity(ppm)

Effect of Different Cu Concentration Towards Adsorption Capacity



Sheet8

		

						concentration		Initial intensity		Final intensity		Initial concentration		Final concentration		Adsorption capacity

						(mg/l)		(mg/l)		(mg/l)		(mg/l)		(mg/l)		(mg/g)

						300		4.09E+04		15157		2.45E+00		8.93E-01		1.56E+02

						300		4.09E+04		15132		2.45E+00		8.91E-01		1.56E+02

						300		4.09E+04		1.52E+04		2.45E+00		8.97E-01		1.56E+02

						Average										1.56E+02

						Std Dev										3.24E-01

						600		8.24E+04		4.84E+04		4.94E+00		2.88E+00		2.06E+02

						600		8.24E+04		4.95E+04		4.94E+00		2.95E+00		1.99E+02

						600		8.24E+04		4.95E+04		4.94E+00		2.95E+00		1.99E+02

						Average										2.01E+02

						Std Dev										3.84E+00

						900		1.24E+05		8.72E+04		7.40E+00		5.20E+00		2.21E+02

						900		1.24E+05		8.57E+04		7.40E+00		5.11E+00		2.30E+02

						900		1.24E+05		8.71E+04		7.40E+00		5.19E+00		2.21E+02

						Average										2.24E+02

						Std Dev										5.22E+00

						1200		1.71E+05		1.24E+05		1.02E+01		7.42E+00		2.80E+02

						1200		1.71E+05		1.26E+05		1.02E+01		7.54E+00		2.68E+02

						1200		1.71E+05		1.19E+05		1.02E+01		7.12E+00		3.10E+02

						Average										2.86E+02

						Std Dev										2.15E+01

						1500		2.19E+05		1.71E+05		1.31E+01		1.02E+01		2.86E+02

						1500		2.19E+05		1.71E+05		1.31E+01		1.02E+01		2.87E+02

						1500		2.19E+05		1.68E+05		1.31E+01		1.00E+01		3.06E+02

						Average										2.93E+02

						Std Dev										1.16E+01





Sheet9

		

				Concentration		Adsorption capacity

				(mg/l)		(mg/g)

				300		1.56E+02

				600		2.01E+02

				900		2.24E+02

				1200		2.86E+02

				1500		2.93E+02

				Concentration		Stdev

				(mg/l)

				300		0.324

				600		3.838

				900		5.221

				1200		21.504

				1500		11.600





Sheet9

								0.3243489167		0.3243489167

								3.8382333525		3.8382333525

								5.2213833501		5.2213833501

								21.5035044457		21.5035044457

								11.6		11.6



concentration(ppm)

Adsorption capacity(ppm)

Effect of Cu Concentration towards the Adsorption Capacity



Sheet10

		

				Concentration		Adsorption capacity		Stdev

				(mg/l)		(mg/g)

				300		156.03		0.32

				600		201.13		3.84

				900		223.87		5.22

				1200		286.11		21.50

				1500		293.06		11.60





Sheet10

				0.3243489167		0.3243489167

				3.8382333525		3.8382333525

				5.2213833501		5.2213833501

				21.5035044457		21.5035044457

				11.6		11.6



Adsorption capacity (mg/g)

Conc (mg/l)

Adsorption capacity(mg/g)

copper(II) concentration




