Malaysian Journal of Analytical Sciences Vol 20 No 3 (2016): 578 - 584

IMMOBILISED METAL AFFINITY CHROMATOGRAPHY (IMAC) BEADS FOR LYSOZYME SEPARATION: SYNTHESIS AND CHARACTERIZATION STUDY

# (Kromatografi Afiniti Logam Dipegun (IMAC) untuk Pemisahan Lysozim: Sintesis dan Kajian Pencirian)

# Fatin Mohd Nasir1, Sofiah Hamzah1*, Amirah Hamzah1, Nora’aini Ali1, Marinah Mohd Ariffin2

# 1School of Ocean Engineering

# 2School of Marine Science and Environment

# Universiti Malaysia Terengganu, 21030 Kuala Terengganu, Terengganu, Malaysia

*Corresponding author: sofiah@umt.edu.my

Received: 24 February 2015; Accepted: 27 October 2015

Abstract

Immobilized metal affinity chromatography (IMAC) has been established as a highly specific chromatographic technique for the production of enzymes and proteins including lysozyme. This study aimed to prepare and characterize the IMAC beads for lysozyme separation. Silica gel served as chromatographic matrix which has been coated with chitosan layer and crosslinked with glutaraldehyde (GTA-CTS-SiO2) since it is very convenient to promote fixation. Various IMAC ligands were immobilized by chelating 1500 mg/l Cu2+, Zn2+, Fe2+, Fe3+ and Al3+ ions, respectively on GTA-CTS-SiO2. IMAC which was immobilized with 1200mg/l Cu2+ exhibited the maximal immobilization capacity (27.08mg/g) of within 30 minutes incubation time. This fundamental study can be a momentous pathway to develop an efficient chromatographic system for lysozyme separation in the future.

Keywords: silica gel, chitosan, glutaraldehyde, metal ions, copper (II) ion

Abstrak

Kromatografi afiniti logam dipegun (IMAC) telah diperlihatkan sebagai satu teknik kromatografi yang sangat spesifik untuk pengeluaran enzim dan protein termasuk lysozim. Kajian ini bertujuan untuk menyediakan dan mencirikan manik IMAC bagi tujuan pemisahan lysozim. Gel silika berperanan sebagai sokongan kepada kromatografi yang telah dilapisi dengan lapisan kitosan dan diaktifkan dengan glutaraldehid (GTA-CTS-SiO2) kerana kesesuaiannya yang berupaya menggalakkan lekatan. Beberapa ligan IMAC dengan kepekatan 1500mg/l (Cu2+, Zn2+, Fe2+, Fe3+ dan Al3+ ion) telah dipegunkan pada GTA-CTS-SiO2. IMAC yang dipegunkan dengan kepekatan 1200mg/l Cu2+ menunjukkan penjerapan  kapasiti yang maksimum (27.08 mg) dalam tempoh 30 minit masa pengeraman. Kajian asas ini boleh menjadi satu anjakan dalam langkah membangunkan sistem kromatografi yang berkesan untuk pengasingan lysozim pada masa akan datang.

# Kata kunci: gel silika, kitosan, glutaraldehid, ion logam, ion kuprum (II)

References

- Evrim, B. A., Nalan, T., Candan, N. and Adil, D. (2007). Use of magnetic poly(glycidyl methacrylate)  monosize beads for the purification of lysozyme in batch system. Journal of Chromatography, 853(1-2): 105 – 113.

- Mooney, J. T., Fredericks, D. P., Hearn and Milton T. W. (2013). Application of an IMAC cassette for the purification of N-terminally tagged proteins. Separation and Purification Technology, 120: 265 –274.

- Arnold F. H. (1991). Metal affinity separations: a new dimension in protein processing. Biotechnology, 9 (2): 151– 156.

- Gaberc-Porekar, V. and Menart, V. (2001). Perspectives of immobilized-metal affinity chromatography. Journal Biochemical and Biophysical Methods, 49 (1-3): 335 – 360.

- Wu, F., Zhu, Y. and Jia Z. (2006). Preparation of dye–ligand affinity chromatographic packing’s based on monodisperse poly (glycidylmethacrylate-coethylenedimethacrylate) beads and their chromatographic properties. Journal Chromatography A, 1134(1–2): 45 – 50.

- Tan, T. W., Xu, W. J. and Zhang, S. R. (1997). The synthesis of chitosan coated affinity chromatography absorbent. Ion Exchange Adsorption. 13: 141 – 146.

- Rose, D., Jöris, J., Hackermüller, J., Reiche, K., Li, Q. and Stadler, P. F.(2008). Duplicated RNA genes in teleost fish genomes. Journal of Bioinformatics and Computational Biology, 6(6): 1157 – 1175.

- Shi, Q-H, Tian, Y, Dong, X-Y, Bai, S. and Sun. Y. (2003). Chitosan-coated silica beads as immobilized metal affinity support for protein adsorption. Biochemical Engineering Journal, 16: 317 – 322.

- Xi, F. N. and Wu, J. M. (2004). Macroporous chitosan layer coated on non-porous silica gel as a support for metal chelate affinity chromatographic adsorbent. Journal Chromatography A, 1057: 41 – 47.

- Singla, A. K. and Chawla, M. (2001). Chitosan: some pharmaceutical and biological aspects – an update. Journal of Pharmacy and Pharmacology, 53: 1047 – 1067.

- Lee, Y. M., Nam, S. Y. and Woo, D. J. (1998). PV performance of β–chitosan membrane for water/alcohol mixtures. Journal of Polymer Engineering, 18(12): 131 – 146.

- Altun, G. D and Cetinus, S. A. (2007). Immobilization of pepsin on chitosan beads. Food Chemistry 100:  964 – 971.

- Qu, R., Zhang,Y., Qu, W., Sun, C., Chen, J., Ping, Y., Chen, H. and Niu, Y. (2013). Mercury adsorption by sulfur- and amidoxime-containing bifunctional silica gel based hybrid materials. Chemical Engineering Journal, 219: 51 – 61.

- Cetinus, S. A., Sßahin, E. and Saraydin, D., (2009). Preparation of Cu(II) adsorbed chitosan beads for catalase immobilization. Food Chemistry, 114: 962 – 969.

- Bal, W., Liang, R., Lukszo, J., Lee, S. H., Dizdaroglu, M. and Kasprzak, K. S. (2000). Ni(II) specifically cleaves the C-Terminal tail of the major variant of histone H2A and forms an oxidative damage-mediating complex with the cleaved-off octapeptide. Chemistry Research Toxicology, 13(7): 616 – 624.

- Zachariou, M, Traverso, I. and Hearn, M. T. (1993). High-performance liquid chromatography of amino acids, peptides and proteins. CXXXI. O-phosphoserine as a new chelating ligand for use with hard Lewis metal ions in the immobilized-metal affinity chromatography of proteins. Journal of Chromatography, 646(1): 107 – 120.

- Sun, J., H. Ma, Y. Liu, Y. Su, W. Xia and Yang, Y. (2012). Improved preparation of immobilized trypsin on superparamagnetic nanoparticles decorated with metal ions. Colloids Surfaces A: Physicochemical Engineering Aspects, 414: 190 – 197.

- Guo, W. and Ruckenstein, E. (2003). Crosslinked glass fiber affinity membrane chromatography and its application to fibronectin separation. Journal Chromatography B,795: 61 – 72