Malaysian Journal of Analytical Sciences Vol 20 No 3 (2016): 642 - 650

FABRICATION OF Y-TZP FOR DENTAL CROWNS APPLICATIONS BY COMBINING SLIP CASTING AND COLD ISOSTATIC PRESSING

(Pembangunan Y-TZP untuk Aplikasi Korona Gigi melalui Penggabungan Kaedah Penuangan Buburan dan Penekanan Isostatik Sejuk)

Chin Chuin Hao1, Andanastuti Muchtar1,2*, Che Husna Azhari1, Masfueh Razali3, Mohamed Aboras1

1Department of Mechanical and Materials Engineering, Faculty of Engineering and Built Environment

2Fuel Cell Institute

Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor, Malaysia.

3Periodontology Department, Faculty of Dentistry,

Universiti Kebangsaan Malaysia, Jalan Raja Muda Abdul Aziz, 50300 Kuala Lumpur, Malaysia.

*Corresponding author: muchtar@ukm.edu.my

Received: 5 February 2016; Accepted: 22 April 2016

Abstract

Yttria-stabilized tetragonal zirconia polycrystalline (Y-TZP) is a popular material for dental restoration because of its outstanding mechanical properties and biocompatibility. Cold isostatic pressing (CIP) and slip casting are among several consolidation methods for Y-TZP. These methods produce Y-TZP with high mechanical properties. This study aims to enhance the mechanical properties of Y-TZP by combining slip casting and CIP. Y-TZP samples were fabricated using CIP, slip casting, and their combination. Subsequently, the green bodies of the samples were sintered at 1600 °C. Their mechanical properties (density and hardness) were tested and their microstructures were scrutinized under a scanning electron microscope. Compared with the other two methods, the combined method significantly improved the mechanical properties of Y-TZP. In addition, the combined method also produced a compact and homogeneous microstructure. Therefore, the combination of slip casting and CIP is recommended in the production of Y-TZP with high mechanical properties for dental crown applications.

Keywords:  cold isostatic pressing, slip casting, colloidal processing

Abstrak

Polikristal tetragon zirkonia yang distabilkan dengan yttria (Y-TZP) merupakan bahan restorasi pergigian yang popular disebabkan sifat mekanik dan bioserasi yang baik. Kaedah penekanan isostatik sejuk (CIP) dan penuangan buburan adalah kaedah pengukuhan yang lazim digunakan untuk Y-TZP. Kedua-dua kaedah ini berupaya menghasilkan Y-TZP yang bersifat mekanik tinggi. Kajian ini bertujuan meningkatkan sifat mekanik Y-TZP melalui gabungan penuangan buburan dan CIP. Sampel Y-TZP dihasilkan melalui kaedah penuangan buburan, CIP dan gabungan kedua-dua kaedah tersebut. Seterusnya, jasad anum yang terhasil disinter pada suhu 1600 ˚C. Sifat mekanik sampel Y-TZP (ketumpatan dan kekerasan) diuji dan mikrostruktur juga diteliti di bawah mikroskop elektron imbasan. Kaedah gabungan didapati meningkatkan sifat mekanik Y-TZP dengan ketara. Selain itu, mikrostruktur yang padat dan homogen juga diperolehi. Justeru, gabungan kaedah penuangan buburan dan CIP dicadangkan untuk penghasilan Y-TZP yang bersifat mekanik tinggi dalam aplikasi korona gigi.

Kata kunci:  penekanan isostatik sejuk, penuangan buburan, pemprosesan berkoloid

References

- Vleugels, J., Yuan, Z. X. and Van Der Biest, O. (2002). Mechanical properties of Y2O3/Al2O3-coated Y-TZP ceramics. Journal of the European Ceramic Society, 22 (6): 873 - 881.

- Xu, T., Vleugels, J., Van Der Biest, O., Kan, Y. and Wang, P. (2006). Phase stability and mechanical properties of TZP with a low mixed Nd2O3/Y2O3 stabiliser content. Journal of the European Ceramic Society, 26 (7): 1205 - 1211.

- Piconi, C., Condo, S. G. and Kosmač, T. (2014). Chapter 11 - Alumina- and zirconia-based ceramics for load-bearing applications. Advanced Ceramics for Dentistry, 219 - 253.

- Ozturk, O., Uludag, B., Usumez, A., Sahin, V. and Celik, G. (2008). The effect of ceramic thickness and number of firings on the color of two all-ceramic systems. The Journal of Prosthetic Dentistry, 100 (2): 99 - 106.

- Manicone, P. F., Rossi, I. P. and Raffaelli, L. (2007). An overview of zirconia ceramics: basic properties and clinical applications. Journal of Dentistry, 35 (11): 819 - 826.

- Persson, C., Unosson, E., Ajaxon, I., Engstrand, J., Engqvist, H. and Xia, W. (2012). Nano grain sized zirconia–silica glass ceramics for dental applications. Journal of the European Ceramic Society, 32 (16): 4105 - 4110.

- Lewis, J. A. (2000). Colloidal processing of ceramics. Journal of the American Ceramic Society, 83 (10): 2341 - 2359.

- Briscoe, B. J., Khan, A. U. and Luckham, P. F. (1998). Stabilising zirconia aqueous suspensions using commercial polyvalent electrolyte solutions. Journal of the European Ceramic Society, 18 (14): 2169 - 2173.

- Rafferty, A., Alsebaie, A. M., Olabi, A. G. and Prescott, T. (2009). Properties of zirconia-toughened-alumina prepared via powder processing and colloidal processing routes. Journal of Colloid and Interface Science, 329 (2): 310 - 315.

- Zakaria, H., Muhamad, N., Sulong, A. B., Ibrahim, M. H. I. and Foudzi, F. (2014). Moldability characteristics of 3 mol% yttria stabilized zirconia feedstock for micro-powder injection molding process. Sains Malaysiana, 43 (1): 129 - 136.

- Osman, N., Ibarahim, N., Ishak, M. A. M. and Hassan, O. H. (2014). Characterization of cerate-zirconate ceramics powder prepared by three different methods: A comparative study. Sains Malaysiana, 43 (9): 1373 - 1378.

- Ani, S. M., Muchtar, A., Muhamad, N. and Ghani, J. A. (2013). Characterisation of mixing uniformity and rheological properties of alumina-zirconia powder for ceramic injection moulding.  Sains Malaysiana, 42 (9): 1311 - 1317.

- Ng, L. S., Loh, N. L. and Boey, F. Y. C. (1997). Cold-hot isostatic pressing of Mar M200 superalloy powders. Journal of Materials Processing Technology, 67 (1-3): 143 - 149.

- Henderson, R. J., Chandler, H. W., Akisanya, A. R., Barber, H. and Moriarty, B. (2000). Finite element modelling of cold isostatic pressing.  Journal of the European Ceramic Society, 20 (8): 1121 - 1128.

- Mouzon, J., Glowacki, E. and Odén, M. (2008). Comparison between slip-casting and uniaxial pressing for the fabrication of translucent yttria ceramics. Journal of Materials Science, 43 (8): 2849 - 2856.

- Rafferty, A., Alsebaie, A. M., Olabi, A. G. and Prescott, T. (2009). Properties of zirconia-toughened-alumina prepared via powder processing and colloidal processing routes. Journal of Colloid and Interface Science, 329 (2): 310 - 315.

- Rami, M.-L., Meireles, M., Cabane, B. and Guizard, C. (2009). Colloidal stability for concentrated zirconia aqueous suspensions. Journal of the American Ceramic Society, 92: 50 - 56.

- Amat, N. F., Muchtar, A., Ghazali, M. J. and Yahaya, N. (2014). Suspension stability and sintering influence on yttria-stabilized zirconia fabricated by colloidal processing. Ceramics International, 40 (4): 5413 - 5419.

- Liu, Y. and Gao, L. (2003). Deflocculation study of aqueous nanosized Y–TZP suspensions. Materials Chemistry and Physics, 78 (2): 480 - 485.

- Chin, C. H., Muchtar, A., Azhari, C. H., Razali, M. and Aboras, M. (2015). Optimization of pH and dispersant amount of Y-TZP suspension for colloidal stability. Ceramics International, 41 (8): 9939 - 9946.

- Balakrishna, P., Narasimha Murty, B. and Anuradha, M. (2009). A New process based agglomeration parameter to characterize ceramic powders. Journal of Nuclear Materials, 384 (2): 190 - 193.

- Trunec, M. and Maca, K. (2014). Chapter 7 - Advanced ceramic processes. Advanced Ceramics for Dentistry, 123 - 150.

- Muchtar, A. and Lim, L. C. (1998). Indentation fracture toughness of high purity submicron alumina. Acta Materialia, 46 (5): 1683 - 1690.

- Lange, F. F. (1982). Transformation toughening. Journal of Materials Science, 17 (1): 240 - 246.

- Bravo-Leon, A., Morikawa, Y., Kawahara, M. and Mayo, M. J. (2002). Fracture toughness of nanocrystalline tetragonal zirconia with low yttria content. Acta Materialia, 50 (18): 4555 - 4562.

- Zhang, Y. (2014). Making yttria-stabilized tetragonal zirconia translucent. Dental Materials, 30 (10): 1195 - 1203.