Malaysian Journal of Analytical Sciences Vol 20 No 3 (2016): 484 - 490

CORROSION INHIBITION OF Q235A STEEL IN ACID MEDIUM USING ISATIN DERIVATIVES: A QSAR STUDY

(Perencatan Kakisan Keluli Q235A di dalam Medium Asid Menggunakan Terbitan Isatin: Satu Kajian QSAR)

Abdo M. Al-Fakih1,2, Madzlan Aziz1*, Hassan H. Abdallah3, Hasmerya Maarof1, Rosmahaida Jamaludin1,

Bishir Usman1

1Department of Chemistry, Faculty of Science,

University Technology Malaysia, 81310 UTM Johor Bahru, Johor, Malaysia

2Department of Chemistry, Faculty of Science,

Sana’a University, Sana’a, Yemen

3Department of Chemistry, College of Education,

Salahaddin University, Erbil, Iraq

*Corresponding author: madzlan@utm.my

Received: 9 December 2014; Accepted: 22 March 2016

Abstract

Quantitative Structure-Activity Relationship (QSAR) study was performed on 10 isatin derivatives which were reportedly used as corrosion inhibitors. Dragon software was used to calculate the molecular descriptors. Partial least square (PLS) method was used to run the regression analysis between the descriptors and the corrosion inhibition efficiencies (IE) of the inhibitors. A predictive QSAR model was developed with a correlation coefficient (r2cal) of 0.9676. The model validity was assessed through internal and external validation. The results show that cross-validation regression coefficient (r2cv) and prediction regression coefficient (r2pred) are 0.8163 and 0.9189, respectively. The model was used to predict the IE for ten isatin derivatives. The results confirm a good stability and predictive ability of the model. Dragon-based descriptors provide a very good description of the corrosion inhibition properties of the inhibitors. The results of the QSAR study were found to be consistent with the experimental data.

Keywords: QSAR modeling study, corrosion inhibition, isatin derivatives, partial least square

Abstrak

Kajian hubungan aktiviti-struktur kuantitatif (QSAR) dilaksanakan ke atas 10 terbitan isatin yang dilaporkan diguna sebagai perencat kakisan.  Perisian Dragon digunakan untuk mengira pemerihal molekul.  Kaedah kuasa dua terkecil separa (PLS) digunakan untuk melaksanakan analisis regresi antara pemerihal dan keberkesanan perencatan kakisan (IE) terhadap perencat kakisan.  Ramalan model QSAR dibangunkan dengan pekali kolerasi (r2cal) bernilai 0.9676.  Kesahan model dinilai melalui pengesahan dalaman dan luaran.  Keputusan menunjukkan bahawa pekali regresi kesahan-silang (r2cv) dan pekali regresi ramalan (r2pred) adalah masing-masingnya 0.8163 dan 9189.  Model tersebut digunakan untuk meramal IE bagi 10 terbitan isatin.  Keputusan mengesahkan kestabilan dan kemampuan ramalan yang baik terhadap model.  Pemerihal berasaskan Dragon memberi penerangan yang baik tentang sifat perencatan kakisan bagi perencat-perencat kakisan.  Keputusan kajian QSAR ini adalah konsisten dengan data eksperimen.

Kata kunci: kajian pemodelan QSAR, perencatan kakisan, terbitan isatin, kuasa dua terkecil separa

References

- Abdallah, M., Helal, E. A. and Fouda, A. S. (2006). Aminopyrimidine derivatives as inhibitors for corrosion of 1018 carbon steel in nitric acid solution. Corrosion Science, 48 (7): 1639 - 1654.

- Badr, G. E. (2009). The role of some thiosemicarbazide derivatives as corrosion inhibitors for C-steel in acidic media. Corrosion Science, 51 (11): 2529 – 2536.

- Pavithra, M. K., Venkatesha, T.V., Punith Kumar, M. K. and Tondan, H. C. (2012). Inhibition of mild steel corrosion by Rabeprazole sulfide. Corrosion Science, 60: 104 – 111.

- Musa, M., Rodhi, M. N. M., Najmiddin Yaakob, N., Hamid, K.H.K. and Idris. J. (2013). Development of bio-based paint by using methyl esters from palm oil for corrosion inhibitor. Malaysian Journal of Analytical Sciences, 17 (1): 30 – 37.

- Raja, P. B., Qureshi, A. K., Abdul Rahim, A., Osman, H. and Awang, K. (2013). Neolamarckia cadamba alkaloids as eco-friendly corrosion inhibitors for mild steel in 1M HCl media. Corrosion Science, 69: 292 – 301.

- Kamal, N. K. M., Fadzil, A. H., Kassim, K., Rashid, S. H. and Mastuli, M. S. (2014). Synthesis, characterization and corrosion inhibition studies of o,m,p-decanoyl thiourea derivatives on mild steel in 0.1 M H2SO4 solutions. Malaysian Journal of Analytical Sciences, 18 (1):21 – 27.

- Solmaz, R. (2014). Investigation of adsorption and corrosion inhibition of mild steel in hydrochloric acid solution by 5-(4-Dimethylaminobenzylidene)rhodanine. Corrosion Science, 79: 169 – 176.

- Zhao, H., Zhang, X., Ji, L., Hu, H. and Li, Q. (2014). Quantitative structure–activity relationship model for amino acids as corrosion inhibitors based on the support vector machine and molecular design. Corrosion Science, 83: 261 – 271.

- Zhang, J., Liu, J., Yu, W., Yan, Y., You, L. and Liu, L. (2010). Molecular modeling of the inhibition mechanism of 1-(2-aminoethyl)-2-alkyl-imidazoline, Corrosion Science, 52 (6): 2059 – 2065.

- Khaled, K.F. (2011). Modeling corrosion inhibition of iron in acid medium by genetic function approximation method: A QSAR model. Corrosion Science, 53 (11): 3457 – 3465.

- Bababdani, B.M. and Mousavi, M. (2013). Gravitational search algorithm: A new feature selection method for QSAR study of anticancer potency of imidazo[4,5-b]pyridine derivatives. Chemometrics and Intelligent Laboratory Systems, 122: 1 – 11.

- Talete srl. (2010), Dragon (software for molecular descriptor calculation), version 6.0. Milano, Italy: Talete. http://www.talete.mi.it/

- Riahi, S., Ganjali, M.R., Norouzi, P. and Jafari, F. (2008). Application of GA-MLR, GA-PLS and the DFT quantum mechanical (QM) calculations for the prediction of the selectivity coefficients of a histamine-selective electrode. Sensors and Actuators B: Chemical, 132 (1): 13 – 19.

- Soltani, S., Abolhasani, H., Zarghi, A. and Jouyban, A. (2010). QSAR analysis of diaryl COX-2 inhibitors: Comparison of feature selection and train-test data selection methods. European Journal of Medicinal Chemistry, 45 (7): 2753 – 2760.

- Chen, Q., Jiang, P. and Zhao, J. (2010). Measurement of total flavone content in snow lotus (Saussurea involucrate) using near infrared spectroscopy combined with interval PLS and genetic algorithm. Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy, 76 (1): 50 – 55.

- Abrahamsson, C., Johansson, J., Sparén, A. and Lindgren, F. (2003). Comparison of different variable selection methods conducted on NIR transmission measurements on intact tablets. Chemometrics and Intelligent Laboratory Systems, 69: 3 – 12.

- Chen, G., Su, H.-J., Song, Y.-P., Gao, Y., Zhang, J., Hao, X.-J. and Zhao, J.-R. (2013). Synthesis and evaluation of isatin derivatives as corrosion inhibitors for Q235A steel in highly concentrated HCl. Research on Chemical Intermediates, 39 (8): 3669 – 3678.

- Consonni, V., Todeschini, R., Pavan, M. and Gramatica, P. (2002). Structure/Response Correlations and Similarity/Diversity Analysis by GETAWAY Descriptors. 2. Application of the Novel 3D Molecular Descriptors to QSAR/QSPR Studies. Journal of Chemical Information and Computer Sciences, 42(3): 693 – 705.

- Pourbasheer, E., Aalizadeh, R., Ganjali, M. R., Norouzi, P. and Shadmanesh, J. (2014). QSAR study of ACK1 inhibitors by genetic algorithm–multiple linear regression (GA–MLR). Journal of Saudi Chemical Society, 18(5): 681 – 688.

- Todeschini, R., Bettiol, C., Giurin, G., Gramatica, P., Miana, P. and Argese, E. (1996). Modeling and prediction by using WHIM descriptors in QSAR studies: submitochondrial particles (SMP) as toxicity blosensors of chlorophenols. Chemosphere, 33(1): 71 –79.

- Melagraki, G. and Afantitis, A. (2013). Enalos KNIME nodes: Exploring corrosion inhibition of steel in acidic medium. Chemometrics and Intelligent Laboratory Systems, 123: 9 – 14.