Malaysian Journsl of Analytical Sciences Vol 20 No 4 (2016): 806 - 811

PREPARATION AND PHYSICOCHEMICAL PROPERTIES OF OCTENYL SUCCINIC ANHYDRIDE (OSA) MODIFIED SAGO STARCH

(Penyediaan dan Sifat Fizikokimia Oktenil Suksinat Anhidrat (OSA) Modifikasi Kanji Sagu)

Nur Farhana Zainal Abiddin, Anida Yusoff*, Noorlaila Ahmad

Department of Food Science and Technology,

Faculty of Applied Sciences,

Universiti Teknologi MARA, 40450 Shah Alam, Selangor, Malaysia

*Corresponding author: anida@salam.uitm.edu.my

Received: 24 February 2015; Accepted: 27 October 2015

Abstract

# Starch from sago (Metroxylon sagu) was esterified with octenyl succinic anhydride (OSA) in order to regulate its shortcoming by adding amphiphilic properties. The objective of this work is to determine the physicochemical properties of native sago and OSA sago starches. The OSA sago starch was produced according to the optimum condition generated via response surface methodology (RSM) with 5.00 % OSA at pH 7.20 and a reaction time of 9.65 hours. The esterified sago starch gives a degree of substitution (DS) value of 0.012. The physicochemical properties of OSA sago starch was determined by measuring the amylose content, laser diffraction particle size analyzer, scanning electron microscopy (SEM) and Fourier transform infrared (FT-IR). The amylose content for OSA sago starch was found to be reduced after esterification reaction. The particle size of OSA sago starch was found to increase significantly (p < 0.05) compared to their native starches. Scanning electron microscopy (SEM) revealed that OSA starch developed slightly rough surface and their edges lost some definition. FT-IR spectroscopy shows that there was appearance of new absorption correspond to ester carbonyl group (1717 cm-1) and carboxylate RCOO- (1569 cm-1). This study showed that the physicochemical properties of modified starches were influenced not only by DS but also on the botanical origin of the starches.

# Keywords: physicochemical properties, sago starch, octenyl succinic anhydride, esterification

Abstrak

# Kanji daripada sagu (Metroxylon sagu) telah diesterifikasi dengan oktenil suksinat anhidrat (OSA) sebagai usaha untuk mengawal kelemahan dengan menambah sifat amfifilik. Objektif kajian ini adalah untuk menentukan sifat – sifat fizikokimia kanji sagu asli dan OSA kanji sagu. OSA kanji sagu disediakan mengikut keadaan optima berdasarkan kaedah gerak balas permukaan (RSM) dengan 5.00 % OSA pada pH 7.20 dan masa tindak balas selama 9.65 jam. Esterifikasi kanji sagu memberikan nilai darjah pengantian (DS) sebanyak 0.012. Ciri-ciri fizikokimia OSA kanji sagu ditentukan dengan mengira kandungan amilosa, saiz partikel laser pembelauan analisis, mikroskop imbasan elektron (SEM) dan Fourier transformasi inframerah (FT-IR). Kandungan amilosa untuk OSA kanji sagu didapati berkurangan selepas tindak balas esterifikasi. Saiz partikel OSA kanji sagu didapati meningkat dengan ketara (p < 0.05) berbanding saiz kanji sagu asli. Mikroskop imbasan elektron (SEM) menunjukkan bahawa OSA kanji sagu menghasilkan permukaan sedikit kasar dan kehilangan beberapa sisi definisi. FT-IR spektroskopi menunjukkan bahawa terdapat kemunculan penyerapan baru yang bersesuaian dengan kumpulan ester karbonil (1717 cm-1) dan RCOO- karboksilik (1569 cm-1). Kajian ini menunjukkan bahawa ciri-ciri fizikokimia kanji diubahsuai bukan hanya dipengaruhi oleh DS tetapi juga berdasarkan pada asal usul botanikal kanji tersebut.

# Kata kunci: sifat-sifat fizikokimia, kanji sagu, oktenil suksinat anhidrat, esterifikasi

References

- Steeneken, P. A. M. and Woortman, A. J. J. (2008). Surface effects in the acetylation of granular potato starch. Carbohydrate Research, 343(13): 2278 – 2284.

- Chang, P. R., Qian, D., Anderson, D. P. and Ma, X. (2012). Preparation and properties of the succinic ester of porous starch. Carbohydrate Polymers, 88: 604 – 608.

- Segura-Campos, M., Chel-Guerrero, L. and Betancur-Ancona, D. (2010). Effects of octenylsuccinylation on functional properties of lima bean (Phaseolus Lunatus) starch. Journal of Food Process Engineering, 33(4): 712 – 727.

- Segura-Campos, M., Chel-Guerrero, L. and Betancur-Ancona, D. (2008). Synthesis and partial characterization of octenylsuccinic starch from Phaseolus Lunatus. Food Hydrocolloids, 22(8): 1467 – 1474.

- Singh, N., Singh, J., Kaur, L., Sodhi, N. S. and Gill, B. S. (2003). Morphological, thermal and rheological properties of starches from different botanical sources. Food Chemistry, 81(2): 219 – 231.

- Singh, J., Kaur, L. and McCarthy, O. J. (2007). Factors influencing the physico-chemical, morphological, thermal and rheological properties of some chemically modified starches for food applications – A review. Food Hydrocolloids, 21(1): 1 – 22.

- Wang, J., Su, L. and Wang, S. (2010). Physicochemical properties of octenyl succinic anhydride-modified potato starch with different degrees of substitution. Journal of the Science of Food and Agriculture, 90(3): 424 – 429.

- Kaur, L., Singh, N. and Sodhi, N. S. (2002). Some properties of potatoes and their starches II. Morphological, thermal and rheological properties of starches. Food Chemistry, 79(2): 183 – 192.

- Zainal Abiddin, N. F., Yusoff, A. and Ahmad, N. (2015). Optimisation of reaction conditions of octenyl succinic anhydride (OSA) modified sago starch using response surface methodology (RSM). International Food Research Journal, 22(3): 930 – 935.

- Bhosale, R. and Singhal, R. (2006). Process optimization for the synthesis of octenyl succinyl derivative of waxy corn and amaranth starches. Carbohydrate Polymers, 66(4): 521 – 527.

- Ratnayake, W. S., Hoover, R., Shahidi, F., Perera, C. and Jane, J. (2001). Composition, molecular structure, and physicochemical properties of starches from four field pea (Pisum sativum L.) cultivars. Food Chemistry, 74(2): 189 – 202.

- McGrance, S. J., Cornell, H. J. and Rix, C. J. (1998). A simple and rapid colorimetric method for the determination of amylose in starch products. Starch-Stärke, 50(4): 158 – 163.

- Tester, R. F., Karkalas, J. and Qi, X. (2004). Starch-composition, fine structure and architecture. Journal of Cereal Science, 39(2): 151 – 165.

- Ahmad, F. B., Williams, P. A., Doublier, J-L., Durand, S. and Buleon, A. (1999). Physico-chemical characterisation of sago starch. Carbohydrate Polymers, 38(4): 361 – 370.

- van der Burgt, Y. E. M., Bergsma, J., Bleeker, I. P., Mijland, P. J. H. C., van der Kerk-van Hoof, A., Kamerling, J. P. and Vliegenthart, J. F. G. (2000). Distribution of methyl substituents im amylose and amylopectin from methylated potato starches. Carbohydrate Research, 325(3): 183 – 191.

- Nor Nadiha, M. Z., Fazilah, A., Bhat, R. and Karim, A. A. (2010). Comparative susceptibilities of sago, potato and corn starches to alkali treatment. Food Chemistry, 121(4): 1053 – 1059.

- Kaur, B., Fazilah, A. and Karim, A. A. (2011). Alcoholic-alkaline treatment of sago starch and its effect on physicochemical properties. Food and Bioproducts Processing, 89(4): 463 – 471.

- Bello-Flores, C.A., Nuñez-Santiago, M. C., Martín-Gonzalez, M. F., BeMiller, J. N. and Bello-Pérez, L. A. (2014). Preparation and characterization of octenylsuccinylated plantain starch. International Journal of Biological Macromolecules, 70: 334 – 339.

- Karim, A. A., Nadiha, M. Z., Chen, F. K., Phuah, Y. P., Chui, Y. M. and Fazilah, A. (2008). Pasting and retrogradation properties of alkali-treated sago (Metroxylon sagu) starch. Food Hydrocolloids, 22(6): 1044 – 1053.

- Wang, X., Li, X., Chen, L., Xie, F., Yu, L. and Li, B. (2011). Preparation and characterisation of octenyl succinate starch as a delivery carrier for bioactive food components. Food Chemistry, 126(3): 1218 – 1225.

- Hui, R., Qi-he, C., Ming-liang, F., Qiong, X. and Guo-qing, H. (2009). Preparation and properties of octenyl succinic anhydride modified potato starch. Food Chemistry, 114(1): 81 – 86.

- Chi, H., Xu, K., Xue, D., Song, C., Zhang, W. and Wang, P. (2007). Synthesis of dodecenyl succinic anhydride (DDSA) corn starch. Food Research International, 40(2): 232 – 238.

- Zhang, B., Huang, Q., Luo, F-X., Fu, X., Jiang, H. and Jane, J-l. (2011). Effects of octenylsuccinylation on the structure and properties of high-amylose maize starch. Carbohydrate Polymers, 84(4): 1276 –1281.