# Malaysian Journal of Analytical Sciences Vol 20 No 4 (2016): 704 - 712

# A FLUORESCENCE PHOSPHATE SENSOR BASED ON POLY(GLYCIDYL METHACRYLATE) MICROSPHERES WITH ALUMINIUM-MORIN

# (Sensor Fosfat Berpendarfluor Berasaskan Mikrosfera Poli(Glisidil Metakrilat) dengan Aluminium-Morin)

# Amalina Ahmad1, Norhadisah Mohd Zaini1, Normazida Rozi1, Nurul Huda Abd Karim1, Siti Aishah Hasbullah1, Lee Yook Heng1, Sharina Abu Hanifah1,2*

# 1School of Chemical Sciences and Food Technology

# 2Center for Water Research and Analysis

# Faculty of Science and Technology,

# Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor, Malaysia

*Corresponding author: sharina@ukm.edu.my

Received: 8 December 2015; Accepted: 11 March 2016

Abstract

The performance of new phosphate sensor was investigated using fluorescence spectrometer in the form of immobilized Al-morin on poly(glycidyl methacrylate) (pGMA) microspheres. pGMA microspheres that were synthesized by using suspension photopolymerization exhibited spherical-shaped morphology with diameters from 1.5 to 5.3 μm. The studies were carried out at pH 5 and the ratio of aluminium (III) chloride hexahydrate to morin was 3:1 (v/v). At pH 5, H2PO4- was measured at 548 nm emission wavelength. The relative fluorescence intensity was inversely proportional to H2PO4- concentrations. The linear range was observed between 6.6 – 58.8 µmol/L with detection limit (LOD) of 0.7 µmol/L. Ion interference study demonstrated that Al-morin was highly selective towards H2PO4-.

# Keywords: phosphate sensor, polymer microspheres, aluminium-morin, fluorescence

Abstrak

# Prestasi sensor fosfat baru telah dikaji dengan menggunakan spektrometer pendarfluor dalam bentuk  Al-morin terpegun pada mikrosfera poli(glisidil metakrilat) (pGMA). Mikrosfera pGMA yang disintesis dengan menggunakan pemfotopolimeran ampaian mempamerkan morfologi berbentuk sfera dengan diameter 1.5 hingga 5.3 µm. Kajian telah dijalankan pada pH 5 dan nisbah aluminium (III) klorida heksahidrat kepada morin adalah 3: 1 (v/v). Pada pH 5, H2PO4- diukur pada gelombang pancaran 548 nm. Keamatan pendarfluor relatif adalah berkadar songsang dengan kepekatan H2PO4- Julat linear diperhatikan antara 6.6 – 58.8 μmol/L dengan had pengesanan (LOD) pada 0.7 μmol/L. Kajian gangguan ion menunjukkan  Al-morin adalah sangat selektif kepada H2PO4-.

# Kata kunci: sensor fosfat, polimer mikrosfrera, aluminium-morin, pendafluor

References

- Kramer, M. (2008). Protein engineering of pyruvate oxidase from Lactobacillus plantarum for application in biosensors. Thesis Diss. Naturwissenschaften, Eidgenössische Technische Hochschule ETH Zürich, Nr. 17765.

- Carpenter, S. R. (2005). Eutrophication of aquatic ecosystems: biostability and soil phosphorus. Proceedings of the National Academy of Sciences of the United States of America, 102(29): 10002 – 10005.

- Lawal, A. T. and Adeloju, S. B. (2013). Progress and recent advances in phosphate sensors: A review. Talanta, 114: 191 – 203.

- Kumar, R. (2009). Phosphate sensing. Current Opinion in Nephrology and Hypertension, 18(4): 281 – 284.

- Slatopolsky, E. (2011). The intact nephron hypothesis: the concept and its implications for phosphate management in CKD-related mineral and bone disorder. Kidney International, 79: 3 – 8.

- Engblom, S. O. (1998). The phosphate sensor. Biosensors and Bioelectronics, 13(9): 981 – 994.

- Kawasaki, H., Sato, K., Ogawa, J., Hasegawa, Y. and Yuki, H. (1989). Determination of inorganic phosphate by flow injection method with immobilized enzymes and chemiluminescence detection. Analytical Biochemistry, 182(2): 366 – 370.

- Ahuja, D. and Parande, D. (2012). Optical sensors and their applications. Journal of Scientific Research and Reviews, 1(5): 60 – 68.

- Noh, J. Y., Hwang, I. H., Kim, H., Song, E. J., Kim, K. B. and Kim, C. (2013). Salicylimine-based colorimetric and fluorescent chemosensor for selective detection of cyanide in aqueous buffer. Bulletin Korean Chemical Society, 34(7): 1985 – 1989.

- Willard, H. H. and Horton, C. A. (1952). Fluorometric determinations of traces of fluoride. Analytical Chemistry, 24(5): 862 – 865.

- Xie, Z. H., Lin, X. C. and Chen, G. N. (2003). Novel phosphate-sensitive fluorescent composite matrix. Chemical Research Chinese Universities, 19(2): 201 – 205.

- Lin, X., Wu, X., Xie, Z. and Wong, K. Y. (2006). PVC matrix membrane sensor for fluorescent determination of phosphate. Talanta, 70(1): 32 – 36.

- Ahmad, A., Hanifah, S. A., Hasbullah, S. A., Suhud, K., Zaini, N. M. and Heng, L. Y. (2014). Phosphate sensor based on immobilized aluminium-morin in poly(glycidyl methacrylate) microspheres. AIP Conference Proceedings, 1614(1): 486 – 491.

- Denizli, A., Garipcan, B., Karabakan, A. and Senoz, H. 2005. Synthesis and characterization of poly(hyroxyethyl methacrylate-N-methacryloyl-(L)-glumatic acid) copolymer beads for removal of leads ions. Materials Sciences and Engineering Journal C, 25(4): 448 – 454.

- Peper, S., Tsagkatakis, I. and Bakker, E. 2001. Cross-linked dodecyl acrylate microspheres: novel matrices for plasticizer-free optical ion sensing. Analytica Chimica Acta 442(1): 25 – 33.

- Xu, C., Wygladacz, K., Qin, Y., Retter, R., Bell, M. and Bakker, E. 2005. Microsphere optical ion sensors based on doped silica gel templates. Analytica Chimica Acta 537(1): 135 – 143.

- Mohr, G. J. and Wolfbeis, O. S. 1995. Optical sensing of anions via polarity-sensitive dyes: a bulk sensor membrane for nitrate. Analytica Chimica Acta 316(1995) 239 – 246.

- Chandra, S., Raizada S. and Sharma, S. 2012. Highly selective monohydrogen phosphate anion sensor for [CrL](NO3)3. Journal of Chemical and Pharmaceutical Research 4(8): 3769 – 3777.

- Mulon, J. B., Destandau, É., Alain, V. and Bardez, É. 2005. How can aluminium(III) generate fluorescence? Journal of Inorganic Biochemistry 99(2005): 1749 – 1755.

- Ulianas, A., Heng, L. Y., Hanifah, S. A. and Ling, T. L. (2012). An electrochemical DNA microbiosensor based on succinimide-modified acrylic microspheres. Sensors 12: 5445 – 5460.

- Williams, N. J., Gan, W., Reibenspies, J. H. and Hancock, R. D. (2009). Possible steric control of the relative strength of chelation enhanced fluorescence for zinc(II) compared to cadmium(II): Metal ion complexing properties of tris(2-quinolylmethyl)amine, a crystallographic, UV-visible, and fluorometric study. Inorganic Chemistry, 48: 1407 – 1415.

- De Silva, A. P., Gunaratne, H. N., Gunnlaugsson, T., Huxley, A. J., McCoy, C. P., Rademacher, J. T. and Rice, T. E. (1997). Signaling recognition events with fluorescent sensors and switches. Chemistry Reviews, 97(5): 1515 – 1566.

- Kaur, S., Hwang, H., Lee, J. T. and Lee, C. H. (2013). Displacement-based, chromogenic calix [4] pyrrole-indicator complex for selective sensing of pyrophosphate anion. Tetrahedron Letters, 54(29): 3744 – 3747.

- Neri, T. S., Carvalho, D. C., Alves, V. N. and Coelho, N. M. (2015). Noteworthy method for direct determination of SbIII and total inorganic antimony in natural waters. Journal of the Brazilian Chemical Society, 26(5), 985 – 991.

- Zhang, Y., Hu, Y., Wilson, G. S., Moatti-Sirat, D., Poitout, V., and Reach, G. (1994). Elimination of the acetaminophen interference in an implantable glucose sensor. Analytical Chemistry, 66(7): 1183 – 1188.

- Edwards, H. A. (1982). Ion concentration and activity in the haemolymph of Aedes aegypti larvae. Journal of Experimental Biology, 101(1): 143 – 151.