# Malaysian Journal of Analytical Sciences Vol 20 No 4 (2016): 856 - 862

# IMMOBILIZATION OF HIGHLY EFFECTIVE PALLADIUM CATALYST ONTO POLY(4-VINYLPYRIDINE): SYNTHESIS AND CHARACTERIZATION

# (Pemegunan Mangkin Paladium yang Efektif ke atas Poli(4-vinilpiridina):

# Sintesis dan Pencirian)

# Siti Kamilah Che Soh1*, Intan Shafinass Kassim1, Siti Aminah Jusoh1, Mustaffa Samsuddin2, 3

# 1Analytical & Environmental Chemistry Program, School of Marine Science and Environment,

# Universiti Malaysia Terengganu, 21030 Kuala Terengganu, Terengganu, Malaysia

# 2Department of Chemistry, Faculty of Science

# 3Ibnu Sina Institute for Fundamental Science Studies

Universiti Teknologi Malaysia, 81310 Johor Bahru, Johor, Malaysia

*Corresponding author: sitikamilah@umt.edu.my

Received: 24 February 2015; Accepted: 27 October 2015

Abstract

# A commonly known weakness of homogeneous catalysts is the difficulty to recover the active catalyst from the product. Due to the disadvantage, the designing of supported catalyst has been approached to overcome the separation difficulty of the palladium-based homogeneous catalyst. New polymer supported N2O2 metal complex was successfully immobilized by mixing of poly(4-vinylpyridine) with palladium(II) complex in the presence of ethyl acetate as solvent. Then, the reaction was stirred for 72 hours at room temperature to form corresponding P4VP-Pd catalyst. The properties of immobilized catalyst were characterized by various techniques such as fourier transform infrared (FTIR), thermogravimetric (TGA), X-ray diffraction (XRD), scanning electron microscopy/energy dispersive X-ray (SEM/EDX) and inductively coupled plasma-optical emission (ICP-OES) spectroscopy.

# Keywords:  immobilized catalyst, palladium(II) complex, poly(4-vinylpyridine)

Abstrak

# Satu kelemahan penggunaan mangkin homogen adalah umum diketahui bahawa kesukaran untuk memperoleh kembali mangkin yang aktif daripada hasil produk. Oleh kerana kelemahan ini, reka bentuk mangkin berpenyokong telah diperkenalkan untuk mengatasi kesukaran pemisahan mangkin homogen berasaskan logam paladium. Kompleks logam N2O2 berpenyokong polimer baru telah berjaya dipegunkan dengan mencampurkan poli(4-vinilpiridina) dengan kompleks paladium(II) dengan kehadiran etil asetat sebagai pelarut. Kemudian, campuran tindak balas dikacau selama 72 jam pada suhu bilik untuk menghasilkan mangkin P4VP-Pd. Sifat – sifat mangkin yang berjaya dipegunkan telah dicirikan dengan pelbagai teknik spektroskopi antaranya infra merah transformasi fourier (FTIR), analisis termogravimetrik (TGA), pembelauan sinar-X (XRD), mikroskopi elektron imbasan/ sinar-X tenaga tersebar (SEM/EDX) dan spektroskopi pancaran optik-aruhan (ICP-OES).

# Kata kunci:  mangkin terpegun, kompleks paladium(II), poli(4-vinilpiridina)

References

- Kulkarni, S., Alurkar, M. and Kumar. A. (1996). Polymer supported with Schiff base functional group with cobaltous palmitate as oxidation catalyst for cyclohexane. Applied Catalysis A: General, 142(2): 243 – 254.

- Dunnewijk, J., Bosch, H., and de Haan, A. B. (2004). Reverse flow adsorption: Integrating the recovery and recycling of homogeneous catalyst. Separation and Purification Technology, 40 (3):317 – 320.

- Daniel, S., Rao, P. P., Nandakumar, M. and Rao, T. P. (2005). Synthesis of heterogenous phosphine-free palladium based catalyst assemblies via solid phase extraction and their characterization. Materials Chemistry and Physics, 90(1): 99 – 105.

- Augustine, R. L., Goel, P., Mahata, N., Reyes, C. and Tanielyan, S. K. (2004). Anchored homogeneous catalysts: high turnover applications. Journal of Molecular Catalysis A: Chemical, 216(2):189 – 197.

- Tyrrell, E., Whiteman, L. and Williams, N. (2011). The synthesis and characterization of immobilized palladium carbene complexes and their applications to heterogeneous catalysis. Journal of Organometallic Chemistry, 22: 3465 – 3472.

- Petruci, J., and Cardoso, A. A. (2013). A new palladium chelate compound for determination of sulfide. Microchemical Journal, 106: 368 – 372.

- Evangelisti, C., Panziera, N., Pertici, P., Vitulli, G., Salvadori, P., Battocchio, C. and Polzonetti, G. (2009).  A readily prepared, highly reusable and active polymer-supported molybdenum carbonyl Schiff base complex as epoxidation catalyst. Inorganic Chemistry Communication, 10(8): 914 – 917.

- Emregul, K. C., Duzgun, E. and Atakol, O. (2006). The application of some polydentate Schiff base compounds containing aminic nitrogen as corrosion inhibitors for mild steel in acidic media. Corrosion Science, 48 (10): 3243 – 3260.

- Cimerman, Z., Galic, N. and Bosner, B. (1997), The Schiff bases of salicylaldehyde and aminopyridines as highly sensitive analytical reagents. Analytica Chimica Acta, 343(2): 145 – 153.

- He, Y. and Cai, C. (2011). Polymer-supported macrocyclic Schiff base palladium complex: An efficient and reusable catalyst for Suzuki cross-coupling reaction under ambient condition. Catalysis Communication 12(7): 678 – 683.

- Zhongmin, D. and Zhibin, Y. (2015).  Heterogeneous palladium catalyst constructed with cross-linked hyperbranched poly(phenylacetylene) as polymer support: A reusable highly active PPM-level catalyst for multiple cross-coupling reactions, Applied Catalysis A: General., 489: 61 – 71.

- Selvakumar, J., Varghese, B., Raghunathan, V. S. and Nagaraja, K. S. (2007). 2,2’-[1,1’-(Propane-1,3-diyl)bis(nitriloethylidyne)]diphenol, Acta Crystallographica Section E Structure Reports Online 63: 1924 – 1925.

- Fonseca, J., Martinez, J., Cunha-Silva, L., Magalhaes, A. L., Duarte, M. T. and Freire, C. (2010). Insights into electronic and structural properties of novel Pd(II) Salen-type complexes. Inorganica Chimica Acta, 363(14): 4096 – 4107.

- Fan, Y., You, W., Huang, W., Liu, J. L. and Wang, Y. N. (2010).  Salen-type nickel(II), palladium(II) and copper(II) complexes having chiral and racemic camphoric diamine components. Polyhedron, 29(3): 1149 – 1155.

- Soh, S. K. C. and Shamsuddin, M. (2013). Tetradentate N2O2 chelated palladium(II) complexes: Synthesis, characterization, and catalytic activity towards Mizoroki-Heck reaction of aryl bromides. E-Journal of Chemistry, 2013: 1 – 8.