Malaysian Journal of Analytical Sciences Vol 20 No 5 (2016): 1090 - 1094

PREPARATION AND CHARACTERIZATION OF EPOXIDISED NATURAL RUBBER (ENR)/POLY (VINYLIDENE FLUORIDE) (PVDF) (ENR/PVDF) COMPOSITE MEMBRANE

(Penyediaan dan Pencirian Membran Komposit Getah Asli Terepoksida (ENR) / Poli (Vinilinida Fluorida) (PVDF) (ENR/PVDF)

Norliyana Mod1, Farah Hannan Anuar1,2, Rizafizah Othaman1,2*

1School of Chemical Sciences and Food Technology, Faculty of Science and Technology

2Polymer Research Center, Faculty of Science and Technology

Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor, Malaysia

*Corresponding author: rizafizah@ukm.edu.my

Received: 10 June 2015; Accepted: 21 July 2016

Abstract

The focus of this research is to prepare epoxidised natural rubber (ENR)/poly(vinylidene fluoride) (PVDF) (ENR/PVDF) membrane using solution casting method and to characterize the ENR/PVDF membrane using universal tensile machine (UTM) and scanning electron microscope (SEM). Composite membrane of ENR/PVDF was prepared by solution casting technique. The tensile strain increases when ratio of ENR increases in the composite. SEM micrograph shows the compatibility of ENR and PVDF in 40/60 wt% sample but agglomeration of ENR in 60/40 wt% ENR/PVDF sample was observed. The micrograph also shows the existence of pores in the composite membrane which is essential when applying the membrane for separation of gas and waste water treatment.

Keywords:  composite membrane, epoxidised natural rubber, poly(vinylidene fluoride)

Abstrak

Fokus kajian ini adalah untuk menyediakan membran getah asli terepoksida (ENR)/ poli (vinilidina fluorida) (PVDF) (ENR/PVDF) menggunakan kaedah penuangan larutan dan untuk mencirikan membran ENR/PVDF menggunakan mesin ujian tensil (UTM) dan mikroskop imbasan elektron (SEM). Membran komposit ENR/PVDF telah disediakan menggunakan teknik penuangan larutan. Rintangan tegangan bertambah apabila ratio ENR bertambah didalam komposit. Mikrograf SEM menunjukkan kesesuaian ENR dan PVDF pada sampel 40/60 wt%  tetapi terdapat penggumpalan ENR pada sampel ENR/PVDF 60/40 wt%. Mikrograf juga menunjukkan kehadiran liang pada membran komposit tersebut dimana ianya penting untuk diaplikasikan sebagai membran pemisahan gas dan rawatan air buangan.

Kata kunci:  membran komposit, getah asli terepoksida, poli (vinilidina fluorida)

References

- Salaeh, S., Nakason, C., Boiteux, G. and Cassagnau, P. (2013). Co-continuous phase structure and properties of poly(vinylidene fluoride)/epoxidized natural rubber blends. Advanced Materials Research, 626: 71 – 74.

- Bottino, A., Camera-Roda, G., Capannelli, G. and Munari, S. (1991). The formation of microporous polyvinylidene difluoride membranes by phase separation. Journal of Membrane Science, 57: 1 –20.

- Yan, L., Hong, S., Li, M. L. and Li, Y. S. (2009). Application of the Al2O3–PVDF nanocomposite tubular ultrafiltration (UF) membrane for oily wastewater treatment and its antifouling research. Separation and Purification Technology, 66: 347 – 352.

- Salaeh, S. (2014). Processing of natural rubber composites and blends: Relation between structure and properties. PhD dissertation, Prince Of Songkla University (Psu) - Pattani (Thailand).

- Hasegawa, R., Takahashi, Y., Chatani, Y. and Tadokoro, H. (1972). Crystal structures of three crystalline forms of poly(vinylidene fluoride). Polymer Journal, 3: 600 – 610.

- Boccaccio, T., Bottino, A., Capannelli, G. and Piaggio, P. (2002). Characterization of PVDF 	membranes by vibrational spectroscopy. Journal of Membrane Science, 210: 315 – 329.

- Tao, M.-M., Liu, F., Ma, B.-R. and Xue, L.-X. (2013). Effect of solvent power on PVDF membrane polymorphism during phase inversion. Desalination, 316: 137 – 145.

- Wang, X., Zhang, L., Sun, D., An, Q. and Chen, H. (2009). Formation mechanism and crystallization of poly(vinylidene fluoride) membrane via immersion precipitation method. Desalination, 236: 170 – 178.

- Sulaiman, N. M. N. and Ling, C. K. (2004). Membrane ultrafiltration of treated palm oil mill effluent (POME). Jurnal Teknologi, 41(1): 113 – 120.

- Cao, X., Ma, J., Shi, X. and Ren, Z. (2006). Effect of TiO2 nanoparticle size on the performance of PVDF membrane. Applied Surface Science, 253: 2003 – 2010.

- Yoksan, R. (2008). Epoxidized natural rubber for adhesive applications. Kasetsart Jurnal (Natural Science), 42: 325 – 332.

- Sharma, S. K., Singh, G., Kumar, H. and Kataria, R. (2015). Study of solute–solute and solute–solvent interactions of N-acetyl glycine in aqueous D-fructose solutions at different temperatures. Thermochimica Acta, 607: 1 – 8.

- Bagheripour, E., Moghadassi, A. R. and Hosseini, S.M. (2014). Novel nanofiltration membrane with low concentration of polyvinylchloride: Investigation of solvents’ mixing ratio effect (dimethyl acetamide/tetrahydrofuran). Arabian Journal of Chemistry, 1 – 6.

- Jon, N., Abdullah, I. and Othaman, R. (2013). Effects of silica on the formation of epoxidised natural rubber/polyvinyl chloride membrane. Sains Malaysiana, 42(4): 469 – 473.