Malaysian Journal of Analytical Sciences Vol 20 No 5 (2016): 1138 - 1144

VIBRATION EXPOSURE ANALYSIS OF POLYDIMETHYLSILOXANE REINFORCED SILICA DERIVED RICE HUSK ASH

(Kajian Pendedahan Getaran Terhadap Polidimetilsiloksana yang Diperkuat Silika Dari Abu Sekam Padi)

Mohd Azham Azmi*, Mohd Syahmi Muin @ Marsayid, Shahruddin Mahzan, Sufizar Ahmad, Hariati Taib

Faculty of Mechanical and Manufacturing Engineering,

Universiti Tun Hussein Onn Malaysia, 86400 Parit Raja, Batu Pahat, Johor, Malaysia

*Corresponding author: azham@uthm.edu.my

Received: 10 June 2015; Accepted: 21 July 2016

Abstract

The study investigates the vibration and mechanical properties of rice husk silica (RHS) in enhancing the properties of Polydimethylsiloxane (PDMS). The PDMS/RHS composites panel were fabricated by using casting technique and cured at room temperature. PDMS panels were filled with 2 – 12 wt% of RHS. Vibration analysis of PDMS/RHS composites panel were guided by ISO 8662 standard in evaluation of hand arm vibration for hand grinder machine. The vibration exposure analysis showed that application of PDMS/RHS as a vibration absorber successfully decreased the vibration exposure to 46%. Tensile properties analysis conducted using ASTM D412 standard showed that the PDMS/10 wt% RHS properties increased to 9.6% compared to PDMS without RHS. Thus it is concluded that the addition of RHS had improved both properties of PDMS. RHS has successfully acts as a reinforcement when load is applied to the panel and during vibration exposure, RHS has acts as an absorber and distributed the vibration.

Keywords:  polydimethylsiloxane, vibration exposure, rice husk silica, tensile properties

Abstrak

Kajian ini dijalankan untuk mengenalpasti sifat – sifat getaran dan tegangan silika sekam padi (RHS) yang digunakan untuk meningkatkan sifat – sifat polidimetilsiloksana (PDMS). Panel komposit PDMS/RHS dihasilkan menggunakan kaedah tuangan dan dirawat pada suhu bilik. Panel PDMS di isi dengan RHS sebanyak 2 – 12 wt%. Analisa getaran panel komposit PDMS/RHS dikendalikan menurut piawaian ISO 8662 bertujuan menilai pendedahan getaran pada tangan bagi penggunaan mesin canai tangan. Keputusan analisa terhadap pendedahan getaran menunjukkan bahawa penggunaan PDMS/RHS sebagai penyerap getaran telah berjaya menurunkan pendedahan getaran sebanyak 46%. Analisa sifat – sifat tegangan yang dijalankan berpandukan piawaian ASTM D412 menunjukkan sifat - sifat PDMS/10 wt% RHS telah meningkat sebanyak 9.6% jika dibandingkan dengan PDMS tanpa RHS. Ini menunjukkan bahawa penambahan RHS telah meningkatkan kedua – dua sifat PDMS. RHS telah berjaya bertindak sebagai penguat apabila beban dikenakan pada panel dan bertindak sebagai penyerap dan penyebar apabila getaran dikenakan.

Kata kunci:  polidimetilsiloksana, pendedahan getaran, silika sekam padi, sifat terikan

References

- British Standards Institution (2001). Mechanical vibration - Measurement and evaluation of human exposure to hand-transmitted vibration - Part 1: General requirements. London: EN ISO 5349-1.

- Pal, R. (2010). Rheology of Particulate Dispersions and Composites Surfactant Science. 1st ed. London: Taylor and Francis.

- Leblanc, J. L. (2010). Filled Polymers: Science and Industrial Applications. 1st ed. Florida: CRC Press.

- Ahmed, K., Nizami, S. S. and Riza, N.Z. (2014). Reinforcement of natural rubber hybrid composites based on marble sludge/Silica and marble sludge/rice husk derived silica. Journal of Advanced Research, 5(2): 165 – 173.

- Shah, J., Yuan, Q. and Misra, R. D. K. (2009). Synthesis, structure and properties of a novel hybrid bimodal network elastomers with inorganic cross-links: The case of silicone-nanocrystalline titania. Materials Science and Engineering A, 523(1-2): 199 – 206.

- Duo, S., Li, M., Zhu, M. and Zhou, Y. (2008). Polydimethylsiloxane/silica hybrid coatings protecting Kapton from atomic oxygen attack. Materials Chemistry and Physics. 112: 1093 – 1098.

- Yingze, S., Jinhong, Y., Dan, D., Lixian, S. and Nan, J. (2014). Effect of silica particles modified by in-situ and ex-situ methods on the reinforcement of silicone rubber. Materials and Design. 64: 687 – 693.

- Camenzind, A., Schweizer, T., Sztucki, M. and Pratsinis, S. E. (2010). Structure & strength of silica-PDMS nanocomposites. Polymer, 51(8): 1796 – 1804.

- Prasertsri, S. and Rattanasom, N. (2012). Fumed and precipitated silica reinforced natural rubber composites prepared from latex system: Mechanical and dynamic properties. Polymer Testing, 31(5): 593 – 605.

- Yan, Z., Yanwu, Z., Gui, L., Ruoff, R. S., Naiping H., Schaefer, D. W. and Mark, J. E. (2013). What factors control the mechanical properties of poly (dimethylsiloxane) reinforced with nanosheets of 3-aminopropyltriethoxysilane modified graphene oxide? Polymer, 54(14): 3605 – 3611.

- Jones, R. G., Ando, W. and Chojnowski, J. (2001). Silicon-Containing Polymers: The Science and Technology of Their Synthesis and Applications. Dordrecht: Kluwer Academic

- Carponcin, D., Dantras, E., Michon, G., Dandurand, J., Aridon, G., Levallois, F., Cadiergues, L. and  Lacabanne, C. (2015). New hybrid polymer nanocomposites for passive vibration damping by incorporation of carbon nanotubes and lead zirconate titanate particles. Journal of Non-Crystalline Solids, 409: 20 – 26.

- Sharma, S. K., Gaur, H., Kulkarni, M., Patil, G., Bhattacharya, B. and Sharma, A. (2013). PZT–PDMS composite for active damping of vibrations. Composites Science and Technology, 77: 42 – 51.