Malaysian Journal of Analytical Sciences Vol 20 No 5 (2016): 1052 - 1058

PERFORMANCE OF EGZrO2-EGFe2O3/HY AS PHOTOCATALYST AND ITS EFFICACY IN DECOLORIZATION OF DYE-CONTAMINANTS

(Keupayaan EGZrO2-EGFe2O3/HY sebagai Fotomangkin dan Keberkesanannya Dalam Penyahwarnaan Bahan Cemar Pewarna)

Muhammad Farhan Hanafi, Norzahir Sapawe*, Mohd Zulkhairi Abdul Rahim, Nurul Nabihah Rahman,

Abu Hassan Abd Rahman, Asimi Ana Ahmad

Section of Technical Foundation,

Universiti Kuala Lumpur-Malaysian Institute of Chemical and Bioengineering Technology (UniKL-MICET),

Lot 1988 Vendor City, Taboh Naning, 78000 Alor Gajah, Melaka, Malaysia

*Corresponding author: norzahir@unikl.edu.my

Received: 17 August 2015; Accepted: 13 June 2016

Abstract

The performance of electrogenerated metals supported on HY zeolite (EGZrO2-EGFe2O3/HY) was studied under sunlight irradiation for the decolorization of methylene blue (MB) and Congo red (CR) in aqueous solutions. The prepared photocatalysts were examined using X-ray diffraction (XRD), transmission electron microscopy (TEM), and Brunnauer-Emmett-Teller surface area analysis (BET). An amount of 0.375 g L−1 EGZrO2-EGFe2O3/HY was found to be the optimum dosage for 10 mg L−1 dyes, which gave almost complete photodecolorization of both MB and CR dye after 2 hours of contact time at pH 9 and pH 7, respectively. In addition, a control experiment was also conducted under similar conditions to confirm the efficacy of the prepared photocatalyst. The simple preparation of the photocatalyst and low amount of metal loading required, with simultaneously existence of synergistic effect from both metal oxides exhibits the great potential of the system that could be applied in textile or other industries wastewater treatment.

Keywords:  photocatalyst, dyes, decolorization, sunlight

Abstrak

Keupayaan logam elektrogenerasi disokong pada zeolit HY (EGZrO2-EGFe2O3/HY) telah dijalankan di bawah sinar matahari untuk penyahwarnaan metilena biru (MB) dan Congo merah (CR) dalam larutan akues. Fotomangkin telah dikaji menggunakan pembelauan sinar X-ray (XRD), mikroskopi elektron transmisi (TEM), dan analisis luas permukaan Brunnauer-Emmett-Teller (BET). Sejumlah 0.375 g L−1 EGZrO2-EGFe2O3/HY telah didapati sebagai dos optimum untuk 10 mg L−1 larutan pewarna, yang memberikan penyahwarnaan hampir lengkap bagi kedua-dua pewarna MB dan CR selepas 2 jam tindak balas pada pH 9 dan pH 7. Di samping itu, satu eksperimen kawalan juga telah dijalankan pada keadaan yang sama untuk mengesahkan keberkesanan fotomangkin yang disediakan. Penyediaan yang mudah untuk fotomangkin dan jumlah muatan logam sedikit yang diperlukan, pada masa yang sama dengan kewujudan kesan sinergi dari kedua-dua oksida logam mempamerkan potensi besar untuk sistem ini digunakan dalam industri tekstil atau industri rawatan air sisa yang lain.

Kata kunci:  fotomangkin, pewarna, peyahwarnaan, sinar matahari

References

- Mahmoodi, N. M. (2013). Magnetic ferrite nanoparticle–alginate composite: Synthesis, characterization and binary system dye removal. Journal of Taiwan Institute of Chemical Engineer, 44: 322 – 330.

- Jaafar, N. F., Jalil, A. A., Triwahyono, S., Muhid, M. N. M., Sapawe, N., Satar, M. A. H. and Asaari H. (2012). Photodecolorization of methyl orange over α–Fe2O3–supported HY catalysts: The effects of catalyst preparation and dealumination. Chemical Engineering Journal, 191: 112 – 122.

- Sapawe, N., Jalil, A. A., Triwahyono, S., Adam, S. H., Jaafar, N. F. and Satar, M. A. H. (2012). Isomorphous substitution of Zr in the framework of aluminosilicate HY by an electrochemical method: Evaluation by methylene blue decolorization. Applied Catalysis B: Environment, 125: 311 – 323.

- Sapawe, N., Jalil, A. A., Triwahyono, S., Sah, R. A. R. N., Jusoh, N. W. C., Hairom, N. H. H. and Efendi. (2013). Electrochemical strategy for grown ZnO nanoparticles deposited onto HY zeolite with enhanced photodecolorization of methylene blue: Effect of the formation of Si–O–Zn bonds. Applied Catalysis A: General, 456: 144 – 158.

- Sapawe, N., Jalil, A. A., Triwahyono, S., Shah, M. I. A., Jusoh, R., Salleh, N. F. M., Hameed, B. H. and Karim, A. H. (2013). Cost–effective microwave rapid synthesis of zeolite NaA for removal of methylene blue. Chemical Engineering Journal, 229: 388 – 398.

- Jalil, A. A., Triwahyono, S., Yaakob, M. R., Azmi, Z. Z. A., Sapawe, N., Kamarudin, N. H. N., Setiabudi, H. D., Jaafar, N. F., Sidik, S. M., Adam, S. H. and Hameed, B. H. (2012). Utilization of bivalve shell–treated Zea mays L. (maize) husk leaf as a low–cost biosorbent for enhanced adsorption of malachite green. Bioresource Technology, 120: 218 – 224.

- Jalil, A. A., Triwahyono, S., Sapawe, N., Ahmed, I. H., Aziz, M. A. A. (2014). Low–temperature stabilization of electrolysynthesized tetragonal zirconia, its photoactivity toward methylene blue decolorization. Desalination and Water Treatment, 56(9): 1–15.

- Rodrigues, C. D. S., Madeira, L. M. and Boaventura, R. A. R. (2009). Treatment of textile effluent by chemical (Fenton’s Reagent) and biological (Sequencing batch reactor) oxidation. Journal of Hazardous Material, 172: 1551 – 1559.

- Damodar, R. A., You, S. J., Ou, S. H. (2010). Coupling of membrane separation with photocatalytic slurry reactor for advanced dye wastewater treatment. Separation and Purification Technology, 76: 64 – 71.

- Aleksic, M., Kusic, H., Koprivanac, N., Leszczynska, D. and Bozic, A. L. (2010). Heterogenous fenton type processes for the degradation of organic dye pollutant in water – The application of zeolite assisted AOPs. Desalination, 257: 22 – 29.

- Jalil, A. A., Satar, M. A. H., Triwahyono, S., Setiabudi, H. D., Kamarudin, N. H. N., Jaafar, N. F., Sapawe, N. and Ahmad, R. (2013). Tailoring the current density to enhance photocatalytic activity of CuO/HY for decolorization of malachite green. Journal of Electroanalytical Chemistry, 701: 50 – 58.

- Jusoh, N. W. C., Jalil, A. A., Triwahyono, S., Setiabudi, H. D., Sapawe, N., Satar, M. A. H., Karim, A. H., Kamarudin, N. H. N., Jusoh, R., Jaafar, N. F., Salamun, N. and Efendi, J. (2013). Sequential desilication–isomorphous substitution route to prepare mesostructured silica nanoparticles loaded with ZnO and their photocatalytic activity. Applied Catalysis A: General, 468: 276 – 287.

- Jusoh, R., Jalil, A. A., Triwahyono, S., Idris, A., Haron, S., Sapawe, N., Jaafar, N. F., Jusoh, N. W. C. (2014). Synthesis of reverse micelle α–FeOOH nanoparticles in Ionic liquid as an only electrolyte: Inhibition of electron-hole pair recombination for efficient photoactivity. Applied Catalysis A: General, 469: 33 – 44.

- Sapawe, N. (2015). Effective solar-based iron oxide supported HY zeolite catalyst for the decolorization of organic and simulated dyes. New Journal of Chemistry, 39: 6377 – 6387.

- Sapawe, N., Jaafar, N. F., Hairom, N. H. H., Satar, M. A. H., Ariffin, M. N., Triwahyono, S. and Jalil, A. A. (2011). A facile preparation of nanosized ZnO and its use in photocatalytic decorization of methyl orange. Malaysian Journal of Fundamental and Applied Sciences, 7: 19 – 23.

- Sapawe, N., Jalil, A. A. and Triwahyono, S. (2013). One–pot electro–synthesis of ZrO–ZnO/HY nanocomposite for photocatalytic decolorization of various dye–contaminants. Chemical Engineering Journal, 225: 254 – 265.

- Sapawe, N. (2015). Hybridization of zirconia, zinc and iron supported on HY zeolite as a solar-based catalyst for the rapid decolorization of various dyes. New Journal of Chemistry, 39: 4526 – 4533.

- Sapawe, N. and Hanafi, M. F. (2016). Facile one-pot electrolysis of high photoreactive hexacoordinated Si with Zr and Zn catalyst. RSC Advances, 5: 75141 – 75144.