# Malaysian Journal of Analytical Sciences Vol 20 No 6 (2016): 1524 - 1529

# THE EFFECT OF POLYMER CONCENTRATION AND SURFACTANT TYPES ON NANOFILTRATION-SURFACTANT MEMBRANE FOR TEXTILE WASTEWATER

# (Kesan Kepekatan Polimer dan Jenis Surfaktan pada Membran Surfaktan Penurasan-Nano untuk Air Sisa Tekstil)

# Sarah Husnaini Zainal, Abdul Rahman Hassan*, Mohd Hafez Mohd Isa

# Industrial Membrane Technology Laboratory, Department of Industrial Chemical Technology,

# Faculty of Science and Technology,

# Universiti Sains Islam Malaysia, 71800 Nilai, Negeri Sembilan, Malaysia

*Corresponding author: abdrahman@usim.edu.my

Received: 24 February 2015; Accepted: 27 October 2015

Abstract

In this study, an asymmetric nanofiltration-surfactant (NFS) membrane was prepared via simple dry/wet phase inversion technique. A newly dope formulation consisting of different surfactants (SDS, CTAB) and polymer concentration (17 wt% - 21 wt%) were developed. The effect of these parameters on dyes performance in terms of dyes flux, rejection and morphological structure were examined. Experimental data showed that, at different ranges of polymer concentration, NFS membranes shows low permeation flux of dyes ranging from 9.256 L/m2h to 14.315 L/m2h at 4 bar operating pressure. Significantly, the addition of SDS and CTAB surfactants were found to promote the increasing of dyes flux and rejection up to 79.698 L/m2h and 99.5% respectively. Addition of surfactant shows the membrane surface morphology with upper layer and support layer consists of finger-like structure, finger-like channel, macrovoids and spongy structure.

# Keywords:  nanofiltration, surfactant, flux, rejection, morphological structure

# Abstrak

# Dalam kajian ini, membran surfaktan penurasan-nano telah disediakan melalui teknik fasa berbalik kering/basah mudah. Satu formulasi baru polimer yang terdiri daripada surfaktan yang berbeza (SDS,CTAB) dan kepekatan polimer (17 wt% - 21 wt%) telah disediakan. Kesan parameter ini terhadap prestasi pewarna dari segi fluks warna, penolakan dan struktur morfologi telah diperiksa. Data ujikaji menunjukkan bahawa, pada jarak yang berbeza kepekatan polimer, keputusan fluks membran NFS menyerap rendah pewarna antara 9.256 L/m2h kepada 14.315 L/m2h pada 4 bar tekanan operasi. Lebih penting lagi, penambahan SDS dan CTAB sebagai surfaktan didapati menggalakkan peningkatan fluks pewarna dan penolakan sehingga masing – masing adalah 79.698 L/m2h dan 99.5%. Penambahan surfaktan menunjukkan morfologi permukaan membran dengan lapisan atas dan lapisan sokongan yang terdiri daripada struktur jejari, saluran jejari, makrovoid dan struktur lembut.

# Kata kunci:  penurasan-nano, surfaktan, fluks, penolakan, struktur morfologi

References

- Wang, X. L., Shang, W. J., Wang, D. X., Lu, L. and Tu, C. H. (2009). Characterization and applications of nanofiltration membranes: State of the art, Desalination, 236: 316 – 326.

- Ismail, A. F. and Hassan, A. R. (2004). The deduction of fine structural details of asymmetric nanofiltration membranes using theoretical models. Journal of Membranes Science, 231: 25 – 36.

- Ismail, A. F. and Hassan, A. R. (2006). Formation and characterization of asymmetric nanofiltration membrane: Effect of shear rate and polymer concentration. Journal of Membrane Science, 270: 57 – 72.

- Kowalska, I., Korbutowicz, M. K., Nowak, K. M. and Winnicki, T. (2004). Separation of anionic surfactants on ultrafiltration membranes. Desalination, 162: 33 – 40.

- Tsai, H.A., Li, L. D., Lee, K. R., Wang, Y. C., Li, C. L., Huang, J. and Lai, J. Y. (2000). Effect of surfactant addition on the morphology and pervaporation performance of asymmetric polysulfone membranes. Journal of Membrane Science, 176: 97 – 103.

- Amirilargani, M., Saljoughi, E. and Mohammadi, T. (2009). Effects of Tween-80 concentration as a surfactant additive on morphology and permeability of flat sheet polyethersulfone (PES) membrane. Desalination, 249: 837 – 842.

- Rahimpour, A., Madaeni, S. S. and Mansourpanah, Y. (2007). The effect of anionic, non-ionic and cationic surfactants on morphology and performance of polyethersulfone ultrafiltration membranes for milk concentration. Journal of Membrane Science, 296: 110 – 121.

- Akbari, A., Remigy, J. C. and Aptel, P. (2002). Treatment of textile effluent using a polyamide-based nanofiltration membrane. Chemical Engineering and Processing, 41: 601 – 609.

- Huang, J., Liu, L., Zeng, G., Li, X., Peng, L., Li, F., Jiang, Y., Zhao, Y. and Huang, X. (2014). Influence of feed concentration and transmembrane pressure on membrane fouling and effect of hydraulic on the performance of ultrafiltration. Desalination, 335: 1 – 8.

- Saedi, S., Madaeni, S. S., Shamsabadi, A. A. and Mottaghi, F. (2012). The effect of surfactants on the structure and performance of pes membrane for separation of carbon dioxide from methane. Separation and Purification Technology, 99: 104 – 119.