# Malaysian Journal of Analytical Sciences Vol 20 No 6 (2016): 1278 - 1285

# SYNTHESIS AND PHYSICOCHEMICAL CHARACTERIZATION OF CATIONIC POLYMERIC SURFACTANT FROM Dioscorea pyrifolia STARCH

# (Sintesis dan Pencirian Fizikokimia Surfaktan Polimer Kationik daripada Kanji Dioscorea pyrifolia)

# Elmi Sharlina Md. Suhaimi, Wan Yaacob Wan Ahmad*, Azwan Mat Lazim

# School of Chemical Sciences and Food Technology, Faculty of Science and Technology

# Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor, Malaysia

# *Corresponding author: wanyaa@ukm.edu.my

Received: 21 April 2016; Accepted: 3 October 2016

Abstract

# Cationic starch-based polymeric surfactant, 2-hydroxy-3-(N,N,N-trimethylammonium)propyloxy starch (S-ETAC) from Dioscorea pyrifolia tubers, was synthesized by etherification using 2,3-epoxytrimethylammonium chloride (ETAC) in the mass ratio of ETAC/starch (St) of 0.15:1, 0.25:1, 0.5:1, 1:1, 2:1 g/g and sodium hydroxide as a catalyst in aqueous medium. The degree of substitution (DS) and reaction efficiency (RE) were calculated using the percentage of nitrogen derived from the elemental analysis. The study found that the more the ETAC used, the higher the DS (0:11 to 0.76), but the RE decreased (69% to 35%). This S-ETAC was characterized by using the solubility and swelling power tests as well as attenuated total reflectance - Fourier transform infra-red (ATR - FTIR) spectroscopy, differential scanning calorimetry (DSC) and X-ray diffraction (XRD) to prove the reaction occurs at the starch structure.

# Keywords:  cationic starch, etherification, Dioscorea pyrifolia

# Abstrak

# Surfaktan polimer berasaskan kanji kationik, kanji 2-hidroksi-3-(N,N,N-trimetilammonium)propiloksi (S-ETAC) dari ubi Dioscorea pyrifolia, telah disintesis melalui tindak balas pengeteran menggunakan 2,3-epoksitrimetil-ammonium klorida (ETAC) dalam nisbah jisim ETAC/kanji (St) 0.15: 1, 0.25: 1, 0.5: 1, 1: 1, 2: 1 g/g dan natrium hidroksida sebagai pemangkin dalam medium akueus. Darjah penukargantian (DS) dan kecekapan tindak balas (RE) telah dikira menggunakan peratusan nitrogen yang diperolehi daripada penganalisis unsur. Kajian ini mendapati bahawa lebih banyak ETAC yang digunakan, semakin tinggi DS (0:11 kepada  0.76), tetapi RE menurun (69% kepada 35%). S-ETAC dicirikan dengan menggunakan kelarutan dan ujian kuasa pembengkakkan serta spektroskopi transformasi Fourier infra merah - jumlah pantulan teratenuat (FTIR - ATR), kalorimetri pengimbas pembezaan (DSC) dan pembelauan sinar-X (XRD) untuk membuktikan bahawa tindak balas berlaku pada struktur kanji.

# Kata kunci:  kanji kationik, pengeteran, Dioscorea pyrifolia

References

- Wang, Y. and Xie, W. (2010). Synthesis of cationic starch with a high degree of substitution in an ionic liquid. Carbohydrate Polymers, 80 (4): 1172 – 1177.

- Chiu, C. and Solarek, D. (2009). Modification of starches. starch: Chemistry and technology. New York: Academic Press: pp. 629 – 655.

- Wang, P., Wu, X., Dong-Hua, X., Kun, X., Ying, T., Xi-Bing, D. and Wen-Bo, L. (2009). Preparation and characterization of cationic corn starch with a high degree of substitution in dioxane-THF-water media. Carbohydrate Research, 344 (7): 851 – 855.

- Heinze, T., Haack, V. and Rensing, S. (2004). Starch derivatives of high degree of functionalization preparation of cationic 2-hydroxy-propylthrimethylammonium chloride starches. Starch/Starke, 50: 487 – 492.

- Burkill, I. H. (1966). A dictionary of the economic products of the Malay Peninsula. Kuala Lumpur: Government of Malaysia and Singapore. I (A - H).

- Lin, Q., Qian, S., Li, C., Pan, H., Wu, Z. and Liu, G. (2012). Synthesis, flocculation and adsorption performance of amphoteric starch. Carbohydrate Polymers, 90 (1): 275 – 283.

- Zhang, M. (2007). Synthesis of cationic hydrolyzed starch with high DS by dry process and use in salt-free dyeing. Carbohydrate Polymers, 69: 123 – 129.

- Jiang, Q., Gao, W., Li, X., Xia, Y., Wang, H., Wu, S., Huang, L., Liu, C. and Xiao, P. (2012). Characterization of starches isolated from five Dioscorea L. Species. Food Hydrocolloids, 29 (1): 35 – 41.

- Chen, G., Zhang, B., Zhao, J. and Chen, H. (2013). Improved process for the production of cellulose sulfate using sulfuric acid / ethanol solution. Carbohydrate Polymers, 95 (1): 332 – 337.

- Regina, S. A. S., Yaacob, W. W. A., Shazrul, F., Nurul, I. H. and Azwan, M. L. (2016). Transformation of crystalline starch nanoparticles into high luminescent carbon nanodots: Toxicity studies and their application. Carbohydrate Polymers, 137: 488 – 496.

- Kavaliauskaite, R., Klimaviciute, R. and Zemaitaitis, A. (2008). Factors influencing production of cationic starches. Carbohydrate Polymers, 73: 665 – 675.

- Zhang, B., Ni, B., Lu, S., Cui, D., Liu, M., Gong, H. and Han, F. (2012). Synthesis and characterization of novel potato starch derivative with cationic acetylcholine groups. International Journal of Biological Macromolecules, 50: 701 – 706.