# Malaysian Journal of Analytical Sciences Vol 21 No 1 (2017): 105 - 112

# CYCLIC VOLTAMMETRY STUDIES OF THE CORROSION PROCESS

# ON THE STAINLESS STEEL ELECTRODES IN THE ACIDIC THIOUREA SOLUTION

# (Kajian Voltammetri Berkitar Terhadap Proses Pengkakisan di atas Permukaan Elektrod Keluli Tahan Karat di dalam Larutan Tiourea Bersasid)

# Amirul Islah Nazri, Nor Irwin Basir, Muhamad Nazri Murat*

# School of Chemical Engineering, Engineering Campus,

# Universiti Sains Malaysia, 14300 Nibong Tebal, Pulau Pinang, Malaysia

*Corresponding author: chnazri@usm.my

Received: 21 October 2015; Accepted: 14 June 2016

Abstract

# A cyclic voltammetry study has been carried out in order to determine the voltage range that contributes to the initiation of the corrosion on the surface of stainless steel in the acidic thiourea solution. In this study, the knowledge of corrosion on stainless steel is useful in the optimisation process for gold recovery from electronic waste based on electrodeposition technique.  Since stainless steel material has been used as both anode and cathode in the experimental setup, under certain applied voltage, corrosion might occur and hinder the gold recovery process by damaging the electrodes. With the aid of cyclic voltammetry study, the suitable applied voltage for electrodeposition process has been investigated and found to be approximately 1.4 V for two-electrode setup for a system with sulfuric acid concentration of 0.1 M in the presence of 0.1 M thiourea. The data obtained can be used as a basis to determine a suitable pre-set applied voltage in the electrodeposition process such that corrosion on the electrodes can be avoided.

# Keywords:  cyclic voltammetry, stainless steel, corrosion, acidic thiourea solution

# Abstrak

# Suatu kajian menggunakan kaedah voltammetri berkitar (CV) telah dijalankan bertujuan untuk menentukan julat voltan yang menyumbang kepada permulaan proses pengkakisan di atas permukaan keluli tahan karat di dalam larutan tiourea berasid. Dalam kajian ini, pengetahuan mengenai proses pengkakisan terhadap keluli tahan karat berguna dalam proses pengoptimuman terhadap perolehan emas daripada sisa buangan elektronik berasaskan kepada teknik elektropeendapan. Memandangkan bahan keluli tahan karat digunakan sebagai anod dan katod di dalam persediaan eksperimen, di bawah voltan gunaan tertentu, proses pengkakisan berkemungkinan berlaku dan boleh menghalang proses perolehan emas dengan merosakkan elektrod. Dengan bantuan dari kajian voltammetri berkitar, voltan gunaan yang sesuai untuk proses elektropeendapan telah dikaji dan hasil dari kajian mendapati bahawa nilai voltan gunaan tersebut adalah sebanyak lebih kurang 1.4 V untuk konfigurasi dua-elektrod untuk satu sistem dengan kepekatan asid sulfurik sebanyak 0.1 M dalam kehadiran tiourea 0.1 M. Data yang diperolehi dapat digunakan sebagai asas bagi menentukan voltan gunaan yang sesuai dalam proses elektropeendapan, dalam masa yang sama proses pengkakisan terhadap elektrod dapat dielakkan.

# Kata kunci:  oltammetri berkitar, keluli tahan karat, pengkakisan, larutan tiourea bersifat asid

References

- Revie, R. W. and Uhlig, H. H. (2008). Corrosion and corrosion control. 4th ed. United States of America: John Wiley & Sons.

- Albrimi, Y. A., Eddib, A., Douch, J., Berghoute, Y., Hamdani, M. and Souto, R. M. (2011). Electrochemical behaviour of AISI 316 austenitic stainless steel in acidic media containing chloride ions. International Journal of Electrochemical Science, 6: 4614 – 4627.

- Iliyasu, I., Yawas, D. S. and Aku, S. Y. (2012). Corrosion behavior of austenitic stainless steel in sulfuric acid at various concentration. Advances in Applied Science Research, 3 (6): 3909 – 3915.

- Bolzan, A. E., Piatti, R. C. V. and Arvia, A. J. (2003). Electrochemical processes at gold∣thiourea-containing aqueous acid solution interfaces. Journal of Electroanalytical Chemistry, 552: 19 –  34.

- Gomez, H., Lizama, H., Suarez, C. and Valenzuela, A. (2009). Effect of thiourea concentration on the electrochemical behavior of gold and copper electrodes in presence and absence of Cu (II) ions. Journal of the Chilean Chemical Society, 54 (4): 439 – 444.

- Shetsova, O. N., Bek, R. Y., Zelinskii, A. G. and Vais, A. A. (2006). Anodic behavior of gold in acid thiourea solutions: A cyclic voltammetry and quartz microgravimetry study. Russian Journal of Electrochemistry, 42 (3): 239 – 244.

- Yang, X. Y., Moats, M. S. and Miller, J. D. (2010). The interaction of thiourea and formamidine disulfide in the dissolution of gold in sulfuric acid solutions. Minerals Engineering, 23 (9): 698 – 704.

- Zhang, H., Ritchie, I. M. and La Brooy, S. R. (2001). Electrochemical oxidation of gold and thiourea in acidic thiourea solutions. Journal of the Electrochemical Society, 148 (10): 146 – 153.

- Hilson, G. and Monhemius, A. J. (2006). Alternatives to cyanide in the gold mining industry: What prospects for the future?. Journal of Cleaner Production, 14 (12–13): 1158 – 1167.

- Nazri, A. I., Basir, N. I. and Murat, M. N. (2015). A conceptual reactor design based on combination of pressure leaching - electrochemical deposition techniques for study of gold recovery from e-waste. Advanced Materials Research, 1113: 187 – 192.

- Nazri, A. I., Basir, N. I. and Murat, M. N. (2015). Cyclic voltammetry application in determining oxidation and reduction of gold in acidic thiourea solution using gold-stainless steel paired electrode. 5th International Conference on Environment 2015 (ICENV 2015), Eastin Hotel, Penang, Malaysia.

- Pavlishchuk, V. V. and Addison, A. W. (2000). Conversion constants for redox potentials measured versus different reference electrodes in acetonitrile solutions at 25 °C. Inorganica Chimica Acta, 298 (1): 97 – 102.