# Malaysian Journal of Analytical Sciences Vol 21 No 1 (2017): 127 - 135

# Comparison Study between Extrusion and Injection Molding on Cellular Structure of PP/PS/PMMA Ternary Blend Foam

# (Kajian Perbandingan di antara Kaedah Proses Penyemperitan dan Proses Pengacuan Suntikan ke atas Struktur Sel PP/PS/PMMA Campuran Pertigaan Busar Polimer)

# Rahida Wati Sharudin1,3* and Masahiro Ohshima2

# 1Faculty of Chemical Engineering,

# Universiti Teknologi MARA, 40450 Shah Alam, Selangor, Malaysia

# 2Department of Chemical Engineering,

# Kyoto University, Kyoto 615-8510, Japan

3Institute for Infrastructure Engineering & Sustainable Management (IIESM), Faculty of Civil Engineering,

Universiti Teknologi MARA, 40450 Shah Alam, Malaysia

# *Corresponding author: rahida@salam.uitm.edu.my

Received: 21 October 2015; Accepted: 14 June 2016

Abstract

# The effect of blending method on the blend morphology as well as cellular structure of Polypropylene (PP)/Polystyrene (PS)/ Polymethyl methacrylate (PMMA) ternary polymer blend was investigated. The blending method highly influenced the dispersion and size of dispersed domain where the injection molding method was successfully reduced the size of dispersed domain from 10 µm by extrusion further down to 1 µm in average diameter. The batch pressure quenched foaming of the ternary blend prepared by extrusion and injection molding with supercritical carbon dioxide (CO2) was conducted in the temperature range of 130 to 160°C to observe the controllability of bubble location and size in two different ternary blend systems. The experimental results showed that method of sample preparation is one of the important factors in controlling the cellular structure of ternary blend foam besides interfacial tension, foaming temperature, and viscoelasticity.

# Keywords:  polymer blend, extrusion, injection molding, cellular structure, foam

# Abstrak

# Kesan kaedah pencampuran pada morfologi dan juga struktur sel Polipropena (PP)/Polisterina (PS)/ Polimetil metaakrilat (PMMA) campuran pertigaan polimer telah dikaji. Kaedah pencampuran sangat mempengaruhi penyebaran dan saiz domain di mana kaedah pengacuan suntikan telah berjaya mengurangkan saiz domain dari 10 μm oleh kaedah penyemperitan kepada serendah 1 μm diameter purata. Proses pelepasan tekanan secara mendadak dengan karbon dioksida genting lampau (CO2) telah dijalankan bagi penghasilan sampel busar daripada gabungan pertigaan polimer dalam lingkungan suhu 60-130°C untuk melihat kebolehkawalan lokasi gelembung dan saiz. Keputusan eksperimen menunjukkan bahawa kaedah penyediaan sampel, tegangan antara permukaan dua polimer, suhu pembentukan busar dan likat-kenyal adalah faktor penting untuk mengawal struktur sel dalam sistem gabungan pertigaan polimer.

# Kata kunci:  percampuran polimer, penyemperitan, pengacuan suntikan, struktur sel, busar

References

- Hsu, W.P. (2007).  A closed-loop  behavior  of  ternary  polymer  blends  composed of three miscible binaries. Thermochimica Acta, 454: 50 – 56.

- Tseng, F. P., Lin, J. J., Tseng, C. R. and Chang, F. C. (2001). Poly(oxypropylene)-amide grafted polypropylene as novel compatibilizer for PP and PA6 blends. Polymer, 42: 713 – 725.

- Radusch, H. J., Dosher, P. and Lause, G. (2005).  Phase  behaviour  and mechanical properties of heterophasic polypropylene-ethylene/ propylene copolymers systems. Polymer, 50: 279 – 285.

- Li,  X.,  Han, Y. and  An, L. (2003).  Surface  morphology  control  of  immiscible  polymer-blend  thin  films. Polymer, 44:  8155 – 8165.

- Guo, H. F., Packirisamy, S., Gvozdic, N. V. and Meier D. J. (1997). Prediction and manipulation of the phase morphologies of multiphase polymer blends: 1. Ternary systems. Polymer, 38: 785 – 794.

- Sharudin, R.W., Alwi, H. and Ohshima, M. (2013).   PP/PS/PMMA  ternary  blend foaming using supercritical co2. Advanced Materials Research, 701: 17 – 22.

- Gnatowski, A. and Koszkul, J. (2005).  Investigations  of  the influence of compatibilizer and filler type on the properties of chosen polymer blends. Journal of Materials Processing Technology, 162 – 163: 52 – 58.

- Kim, J. K., Yi, D. K., Jeon, H. K. and Park, C. E. (1999).  Effect  of  the  functional group inhomogeneity of an in situ  reactive  compatibilizer  on  the  morphology  and  rheological properties of immiscible polymer blends. Polymer, 40: 2737 – 2743.

- Zhai,  W.,  Wang, H., Yu, J., Dong, J. and He, J. (2008).  Foaming  behaviour  of  polypropylene/  polystyrene blends enhanced by improved interfacial compatibility. Journal of Polymer Science Part B: Polymer Physics, 46: 1641 – 1651.

- Zhang, Q., Yang, H. and Fu, Q. (2004).  Compatibilization  of  immiscible poly(propylene)/polystyrene blends using clay. Polymer, 45 : 1913 – 1922.

- Elias, L., Fenouillot, F., Majeste, J. C. and Cassagnau, P. H. (2007).  Morphology  and rheology of immiscible polymer blends filled with silica nanoparticles. Polymer, 48: 6029 – 6040.

- Son, Y., Ahn, K. H. and Char, K. (2011).  Effects of processing conditions and reactive compatibilizers on the morphology of injection molded poly(phenylene oxide)/Nylon 6 Blends. Polymer Engineering and Sciences, 40: 1385 – 1394.

- Reignier, J., Favis, B. D. and Heuzey, M-C. (2003).  Factors  influencing  encapsulation behavior in composite droplet-type polymer blends. Polymer, 44(1): 49 – 59.

- Valera, T. S., Morita, A. T. and Demarquette, N. R. (2006).  Study  of  morphologies of PMMA/PP/PS ternary blends. Macromolecules, 39(7): 2663 – 2675.

- Zhong, G. J. and Li, Z. M. (2005).  Injection  molding-induced  morphology  of thermoplastic polymer blends. Polymer Engineering and Sciences, 45(12): 1655 – 1665.