Malaysian Journal of Analytical Sciences Vol 21 No 1 (2017): 136 - 148

SYNTHESIS AND CHARACTERIZATION OF HYDROXYAPATITE NANOPARTICLE

# (Sintesis dan Pencirian Nanozarah Hidrosiapatit)

# Sahlil Miraz Mohamed Rafie* and Darman Nordin

# Department of Chemical and Process Engineering,

# Faculty of Engineering and Built Environment,

# Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor, Malaysia

*Corresponding author: sahlilmiraz.rafie@gmail.com

Received: 21 October 2015; Accepted: 14 June 2016

Abstract

# In this research, hydroxyapatite (HA) nano-size powder was synthesized using wet chemical precipitation technique under atmospheric pressure where calcium hydroxide (Ca(OH)2) and ortho-phosphoric acid (H3PO4) were used as precursors. Distilled water was used as a diluting media for the reaction and sodium hydroxide (NaOH) was used to control the initial pH. The initial pH values, reaction temperature and calcined temperature play an important role in the morphology on HA as well as the phase formation and degree of crystallinity. Nano HA powder has been studied at different initial pH value which is between 9.00 to 11.00, reaction temperature from 80 °C to 100 °C and calcined temperature at 700 °C to 800 °C. The optimum initial pH value was found at pH 10.00, reaction temperature at 100 °C and calcined temperature was at 800 °C. The crystallographic properties were evaluated by X-ray diffraction (XRD), Fourier Transform Infrared (FTIR) and Field Emission Scanning Microscope (FESEM). The Design Expert version 9.0.2 with statistical and graphical analysis of the result, by using analysis of variance (ANOVA) was applied to optimize variable in the process of synthesis of HA. Based on analysis of variance (ANOVA) that has been perform, calcined temperature was to be influential variables on mass of HA with value of probability less than 0.05.

# Keywords:  hydroxyapatite, chemical precipitation, crystallinity, morphology, optimization

# Abstrak

Dalam kajian ini, nanozarah hidroksiapatit (HA) dihasilkan melalui kaedah pemendakan di bawah tekanan atmosfera di mana kalsium hidroksida (Ca(OH)2) dan asid orto fosforik (H3PO4) merupakan larutan asas bagi penyediaan HA. Air suling digunakan sebagai agen pelarut dalam menyediakan larutan asas bagi proses pemendakan ini. Larutan natrium hidroksida di gunakan bagi mengawal nilai pH. Nilai pH, suhu tindak balas dan suhu relau merupakan faktor penting dalam pencirian dan penghabluran nanozarah HA. Nanozarah HA disediakan pada nilai pH antara 9.00 hingga 11.00, suhu tindak balas 80 °C hingga 100 °C dan suhu relau pada 700 °C hingga 800 °C. Pencirian nanozarah HA di uji menggunakan X-ray Difractometer (XRD), Inframerah Transformasi Fourier (FTIR), dan Mikroskop Pengimbas Pancaran Medan (FESEM). Perisian Design-Expert 9.0.2 digunakan untuk menganalisis data dan pengoptimuman penghasilan mendakan HA.  Berdasarkan analisis varian (ANOVA) yang dilakukan, suhu relau merupakan pemboleh ubah yang mempengaruhi berat HA dengan nilai kemungkinan kurang dari 0.05.

# Kata kunci:  hikdroksiapatit, mendakan bahan kimia, penghabluran, pencirian, pengoptimuman

References

- Eshtiagh-Hosseini, H., Housaindokht, M. R. and Chahkandi, M. (2007). Effects of parameters of sol–gel process on the phase evolution of sol–gel-derived hydroxyapatite. Materials Chemistry and Physics, 106(2): 310 – 316.

- Feng, W., Mu-Sen, L., Yu-Peng, L. and Yong-Xin, Q. (2005). A simple sol–gel technique for preparing hydroxyapatite nanopowders. Materials Letters, 59(8): 916 – 919.

- Yin, G., Liu, Z., Zhan, J., Ding, F. and Yuan, N. (2002). Impacts of the surface charge property on protein adsorption on hydroxyapatite. Chemical Engineering Journal, 87(2): 181 – 186.

- Kramer, E., Podurgiel, J. and Wei, M. (2014). Control of hydroxyapatite nanoparticle morphology using wet synthesis techniques: Reactant addition rate effects. Materials Letters, 131: 145 – 147.

- Mostafa, A. A., Oudadesse, H., Mohamed, M. B., Foad, E. S., Le Gal, Y. and Cathelineau, G. (2009). Convenient approach of nanohydroxyapatite polymeric matrix composites. Chemical Engineering Journal, 153(1): 187 – 192.

- Wang, P., Li, C., Gong, H., Jiang, X., Wang, H. and Li, K. (2010). Effects of synthesis conditions on the morphology of hydroxyapatite nanoparticles produced by wet chemical process. Powder Technology, 203(2): 315 – 321.

- Wijesinghe, W. P. S. L., Mantilaka, M. M. M. G. P. G., Premalal, E. V. A., Herath, H. M. T. U., Mahalingam, S., Edirisinghe, M., Rajapakse, R.  P. V. J. and Rajapakse, R. M. G. (2014). Facile synthesis of both needle-like and spherical hydroxyapatite nanoparticles: Effect of synthetic temperature and calcination on morphology, crystallite size and crystallinity. Materials Science and Engineering: C, 42: 83 – 90.

- Abidi, S. S. A. and Murtaza, Q. (2014). Synthesis and characterization of nano-hydroxyapatite powder using wet chemical precipitation reaction. Journal of Materials Science & Technology, 30(4): 307 –310.

- Stanić, V., Dimitrijević, S., Antonović, D. G., Jokić, B. M., Zec, S. P., Tanasković, S. T. and Raičević, S. (2014). Synthesis of fluorine substituted hydroxyapatite nanopowders and application of the central composite design for determination of its antimicrobial effects. Applied Surface Science, 290: 346 – 352.