# Malaysian Journal of Analytical Sciences Vol 21 No 2 (2017): 452 - 459

# RESPONSE SURFACE METHODOLOGY ON WAX DEPOSIT OPTIMIZATION

# (Pengoptimuman Lilin Mendap Menggunakan Kaedah Gerak Balas Permukaan)

# Norida Ridzuan*, Zulkefli Yaacob, Fatmawati Adam

# Faculty of Chemical Engineering & Natural Resources,

# Universiti Malaysia Pahang, 26300 Gambang, Pahang, Malaysia

*Corresponding author: norida@ump.edu.my

Received: 21 October 2015; Accepted: 14 June 2016

Abstract

# In this study, the application of response surface method design based on rotatable central composite design (CCD) was used to optimize wax deposit using Design Expert 7.1.6 software. The process consisted of 13 experiments involving eight factorial points and five replications at the center point. The influence of operating parameters on the weight of wax deposit was investigated using cold finger apparatus. The experimental result indicated that the amount of wax deposit was significant due to factors of cold finger temperature and experimental duration. The wax deposit amount decreased significantly with the decrease of experimental duration when the cold finger temperature increased to 25 °C. The minimum value of 0.0042 g of wax deposit was obtained at the optimized conditions of 1.5 hours  and 25 °C, respectively.

# Keywords:  cold finger method, crude oil, optimization

# Abstrak

# Dalam kajian ini, penggunaan kaedah gerak balas permukaan berdasarkan reka bentuk komposit berpusat berputar (CCD) digunakan bagi mengoptimumkan lilin mendap menggunakan perisian Design Expert 7.1.6. Proses ini terdiri daripada 13 eksperimen yang melibatkan lapan titik faktorial dan lima ulangan di titik pusat. Pengaruh parameter operasi terhadap berat lilin mendap telah dikaji dengan menggunakan radas jejari sejuk. Hasil eksperimen menunjukkan bahawa jumlah lilin mendap dipengaruhi oleh faktor suhu jejari sejuk serta tempoh eksperimen.  Jumlah lilin mendap akan berkurang sekiranya tempoh eksperimen dikurangkan berserta peningkatan suhu jejari sejuk kepada 25 °C. Nilai minimum 0.0042g lilin mendap telah diperolehi pada keadaan yang optimum iaitu pada 1.5 jam dan 25 °C .

# Kata kunci:  kaedah jejari sejuk, minyak mentah, pengoptimuman

References

- Adewusi, V. (1997).  Prediction  of  wax  deposition potential of hydrocarbon systems from viscosity-pressure correlations. Fuel, 76: 1079 – 1083.

- Alben, K. (2002). Design, analyze, and optimize with Design-Expert. Analytical Chemistry, 74: 222 –223.

- Alghanduri, L. M., Elgarni, M. M., Daridon, J.L., and  Coutinho, J. A. P. (2010).  Characterization  of  Libyan waxy crude oils. Energy & Fuels, 24: 3101 – 3107.

- Azevedo, L.F.A., and Teixeira, A. M. (2003). A critical review of the modeling of wax deposition mechanisms. Petroleum Science and Technology, 21: 393 – 408.

- Benallal, A., Maurel, P., Agassant, J. F., Darbouret, M., Avril, G. and Pueriere, E. (2008).  Wax  deposition  in pipelines:  Flow-loop  experiments  and  investigations  on  a  novel  ppproach.   In Proceeding of SPE Annual Technical Conference and Exhibition: pp. 1 – 17.

- Huang, Z. (2011).   Application   of   the  fundamentals  of  heat  and  mass transfer to the investigation of wax deposition in subsea pipelines.Ph.D Thesis. University of Michingan,USA.

- Huang, Z., Lu, Y.,  Hoffmann, R. and  Fogler, H. S. (2011).   The   effect  of  operating  temperatures  on  wax deposition. Energy & Fuels, 25: 5180 – 5188.

- Jennings, D. W., and Breitigam, J. (2010).   Paraffin  inhibitor  formulations for different application  environ-ments:  From  heated  injection  in  the desert  to extreme cold arctic temperatures. Energy & Fuels, 24: 2337 – 2349.

- Jennings, D. W. and Weispfennig, K. (2005).  Effects of  shear  and temperature on wax deposition: Coldfinger investigation with a Gulf of Mexico crude oil. Energy & Fuels, 19:1376 – 1386.

- Jennings, D. W., and Weispfennig, K. (2006).  Effect of  shear on the  performance of paraffin inhibitors: Cold finger investigation with Gulf of Mexico crude oils. Energy & Fuels, 20: 2457 – 2464.

- Kelechukwu, E., Said Al-Salim, H. S., and Yassin, A. A. M. (2010). Influencing factors governing paraffin wax deposition during crude production. International Journal of the Physical Sciences, 5: 2351 – 2362.

- Kelland, M. A. (2014). Production Chemicals for the oil and gas industry. Second Edition. CRC Press.

- Lashkarbolooki, M., Esmaeilzadeh, F. and  Mowla, D. (2011).  Mitigation  of  wax  deposition by wax-crystal modifier for Kermanshah crude oil. Journal of Dispersion Science and Technology, 32: 975 –985.

- Lashkarbolooki, M.,  Seyfaee, A.,  Esmaeilzadeh, F.  and  Mowla, D. (2010).   Experimental  investigation  of wax deposition in Kermanshah crude oil through a monitored flow loop apparatus. Energy & Fuels, 24: 1234 – 1241.

- Lazić, Ž. R. (2004). Design of experiments in chemical engineering: A practical guide. John Wiley & Sons.

- Lee, H.V. and Taufiq-yap, Y. H. (2015). Optimization study of binary metal oxides catalyzed transesterification system for biodiesel production. Process Safety and Environmental Protection, 94: 430 – 440.

- Mahto, V., Verma, D., Kumar, A. and Sharma, V. P.  (2014).  Wax  deposition  in  flow  lines  under  dynamic conditions. Petroleum Science and Technology, 32: 1996 – 2003.

- Misra, S., Baruah, S. and Singh, K. (1995).  Paraffin  problems  in crude  oil  production  and transportation: A review. SPE Production & Facilities, 10: 50 – 54.

- Kelechukwu, E. M., Said Al-Salim, H., and Saadi, A. 2013.  Prediction  of  wax  deposition problems of hydro-carbon production system. Journal Petroleum Science and Engineering, 108: 128 – 136.

- Dos Santos, J. D. S. T., Fernandes, A. C. and Giulietti, M. (2004). Study of the paraffin deposit formation using the cold finger methodology for Brazilian crude oils. Journal Petroleum Science and Engineering, 45: 47 – 60.

- Towler, B. F., Jaripatke, O., and Mokhatab, S. 2011.  Experimental investigations of the mitigation of paraffin wax deposition in crude oil using chemical additives. Petroleum Science and Technology, 29: 468 – 483.

- Valinejad, R. and Nazar, A. R. S. (2013).  An  experimental  design  approach  for  investigating  the effects of operating factors on the wax deposition in pipelines. Fuel, 106: 843 – 850.

- Wei, B. (2015). Recent advances on mitigating wax problem using polymeric wax crystal modifier. Journal of Petroleum Exploration and Production Technology, 5: 391 – 401.

- Ridzuan,  N., Yaacob,  Z. and Adam,  F. (2016).  Screening  of  factor  influencing  wax  deposition  using  full factorial experimental design. Petroleum Science and Technology, 34: 84 – 90.