Malaysian Journal of Analytical Sciences Vol 21 No 2 (2017): 346 - 355

A COMPARATIVE STUDY ON THE INHIBITORY ACTION OF SOME GREEN INHIBITORS ON THE CORROSION OF MILD STEEL  IN HYDROCHLORIC ACID MEDIUM

(Kajian Perbandingan Tindakan Rencatan oleh Perencat Hijau ke atas Pengaratan Keluli Lembut di dalam Medium Asid Hidroklorik)

Moorthy Shyamala1* and Arthanas Arulanantham2

1Department of Chemistry,

Government College of Technology, Coimbatore-641013, Tamil Nadu, India

2Department of Chemistry,

S.N.S College of Technology, Coimbatore-641013, Tamil Nadu, India

*Corresponding author: shyamphd@yahoo.com

Received: 24 February 2015; Accepted: 9 February 2017

Abstract

The inhibitive action of the extracts of three green inhibitors namely Adathoda vasica, Eclipta alba and Centella asiatica were investigated.  Polarization method indicates that the plant extracts are under mixed control i.e promoting retardation of both anodic and cathodic reactions. The impedance method reveals that charge-transfer process controls the corrosion of mild steel. The plant-extracts obeys Langmuir adsorption isotherm. Kinetics and reason for the corrosion inhibition or the nature of adsorption is clearly shown. Physisorption mechanism has been proposed for the inhibition action of these plant extracts. The protective film formed on the surface was confirmed by Scanning Electron Microscopy (SEM). From hydrogen permeation method, all the plant extracts were able to reduce the permeation current. Results obtained in all the methods are very much in good agreement with increasing inhibition efficiency in the order: Eclipta alba > Adathoda vasica  > Centella asiatica. Among the three plant extracts studied, the maximum inhibition efficiency was found in Eclipta alba which showed 99.6% inhibition efficiency at 8.0 % v/v concentration of the extract.

Keywords:  mild steel, corrosion inhibition, plant-extracts, hydrochloric acid, physisorption

Abstrak

Tindakan perencatan oleh tiga ekstrak perencat hijau iaitu Adathoda vasica, Eclipta alba dan Centella asiatica telah dikaji. Kaedah polarisasi menunjukkan bahawa ekstrak tumbuhan di bawah kawalan campuran akan menghasilkan tindak balas perencatan bagi kedua–dua anod dan katod. Kaedah galangan mendedahkan bahawa proses pemindahan cas mengawal kakisan terhadap keluli lembut. Bahan ekstrak tumbuhan mematuhi penjerapan isoterma Langmuir. Kinetik dan sebab bagi perencatan kakisan atau sifat penjerapan jelas dapat ditunjukkan. Tindakan perencatan dari ekstrak tumbuhan adalah dicadangkan sebagai mekanisma serapan fizikal. Filem pelindung yang terbentuk di permukaan telah disahkan melalui mikroskopi elektron pengimbasan (SEM). Melalui kaedah penyerapan hidrogen, semua ekstrak tumbuhan dikenalpasti dapat mengurangkan penelapan arus. Keputusan yang diperolehi dalam semua kaedah amat bersetuju dengan peningkatan kecekapan rencatan adalah mengikut tertib iaitu Eclipta alba > Adathoda vasica > Centella asiatica. Di antara ketiga–tiga ekstrak tumbuhan yang dikaji, kecekapan rencatan maksimum diperolehi dari Eclipta alba iaitu 99.6% pada 8.0% v/v kepekatan ekstrak.

Kata kunci:  keluli lembut, perencat kakisan, ekstrak tumbuhan, asid hidroklorik, serapan fizikal

References

- Muthukrishnan, P., Saravana Kumar, K., Jeyaprabha, B. and Prakash, P. (2014). Anticorrosive activity of Kigelia pinnata leaves extract on mild steel in acidic media. Metallurgical and Materials Transactions  A, 45:  4510 – 4524.

- Nazeer, A. A., Shalabi, K. and Fouda, A. S. (2015). Corrosion inhibition of carbon steel by Roselle extract in hydrochloric acid solution: Electrochemical and surface study. Research on Chemical Intermediates, 41(7): 4833 – 4850.

- Gülşen, A. (2012). Corrosion inhibition of mild steel by Laurus nobilis leaves extract as green inhibitor. Research on Chemical Intermediates, 38(7): 1311 – 1321.

- Shalabi, K., Fouda, A. S., Elewady, G. Y. and El-Askalany, A. (2014). Adsorption and inhibitive properties of Phoenix dactylifera L. extract as a green inhibitor for aluminum and aluminum-silicon alloy in HCl. Protection of Metals and Physical Chemistry of Surfaces, 50(3): 420 – 431.

- Herb Information (2015). Access from www.himalayahealthcare.com/herbfinder.

- Bhargava, K. K. (1970). Himalaya herbal monograph. Indian Journal of Chemistry, 8: 664.

- Anupama, K. K. and Abraham, J. (2013). Electroanalytical studies on the corrosion inhibition behavior of guava (Psidium guajava) leaves extract on mild steel in hydrochloric acid. Research on Chemical Intermediates, 39(9): 4067 – 4080.

- Al-Otaibia, M. S., Al-Mayoufa, Khana, M., Mousaa, A. A., Al-Mazroab, S. A and Alkhathlana, H. Z. (2014). Corrosion inhibitory action of some plant extracts on the corrosion of mild steel in acidic media,  Arabian Journal of Chemistry, 7(3): 340 – 346.

- Benali, O., Selles, C. and Salghi, R. (2014). Inhibition of acid corrosion of mild steel by Anacyclus pyrethrum L. extracts. Research on Chemical Intermediates, 40(1): 259 – 268.

- Patel, N. S., Jauhariand, S., Mehta, G. N., Al-Deyab, S. S., Warad, I., and Hammouti, B. (2013). Mild steel corrosion inhibition by various plant extracts in 0.5 M sulphuric acid. International Journal of Electrochemical Science, 8: 2635 – 2655.