Malaysian Journal of Analytical Sciences Vol 21 No 4 (2017): 871 - 879

PALLADIUM PINCER COMPLEXES AS CATALYSTS FOR SELECTIVE ACTIVATION AND FUNCTIONALIZATION OF 1-PROPANOL

(Kompleks Paladium Pincer Sebagai Mangkin untuk Pengaktifan dan Pefungsian Terpilih

1-Propanol)

Sri Sugiarti1* and Craig M Jensen2

1Department of Chemistry, Faculty of Mathematics and Natural Sciences,

Bogor Agricultural University, 16680 Bogor, Indonesia

2Department of Chemistry,

University of Hawaii at Manoa, Honolulu, 96822 Hawaii, United States

*Corresponding author:  sri.sw07@gmail.com

Received: 20 September 2016; Accepted: 16 May 2017

Abstract

Selective activation and functionalization of saturated C-H bonds in the original Shilov system used a combination of PtCl42- and PtCl62- in aqueous solution to transform methane into methanol and/or methyl chloride.  On the other hand, palladium phosphinito PCP pincer halides (PdX{C6H3-2,6-(OPri2)2}, X=Cl, Br, I) have been developed for the Heck reactions of aryl halide, and they are believed to operate by an alternative Pd(II)/Pd(IV) mechanism, made this catalyst potentially used for the Shilov type reaction.  Palladium pincer complexes showed selectivity for terminal functionalization of 1-propanol at lower temperature.  Successful substitution of PtCl4 by the less expensive oxidation system, CuCl2 and air was achieved.  In the presence of CuCl2, the Wacker-like oxidation is apparently involved in the reaction.  The phosphorous donor palladium pincer complexes showed better activity and selectivity than other types of palladium pincer complexes such as NCN-Pd-Br and SCS-Pd-Cl.

Keywords:  C-H bonds activation, palladium pincer complexes, 1-propanol, selective functionalization, Shilov system

Abstrak

Pengaktifan dan pefungsian terpilih ikatan C-H tepu pada sistem asal Shilov menggunakan kombinasi larutan akueus daripada PtCl42- dan PtCl62- untuk mengubah metana menjadi metanol dan/atau metil klorida. Selain itu, paladium fosfinito PCP pincer halida (PdX{C6H3-2,6-(OPri2)2}, X=Cl, Br, I) telah digunakan untuk tindak balas Heck daripada aril klorida, dan dipercayai beroperasi melalui mekanisme alternatif Pd(II)/Pd(IV), menjadikan mangkin ini berpotensi untuk digunakan pada tindak balas jenis Shilov.  Kompleks – kompleks paladium pincer menunjukkan kepilihan terhadap pefungsian terminal 1-propanol pada suhu rendah.  Kejayaan penggantian PtCl4 oleh sistem pengoksidaan yang lebih murah iaitu CuCl2 dan udara telah dicapai. Dengan kehadiran CuCl2, tindak balas pengoksidaan Wacker terlibat secara tidak langsung. Kompleks pincer paladium dengan penderma fosforus menunjukkan aktiviti dan kepilihan yang lebih baik dibandingkan dengan jenis lain dari kompleks paladium pincer, seperti NCN-Pd-Br dan SCS-Pd-Cl.

Kata kunci:  pengaktifan ikatan C-H, kompleks paladium pincer, 1-propanol, pefungsian terpilih, sistem Shilov

References

- Konnick, M. M., Hashiguchi, B. G., Devarajan, D., Boaz, N. C., Gunnoe, T. B., Groves, J. T., Gunsalus, N., Ess, D. H., Periana, R. A. (2014). Selective CH functionalization of methane, ethane, and propane by perfluoroarene iodine(III) complex.  Angewandte Chemie, 126(39): 10658  10662.

- Labinger, J. A. and Bercaw, J. E. (2002). Understanding and exploiting C-H bond activation. Nature, 417: 507  514.

- Crabtree, R. H. (2004). Organometallic alkane CH activation. Journal of Organometallic Chemistry, 689 (24): 4083  4091.

- Shilov, A. E. and Shul’pin G. B. (1997). Activation of C-H bonds by metal complexes. Chemical Reviews, 97(8): 2879  2932.

- DeVries, N., Roe, D. C., Thorn, D. L. (2002). Catalytic hydroxylation using chloroplatinum compounds. Journal of Molecular Catalysis A: Chemical, 189 (1): 17  22.

- Jensen, C. M. (1999). Irridium PCP complexes: Highly active and robust catalysts for novel homogenous aliphatic dehydrogenation. Chemical Communications, 24: 2443  2449.

- Morales-Morales, D., Redon, R., Yung, C. and Jensen, C. M. (2004). Dehydrogenation of alkanes catalyzed by an irridium phosphinito PCP pincer complex. Inorganica Chimica Acta, 357(10): 2953  2956.

- Wang, Z., Sugiarti, S., Morales, C. M., Jensen, C. A. and Morales-Morales, D. (2006). Catalytic hydroxylation of 1-propanol by platinum NCN and PCP pincer complexes using CuCl2 as oxidant. Inorganica Chimica Acta, 359(6): 1923  1928.

- Morales-Morales, D., Grause, C., Kasaoka, K., Redon, R., Cramer, R. E. and Jensen, C. M. (2000). Highly efficient and regioselective production of trisubstituted alkenes through Heck couplings catalyzed by a palladium phosphinito PCP pincer complex.Inorganica Chimica Acta, 300: 958  963.

- Ohff, M., Ohff, A., van der Boom, M. E. and Milstein, D. (1997). Highly active Pd(II) PCP-type catalysts for the Heck reaction. Journal of the American Chemical Society, 119: 11687  11688.

- Van Beek, J. A. M., Van Koten, G., Dekker, G., Wissing, E., Zoutberg, M. C., Stam, C. H. (1990). Synthesis and reactivity towards diiodine of palladium(II) and platinum(II) complexes with non-cyclic and cyclic ligands (C6H3{CH2NR1R2}2-2,6)- End-on diiodine platinum(II) bonding in macrocyclic [PtI(C6H3{CH2NMe(CH2)7MeNCH2}-2,6)(1-I2)]. Journal of Organometallic Chemistry, 394: 659  678.

- Errington, J., McDonald, W. S. and Shaw, B. L. (1980). Cyclopalladation of C6H4(CH2SBut)2-1,3 and the crystal structure of [PdCl{C6H3(CH2SBut)2-2,6]. Journal of the Chemical Society-Dalton Transactions: 2312  2314.

- Smidt, J., Hafner, W., Jira, R., Sedlmeier, J., Sieber, R., Ruttinger, R. and Kojer, H. (1959). Katalytische umsetzungen von olefinen an platinmetall-verbindungen das consortium verfahren zur herstellung von acetaldehyd. Angewandte Chemie, 71(5): 176  182.

- Keith, J. A., Nielsen, R. J., Oxgaard, J. and Goddard, W. A. (2007). Unraveling the Wacker oxidation mechanisms. Journal of the American Chemical Society, 129(41): 12342  12343.

- Jaworski, M. A., Vega, S. R., Siri, G. J., Casella, M. L., Salvador, A. R. and Lopez, A. S. (2015). Glycerol etherification with benzyl alcohol over zirconia catalysts. Applied Catalysys A: General, 505: 36 – 43.

- Dijkstra, H. P., Meijer, M. D., Patel, J., Kreiter, R., van Klink, G. P. M., Lutz, M., Spek, A. L., Canty, A. J. and van Koten, G. (2001). Design and performance of rigid nanosize multimetallic cartwheel pincer compounds as Lewis acid catalysts. Organometallics, 20(14): 3159  3168.

- Tsuji, J. (1984). Synthetic applications of palladium catalyzed oxidation of olefins to ketones. Synthesis, 1984(05): 369  384.