# Malaysian Journal of Analytical Sciences Vol 21 No 4 (2017): 770 - 777

# CHITIN AND CHITOSAN EXTRACTION FROM Portunus pelagicus

# (Pengekstrakan Kitin dan Kitosan dari Portunus pelagicus)

# Norhidayah M. Ahyat, Faridah Mohamad, Azrilawani Ahmad, Alyza A. Azmi*

# School of Marine and Environmental Sciences,

# Universiti Malaysia Terengganu, 21030 Kuala Nerus, Terengganu, Malaysia

# *Corresponding author: alyza.azzura@umt.edu.my

Received: 30 March 2017; Accepted: 4 June 2017

Abstract

Isolation of chitin and chitosan from natural sources are widely known as they can be used in many applications. Extraction of chitin and chitosan are carried out in exoskeleton of flower crab, Portunus pelagicus. Chemical treatments such as demineralization and deproteinzation processes are used for chitin extraction, and followed by deacetylation process of chitin, which is to produce its derivatives that known as chitosan. Characterization of chitin and chitosan has been done using Fourier Transform Infrared (FTIR) Spectroscopy, X-ray diffraction (XRD), CHNS elemental analysis and Thermogravimetric analysis (TGA). Preliminary results of FTIR vibrations patterns showed stretching of hydroxyl (O-H), amine (N-H) and carbonyl (C-O) groups indicated the presence of chitin and chitosan. XRD analysis indicates the crystalline nature of chitin and chitosan. The degree of deacetylation of chitin was characterized using CHNS elemental analyzer. The extracted chitosan will be used as reducing agent for silver nanoparticles synthesis in the future studies.

# Keywords:  crustacean, marine invertebrates, bio-polymers, natural reductant

# Abstrak

# Pengasingan kitin dan kitosan daripada sumber semulajadi telah dikenali secara meluas kerana dapat digunakan dalam banyak aplikasi. Pengekstrakan kitin dan kitosan dari exoskeleton ketam bunga, Portunus pelagicus telah dilakukan. Rawatan kimia seperti proses demineralisasi dan proses deprotenisasi telah digunakan untuk pengekstrakan kitin dan diikuti dengan proses deasetilasi daripada ktin untuk penghasilan terbitannya yang dikenali sebagai kitosan. Pencirian kitin dan kitosan telah dilakukan dengan menggunakan Spektoskopi Inframerah Transformasi Fourier (FTIR), pembelauan Sinar X (XRD), analisis unsur CHNS dan analisis termogravimetri (TGA). Dapatan awal getaran FTIR menunjukkan regangan bagi kumpulan hidroksil (O-H), amino (N-H) dan karbonil (C-O) menunjukan kehadiran sebatian kitin dan kitosan. Analisis XRD menunjukkan sifat kristal bagi kitin dan kitosan. Pencirian darjah deasetilasi kitin telah dilakukan menggunakan penganalisis unsur CHNS. Ekstrak kitosan akan digunakan sebagai agen penurun bagi sintesis nanopartikel perak untuk kajian masa hadapan.

# Kata kunci:  krustasea, invertebrata marin, bio-polimer, penurun semula jadi

References

- Younes, I., Hajji, S., Frachet, V., Rinaudo, M., Jellouli, K. and Nasri, M. (2014). Chitin extraction from shrimp shell using enzymatic treatment. Antitumor, antioxidant and antimicrobial activities of chitosan. International Journal of Biological Macromolecules, 69: 489 – 498.

- Hajji, S., Ghorbel-bellaaj, O., Younes, I., Jellouli, K. and Nasri, M. (2015). Chitin extraction from crab shells by Bacillus bacteria. Biological activities of fermented crab supernatants. International Journal of Biological Macromolecules, 79: 167 – 173.

- Kumari, S. and Kumar, P. (2014). Extraction and characterization of chitin and chitosan from (Labeo rohit) fish scales. Procedia Materials Science, 6: 482 – 489.

- Palpandi, C., Shanmugam, V. and Shanmugam, A. (2009). Extraction of chitin and chitosan from shell and operculum of mangrove gastropod Nerita (Dostia) crepidularia Lamarck. International Journal of Medicine and Medical Sciences, 1(5): 198 – 205.

- Abdel-Rahman, R. M., Hrdina, R., Abdel-Mohsen,  A. M., Fouda, M. M. G., Soliman,  A. Y., Mohamed, F. K., Mohsin, K. and Pinto, T. D. (2015). Chitin and chitosan from Brazilian Atlantic Coast: Isolation, characterization and antibacterial activity. International Journal of Biological Macromolecules, 80: 107 –120.

- Gomes, J. R. B., Jorge, M., and Gomes, P. (2014). Interaction of chitosan and chitin with Ni, Cu and Zn ions : A computational study. Journal of Chemical Thermodynamics, 73: 121 – 129.

- Mohan, C. O., Ravishankar, C. N., Lalitha, K. V. and Gopal, T. K. S. (2012). Effect of chitosan edible coating on the quality of double filleted Indian oil sardine (Sardinella longiceps) during chilled storage. Food Hydrocolloids, 26: 167 – 174.

- Jayakumar, R., Prabaharan, M., Nair, S. V. and Tamura, H. (2010). Novel chitin and chitosan nanofibers in biomedical applications. Biotechnology Advances, 28 (1): 142 – 150.

- Shavandi, A., Bekhit, A. E.-D. A., Ali, M. A., Sun, Z. and Gould, M. (2015). Development and characterization of hydroxyapatite/β-TCP/chitosan composites for tissue engineering applications. Materials Science and Engineering: C, 56: 481 – 493.

- Demarchi, C. A., Campos, M. and Rodrigues, C. A. (2013). Adsorption of textile dye Reactive Red 120 by the chitosan–Fe(III)-crosslinked: Batch and fixed-bed studies. Journal of Environmental Chemical Engineering, 1(4): 1350 – 1358.

- Chandrasekar, S., Vijayakumar, S. and Rajendran, R. (2014). Application of chitosan and herbal nanocomposites to develop antibacterial medical textile. Biomedicine and Aging Pathology, 4(1): 59 – 64.

- Bae, M. J., Shin, H. S., Kim, E. K., Kim, J. and Shon, D. H. (2013). Oral administration of chitin and chitosan prevents peanut-induced anaphylaxis in a murine food allergy model. International Journal of Biological Macromolecules, 61: 164 – 168.

- Shanmugam, A., Subhapradha, N., Suman, S., Saravanan, R., Shanmugam, V. and Srinivasan, A. (2012). Characterization of biopolymer “chitosan” from the shell of donacid clam donax scortum (Linnaeus, 1758) and its antioxidant activity. International Journal of Pharmacy and Pharmaceutical Sciences, 4 (2): 460 – 465.

- Puvvada, Y. S., Vankayalapati, S. and Sukhavasi, S. (2012). Extraction of chitin from chitosan from exoskeleton of shrimp for application in the pharmaceutical industry. International Current Pharmaceutical Journal, 1(9): 258 – 263.

- Abdou, E. S., Nagy, K. S. A. and Elsabee, M. Z. (2008). Extraction and characterization of chitin and chitosan from local sources. Bioresource Technology, 99: 1359 – 1367.

- Sagheer, F. A., Al-Sughayer, M. A., Muslim, S. and Elsabee, M. Z. (2009). Extraction and characterization of chitin and chitosan from marine sources in Arabian Gulf. Carbohydrate Polymers, 77 (2): 410 – 419.

- Benhabiles, M. S., Salah, R., Lounici, H., Drouiche, N., Goosen, M. F. A. and Mameri, N. (2012). Antibacterial activity of chitin, chitosan and its oligomers prepared from shrimp shell waste. Food Hydrocolloids, 29: 48 –56.

- Bolat, Y., Bilgin, Ş., Günlü, Izci, L., Koca, D. B., Çetinkaya, S. and Koca, H. U. (2010). Chitin – chitosan yield of freshwater crab (Potamon potamios, Olivier 1804) Shell. Paskitan Veterinanry Journal, 30 (4): 227 – 231.

- Das, N. G., Khan, P. A. and Hossain, Z. (1996). Chitin from the shell of two coastal portunid crabs of Bangladesh. Indian Journal of Fisheries, 43(4): 413 – 415.

- Ramasamy, P., Subhapradha, N., Shanmugam, V. and Shanmugam, A. (2014). Extraction,   characterization and antioxidant property of chitosan from cuttlebone Sepia kobiensis (Hoyle 1885). International Journal of Biological Macromolecules, 64: 202 – 212.

- Kaya, M., Baran, T. and Mentes, A. (2014). Extraction and characterization of α -chitin and chitosan from six different aquatic invertebrates. Food Biophysics, 145 – 157.

- Kaya, M., Baublys, V., Can, E., Šatkauskiene, I., Bitim, B., Tubelyte, V. and Baran, T. (2014). Comparison of physicochemical properties of chitins isolated from an insect (Melolontha melolontha) and a crustacean species (Oniscus asellus). Zoomorphology, 133(3): 285 – 293.