# Malaysian Journal of Analytical Sciences Vol 21 No 4 (2017): 950 - 957

# DODECYLBENZENE SULFONIC ACID CONCENTRATION EFFECT ON ELECTRICAL AND THERMAL PROPERTIES OF POLYANILINE

# (Kesan Penumpuan Asid Sulfonik Dodekilbenzena ke atas Sifat Elektrik dan Termal Polianilin)

Nurul Akmil Mustaffa1*, Qumrul Ahsan1, Mohd Asyadi Azam1, Luqman Chuah Abdullah2

1Faculty of Manufacturing Engineering,

Universiti Teknikal Malaysia Melaka, Hang Tuah Jaya, 76100 Durian Tunggal, Melaka, Malaysia

2Material Processing and Technology Laboratory, Institute of Advance Technology,

Universiti Putra Malaysia, 42400 UPM Serdang, Selangor, Malaysia

# *Corresponding author: akmil.mustaffa@gmail.com

Received: 28 November 2016; Accepted: 5 February 2017

Abstract

Polyaniline (PANI) doped with various concentration of dedocylbenzene sulfonate acid (DBSA) were prepared by oxidative polymerization with presence of ammonium persulfate. Emerald green PANI powder obtained were characterized by Fourier transform infrared spectroscopy (FTIR), differential scanning calorimetry (DSC), and carried out electrical conductivity test. In this research, the conductivity and thermal properties of PANI has been changed with the effect of doping. With increasing concentration of DBSA, the conductivity raises up to certain concentration (1.65 mmol of DBSA), afterwards with further increase of DBSA concentration, conductivity value declines and reaches to a value lower than that of pristine PANI. The similar trend is also observed for enthalpy values (ΔH) determined by DSC of pristine PANI and DBSA doped PANIs’ which may attribute the effect of concentration of DBSA on molecular arrangement in PANI. Results from polymeric structure obtained from FTIR clearly indicate the disruption in bond when PANI doped with DBSA and it may indicate that the DBSA changes molecule structure of PANI in term of segmented local structure of polymer.

Keywords:  polyaniline, advanced material, dodecylbenzene sulfonate acid, conductivity, differential scanning calorimetry

# Abstrak

# Polianilin (PANI) didopkan dengan pelbagai kepekatan asid sulfonat dodekilbenzena (DBSA) telah disediakan dengan kaedah pempolimeran oksidatif dengan kehadiran ammonium persulfat. Serbuk hijau zamrud PANI yang diperolehi dicirikan oleh spektroskopi inframerah Fourier (FTIR), kalorimeter imbasan pembeza (DSC), dan ukuran kekonduksian. Dalam kajian ini, didapati bahawa kekonduksian haba dan sifat – sifat PANI telah ditukar sebagai kesan daripada pendopan. Dengan peningkatan kepekatan DBSA, kekonduksian juga meningkat sehingga kepekatan tertentu (1.65 mmol daripada DBSA). Kemudian, kekonduksian berkurangan dengan peningkatan kepekatan DBSA selanjutnya. Keputusan PANI daripada DSC, yang mengandungi nilai entalpi yang berbeza (ΔH) menunjukkan bahawa DBSA tidak mengubah struktur molekul PANI dari segi segmen struktur tempatan polimer dan ΔH juga menunjukkan ke arah kesan kepekatan DBSA pada susunan molekul dalam PANI.

# Kata kunci:  polianilin, bahan termaju, asid sulfonat dodekilbenzena, konduktiviti, kalorimeter imbasan pembeza

References

- Basavaraja, C., Pierson, R., Kim, J. H. and Huh, D. S. (2008). Microscopic studies of polyaniline-poly-n-isopropylacrylamide/alumina composites containing dodecylbenzene sulfonic acid. Bulletin of the Korean Chemical Society, 29(9): 1699 – 1704.

- Skotheim, T. A. (1986). Handbook of Conducting Polymer, Marcel Dekker, New York.

- Saini, P. and Choudhary, V. (2015). Structural, spectral and thermal properties of bulky organic sulfonic acids doped polyanilines and antistatic performance of its melt blend. Indian Journal of Pure & Applied Physics, 53(5): 320 – 327.

- Wang, Y., Ji, H., Shi, H., Zhang, T. and Xia, T. (2015). Fabrication and characterization of stearic acid/polyaniline composite with electrical conductivity as phase change materials for thermal energy storage. Energy Conversion and Management, 98: 322 – 330.

- Wallace, G. G., Spinks, G. M. and Teasdale, P. R. (1997). Conductive electroactive polymers;                         intelligent materials systems. Lancaster: Technomic.

- Socrates, G. (2004). Infrared and Raman characteristic group frequencies: tables and charts. John Wiley & Sons.

- Molapo, K. M., Ndangili, P. M., Ajayi, R. F., Mbambisa, G., Mailu, S. M., Njomo, N., Masikini, M., Baker, P. and Iwuoha, E. I. (2012). Electronics of conjugated polymers (I): polyaniline. International Journal of Electrochemical Science, 7(12): 11859 – 11875.

- Khokhlov, A. R. (1981). Theory of the polymer chain collapse for the d-dimensional case. Physica A: Statistical Mechanics and its Applications, 105(1-2): 357 – 362.

- Abrams, C. F., Lee, N. K. and Obukhov, S. P. (2002). Collapse dynamics of a polymer chain: Theory and simulation. EPL (Europhysics Letters), 59(3): 391.

- Hatakeyama, T. and Quinn, F. X. (1999). Thermal analysis: fundamentals and applications to polymer science. , 2nd Edition, John Wiley & Sons.

- Menczel, J. D. and Prime, R. B. (2014). Thermal analysis of polymers: fundamentals and applications. John Wiley & Sons.

- Pitchimani, R., Zheng, W., Simon, S. L., Hope-Weeks, L. J., Burnham, A. K. and Weeks, B. L. (2007). Thermodynamic analysis of pure and impurity doped pentaerythritol tetranitrate crystals grown at room temperature. Journal of Thermal Analysis and Calorimetry, 89(2): 475 – 478.

- Imre, Á. W., Schönhoff, M. and Cramer, C. (2008). A conductivity study and calorimetric analysis of dried poly (sodium 4-styrene sulfonate)/poly (diallyldimethylammonium chloride) polyelectrolyte complexes. The Journal of Chemical Physics, 128(13): 134905.

- Wang, Y., Ji, H., Shi, H., Zhang, T. and Xia, T. (2015). Fabrication and characterization of stearic acid/polyaniline composite with electrical conductivity as phase change materials for thermal energy storage. Energy Conversion and Management, 98: 322 – 330.

- Mustaffa, N. A., Ahsan, Q., Azam, M. A. and Abdullah, L. C. (2016). Effect of dodecylbenzene sulfonic acid dopant concentration on the synthesis of polyaniline. Jurnal Teknologi.