Malaysian Journal of Analytical Sciences Vol 21 No 4 (2017): 784 - 792

OPTICAL CHEMICAL SENSOR OF Cd(II) IN WATER BASED

ON 1-(2-PYRIDYLAZO)-2-NAPHTOL IMMOBILIZED ON

POLY(METHYL METHACRYLATE) AND 2-NITROPHENYL OCTYL ETHER MATRIX

(Sensor Kimia Optik untuk Penentuan Cd(II) dalam Air Berasaskan

1-(2-Piridilazo)-2-Naftol yang Dipegun dalam Matriks Poli(metil metaakrilat) dan

2-Nitrofenil Oktil Eter)

Moersilah1,2, Dwi Siswanta1, Roto Roto1, Mudasir Mudasir1*

1Department of Chemistry, Faculty of Mathematics and Natural Sciences,

Universitas Gadjah Mada, Sekip Utara, Yogyakarta, 55281 Indonesia

2Department of Chemistry, Faculty of Mathematics and Science,

State University of Jakarta, Jl. Pemuda No. 10 Jakarta Timur, Jakarta, Indonesia

*Corresponding author: mudasir@ugm.ac.id

Received: 18 January 2017; Accepted: 22 May 2017

Abstract

An optical chemical sensor for determination of Cd(II) in aqueous solution has been developed by immobilizing 1-(2-pyridylazo)-2-naphtol (PAN) in poly(methyl methacrylate) (PMMA) as a matrix and 2-nitrophenyl octyl ether (NPOE) as a plasticizer. The adsorption of Cd(II) causes the color of the membrane to change from yellow to red-orange with the maximum absorbance (λmax) at 556 nm. The sensor membrane gives the best response towards Cd(II) ion at pH 8.5,  after 120 minutes of contact time, at 2 ppm Cd(II), and 2 mL solution. A linear Cd(II) calibration curve can be developed in the concentration range of 0.8 - 1.8 ppm with R2 = 0.960. The limit of the detection and limit of quantification are 0.041 ppm and 0.126 ppm, respectively. The molar absorptivity is found to be 2.3 x 105 L mol-1 cm-1.  The proposed sensor membrane has been applied to the determination of Cd(II) in the river water with internal standard addition method. The observed percent recovery is in the range of 100.24 – 107.52%.

Keywords:  optical chemical sensor, 1-(2-pyridylazo)-2-naphtol, Cd(II) analysis,  poly(methyl methacrylate)

Abstrak

Reagen 1-(2-piridilazo)2-naftol (PAN) yang dipegun dalam poli(metil metaakrilat) (PMMA) dengan 2-nitrofenil oktil eter (NPOE) sebagai pemplastik untuk sensor kimia optik bagi penentuan ion Cd(II) dalam larutan akues telah dibangunkan. Jerapan ion Cd(II) telah menyebabkan penukaran warna dari kuning menjadi merah-oren dengan serapan maksimum pada (λmax) iaitu 556 nm. Membran sensor memberikan tindak balas maksimum apabila dicelupkan dalam larutan Cd(II) pada pH 8.5, selepas 120 minit masa sentuhan pada kepekatan 2 ppm Cd(II) dan 2 ml isipadu larutan. Berdasarkan kajian yang dijalankan, julat linear lengkung kalibrasi kepekatan ion Cd(II) ialah 0.8 - 1.8 ppm dan nilai R2 = 0.960. Had pengesanan dan pengkuantitian yang diperolehi masing – masing ialah 0.041 ppm dan 0.126 ppm. Daya penyerapan molar dikira pada 2.3 x 105 L mol-1 cm-1. Membran sensor ini telah dikaji untuk menentukan kepekatan Cd(II) dalam air sungai yang dipaku kaesah larutan piawai dalam. Ia telah menghasilkan pemulihan semula pada nilai 100.24 – 107.52%.

Kata kunci: Sensor kimia optik, 1-(2-piridilazo)2-naftol, analisis Cd(II), poli(metil metaakrilat)

References

- Mirzaei, M. and Pili, H. B. (2015). Potentiometric determination of cadmium using coated platinum and PVC membrane sensors based on N, N′-bis (salicylaldehyde) phenylenediamine (salophen). Journal of Analytical Chemistry, 70 (6): 731 – 737.

- Manahan, S. and Manahan, S. E. (2009). Environmental Chemistry, Ninth Edition. CRC Press, London: pp. 200 – 239.

- van der Perk, M. (2006). Soil and water contamination: from molecular to catchment scale. CRC Press, London: pp. 125 – 137.

- Urek, Š. K., Frančič, N., Turel, M. and Lobnik, A. (2013). Sensing heavy metals using mesoporous-based optical chemical sensors. Journal of Nanomaterials, 8: 1 – 13.

- da Silva, M. C. H., da Silva, L. H. M. and Paggioli, F. J. (2005). A novel micellar medium using triblock copolymer for cobalt determination. Analytical Sciences, 21 (8): 933 – 937.

- Ensafi, A. A., and Shiraz, A. Z. (2008). The combination of solid phase extraction and flame atomic absorption spectrometry for trace analysis of cadmium. Brazilian Journal of Analytical Chemistry, 19 (1): 11–17.

- Manahan, S. E. (2006). Green chemistry and the ten commandments of sustainability. 2nd edition.  ChemChar Research, Inc, Columbia: pp.159 – 176.

- Koel, M., and Kaljurand, M. (2006). Application of the principles of green chemistry in analytical chemistry. Pure and Applied Chemistry, 78(11): 1993 – 2002.

- Tobiszewski, M., Mechlińska, A. and Namieśnik, J. (2010). Green analytical chemistry – theory and practice. Chemical Society Reviews, 39(8): 2869 – 2878.

- Wardencki, W. and Namiesnik, J. (2002). Some remarks on gas chromatographic challenges in the context of green analytical chemistry. Polish Journal of Environmental Studies, 11(2): 185 – 187.

- Tharakeswar, Y., Kalyan, Y., Gangadhar, B., Kumar, K. S. and Naidu, G. R. (2012). Optical chemical sensor for screening cadmium (II) in natural waters. Journal of Sensor Technology, (2): 68 – 74.

- Ensafi, A. A., and Isfahani, Z. N. (2011). A simple optical sensor for cadmium ions assay in water samples using spectrophotometry. Journal of Analytical Chemistry, 66(2): 151 – 157.

- Tavallali, H. and Kazempourfard, F. (2009). Determination of cadmium ions by designing an optode based on immobilization of dithizone on a triacetylecelluose membrane in polluted soil and water samples. Journal of the Korean Chemical Society, 53(2): 144 – 151.

- Gavrilenko, N. A. and Saranchina, N. V. (2009). Analytical properties of 1-(2-pyridylazo)-2-naphthol immobilized on a polymethacrylate matrix. Journal of Analytical Chemistry, 64(3): 226 – 230.

- Gavrilenko, N A, Saranchina, N. V. and Gavrilenko, M. A. (2015). A colorimetric sensor based on a polymethacrylate matrix with immobilized 1-(2-pyridylazo)-2-naphthol for the determination of cobalt. Journal of Analytical Chemistry, 70(12): 1475 – 1479.

- Ensafi, A. A and Fouladgar, M. (2014). A new sensitive optical bulk test-system for thallium based on pyridylazo resorcinol. Journal of Analytical Chemistry, 69(2): 143 – 148.

- Ueno, K., Imamura, T. and Cheng, K. L. (1992). Handbook of Organic Analytical Reagent. 2nd edition, CRC Press Inc, Tokyo: pp. 209 – 368.

- De, A. K., Khopkar, A. K. and Chalmers, S. M. (1970). Solvent extraction of metals. Van Nostrand Reinhold Company, London: pp. 117 – 124.

- Mohr, G. J. (2004). Polymers for optical sensors’, in Baldini, F., Chester, A. N., Homola, J. and Martellucci, S. (ed.), Optical chemical sensor, Springer, The Netherland: pp. 297 – 322.

- Hsu, S. L. (1999). Poly(methyl methacrylate), in Mark, J. E. (ed.), Polymer data handbook. Oxford University Press, Inc., Oxford: pp. 655 – 657.

- Moghimi, A. (2011). Cr(III) selective PVC membrane electrodes based on schiff base 1-(2-pyridylazo)2-naphtol complex as an ionophore. Middle-East Journal of Scientific Research, 7(2): 147 –152.

- Sandell, H. and Onishi, E. B. (1978). Photometric determination of traces of metals general aspects 4th edition, John Wiley and Sons, Inc., New York: pp. 449 – 487.

- Moersilah, M., Siswanta, D., Roto, R. and Mudasir, M. (2017). PAN-immobilized PVC-NPOE membrane for environmentally friendly sensing of Cd(II) ions. Indonesian Journal of Chemistry, 17(1): 1 – 6.

- Donagh, C. Mc., Burke, C. S. and MacCraith, B. D. (2008). Optical chemical sensors, Chemical Reviews, 108(2): 400 – 422.

- Sombatsri, S., Wittayakun, J., Sanai, K. and Kajsanthia, K. (2012). An optical sensing film for the determination of Co(II) based on disodium-1-nitroso-2-naphthol-3,6-disulfonate immobilized in chitosan film. Sensor and Actuator B: Chemical, 166 – 167: 772 – 776.