Malaysian Journal of Analytical Sciences Vol 21 No 5 (2017): 1080 - 1090

CALCIUM CONTENT OF LIME MORTARS FROM 19th CENTURY CHURCH RUINS IN THE PHILIPPINES USING VOLUMETRIC ANALYSIS

(Kandungan Kalsium Mortar Batu Kapur dari Runtuhan Gereja Abad Ke 19 di Filipina Menggunakan Analisis Volumetrik)

Jan-Michael C. Cayme* and Aniano N. Asor, Jr

Chemistry Department, College of Science,

De La Salle University, 2401 Taft Avenue, Malate, Metro Manila, Philippines

*Corresponding author:  jm_cayme@yahoo.com

Received: 12 April 2017; Accepted: 25 July 2017

Abstract

A calcium determination method for lime mortars in old church ruins is described. Two volumetric analysis methods were employed: titration using EDTA solution, and with KMnO4 solution. The binder fraction with sieve size (<0.075mm) was used for titration which is abundant in CaCO3 as established by Fourier-Transform Infrared Spectroscopy (FTIR) technique. The mortar sample from Misamis Oriental yields a mean calcium concentration of 59.60% ± 4.64 and 60.48% ± 6.68 for EDTA and KMnO4, respectively, while the Metro Manila mortar sample is 73.54% ± 2.68 for EDTA and 73.33% ± 6.88 for KMnO4. Two tailed t-test and F-test analysis confirm that there is no statistical difference between EDTA and KMnO4 methods in determining the calcium content. Atomic Absorption Spectroscopy (AAS) technique validated the mean concentration values obtained from each method with less than 6.4% difference. The proposed titration methods are simple, rapid and sufficiently precise, without the use of expensive analytical instruments. This study is a good alternative method to easily determine the amount of calcium in historic lime mortars which is valuable in heritage conservation work and restoration of old structures in the Philippines.

Keywords: 	lime mortar, titration, Fourier transform infrared spectroscopy, atomic absorption spectroscopy, cultural heritage conservation

Abstrak

Satu kaedah penentuan kalsium untuk mortar batu kapur dalam runtuhan gereja lama telah dibincangkan. Dua kaedah analisis volumetrik telah dibangunkan; pentitratan menggunakan larutan EDTA dan KMnO4. Pecahan mengikut saiz ayak (<0.075mm) telah digunakan untuk pentitratan yang kaya dengan CaCO3 yang telah ditentukan oleh teknik inframerah transformasi Fourier (FTIR). Sampel mortar batu kapur dari Misamis Oriental menghasilkan purata kepekatan kalsium 59.60% ± 4.64 dan 60.48% ± 6.68 untuk masing-masing EDTA dan KMnO4, manakala sampel mortar batu kapur Metro Manila adalah 73.54% ± 2.68 untuk EDTA dan 73.33% ± 6.88 untuk KMnO4. Analisis ujian-t dan ujian-F mengesahkan bahawa tidak ada perbezaan signifikan antara kaedah EDTA dan KMnO4 dalam penentuan kandungan kalsium. Teknik spektroskopi serapan atom (AAS) telah menentusahkan nilai kepekatan yang diambil dari setiap kaedah memberikan perbezaan kurang daripada 6.4%. Kaedah pentitratan yang dicadangkan adalah mudah, cepat dan cukup tepat, tanpa menggunakan instrumen analisis mahal. Kajian ini merupakan alternatif yang baik dengan mudah menentukan kandungan kalsium dalam mortar batu kapur bersejarah yang berharga dalam kerja-kerja pemuliharaan warisan dan pemulihan struktur lama di Filipina.

Kata kunci: 	mortar kapur, pentitratan, spektroskopi inframerah transformasi Fourier, spektroskopi serapan atom, pemuliharaan warisan budaya

References

- Jose, Jr., R. T. (2003). Palitada: Skin of the church. In: Zero In: Skin surface essence. Ateneo Art Gallery, Ayala Foundation, Inc., Eugenio Lopez Foundation, Inc., and Museum Pambata Foundation, Inc.: pp. 27 –28.

- Elert, K., Rodriguez-Navarro, C., Sebastian Pardo, E., Hansen, E. and Cazallo, O. (2002). Lime mortars for the conservation of historic buildings. Studies in Conservation, 47: 62 – 75.

- Moropoulou, A., Bakolas, A. and Aggelakopoulou, E. (2000). The effects of limestone characteristics and calcinations temperature to the reactivity of the quicklime. Cement and Concrete Research, 31: 633 – 639.

- Neri, L. M. (2011). A report on the archaeological survey along the coastal area of Misamis Oriental, Philippines. Hukay (Journal for Archaeological Research in Asia and the Pacific), 16: 1 – 27.

- Javellana, S. J. R. B. (2010). La Casa de Dios, The legacy of Filipino-Hispanic churches in the Philippines. Pasig: Ortigas Foundation, Inc.: pp. 184 – 187.

- Cheng, K. L., Kurtz, T. and Bray, R. H. (1952). Determination of calcium, magnesium, and iron in limestone. Analytical Chemistry, 24(10):1640 – 1641.

- Skoog, D. A., West, D. M., Holler, F. J. and Crouch, S. R. (2013). Fundamentals of analytical chemistry, 9th Ed. Brooks/Cole, Cengage Learning: pp. 991 – 994.

- Page, J. O. (1968). Compleximetric determination of calcium in impure calcium carbonate and limestone. Analytica Chimica Acta, 42: 233 – 238.

- Malmstadt, H. V. and Hadjiioannou, T. P. (1958). Rapid and accurate automatic titration of calcium and magnesium in dolomites and limestones use of EDTA titran and automatic derivative spectrophotometric end-point termination. Analytica Chimica Acta, 19: 563 – 569.

- Rathore, D. P. S., Kumar, M. and Bhargava, P. K. (1997). Complexometric determination of calcium and magnesium in dolomite, limestone, magnesite, phosphatic and silicate matrices using azochromotropic acid derivative as an indicator. Chemia Analityczna (Warsaw), 42: 725 – 728.

- Hadjiioannou, T. P. and Papastathopoulous, D. S. (1970). EDTA titration of calcium and magnesium with calcium-selective electrode. Talanta, 17(5): 399 – 406.

- De Oliveira, W. and Mendes, A. (1987).  Determination of calcium and magnesium in limestone and dolomite by enthalpimetric flow-injection analysis. Talanta, 34(6): 543 – 546.

- Robinson, P. (1980). Determination of calcium, magnesium, manganese, strontium, sodium and iron in the carbonate fraction of limestones and dolomites. Chemical Geology, 28: 135 – 146.

- Middendorf, B., Hughes, J. J., Callebaut, K., Baronio, G. and Papayianni, I. (2005). Investigative methods for the characterisation of historic mortars. Part 2: Chemical characterization. Materials and Structures, 38: 771 – 780.

- Pires, J. (2015). Simple analysis of historical lime mortars. Journal of Chemical Education, 92: 521 –523.

- Cayme, J. M. and Asor, Jr, A. N. (2015). Extraction methods for quantifying iron, calcium and magnesium in a historic brickwork produced during the Spanish Colonial Period in the Philippines. KIMIKA, 26(1): 28 – 38.

- Reddy, B.V.V. and Gupta, A. (2008). Influence of sand gradation on the characteristics of mortars and soil cement block masonry. Construction and Building Materials, 22: 1614 – 1623.

- Miranda, J., Carvalho, A. P. and Pires, J. (2012). Assessment of the binder in historical mortars by various techniques. Archaeometry, 54(2): 267 – 277.

- Holtz, R. and Kovacs, W. (1981). An introduction to geotechnical engineering. Prentice-Hall, Inc, New Jersey.

- Cayme, J. M., Asor, Jr, A. N., Alano, M. K. A. T. and Miranda, E.T. (2016). Chemical characterization of historical brickwork of the church convento in Pagsanjan, Laguna. KIMIKA, 27(1): 30 – 41.

- Music, S., Filipovic-Vincekovic, N. and Sekovanic, L. (2011). Precipitation of amorphous SiO2 particles and their properties.  Brazilian Journal of Chemical Engineering, 28(1): 89 – 94.

- Couto, M. F., Peternelli, L. A. and Barbosa, M. H. P. (2013). Classification of the coefficients of variation for sugarcane crops. Ciencia Rural, Santa Maria, 43(6): 975 – 961.

- Limentani, G. B., Ringo, M. C., Ye, F., Bergquist, M. L. and McSorley, E. O. (2005). Beyond the t-test: Statistical equivalence testing. Analytical Chemistry, 77(11): 221 – 226.

- Lung, K. R., Gorko, M. A, Llewelyn, J. and Wiggins, N. (2003). Statistical method for the determination of equivalence of automated test procedures. Journal of Automated Methods and management in Chemistry, 25(6): 123 – 127.

- Miller, J. C. and Miller, J. N. (1993). Statistics for analytical chemistry, 3rd Ed. Ellis Horwood PTR Prentice Hall, New York: pp. 5 – 10.