# Malaysian Journal of Analytical Sciences Vol 21 No 5 (2017): 1101 - 1110

# RESPONSE SURFACE METHODOLOGY OPTIMIZATION OF OIL REMOVAL USING BANANA PEEL AS BIOSORBENT

# (Pengoptimuman Kaedah Gerak Balas Permukaan Untuk Penyingkiran Minyak Menggunakan Kulit Pisang sebagai Penjerap-Bio)

Najaa Syuhada Mohamad Thani1, Rozidaini Mohd Ghazi1*, Norhisyam Ismail2

1Faculty of Earth Science,

Universiti Malaysia Kelantan Jeli Campus, 17600 Jeli, Kelantan, Malaysia

2Department of Chemistry, Faculty of Science,

Uni versiti Teknologi Malaysia, 81310, Skudai Johor Bharu, Johor, Malaysia

*Corresponding author:  rozidaini@umk.edu.my

Received: 21 February 2017; Accepted: 24 August 2017

Abstract

Improper waste management of oil causes environmental pollution particularly water pollution. Conventional method in treating oil contaminants are expensive and have low removal efficiency, hence the use of natural adsorbent is suggested because of its reliability and affordability. This study aimed to use banana peel as a biosorbent for oil removal and the application of response surface methodology to identify the optimum conditions of oil removal. The adsorptive capacity of household wastes derived from banana peel towards oil were studied by using different parameters such as oil concentration, adsorbent dosage and contact time. Maximum oil adsorption of 98.86% was achieved using banana peel. The optimum conditions for oil removal were found at a dosage of 4.94 g, for 10.29 hours contact time and the initial oil concentration as high as 8.74%. The rate of oil adsorption was mathematically described as a function of experimental parameters and was modelled through response surface methodology via Box-Behnken design. The results showed that the responses of oil adsorption were significantly affected by the quadratic term of oil concentration, adsorbent dosage and contact time. The statistical analysis was performed by ANOVA which indicated good correlation of experimental parameters.

Keywords:  banana peel, oil removal, response surface methodology

Abstrak

Pengurusan sisa minyak yang tidak teratur menyebabkan pencemaran alam sekitar terutamanya pencemaran air. Kaedah konvensional untuk merawat pencemaran minyak adalah mahal dan tahap penyingkiran minyaknya adalah rendah, maka penggunaan penjerap semulajadi adalah dicadangkan kerana kebolehannya menyerap minyak dan lebih menjimatkan. Matlamat kajian ini adalah untuk menggunakan kulit pisang sebagai biopenjerap untuk penyingkiran minyak dan aplikasi kaedah gerak balas permukaan untuk mengenal pasti keadaan optimum kapasiti penyingkiran minyak. Kapasiti penjerapan daripada sisa rumah yang diambil daripada kulit pisang terhadap minyak telah dikaji dengan menggunakan parameter yang berbeza seperti kepekatan minyak, kuantiti penjerap dan tempoh masa. Penjerapan minyak secara maksimum, pada kadar 98.86% telah dicapai oleh kulit pisang. Keadaan optimum untuk menyingkirkan minyak adalah pada kadar 4.94 g, 10.29 jam dan kepekatan minyak sebanyak 8.74%. Kadar penjerapan minyak telah diterangkan secara matematik dalam fungsi parameter eksperimen dan telah dimodelkan melalui reka bentuk Box-Behnken (kaedah gerak balas permukaan). Hasil kajian menunjukkan bahawa tindak balas penjerapan minyak sangat dipengaruhi oleh kepekatan minyak, kuantiti penjerap dan tempoh masa. Analisis statistik ANOVA menunjukkan korelasi yang baik bagi setiap parameter eksperimen.

Kata kunci:  kulit pisang, penyingkiran minyak, kaedah gerak balas permukaan

References

- Hebbar, A. H. and Jayantha, K. S. (2013). Oil and grease removal from wastewater using laterite as an adsorbent material. International Journal of Emerging Technology and Advanced Engineering, 3(5): 654 – 657.

- Pawlak, Z., Rauckyte, T. and Oloyede, A. (2008). Oil, grease and used petroleum oil management and environmental economic issues. Journal of Achievements in Materials and Manufacturing Engineering, 26(1): 11 – 17.

- El-Nafaty, U. A., Muhammad, I. M. and Abdulsalam, S. (2013). Biosorption and kinetic studies on oil removal from produced water using banana peel. Civil and Environmental Research, 3(7): 125 – 136.

- Volesky, B. and Holan, Z. R. (1994) Biosorption of lead and nickel by biomass of marine algae. Biotechnology and Bioengineering, 43 (11): 1001 – 1009.

- Vlaev, L., Petkov, P., Dimitrov, A. and Genieva, S. (2011). Cleanup of water polluted with crude oil or diesel fuel using rice husks ash. Journal of the Taiwan Institute of Chemical Engineers, 42(6): 957 – 964.

- Hussein, M., Amer, A. and Sawsan, I. I. (2009). Oil spill sorption using carbonized pith bagasse. application of carbonized pith bagasse as loose fiber. Global NEST Journal, 11(4): 440 – 448.

- Cojocaru, C., Macoveanu, M. and Cretescu, I. (2011). Peat-based sorbents for the removal of oil spills from water surface: Application of artificial neural network modelling. Colloids and Surfaces A: Physicochemical and Engineering Aspects, 384 (1-3): 675 – 684.

- Banerjee, S. S., Joshi, M. V. and Jayaram, R. V. (2006). Treatment of oil spill by sorption technique using fatty acid grafted sawdust. Chemosphere, 64(6): 1026 – 1031.

- Brandao, P. C., Souza, T. C., Ferreira, C. A., Hori, C. E. and Romanielo, L. L. (2010). Removal of petroleum hydrocarbons from aqueous solution using sugarcane bagasse as adsorbent. Journal of Hazardous Materials, 175(1-3): 1106 – 1112.

- Said, A., Ludwick, A. G. and Aglan, H. A. (2009). Usefulness of raw bagasse for oil absorption: A comparison of raw and acylated bagasse and their components. Bioresource Technology, 100(7): 2219 – 2222.

- Annunciado, T. R., Sydenstricker, T. H. D. and Amico, S. C. (2005). Experimental investigation of various vegetable fibers as sorbent materials for oil spills sorbent materials for oil spills. Marine Pollution Bulletin, 50(11): 1340 – 1346.

- Yi, J., Wang, Z., Bai, H., Yu, X., Jing, J. and Zuo. L. (2015). Optimization of purification, identification and evaluation of the in vitro antitumor activity of polyphenols from Pinus koraiensis pinecones. Molecules, 20 (6): 10450 – 10467.

- Kadir, S., Matali, S., Mohamad, N. F. and Rani, N. H. A. (2014). Preparation of activated carbon from oil palm empty fruit bunch (EFB) by steam activation using response surface methodology. International Journal of Materials Science and Applications, 3(5): 159 – 163.

- Yang, M. (2011). Produced water.  Springer, Glasgow: pp. 57 – 88.

- Salamatinia, B., Zinatizadeh, A., Kamaruddin, A. and Abdullah, A. Z. (2006). Application of response surface methodology for the optimization of Cu and Zn removals by sorption on pre-treated oil palm frond (OPF). Iranian Journal of Chemical Engineering, 3(2): 73 – 84.

- Singhal, S., Agarwal, S., Bahukhandi, K., Sharma, R. and Singhal, N. (2014). Bio-adsorbent: A cost-effective method for effluent treatment. International Journal of Environmental Sciences and Research, 3(1): 151 – 156

- Abdel-Ghani, N. and El-Chaghaby, G. (2014). Biosorption for metal ions removal from aqueous solutions: A review of recent studies. International Journal of Latest Research in Science and Technology, 3(1): 24 – 42.

- Alkhalssi, R. M., Saeed, E. A. and Khalid, M. G. (2014). Treatment of emulsified oil in produced water from oil wells by adsorption on to corn-cob as sorbent. Nahrain University, College of Engineering Journal, 17(1): 83 – 90.

- Ahmad, A. L., Sumathi, S. and Hameed, B. H. (2005). Adsorption of residue oil from palm oil mill effluent using powder and flake chitosan: Equilibrium and kinetic studies. Water Research, 39(12): 2483 – 2494.

- Kumar, P. S. and Kirthika, K. (2009). Equilibrium and kinetic study of adsorption of nickel from aqueous solution onto bael tree leaf powder. Journal of Engineering Science and Technology, 4(4): 351 – 363.

- Mohammed, S. A., Faisal, I. and Alwan, M. M. (2011). Oily wastewater treatment using expanded beds of activated carbon and zeolite. Journal of Chemical and Petroleum Engineering, 12(1): 13.

- Sidik, S. M., Jalil, A. A., Triwahyono, S., Adam, S. H., Satar, M. A. H. and Hameed, B. H. (2012). Modified oil palm leaves adsorbent with enhanced hydrophobicity for crude oil removal. Chemical Engineering Journal, 203: 9 – 18.

- Rajakovic V., Aleksic, G. and Rajakovic, L. (2008). Governing factors for motor oil removal from water with different sorption materials. Journal of Hazardous Materials, 154(1-3): 558 – 563.