# Malaysian Journal of Analytical Sciences Vol 21 No 6 (2017): 1432 - 1437

# CHARCOAL BASE METALLIC COMPOSITE ELECTRODE FOR WASTEWATER TREATMENT

# (Elektrod Komposit Logam Berasaskan Arang Bagi Rawatan Air Buangan)

# Majd Ahmed Jumaah1*, Mohamed Rozali Othman1, 2, Muhammad Rahimi Yusop1, Jumat Salimon1,

# Baydaa Khalaf1, Wan Mohd Afiq Wan Mohd Khalik3

# 1School of Chemical Sciences and Food Technology

# 2Centre for Water Research and Analysis (ALIR)

# Faculty of Science and Technology,

# Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor, Malaysia

3School of Marine and Environmental Sciences,

Universiti Malaysia Terengganu, 21030 Kuala Nerus, Terengganu, Malaysia

# *Corresponding author:  majd.ahmed88@yahoo.com

Received: 28 September 2016; Accepted: 6 March 2017

Abstract

# In this study, a charcoal base metallic composite electrode which is low in cost and effective to treat wastewater from landfill leachate by electrochemical oxidation technique has been fabricated. The charcoal base metallic composite electrode was prepared by mixing together a weighed portion of charcoal, graphite and metals powder in different composition percentage with PVC as a binder in 4 mL THF which act as a solvent. Metals used in the preparation of the electrodes are Ag, Al, Co, Cu and Ni. The results show that the mixture of commercially available charcoal, metals and PVC at a composition of 50:20:30 (w/w), known as C50M20PVC30 electrode give a good stability, low cost and high formation of hypochlorite ion. Hypochlorite ion has been produced linked to the presence of chloride ions, thus having capability to degrade chemical pollutants in wastewater.

# Keywords:  charcoal, electrode, treatment, wastewater

# Abstrak

# Dalam kajian ini, elektrod komposit logam berasaskan arang dengan kos rendah dan efektif dalam merawat air buangan daripada tanah larut resap melalui teknik pengoksidaan elektrokimia telah dibangunkan. Elektrod komposit logam berasaskan arang telah disediakan dengan mencampurkan arang, grafit dan serbuk logam pada peratus komposisi yang berbeza di mana polivinil klorida sebagai pengikat di dalam 4 mL tetrahidrofuran (THF) sebagai pelarut. Logam yang digunakan dalam penyediaan elektrod ialah Ag, Al, Co, Cu dan Ni. Keputusan menunjukkan campuran arang komersial, logam dan PVC pada nisbah 50:20:30 (w/w), yang dikenali sebagai elektrod C50M20PVC30 memberi kestabilan yang baik, berkos rendah dan menghasilkan ion hipoklorit yang tinggi. Semasa pengoksidaan elektrokimia, ion hipoklorit telah dihasilkan disebabkan oleh kehadiran ion klorida yang membawa kepada keupayaan untuk penyingkiran bahan pencemar kimia di dalam air buangan.

Kata kunci:  arang, elektrod, rawatan, air buangan

# References

- Noruzman, H. A., Ismail, M. B. and Abdul-Majid, Z. (2012). Characteristics of treated effluents and their potential applications for producing concrete. Journal of Environmental Management, 15: 27 – 32.

- Jumaah, M. A., Othman, M. R.  and Yusop, M. R. (2016). Batch method treatment of landfill leachate using charcoal composite. International Journal of Chem Tech Research, 9: 583 – 586.

- Pérez-González, A., Urtiaga, A. M., Ibáñez, R. and Ortiz, I. (2012). State of the art and review on the treatment technologies of water reverse osmosis concentrates. Water Research, 46(2): 267 – 283.

- Martinez-Huitle, C. A. and Ferro, S. (2006). Electrochemical oxidation of organic pollutants for the wastewater treatment: Direct and indirect processes. Chemical Society Reviews 35: 1324 – 1340.

- Deng, Y. and James, D. E. (2007). Electrochemical oxidation for landfill leachate treatment. Waste Management, 27: 380 – 388.

- Mook, W. T., Chakrabarti, M. H., Aroua, M. K., Khan, G. M. A., Ali, B. S., Islam, M. S. and Hassan, M. A. (2012). Removal of total ammonia nitrogen (TAN), nitrate and total organic carbon (TOC) from aquaculture wastewater using electrochemical technology: A review. Desalination, 285: 1 – 13.

- Jumaah, M. A., Othman, M. R. and Yusop, M. R. (2016). Characterization of leachate from Jeram Sanitary Landfill-Malaysia. International Journal of ChemTech Research, 9: 571 – 574.

- MoayeriKashani, M., Soltani, S. M. and Sobri, S. (2012). Treatment of a Malaysian leachate sample using electrocoagulation. International Journal of Chemical Engineering and Applications, 3(1): 63 – 66.

- Zakaria, Z., Nordin, N., Hasan, S. Z., Baharuddin, N. F., Jumaah, M. A. and Othman, M. R. (2015). Decolorization of reactive orange 16 dye using fabricated charcoal base metallic composite electrode. Malaysian Journal of Analytical Sciences, 19: 493 – 502.

- Jumaah, M. A., Othman, M. R. and Zakaria, Z. (2015). Fabrication of selected metal powder composite electrode for landfill leachate treatment using electrochemical method. International Journal of Chemical Sciences 13: 943 – 954.

- Ruiz, V., Blanco, C., Granda, M., Menéndez, R. and Santamaría, R. (2007). Influence of electrode preparation on  the  electrochemical behaviour of carbon-based supercapacitors. Journal of Applied Electrochemistry, 6: 717 – 721.

- Jumaah, M.  A. and Othman, M. R. (2015). Study the efficiency of various metal powder composition electrodes based on landfill leachate treatment. International Journal of ChemTech Research, 8: 559 –563.

- Jumaah, M.  A. and Othman, M. R. (2015). Optimization of operating conditions for landfill leachate treatment using electrochemical oxidation technique. International Journal of ChemTech Research 8: 783 – 787.

- Jumaah, M. A. and Othman, M. R. (2015). COD removal from landfill leachate by electrochemical method using charcoal-PVC electrode. International Journal of ChemTech Research 8: 604 – 609.

- Nordin, N., Amir, S. F. M., Yusop, M. R. and Othman, M. R. (2015). Decolorization of CI reactive orange 4 and textile effluents by electrochemical oxidation technique using silver-carbon composite electrode. Acta Chimica Slovenica, 62: 642 – 651.

- Jumaah, M. A. and Othman, M. R. (2015). Optimization of electrochemical parameters for landfill leachate treatment  using  charcoal  base metallic composite electrode. Malaysian Journal of Analytical Sciences, 19: 531 – 540.

- Othman, M. R. and Riyanto (2012). Electrochemical stability of Cu, Ni, Co, Pt and Ir metals sheet and their composite electrodes in potassium hydrox de solution. International Journal of Electrochemical Science, 7: 8408 – 8419.

- Jumaah, M. A., Othman, M. R. and Yusop, M. R. (2016). Electrochemical treatment of landfill leachate: Optimization of COD removal using charcoal- graphite- cobalt- polyvinyl chloride electrode. Research Journal of Pharmaceutical, Biological and Chemical Science, 7: 2812 – 2816.