Malaysian Journal of Analytical Sciences Vol 22 No 1 (2018): 107 - 114

CLAMSHELL AND SEA SAND AS HETEROGENEOUS CATALYSTS FOR WASTE COOKING OIL BASED BIODIESEL PRODUCTION VIA TRANSESTERIFICATION REACTION

(Kulit Kerang dan Pasir Pantai Sebagai Mangkin Heterogen untuk Penghasilan Biodiesel Berasaskan Minyak Masak Sawit Terpakai Melalui Tindakbalas Transesterifikasi)

# Arsyad Ismail Sanuzi, Syuhada Mohd Tahir*, Siti Norhafiza Mohd Khazaai

Faculty of Applied Sciences,

Universiti Teknologi MARA Cawangan Pahang, 26400 Bandar Tun Abdul Razak Jengka, Pahang, Malaysia

*Corresponding author:  syuhadamohdtahir@pahang.uitm.edu.my

Received: 4 December 2016; Accepted: 1 December 2017

Abstract

This study was carried out to study the effectiveness of clamshell and sea sand as heterogeneous catalyst to produce biodiesel via transesterification of waste cooking oil (WCO). WCO was first pre-treated to discard water and impurities. Clamshell and sea sand were crushed into fine powder, sieved to 500 µm particles and calcined. Next, the pre-treated WCO was used to obtain fatty acid methyl ester (FAME) via transesterification reaction. FTIR and XRD results of calcined clamshell confirmed the formation of CaO and Ca(OH)2 while sea sand contains SiO2 before and after calcination. 2:1 clamshell-to-sea sand ratio produced highest FAME yield. This ratio was used to study the effect of catalyst loading amount. 7 wt% catalyst produced highest FAME yield. Increasing catalyst to 10 wt% reduced the FAME yield due to the soap formation. Analysis of FAME using GC-MS showed the presence of myristic acid, palmitic acid and oleic acid. This study shows that combination of clamshell and sea sand is good potential catalyst for transesterification reaction to produce biodiesel.

Keywords:  biodiesel, heterogeneous catalyst, transesterification, waste cooking oil

# Abstrak

# Kajian ini dijalankan untuk mengkaji keberkesanan kulit kerang dan pasir pantai sebagai mangkin heterogen untuk menghasilkan biodiesel melalui transesterifikasi minyak masak sawit terpakai (WCO). WCO dirawat terlebih dahulu untuk membuang air dan kekotoran. Kulit kerang dan pasir pantai dihancurkan menjadi serbuk halus, ditapis kepada 500 µm dan dikalsinasi. Tindakbalas transesterifikasi WCO dijalankan untuk menghasilkan metil ester (FAME). Data daripada FTIR dan XRD untuk kulit kerang terkalsinasi mengesahkan pembentukan CaO dan Ca(OH)2 manakala pasir pantai pula mengandungi SiO2 sebelum dan selepas kalsinasi. Nisbah 2:1 kulit kerang terhadap pasir pantai menghasilkan FAME yang paling tinggi dan nisbah ini digunakan dalam kajian seterusnya untuk melihat kesan jumlah pemangkin terhadap jumlah FAME yang dihasilkan. Mangkin sebanyak 7 wt% menghasilkan jumlah FAME yang paling tinggi. Penggunaan mangkin sebanyak 10 wt% mengurangkan jumlah FAME yang diperoleh disebabkan pembentukan sabun. Analisis FAME menggunakan GC-MS menunjukkan kehadiran asid miristik, asid palmitik dan asid oleik. Kajian ini menunjukkan campuran kulit kerang dan pasir pantai adalah mangkin yang berpotensi baik untuk tindakbalas transesterifikasi untuk menghasilkan biodiesel.

Kata kunci:  biodiesel, mangkin heterogen, transesterifikasi, minyak masak sawit terpakai

References

- Mandolesi de Araújo, C. D., de Andrade, C. C., de Souza, E., Silva, E. and Dupas, F. A. (2013). Biodiesel production from used cooking oil: A review. Renewable and Sustainable Energy Reviews, 27: 445-452.

- Talebian-Kiakalaieh, A., Amin, N. A. S. and Mazaheri, H. (2013). A review on novel processes of biodiesel production from waste cooking oil. Applied Energy, 104: 683-710.

- Aransiola, E. F., Ojumu, T. V., Oyekola, O. O., Madzimbamuto, T. F. and Ikhu-Omoregbe, D. I. O. (2014). A review of current technology for biodiesel production: State of the art. Biomass and Bioenergy, 61: 276-297.

- Kouzu, M. and Hidaka, J. S. (2012). Transesterification of vegetable oil into biodiesel catalyzed by CaO: A review. Fuel, 93: 1-12.

- Nair, P., Singh, B., Upadhyay, S. N. and Sharma, Y. C. (2012). Synthesis of biodiesel from low FFA waste frying oil using calcium oxide derived from Mereterix mereterix as a heterogeneous catalyst. Journal of Cleaner Production, 29-30: 82-90.

- Muciño, G. G., Romero, R., Ramírez, A., Martínez, S. L., Baeza-Jiménez, R. and Natividad, R. (2014). Biodiesel production from used cooking oil and sea sand as heterogeneous catalyst. Fuel, 138: 143-148.

- Nyoman, P. A., Santi, D. S., Suprapto Kusno, B. and Achmad, R. (2012). Development of heterogeneous alumina supported base catalyst for biodiesel production. 3rd international conference on biology, environment and chemistry, IACSIT Press, Singapore, V46. 25, 117-120.

- El-Gendy, N. S., Deriase, S. F., Hamdy, A. and Abdallah, R. I. (2015). Statistical optimization of biodiesel production from sunflower waste cooking oil using basic heterogeneous biocatalyst prepared from eggshells. Egyptian Journal of Petroleum, 24: 37-48.

- Sivakumar, S., Ravisankar, R., Raghu, Y., Chandrasekaran, A. and Chandramohan, J. (2012). FTIR spectroscopic studies on coastal sediment samples from cuddalore district, Tamilnadu, India. Indian Journal of Advances in Chemical Science, 1: 40-46.

- Jaiyen, S., Naree, T. and Ngamcharussrivichai, C. (2015). Comparative study of natural dolomitic rock and waste mixed seashells as heterogeneous catalysts for the methanolysis of palm oil to biodiesel. Renewable Energy, 74: 433-440.

- Uzun, B. B., Kılıç, M., Özbay, N., Pütün, A. E. and Pütün, E. (2012). Biodiesel production from waste frying oils: Optimization of reaction parameters and determination of fuel properties. Energy, 44(1): 347-351.

- Sirisomboonchai, S., Abuduwayiti, M. and Guan, G. (2015). Biodiesel production from waste cooking oil using calcined scallop shell as catalyst. Energy Conversion and Management, 95: 242-247.