# Malaysian Journal of Analytical Sciences Vol 22 No 1 (2018): 143 -150

# INFLUENCE OF ALKALI TREATMENT ON PHYSICO-CHEMICAL PROPERTIES OF MALAYSIAN BAMBOO FIBER: A PRELIMINARY STUDY

# (Pengaruh Rawatan Alkali terhadap Sifat-sifat Fizikal-Kimia Serat Buluh Malaysia: Satu Kajian Awal)

# Foo Sheng Tong1*, Siew Choo Chin1, 2, Mohd Tamizi Mustafa4, Huei Ruey Ong3, Md. Maksudur Rahman Khan2, 3, Jolius Gimbun2, 3, Shu Ing Doh1

# 1Faculty of Civil Engineering & Earth Resources

# 2Centre of Excellence for Advanced Research in Fluid Flow (CARIFF)

# 3Faculty of Chemical & Natural Resources Engineering

# University Malaysia Pahang, 26300 Gambang, Pahang, Malaysia

# 4Kualiti Kayu dan Hasil Bukan Kayu, Bahagian Keluaran Hutan,

# Forest Research Institute of Malaysia, 52109 Kuala Lumpur, Malaysia

# *Corresponding author:  tongfoosheng@hotmail.com

Received: 4 December 2016; Accepted: 1 December 2017

Abstract

# In the present study, the effect of alkaline treatment on the morphology and physico-chemical properties of Malaysian bamboo fibers was elucidated. The fibers were extracted from raw bamboo culm using alkaline solution with concentrations of 0 and 10 wt% at 24 hours and followed by roller milling techniques. The treated and untreated fibers were characterized by Fourier transform infrared spectroscopy (FTIR), thermogravimetric analysis (TGA) and scanning electron microscope (SEM). Apart from that, the mechanical properties of single fiber were also investigated. It was found that the tensile strength and modulus of the alkali-treated fiber were improved by 45.6 and 72%, respectively, compared to the untreated fiber. The surface morphology of the treated fiber was improved in which the surface roughness has been reduced significantly as proven in SEM. The FTIR and TGA data suggested that alkaline treatment gradually removed the lignin and hemicellulose. These findings highly recommended that, local bamboo fiber could be used as a reinforcement agent for composite making.

# Keywords:  alkaline treatment, bamboo fiber, natural fiber, natural fiber composite, roller milling techniques

# Abstrak

# Dalam kajian ini, kesan rawatan alkali terhadap sifat morfologi dan fizikokimia gentian buluh Malaysia telah dijelaskan. Serat telah diambil dari laras buluh mentah dengan menggunakan larutan alkali dengan kepekatan 0 dan 10% pada 24 jam dan diikuti dengan teknik penggilingan roller. Serat yang dirawat dan tidak dirawat dicirikan oleh spektroskopi transformasi Fourier (FTIR), analisis termogravimetrik (TGA) and mikroskop imbasan elektron (SEM). Selain itu, sifat mekanik serat tunggal juga disiasat. Keputusan telah didapati bahawa kekuatan tegangan dan modulus serat yang dirawat alkali telah meningkat sebanyak 45.6 dan 72%, berbanding dengan serat yang tidak dirawat. Morfologi permukaan serat yang dirawat telah diperbaiki dengan kekasaran permukaan berkurangan dengan nyata, seperti yang dibuktikan oleh SEM. Data FTIR dan TGA mencadangkan rawatan alkali telah menghilangkan lignin dan hemiselulosa secara beransur-ansur. Penemuan ini sangat disyorkan bahawa, serat buluh tempatan boleh digunakan sebagai ejen tetulang untuk pembuatan komposit.

# Kata kunci:  rawatan alkali, serat buluh, serat semulajadi, komposit gentian semulajadi, teknik penggilingan roller

References

- Zhang, X., Wang, F. and Keer, L. M., (2015).  Influence  of  surface  modification  on  the  microstructure  and thermo-mechanical properties of bamboo fibers. Materials, 8: 6597 - 6608.

- Simão, J.A., Carmona, V.B., Marconcin, J.M., Mattoso, L.H.C., Barsberg, S.T. and Sanadi, A.R. (2016). Effect of  fiber  treatment  condition  and  coupling  agent  on  the  mechanical  and thermal properties in highly filled composites of sugarcane bagasse fiber/pp. Materials Research, 19(4): 746 - 751.

- Hossain, S. I.,  Hasan, M., Hasan, M. N. and  Hassan, A. (2013).  Effect  of  chemical  treatment  on  physical, mechanical  and  thermal  properties  of  ladies  finger  natural  fiber.   Advances in Materials Science and Engi-neering, 2013: 1- 7.

- Dalbehera, S. and Acharya, S. K. (2014). Study on mechanical properties of natural fiber reinforced woven jute-glass hybrid epoxy composites. Advances in Polymer Science and Technology: An International Journal, 4(1): 1 - 6.

- Alves, C.,  Ferrão, P. M. C.,  Silva, A. J.,  Reis, L. G., Freitas, M., Rodrigues, L. B. and Alves, D. E. (2010).Eco design of automotive components making use of natural jute fiber composites. Journal of Cleaner Production, 18(4): 313 - 327.

- Summerscales, J., Dissanayake, N. P. J., Virk, A. S. and Hall, W. (2010).   A  review of  bast  fibres  and  their composites. Part 1 - Fibres as reinforcements. Composites Part A: Applied Science and Manufacturing, 41(10): 1329 – 1335.

- Elenga, R. G., Djemia, P., Tingaud, D., Chauveau, T., Maniongui, J. G. and Dirras, G. (2013).  Effects of alkali treatment  on  the  microstructure,  composition,  and properties of the raffia textiles fiber. BioResources, 8(2): 2934 - 2949.

- Zakikhani, P., Zahari, R., Sultan, M. H. and Majid, D. L. (2014).  Bamboo  fibre  extraction  and its reinforced polymer  composite  material.   International  Journal of Chemical, Nuclear, Materials and Metallurgical Engi-neering, 8(4): 287 – 290.

- Biswas, S., Shahinur, S., Hasan, M. and Ahsan, Q. (2015).  Physical,  mechanical and thermal properties of jute and bamboo fiber reinforced unidirectional epoxy composites. Procedia Engineering, 105: 933 - 939.

- Ahmad, S., Raza, A. and Gipta, H. (2014). Mechanical properties of bamboo fibre reinforced concrete. In: 2nd International conference on research in science, engineering and technology (ICRSET 2014). Dubai (UAE): pp 162 - 166.

- Vajje, S. and Murthym N. R. K. (2013) Study on addition of the natural fibers into concrete. International Journal of Scientific & Technology Research, 2 (11): 213 – 218.

- Zakikhani, P., Zahari, R., Sultan, M. T. H. and Majid, D. L. (2014). Extraction and preparation of bamboo fibre-reinforced composites. Materials and Design, 63: 820 - 828.

- Afrin, T., Tsuzuki, T. and Wang, X. (2009).  Bamboo  fibres  and  their  unique  properties.   Bamboo Bulletin, 11(1): 36 - 39.

- Liu, H.,  Huang, Y.,  Yuan, L.,  He, P.,  Cai, Z.,  Shen, Y.,  Xu, Y.,  Yu, Y.  and Xiong, H. (2010).   Isothermal crystallization  kinetics  of  modified  bamboo cellulose/PCL composites. Carbohydrate Polymer, 79(3): 513 – 519.

- Alam, M. A., Nouri, K. and Jumaat, M. Z. (2015).  Flexural  strengthening  of  reinforced  concrete beam using jute rope composite plate. In: The 3rd national Graduate conference (NatGrad2015): pp. 8 - 9.

- Hafizah, N. A. K.,  Bhutta, M. A. R.,  Hamaludin, M. Y.,  Warid, M. H.,  Ismail, M., Rahman, M. S., Yunus, I. and Azman, M. (2014).  Kenaf  fiber  reinforced  polymer composites for strengthening RC beams. Journal of Advanced Concrete Technology, 12(6): 167 - 177.

- Sen, T. and Jagannatha Reddy, H. N. (2014).   Flexural  strengthening  of  RC  beams  using  natural  sisal  and artificial carbon and glass fabric reinforced composite system. Sustainable Cities and Society, 10: 195 - 206.

- Okubo, K., Fujii, T. and Yamamoto, Y. (2004). Development of bamboo-based polymer composites and their mechanical properties. Composites: Part A: Applied Science and Manufacturing, 35(3): 377 - 383.

- Ramli, R., Khan, M. M. R., Yunus, R. M., Ong, H. R., Halim, R. M., Aziz, A. A., Ibrahim, Z. and Zainal, N. H. (2014).  In-situ  impregnation  of  copper  nanoparticles on palm empty fruit bunch powder. Advances in Nano-particles, 3: 65 - 71.

- Chowdhury,  M. N. K., Beg, M. D. H., Khan, M. R. and Mina, M. F. (2013).  Modification  of  oil palm  empty fruit bunch fibers by nanoparticle impregnation and alkali treatment. Cellulose, 20(3): 1477 - 1490.