Malaysian Journal of Analytical Sciences Vol 22 No 1 (2018): 72 - 79

PREPARATION OF EPOXIDIZED NATURAL RUBBER/ POLY(VINYLIDINE FLUORIDE) MEMBRANE BY USING SOLUTION CASTING METHOD FOR PALM OIL MILL EFFLUENT TREATMENT

(Penyediaan Membran Getah Asli Terepoksida/Poli(Vinilidina Fluorida) Dengan Menggunakan Kaedah Pengacuanan Larutan Untuk Rawatan Efluen Kilang Minyak Sawit)

Norliyana Mod, Farah Hannan Anuar, Rizafizah Othaman*

School of Chemical Sciences and Food Technology,

Faculty of Science and Technology,

Universiti Kebangsaan Malaysia, 43600 UKM  Bangi, Selangor, Malaysia

*Corresponding author:  rizafizah@ukm.edu.my

Received: 12 April 2017; Accepted: 4 September 2017

Abstract

Poly(vinylidine fluoride) (PVDF) membrane is generally a chosen membrane for palm oil mill effluent (POME) treatment. The focus is to make freestanding and robust PVDF based composite membranes with different ratio of epoxidized natural rubber (ENR) (ENR/PVDF: 0/100 wt%, 20/80 wt%, 40/60 wt%, 60/40 wt%, 80/20 wt%, 100/0 wt%) by solution casting method. Subsequently, these membranes were characterized using fourier transform infrared (FTIR), differential scanning electron (DSC) and vapor pressure scanning electron microscope (VPSEM). The FTIR spectrums showed that ENR blended well with PVDF and the peak intensity followed the composition of the membranes. Meanwhile, the ENR and PVDF mixtures were miscible due to the formation of single peak glass transition temperature (Tg) as observed in DSC thermogram. Shifting in peaks of Tg suggested important interaction taking place between polymers. Surface morphology by SEM displayed the formation of random pores caused by the nature of PVDF polymer and phase inversion process. High composition of ENR caused a dense membrane and vice-versa while phase inversion contributed to the pores existences. The fluxes during POME treatment were lower than water fluxes. Higher flux was a sign of higher rejection which is efficient for separation of water and effluents. Thus, ENR/PVDF 40/60 wt% and 20/80 wt% has been selected as promising membranes to be applied for POME treatment.

Keywords:  membrane, epoxidised natural rubber, poly(vinylidine fluoride)

Abstrak

Membrane poli(vinilidina fluorida) (PVDF) umumnya adalah membran terpilih untuk rawatan efluen kilang minyak sawit (POME). Tumpuan adalah untuk membuat membran komposit berasaskan yang fleksibel dan PVDF teguh dengan nisbah yang berbeza getah asli terepoksida (ENR) (ENR/PVDF: 0/100 wt%, 20/80 wt%, 40/60 wt%, 60/40 wt%, 80/20 wt%, 100/0 wt%) dengan kaedah pemutus penyelesaian. Selepas itu, membran ini dicirikan menggunakan inframerah transformasi Fourier (FTIR), perbezaan imbasan elektron (DSC) dan tekanan wap imbasan mikroskop elektron (VPSEM). Spektrum FTIR menunjukkan bahawa ENR dicampur dengan baik dengan PVDF dan intensiti puncak di ikuti komposisi membran. Sementara itu, ENR dan PVDF campuran adalah terlarut campur disebabkan oleh pembentukan puncak tunggal suhu peralihan kaca (Tg) sebagaimana yang berlaku di DSC termogram. Peralihan di puncak Tg mencadangkan interaksi penting yang berlaku di antara polimer. Permukaan morfologi oleh SEM dipaparkan pembentukan liang rawak disebabkan oleh sifat polimer PVDF dan proses penyongsangan fasa. Komposisi tinggi ENR menyebabkan membran padat dan sebaliknya manakala fasa penyongsangan menyumbang kepada liang kewujudan. Fluks semasa rawatan POME adalah lebih rendah daripada fluks air. Fluks tinggi adalah tanda penolakan yang lebih tinggi yang cekap untuk pemisahan air dan efluen. Oleh itu, ENR/PVDF 40/60 wt%  dan 20/80 wt% berat telah dipilih sebagai membran yang menyakinkan untuk digunakan bagi rawatan POME.

Kata kunci:  membran, getah asli terepoksida, poli(vinilidina fluorida)

References

- Salaeh, S., Nakason, C., Boiteu, G. and Cassagnau, P. (2013). Co-continuous phase structure and properties of poly(vinylidene fluoride)/epoxidized natural rubber blends. Advanced Materials Research, 626: 71-74.

- Sulaiman, N. M. N. &  Ling, C. K. (2004). Membrane ultrafiltration of treated palm oil mill effluent (POME). Jurnal Teknologi, 41: 113-120.

- Shilton, S. J., Ismail, A. F., Gough, P. J., Dunkin, I. R. and Gallivan, S. L. (1997). Molecular orientation and the performance of synthetic polymeric membranes for gas separation. Polymer, 38(9): 2215-2220.

- Bottino, A., Camera-Rodab, G., Capannelli, G. and Munari, S. (1991). The formation of microporous polyvinylidene difluoride membranes by phase separation. Journal of Membrane Science, 57: l-20.

- Yan, L., Honga, S., Li, M. L. and Li, Y. S. (2009). Application of the Al2O3–PVDF nanocomposite tubular ultrafiltration (UF) membrane for oily wastewater treatment and its antifouling research. Separation and Purification Technology, 66: 347-352.

- Yoksan, R. (2008).  Epoxidized  natural rubber for adhesive applications. Kasetsart Journal (Nat. Sci.), 42: 325-332.

- Ismail, H. and Chia, H. H. (1998). The effects of multifunctional additive and epoxidation in silica filled natural rubber compounds. Polymer Testing, 17: 199-210.

- Hasegawa, R., Takahashi, Y., Chatani, Y. and Tadokoro, H. (1972). Crystal structures of three crystalline forms of poly(vinylidine fluoride). Polymer Journal, 3(5): 600-610.

- Salaeh, S., Boiteux, G., Gain, O., Cassagnau, P. and Nakason, C. (2014). Dynamic mechanical and dielectric properties of poly(vinylidene fluoride) and epoxidized natural rubber blends. Advanced Materials Research, 844: 97-100.

- Tao, M.-M., Liu, F., Ma, B.-R. and Xue, L.-X. (2013). Effect of solvent power on PVDF membrane polymorphism during phase inversion. Desalination, 316: 137-145.

- Wang, X., Zhang, L., Sun, D., An, Q. and Chen, H. (2009). Formation mechanism and crystallization of poly(vinylidene fluoride) membrane via immersion precipitation method. Desalination, 236: 170-178.

- Cao, X., Ma, J., Shi, X. and Ren, Z. (2006). Effect of TiO2 nanoparticle size on the performance of PVDF membrane. Applied Surface Science, 253: 2003-2010.

- Freire, E., Bianchi, O., Monteiro, E. E. C., Nunes, R. C. R. and Forte, M. C. (2009). Processability of PVDF/PMMA blends studied by torque rheometry. Materials Science and Engineering C, 29: 657-661.

- Wang, P., Tan, K. L., Kangb, E. T. and Neohb, K. G. (2002). Plasma-induced immobilization of poly(ethylene glycol) onto poly(vinylidene fluoride) microporous membrane. Journal of Membrane Science, 195: 103-114.

- Zhong, Z., Cao, Q., Jing, B., Wang, X., Li, X. and Deng, H. (2012). Electrospun PVdF–PVC nanofibrous polymer electrolytes for polymer lithium-ion batteries. Materials Science and Engineering B, 177: 86-91.

- Igwe, J. C. and Onyegbado, C.C. (2007). A review of palm oil mill effluent (POME) water treatment. Global Journal of Environmental Research 1(2): 54-62.

- Malaysia Palm Oil Board (MPOB) (2014). Access online http://www.mpob.gov.my/ms/info-sawit/alam-sekitar/520-achievements.

- Chin, K. K., Lee, S. W. and Mohammad, H. H. (1996). A study of palm oil mill effluent treatment using a pond system.  Water Science Technology, 34(11): 119-123.

- Saljoughi, E., Sadrzadeh, M. and Mohammadi, T. (2009). Effect of preparation variables on morphology and pure water permeation flux through asymmetric cellulose acetate membranes. Journal of Membrane Science, 326: 627-634.

- Zurina, M., Ismail, H. and Bakar, A. A. (2004). Rice husk powder–filled polystyrene/styrene butadiene rubber blends. Journal of Applied Polymer Science, 92: 3320-3332.

- Boccaccio, T., Bottino, A., Capannelli, G. and Piaggio, P. (2002). Characterization of PVDF membranes by vibrational spectroscopy. Journal of Membrane Science, 210: 315-329.

- Ma, W., Yuan, H. and Wang, X. (2014). The effect of chain structures on the crystallization behavior and membrane formation of poly(vinylidene fluoride) copolymers. Membranes, 4: 243-256.

- Bourara, H., Hadjout, S., Benabdelghani, Z. and Etxeberria, A. (2014). Miscibility and hydrogen bonding in blends of poly(4-vinylphenol)/poly(vinyl methyl ketone). Polymers, 6: 2752-2763.

- Bottino, A., Capannelli, G., Munari, S. and Turturro, A. (1988). High performance ultrafiltration membranes cast from LiCI doped solutions. Desalination, 68: 167-177.