Malaysian Journal of Analytical Sciences Vol 22 No 2 (2018): 296 - 302

EFFECT OF SILVER ON THE PHYSICAL AND STRUCTURAL PROPERTIES OF LEAD NEODYMIUM BOROTELLURITE GLASS SYSTEM

# (Kesan Perak atas Sifat Fizikal dan Struktur Sistem Kaca Plumbum Neodimium Borotelurit)

Norihan Yahya1*, Azman Kasim1, Azhan Hashim1, Siti Nasuha Rafien1, Wan Aizuddin Wan Razali1,

Syamsyir Akmal Senawi1, Ruziana Mohamed1, Mardhiah Abdullah2

# 1Faculty of Applied Sciences,

# Universiti Teknologi MARA Cawangan Pahang, 26400 Bandar Tun Abdul Razak Jengka, Pahang, Malaysia

# 2Faculty of Applied Sciences,

# Universiti Teknologi MARA Cawangan Terengganu, Kampus Bukit Besi, 23200 Dungun,Terengganu, Malaysia

# *Corresponding author: norihan@pahang.uitm.edu.my

Received: 4 December 2016; Accepted: 1 December 2017

Abstract

# Neodymium doped borotellurite glass is well known to be one of the most promising candidate due to it various applications. Nd3+ doped lead borotellurite glasses containing silver were successfully been prepared by conventional melt-quenching method with the chemical composition (69.5-x)TeO2-20B2O3-10PbO-0.5Nd2O3-xAgNO3 (where x = 0, 0.5, 1.0, 1.5, 2.0 and 2.5 mol %). The physical properties such as density, molar volume and oxygen packing density were measured. Their structural properties of the glass system were studied via X-Ray Diffraction (XRD) analysis and Fourier Transform Infrared (FTIR) spectroscopy. From the result, the amorphous nature of the prepared glass samples have been confirmed through X-ray diffraction spectral analysis. The presence of Te-O-Te or O-Te-O, Ag-O, Te-O-Pb and B-O and characteristic of the hydrogen bond in the prepared glasses were explored through the FTIR spectral studies recorded in the 400-4000 cm-1 wave number range at room temperature. Meanwhile, the results of physical properties are found to vary with respect to concentration of AgNO3 content. Some other results will be reported and discussed.

# Keywords:  neodymium, borotellurite, silver, physical properties, structural properties

# Abstrak

# Kaca borotelurit di dop neodimium merupakan salah satu bahan yang diyakini disebabkan oleh kepelbagaian aplikasinya. Kaca borotelurit di dop Nd3+ mengandungi perak telah berjaya disediakan dengan kaedah konvensional sepuh lindap dengan komposisi kimia (69.5-x)TeO2-20B2O3-10PbO-0.5Nd2O3-xAgNO3 (di mana x = 0, 0.5, 1.0, 1.5, 2.0 dan 2.5 mol%). Sifat-sifat fizikal seperti ketumpatan, isipadu molar dan ketumpatan padat oksigen telah diukur. Sifat-sifat struktur sistem kaca ini telah dikaji melalui analisis pembelauan sinar-X (XRD) dan spektroskopi inframerah transformasi Fourier (FTIR). Dari hasil kajian, sifat semulajadi amorfus sampel kaca yang disediakan telah disahkan melalui analisis spektra pembelauan sinar-X. Kehadiran Te-O-Te atau O-Te-O, Ag-O, Te-O-Pb, B-O dan ciri-ciri ikatan hidrogen dalam kaca yang disediakan telah diterokai melalui kajian spektra FTIR yang direkodkan dalam julat gelombang 400-4000 cm-1 pada suhu bilik. Sementara itu, hasil kajian bagi sifat fizikal didapati berubah mengikut kepekatan kandungan AgNO3. Beberapa keputusan lain akan dilaporkan dan dibincangkan.

# Kata kunci:  neodimium, borotelurit, perak, sifat fizikal, sifat struktur

References

- Selvi, S., Venkataiah, G., Arunkumar, S., Muralidharan, G. and Marimuthu, K. (2014). Structural and luminescence studies on Dy3+ doped lead boro-telluro-phosphate glasses. Physica B, 454: 72-81.

- Karthikeyan, P., Vijayakumar, R. and Marimuthu, K. (2017). Luminescence studies on Dy3+ doped calcium boro-tellurite glasses for White light application.. Physica B, 521: 347-354.

- Selvaraju, K. and Marimuthu, K. (2012). Structural and spectroscopic studies on concentration dependent Er3+ doped boro-tellurite glasses. Journal of Luminescence, 132: 1171-1178.

- Sasikala, T., Rama Moorthy, L. and Mohan Babu, A. (2013). Optical and luminescent properties of Sm3+ doped tellurite glasses. Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy, 104: 445-450.

- Maheshvaran, K., Linganna, K. and Marimuthu, K.. (2011). Composition dependent structural and optical properties of Sm3+ doped boro-tellurite glasses. Journal of Luminescence, 131: 2746-2753.

- Hasim, N., Rohani, M. S. and Sahar, M. R. (2016). Structural Characteristics of Er3+ and Nd3+ doped Lithium Niobate Tellurite Glass. Materials Science Forum, 846: 126-130.

- Linganna, K., Narro-García, R., Desirena, H., De la Rosa, E., Basavapoornima, Ch., Venkatramu, V. and Jayasankar, C. K. (2016). Effect of P2O5 addition on structural and luminescence properties of Nd3+-doped tellurite glasses. Journal of Alloys and Compounds, 684: 322-327.

- Reza Dousti, M. and Raheleh Hosseinian, S. (2014). Enhanced upconversion emission of Dy3+-doped tellurite glass by heat-treated silver nanoparticles. Journal of Luminescence, 154: 218-223.

- Ashur, Z., Mahraz, S., Sahar, M. R. and Ghoshal, S. K. (2015). Enhanced luminescence from silver nanoparticles integrated Er3+-doped boro-tellurite glasses: Impact of annealing temperature. Journal of Alloys and Compounds, 649: 1102-1109.

- Huang, B., Zhou, Y., Cheng, P., Zhou, Z., Li, J. and Yang, G. (2016). The 1.85 μm spectroscopic properties of Er3+/Tm3+ co-doped tellurite glasses containing silver nanoparticles. Journal of Alloys and Compounds, 686: 785-792.

- Yusoff, N. M. and Sahar, M. R. (2015). Effect of silver nanoparticles incorporated with samarium-doped magnesium tellurite glasses. Physica B, 456: 191-196.

- Terny, S., De la Rubia, M.A., Alonso, R. E., J. de Frutos and Frechero, M. A. (2015). Structure and electrical behavior relationship of a magnesium-tellurite glass using Raman and impedance spectroscopy. Journal of Non-Crystalline Solids, 411: 13-18.

- Farouk, M., Samir, A., Metawe, F. and Elokr, M. (2013). Optical absorption and structural studies of bismuth borate glasses containing Er3+ ions. Journal of Non-Crystalline Solids, 371-372: 14-21.

- Farag, M. A., Abd-Allah, K., Turky, G. and Alokr, M. M. (2015). Optical and Upconversion properties of Nd3+ doped lead borate barium glass system. Nature and Science, 13(5): 123-129.

- Ratnakaram, Y. C., Babu, S., Krishna Bharat, L. and Nayak, C. (2016). Fluorescence characteristics of Nd3+ doped multicomponent fluoro-phosphate glasses for potential solid-state laser applications. Journal of Luminescence, 175: 57-66.

- Azevedo, J., Coelho, J., Hungerford, G. and Sooraj Hussain, N. (2010). Lasing transition (4F3/2-4I11/2) at 1.06 μm in neodymium oxide doped lithium boro tellurite glass. Physica B, 405: 4696-4701.

- Surendra, B. S., Rajeswari, R., Kiwan, J. Cho, E. J., Kyoung, H. J., Hyo, J. S. and Jayasankar, C. K. (2010). Spectroscopic investigations of 1.06 μm emission in Nd3+-doped alkali niobium zinc tellurite glasses. Journal of Luminescence, 130: 1021-1025.

- Bolundut, L., Culea, E., Borodi, G., Stefan, R., Munteanu, C. and Pascuta, P. (2015). Influence of Sm3+:Ag codoping on structural and spectroscopic properties of lead tellurite glass ceramics. Ceramics International, 41: 2931-2939.

- Nurbaisyatula, E. S., Azman, K., Azhan, H., Razali, W. A. W. and Noranizah, A. (2014). The structural properties of trivalent rare earth ions (Er3+) doped borotellurite glass. Jurnal Teknologi, 69(2): 97-100.

- Pawar, P. P., Munishwar, S. R. and Gedam, R. S. (2016). Physical and optical properties of Dy3+/Pr3+ Co-doped lithium borate glasses for W-LED. Journal of Alloys and Compounds, 660: 347-355.

- Vijayalakshmi, L., Naveen, K. and Vijayalakshmi, R. P. (2016). Energy transfer based photoluminescence spectra of co-doped (Dy3++Sm3+): Li2O-LiF-B2O3-ZnO glasses for orange emission. Optical Materials, 57: 125-133.