Malaysian Journal of Analytical Sciences Vol 22 No 2 (2018): 303 - 310

EVALUATION OF DOSE SENSITIVITY RESPONSE VIA OPTICAL CHARACTERISTICS FOR CRESOL RED-DYED POLYHYDROXYETHYLMETHACRYLATE GEL (PHEMAG)

(Penilaian Respons Kepekaan Dos Melalui Ciri Optikal Bagi Kresol Merah-Dicelup Polihidrosietilmetakrilik Gel (PHEMAG))

Nur Sha’adah Zainuddin1*, Fairuzdzah Ahmad Lothfy1, Hartini Ahmad Rafaie1, Mazlini Mazlan2,

Iskandar Shahrim Mustafa3, Azhar Abdul Rahman3

1Faculty of Applied Sciences,

Universiti Teknologi MARA Pahang, 26400 Bandar Tun Abdul Razak Jengka, Pahang, Malaysia

2Faculty of Applied Sciences,

Universiti Teknologi MARA Tapah, 35400 Tapah, Perak, Malaysia

3School of Physics,

Universiti Sains Malaysia, 11800 Minden, Pinang, Malaysia

*Corresponding author:  nsz@pahang.uitm.edu.my

Received: 4 December 2016; Accepted: 1 December 2017

Abstract

A new polymer gel blended with the acid base indicator of cresol red were prepared consisted of 4%, 5% and 6% of monomer (2-Hydroxyethyl Methacrylate; HEMA) in order to characterize the radiation induced changes known as cresol red Polyhydroxyethylmethacrylate Gel (PHEMAG). Cresol red-dyed PHEMAG were prepared consisted of gelatin, deionized water, HEMA, cresol red sodium salt stock solution and ascorbic acid. The polymerization Cresol red-PHEMAG was studied with 6 MV photon beam rates 300 Gy/min which received doses up to 40 Gy for the reveletion sensitivity as a function of absorbed dose based on the physical properties by using UV-Vis spectroscopy. It is indicated that 4% of HEMA exhibited a greater sensitivity of the polymer gel dosimeter based on a mathematical model of the fitting equation of the dose response curve. The value of Do (sensitivity parameter) for 4% of HEMA is the lowest about 42.373 Gy. The lower value of Do would cause the higher radiosensitive of the matter which was actively reacted at the time of exposure.

Keywords:  absorbed dose, cresol red, photon beam, polymer gel

Abstrak

Gel polimer  baru dicampur dengan penunjuk asas asid kresol merah telah disediakan yang terdiri daripada 4%, 5% dan 6% daripada monomer (2- hidrosietilmetakrilik; HEMA) untuk mencirikan radiasi mendorong perubahan yang dikenali sebagai Kresol merah-dicelup Polihidrosietilmetakrilik Gel (PHEMAG). Kresol merah – dicelup PHEMAG telah dihasilkan terdiri daripada gelatin, air nyah ion, HEMA, stok larutan kresol merah natrium garam dan asid askobik. Pempolimeran kresol merah PHEMAG telah dikaji dengan pancaran foton 6 MV pada kadar yang berterusan 300 Gy/min yang menerima dos sehingga 40 Gy untuk mendedahkan kepekaan sebagai fungsi dos terserap berdasarkan sifat-sifat fizikal dengan menggunakan spektroskopi UV-Vis. Ia menunjukkan bahawa 4% daripada HEMA menghasilkan kepekaan polimer gel dosimeter yang lebih tinggi berdasarkan model persamaan matematik sesuai tindak balas dos keluk. Nilai Do (parameter sensitiviti) untuk 4% daripada HEMA adalah yang paling rendah kira-kira 42.37 Gy. Nilai yang lebih rendah daripada Do akan menyebabkan radiosensitif jisim yang bertindak balas secara aktif pada masa pendedahan.

Kata kunci:  dos terserap, kresol merah, pancaran foton, gel polimer

References

- Schreiner, L. J., Olding, T. and McAuley, K. B. (2010). Polymer gel dosimetry. Journal of Physics: Conference Series, 250(1): 1-5.

- Mattea, F., Romero, M. R, Vedelago, J., Quiroga, A., Valente, M. and Strumia, M. C. (2015). Molecular structure effects on the post irradiation diffusion in polymer gel dosimeters. Applied Radiation and Isoptopes, 100: 101-107.

- Vandescasteele, J. and De Deene, Y. (2013). Evaluatioin of radiochromic gel dosimetry and polymer gel dosimetry in a clinical dose verification. Physics in Medicine and Biology, 58(18): 6241-6262.

- MacDougall, N. D., Miquel, M. E. and Keevil, S. F. (2014). Effects of phantom volume and shape on the accuracy of MRI BANG gel dosimetry using BANG3TM. The British Journal of Radiology, 81(986): 46-50.

- Mattea, F., Chacon, D., Vedelago, J., Valente, M. and Strumia, M. C. (2015). Polymer gel dosimeter based on itaconic acid. Applied Radiation and Isoptopes, 105: 98-104.

- Doyan, A. (2009). Dose response and optical properties of dyed poly vinyl alcohol-trichloroacetic acid polymeric blends irradiated with gamma-rays. American Journal of Applied Sciences, 6(12): 2071.

- Beshir, W. B. (2013). Radiation sensitive indicator based on tetrabromophenol blue dyed poly (vinyl alcohol). Radiation Phycis and Chemistry, 86:  129-135.

- Saion, E., Doyan, A., Zainal Abidin, S., Azmi, Z., Zulkifli, A., Mohd Zaki, A. and Karni, T. (2005). Changes in the optical band gap and absorption edge of gamma-irradiated polymer blends. Journal of Applied Sciences, 5: 1825-1829.

- Chanda, M. (2000). Advanced polymer chemistry: A problem solving guide. Marcel Dekker: pp. 462-475.

- Rozlan, A. A., Jaafar, M. S. and Rahman, A. A. (2011). A study of normoxic polymer gel dosimeter using  raman spectroscopy analysis. International Conference on Biomedical Engineering and Technology, 11(2011): 19-23.

- Ab Razak, N. N. A. N., Rahman, A. A., Kandaiya, S., Mustafa, I. S., Yahaya, N. Z. and Mahmoud, A. A. J. (2015). Accuracy and precision of magat gel as a dosimeter.  Material Science Research India, 12(1): 01-08.

- Vergote, K. (2005). Development of polymer gel dosimetry for applications in intensity-modulated radiotherapy. Department of Radiotherapy and Nuclear Medicine, Faculty of Medicine and Health Sciences, Gent, Belgium: pp. 20-21.

- MacAuley, K. B. (2006). Fundamentals of polymer gel dosimeters. Journal of Physics: Conference Series, 56(1): 35.

- Attix, F. H. (2008). Introduction to radiological physics and radiation dosimetry. John Wiley & Sons: pp. 34-36.

- Susilawati (2005). Radiation and temperature effects on optical and electrical properties of dyed poly (vinyl alcohol) organic composite containing chlorine. PhD dissertation, Universiti Putra Malaysia.

- Ebraheem, S., Eid, S. and Kovacs, A. (2002). A new dyed poly (vinyl alcohol) film for high-dose applications. Radiation Physics and Chemistry, 63(3): 807-811.

- Morris, S. and Williams, A. (2001). Radiotherapy physics and equipment. Churchill Livingstone: pp. 28-30.

- Abdel-Fattah, A. A., Hegazy, E. S. A. and  El-Din, H. E. (2002). Radiation-chemical formation of HCl in poly (vinyl butyral) films containing chloral hydrate for use in radiation dosimetry. International Journal of Polymeric Materials, 51(9): 851-874.