# Malaysian Journal of Analytical Sciences Vol 22 No 2 (2018): 227 - 237

# THE ELECTROCHEMICAL BEHAVIOR OF ZINC OXIDE/REDUCED GRAPHENE OXIDE COMPOSITE ELECTRODE IN DOPAMINE

# (Sifat Elektrokimia Elektrod Komposit Zink Oksida/Grafin Oksida Terturun dalam Dopamin)

# Farhanini Yusoff1*, Ngai Tze Khing1, Chai Chee Hao1, Lee Pak Sang1, Nurul’ain Basyirah Muhamad1,

# Noorashikin Md Saleh2

# 1School of Marine and Environmental Sciences,

# Universiti Malaysia Terengganu, 21030 Kuala Nerus, Terengganu, Malaysia

# 2Research Centre for Sustainable Process Technology,

# Department of Chemical Engineering, Faculty of Engineering and Built Environment,

# Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor, Malaysia

# *Corresponding author:  farhanini@umt.edu.my

Received: 2 January 2018; Accepted: 6 March 2018

Abstract

# Zinc oxide/reduced graphene oxide (ZnO/rGO) composite was synthesized via the modified Hummers’ method. The presence of ZnO composite on the rGO sheets was confirmed by Scanning Electron Microscope (SEM), X-Ray Diffractometer (XRD) and Fourier Transform Infrared (FTIR) spectrometer. FTIR result showed the formation of ZnO/rGO with the presence ZnO stretching peak and the surface of ZnO/rGO was found to have better morphology with functionalized groups attached to it. XRD analysis also confirms the formation of ZnO/rGO composite by wurtzite structured indexed peak of the diffractogram. The ZnO/rGO composite was drop on the surface of GCE by drop casting method to increase the electrocatalytic activities of bare GCE. The electrochemical behaviour of ZnO/rGO modified electrode shows the enhancement in electron transfer and the system is diffusion-controlled. The electrochemical studies also revealed that the ZnO/rGO/GCE dramatically increased the current response against the dopamine (DA), due to the synergistic effect emerged between ZnO and rGO. This attributed that ZnO/rGO/GCE could exhibit excellent electrocatalytic activity and effective electron transfer kinetics towards the oxidation of DA. Therefore, the ZnO/rGO/GCE could be used to determine the DA concentration and provide an ideal matrix for clinical applications.

# Keywords:  zinc oxide, reduced graphene oxide, composite materials, dopamine, electrocatalysis

# Abstrak

# Komposit zink oksida/grafin oksida terturun (ZnO/rGO) telah disintesis melalui kaedah Hummer terubahsuai. Kehadiran komposit ZnO pada lapisan rGO telah diujikan oleh mikroskop imbasan elektron (SEM), Pembelauan sinar X (XRD) dan Inframerah transformasi Fourier (FTIR). Keputusan FTIR menunjukkan pembentukan ZnO/rGO dengan kehadiran puncak ZnO dan permukaan ZnO/rGO didapati mempunyai morfologi yang lebih baik dengan kumpulan berfungsi melekat padanya. Analisis XRD juga menunjukkan pembentukan komposit ZnO/rGO melalui diffraktogram indeks puncak struktrur wurtzit. Komposit ZnO/rGO telah diubahsuai dengan elektrod karbon berkaca (GCE) dengan menggunakan kaedah alas titis. Perlakuan elektrokimia ZnO/rGO/GCE menunjukkan peningkatan dalam pemindahan elektron dan sistem adalah proses serapan terkawal. Kajian elektrokimia mendedahkan bahawa respon arus ZnO/rGO/GCE meningkat terhadap DA, disebabkan kesan sinergi antara ZnO dan  rGO. Ini disebabkan respon arus ZnO/rGO/GCE boleh mempamerkan aktiviti elektropemangkin yang berkesan terhadap kinetik pemindahan elektron DA. Oleh itu, ZnO/rGO/GCE boleh digunakan untuk menentukan kepekatan DA dan menjadi pemangkin sesuai untuk aplikasi klinikal.

# Kata kunci:  zink oksida, grafin oksida terturun, bahan komposit, dopamin, elektropemangkin

References

- Hu, X., Qi, R., Zhu, J., Luo, Y., Jin, J. and Jiang, P. (2014). Preparation and properties of dopamine reduced graphene oxide and its composites of epoxy. Journal of Applied Polymer Science, 131(2): 39754.

- Siciliano, C. A., Locke, J. L., Mathews, T. A., Lopez, M. F., Becker, H. C. and Jones, S. R. (2017). Dopamine synthesis in alcohol drinking-prone and -resistant mouse strains. Alcohol, 58: 25 – 32.

- Kim, D., Lee. S. and Piao Y. (2017). Electrochemical determination of dopamine and acetaminophen using activated  graphene-nafion  modified  glassy carbon electrode. Journal of Electroanalytical Chemistry, 794: 221 - 228.

- Quan, D. P., Tuyen, D. P., Lam, T. D., Tram, P. T. N., Binh, N. H. and Viet, P. H. (2011). Electrochemically selective determination of dopamine in the presence of ascorbic and uric acids on the surface of the modified nafion/single wall carbon nanotube/poly(3-methylthiophene) glassy carbon electrodes. Colloids and Surfaces B: Bionterfaces, 88(2): 764 - 770.

- Wilson, G. S. and Johnson, M. A. (2008). In-vivo electrochemistry: What can we learn about living systems? Chemical Review, 108 (7): 2462 - 2481.

- Lakshmi, D., Bossi, A., Whitcombe, M. J., Chianella, I., Fowler, S. A., Subrahmanyam, S., Piletska, E. V. and Piletsky, S. A. (2009). Electrochemical sensor for catechol and dopamine based on a catalytic molecularly imprinted polymer-conducting polymer hybrid recognition element. Analytical Chemistry, 81(9): 3578 - 3584.

- Mahshid, S., Li, C., Mahshid, S. S., Askari, M., Dolati, A., Yang, L., Luo, S. and Cai, Q. (2011). Sensitive determination of dopamine in the presence of uric acid and ascorbic acid using TiO2 nanotubes modified with Pd, Pt and Au nanoparticles. Analyst, 136(11): 2322 - 2329.

- Fang, B., Wang, G., Zhang, W., Li, M. and Kan, X. (2005). Fabrication of Fe3O4 nanoparticles modified electrode and its application for voltammetric sensing of dopamine. Electroanalysis, 17(9): 744 - 748.

- Wang, W., Xu, G., Cui, X. T., Sheng, G. and Luo, X. (2014). Enhanced catalytic and dopamine sensing properties of electrochemically reduced conducting polymer nanocomposite doped with pure graphene oxide. Biosensors and Bioelectronics, 58: 153 - 156.

- Liu, X., Peng, Y., Qu, X., Ai, S., Han, R. and Zhu, X. (2011). Multi-walled carbon nanotube-chitosan/poly(amidoamine)/DNA nanocomposite modified gold electrode for determination of dopamine and uric acid under coexistence of ascorbic acid. Journal of Electroanalytical Chemistry, 654 (1-2): 72 - 78.

- Hernandez, Y., Nicolosi, V., Lotya, M., Blighe, F. M., Sun, Z., De, S., McGovern, I. T., Holland, B., Byrne, M., Gun’ko, Y., Boland, J., Niraj, P., Duesberg, G., Krishnamurti, S., Goodhue, R., Hutchison, J., Scardaci, V., Ferrari, A. C. and Coleman, J. N. (2008). High-yield production of graphene by liquid-phase exfoliation of graphite. Nature Nanotechnology, 3(9): 563 - 568.

- Shan, C., Tang, H., Wong, T., He, L. and Lee, S-T. (2012). Facile synthesis of a large quantity of graphene by chemical vapor deposition: an advanced catalyst carrier. Advanced Materials, 24(18): 2491 - 2495.

- Fan, Z. J., Kai, W., Yan, J., Wei, T., Zhi, L. J., Feng, J., Ren, Y. M., Song, L. P. and Wei, F. (2011). Facile synthesis of graphene nanosheets via fe reduction of exfoliated graphite oxide. ACS Nano, 5(1): 191 - 198.

- Ling, Y. Y., Huang, Q. A., Zhu, M. S., Feng, D. X., Li, X. Z. and Wei, Y. (2013). A facile one-step electrochemical fabrication of reduced graphene oxide–multiwall carbon nanotubes–phospotungstic acid composite for dopamine sensing. Journal of Electroanalytical Chemistry, 693: 9 - 15.

- Zhang, F., Wang, Z., Zhang, Y., Zheng, Z., Wang, C., Du, Y. and Ye, W. (2012). Simultaneous electrochemical determination of uric acid, xanthine and hypoxanthine based on poly(l-arginine)/graphene composite film modified electrode. Talanta, 93: 320 - 325.

- Wang, G., Shen, X., Wang, B., Yao, J. and Park, J. (2009). Synthesis and characterization of hydrophilic and organophilic graphene nanosheets. Carbon, 47(5): 1359 - 1364.

- Cui, X., Fang, X., Zhao, H., Li, Z. and Ren, H. (2017). An electrochemical sensor for dopamine based on polydopamine modified reduced graphene oxide anchored with tin dioxide and gold nanoparticles.  Analytical Methods, 36(9): 5322 - 5332.

- Chang, Z., Zhou, Y., Hao, L., Hao, Y., Zhu, X. and Xu, M. (2017). Simultaneous determination of dopamine and ascorbic acid using β-cyclodextrin/au nanopaerticles/graphene-modifie electrodes. Analytical Methods, 9(4): 664 - 671.

- Tang, L., Li, X., Ji, R., Teng, K. S., Tai, G., Ye, J., Wei, C. and Lau, S. P. (2012). Bottom-up synthesis of large-scale graphene oxide nanosheets. Journal of Materials Chemistry, 22(12): 24981 - 24982.

- Babu K. S., Reddy, R., Sujatha, C., Reddy, K. V. and Mallika, A. N. (2013). Synthesis and optical characterization of porous ZnO. Journal of Advanced Ceramic, 2(3): 260 - 265.

- Chen, Y. L., Hu, Z. A., Wang, H. W., Zhang, Z, Y., Yang, Y. Y. and Wu, H. Y. (2011). Zinc oxide/reduced graphene oxide composites and electrochemical capacitance enhanced by homogeneous incorporation of reduced graphene oxide sheets in zinc oxide matrix. The Journal of Physical Chemistry, 115(5): 2563 - 2571.

- Yusoff, F., Aziz, A., Mohamed, N. and Ghani, S. A. (2013). Synthesis and characterizations of BSCF at different pH as future cathode materials of fuel cells. International Journal of Electrochemical Science, 8(8): 10672 - 10687.

- Fritea, L., Goff, A. L., Putaux, J. L., Tertis, M., Cristea, C., Sãndulescu, R. and Cosnier, S. (2015). Design of a reduced-graphene-oxide composite electrode from an electropolymerizable graphene aqueous dispersion using a cyclodextrin-pyrrole monomer. Application to dopamine biosensing. Electrochimica Acta, 178: 108 - 112.

- Avendańo S. C., Angeles, G. A., Silva, M. T. R., Pina, G. R., Romo, M. R. and Pardavĕ, M. P. (2007). On the electrochemistry of dopamine in aqueous solution. Part 1: The role of [SDS] on the voltammetric behavior of dopamine on a carbon paste electrode. Journal of Electroanalytical Chemistry, 609(1): 17 - 26.