# Malaysian Journal of Analytical Sciences Vol 22 No 3 (2018): 477 - 482

# THE EFFECTS OF FE-DOPING ON MECHANICAL PROPERTIES IN Bi1.6Pb0.4Sr2Ca2Cu3-XFeXOY SUPERCONDUCTOR

# (Kesan Dop Ferum Terhadap Sifat Superkonduktor Bi1.6Pb0.4Sr2Ca2Cu3-xFexOy)

# Suazlina Mat Ali1, Azhan Hashim2*, Syamsyir Akmal Senawi2, Azman Kasim2, Wan Aizuddin Wan Razali2, Ruziana Mohamed2,  Fairuzdzah Ahmad Lothfy2

# 1Faculty of Applied Sciences,

# Universiti Teknologi MARA Shah Alam, 40450 Shah Alam, Selangor, Malaysia

# 2Faculty of Applied Sciences,

# Universiti Teknologi MARA Pahang, 26400 Bandar Jengka, Pahang, Malaysia

# *Corresponding author:  dazhan@pahang.uitm.edu.my

Received: 4 December 2016; Accepted: 1 December 2017

Abstract

# Bi-2223 superconductors doped with Fe2O3 at Cu-site were prepared in bulk form using high purity oxide powders via solid state reaction technique with intermediate grinding. The series of Fe stoichiometric ratio (x = 0.00, 0.02, 0.04, 0.06, 0.08 and 0.10) are systematically added to Bi1.6Pb0.4Sr2Ca2Cu3-xFexOy system to study the effect of Fe doping on mechanical and superconducting system properties. Vickers hardness, electrical resistivity, X-ray diffraction and Field Emission Scanning Electron Microscopy have been carried out to assess the effects of Fe doping. These measurements indicate that the Fe doping decreased the critical temperature and deteriorated formation of high Tc phase, compared to undoped sample. Grain size of the samples were also reduced by increasing the amount of Fe and the mechanical properties were found to be escalate with the increasing of Fe concentration.

# Keywords:  BSCCO superconductor, Fe-doped, critical current density, X-ray diffraction, microhardness

# Abstrak

# Superkonduktor Bi-2223 dop Fe2O3 dikawasan kuprum telah dihasilkan secara pukal menggunakan serbuk oksida tulin dengan kisaran perantara melalui kaedah tindak balas keadaan pepejal. Nisbah stokiometri bersiri (x = 0.00, 0.02, 0.04, 0.06, 0.08 and 0.10) ditambah secara sistematik terhadap sistem Bi1.6Pb0.4Sr2Ca2Cu3-xFexOy bagi mengkaji kesan dop Fe terhadap sifat mekanikal dan sistem superkonduktor. Ujian ketahanan Vickers, kerintangan arus, pembelauan Sinar-X dan mikroskopi imbasan elektron pancaran medan telah dilakukan bagi menilai kesan dop Fe. Pencirian ini menunjukkan bahawa kesan dop yang dilakukan mengurangkan suhu genting dan merencatkan pembentukan fasa suhu tinggi berbanding sampel tanpa dop. Saiz butiran sampel turut mengecil dengan penambahan jumlah kehadiran Fe dan sifat mekanikal didapati meningkat seiring dengan penambahan Fe.

# Kata kunci:  Superkonduktor BSCCO, dop-Fe, ketumpatan arus, pembelauan sinar-X, ketahanan mikro

References

- Maeda, H., Tanaka, Y., Fukutomi, M. and Asano T. (1988). A  new high-Tc oxide superconductor without a rare earth element. Japanese Journal of Applied Physics, 27: 209-210.

- Trong On, D., Sato, O., Fujishima, A. and Hashimoto, K. (1999). Change of the critical temperature of high-Tc single (2223) phase Bi-Pb-Sr-Ca-Cu-O supercondcutors by intercalation process. Journal of Physics and Chemistry of Solids, 60: 883-890.

- Mulay, V. N., Siva Prasad, P. V. L. N., Bhupal Reddy, K. and Jaleel M. A. (1990). Studies on the synthesis of Bi2CaSr2Cu2Oδ  by different chemical routes. Journal of Materials Science Letter, 9: 1284-1287.

- Halim, S. A., Mohamed, S. B., Azhan, H., Khawaldeh, S. A. and Sidek, H. A. A. (1999). Effect of barium doping in Bi-Pb-Sr-Ca-Cu-O ceramics supercondcutors. Physica C, 312: 78-84.

- Terzioglu, C., Yilmazlar, M., Ozturk, O. and Yanmaz, E. (2005). Structural and physical properties of Sm-doped Bi1.6Pb0.4Sr2Ca2-xSmxCu3Oy superonductors. Physica C, 423:119-126.

- Suazlina, M. A., Yusainee, S. Y. S., Azhan, H., Abd-Shukor, R. and Mustaqim, R. M. (2014). The effects of nanoparticle addition in Bi-2212 superconductors. Jurnal Teknologi, 69(2): 49-52.

- Gul, I. H., Anis-ur-Rehman, M. and Maqsood, A. (2006). Temperature dependence of thermal and electritrical conductivity of Bi-based high-Tc (2223) superconductor. Physica C, 450: 83-87.

- Shalaby, M. S., Hashem, H. M., Hammad, T. R., Wahab, L. A., Marzouk, K. H. and Soltan, S. (2016). Higher critical current density achieved in Bi-2223 High-Tc superconductors. Journal of Radiation       Research and Applied Sciences, 9: 345–351.

- Godeke, A., Abraimov, D. V., Arroyo, E., Barret, N., Bird, M. D., Francis, A., Jaroszynski, J., Kurtev, D. V. and Markiewicz, W. D. (2017). A feasibility study of high-strength Bi-2223 conductor for high-field solenoids. Superconductor Science and Technology, 30(3), 035011.

- Gul, I. H., Rehman, M. A., Ali, M. and Maqsood. A. (2005). Effect of vanadium and barium on the Bi-based (2223) superconductors. Physica C, 432: 71-80.

- Sarun, P. M., Vinu, S., Shabna, R., Biju, A. and Syamaprasad, U. (2008). Highly enhanced superconducting properties of Eu-doped (Bi,Pb)-2212.  Materials Letter, 62: 2725-2728.

- Yilmazlar, M., Ozturk, O., Aydin, H., Akdogan, M. and Terzioglu, C. (2007). The effect of Sm→ Ca substitution on mechanical properties of BSCCO superconductors. Chinese Journal of Physics, 45: 128-134.

- Khalil, S. M. (2001). Enhancement of superconducting and mechanical properties in BSCCO with Pb additions. Journal of Physics and Chemistry of Solids, 62: 457-466.

- Bruneel, E., Degrieck, J., Van Driessche, I., Hoste, S. (2002). Mechanical properties of Bi-2223/Ag bulk composites. Physica C, 1063: 372-376.

- Ling, H. C. and Yan, M. F. (1988). Microhardness measurements on dopant modified superconducting YBa2Cu3O7 ceramics. Journal of Applied Physics, 64: 1307-1311.