# Malaysian Journal of Analytical Sciences Vol 22 No 4 (2018): 642 - 647

# ADSORBENTS FROM THE BY-PRODUCT OF PALM OIL REFINERY FOR METHYLENE BLUE REMOVAL

# (Penjerap daripada Produk Sampingan Penapisan Minyak Sawit untuk Penyingkiran Metilena Biru)

# Hamzat Bashir Aderemi1, 2, Muhammad Abbas Ahmad Zaini1, 3*, Noor Shawal Nasri3, 4

# 1Centre of Lipids Engineering & Applied Research, Ibnu-Sina Institute for Scientific & Industrial Research

# Universiti Teknologi Malaysia, 81310 UTM Johor Bahru, Johor, Malaysia

# 2Chemical Engineering Department,

# Kaduna Polytechnic, Kaduna, Nigeria

# 3Faculty of Chemical & Energy Engineering

# 4UTM-MPRC Institute for Oil & Gas

# Universiti Teknologi Malaysia, 81310 UTM Johor Bahru, Johor, Malaysia

# *Corresponding author:  abbas@cheme.utm.my

Received: 16 April 2017; Accepted: 7 March 2018

Abstract

The present work was aimed at evaluating the removal of methylene blue by palm fatty acid distillate-based adsorbents. The adsorbents at different weight ratios of palm fatty acid distillate (PFAD) to palm kernel shell (PKS) were prepared at 600 °C for 2 hours. Results show that the yield of adsorbent upon heat treatment decreased with increasing weight ratio, with yield as low as 0.53% was recorded by adsorbent derived by using only PFAD. The methylene blue adsorption data show a promising performance of PFAD-based adsorbents as compared to that of PKS-adsorbent (char) with qe = 7.6 mg/g at Co = 20.8 mg/L. To conclude, PFAD is a potential candidate of dye adsorbent.

# Keyword:  adsorbent, methylene blue, palm fatty acid distillate, palm kernel shell

# Abstrak

Tujuan kajian ini adalah untuk menilai penyingkiran metilena biru oleh penjerap berasaskan distilat asid lemak sawit. Penjerap pada nisbah berat distilat asid lemak sawit (PFAD) kepada isirong sawit (PKS) disediakan pada 600 °C selama 2 jam. Keputusan menunjukkan bahawa hasil penjerap setelah rawatan haba berkurang dengan peningkatan nisbah berat, dengan hasil serendah 0.53% direkodkan oleh penjerap terbitan PFAD sahaja. Data penjerapan metilena biru menunjukkan prestasi menjanjikan oleh penjerap berasaskan PFAD berbanding penjerap berasaskan PKS (arang) dengan qe = 7.6 mg/g pada Co = 20.8 mg/L. Kesimpulannya, PFAD ialah calon berpotensi sebagai penjerap pencelup.

# Kata kunci:  penjerap, metilena biru, distilat asid lemak sawit, isirong sawit

References

- Garlapati, V. K., Shankar, U. and Budhiraja, A. (2016). bioconversion technologies of crude glycerol to value added industrial products. Biotechnology Reports, 9: 9-14.

- Mahmood, W. M. F. W., Ariffin, M. A., Harun, Z., Ishak, N. A. I. Md., Ghani, J. A. and Rahman, M. N. Ab. (2015). Characterisation and potential use of biochar from gasified oil palm wastes. Journal of Engineering Science and Technology, 6: 45-54.

- Ping, B. T. Y. and Yusof, M. (2009). Characteristics and properties of fatty acid distillates from palm oil. Oil Palm Bulletin, 59: 5-11.

- Top, A. G. M. (2010) Production and utilization of palm fatty acid distillates (PFAD). Lipid Technology, 22(1): 11-13.

- Shu-Hui, T. and Zaini, M. A. A. (2015). Potassium hydroxide activation of activated carbon: A commentary. Carbon Letters, 16(4): 275-280.

- Zaini, M. A. A., Mohd-Setapar, S. H., Kamaruddin, M. J. and Yunus, M. A. C. (2013). In-depth studies of cattle-manure-compost activated carbons for Cu(II) ions removal. Agricultural Research Updates, 6: 247 – 265.

- Hamza, U. D., Nasri, N. S., Amin, N. S., Mohammed, J. and Zain, H. M. (2016). Characteristics of oil palm shell biochar and activated carbon prepared at different carbonization times. Desalination and Water Treatment, 57(17): 7999-8006.

- Pezoti Jr., O., Cazetta, A. L., Souza, I. P. A. F., Bedin, K. C., Martins, A. C., Silva, T. L. and Almeida, V. C. (2014). Adsorption studies of methylene blue onto ZnCl2-activated carbon produced from buriti shells (Mauritia flexuosa L.). Journal of Industrial and Engineering Chemistry, 20(6): 4401-4407.

- Zaini, M. A. A., Okayama, R. and Machida, M. (2009). Adsorption of aqueous metal ions on cattle-manure-compost based activated carbons. Journal of Hazardous Materials, 170(2-3): 1119-1124.

- Langmuir, I. (1918). The adsorption of gases on plane surfaces of glass, mica and platinum. Journal of American Chemical Society, 40(9): 1361-1403.

- Freundlich, H. M. F. (1906). Over the adsorption in solution. The Journal of Physical Chemistry, 57: 385-470.

- Zhi, L. L. and Zaini, M. A. A. (2017). Adsorption properties of cationic rhodamine B dye onto metals chloride-activated castor bean residue carbons. Water Science and Technology, 75(4): 864-880.

- Shu-Hui T. and Zaini, M. A. A. (2017). Malachite green adsorption by potassium salts-activated carbons derived from textile sludge: Equilibrium, kinetics and thermodynamics studies. Asia-Pacific Journal of Chemical Engineering, 12: 159-172.

- Zaini, M. A. A. and Mohamad, N. A. (2015). Activated charcoal for oral medicinal purposes: Is it really activated? Journal of Applied Pharmaceutical Science, 5(10): 157-159.