Malaysian Journal of Analytical Sciences Vol 22 No 4 (2018): 735 - 741

REMOVAL OF OIL AND GREASE AND ANIONIC SURFACTANTS IN SYNTHETIC CAR WASH WASTEWATER USING KAPOK FIBER:

A BATCH-SCALE STUDY

(Penyingkiran Minyak dan Gris dan Anionik Surfaktan dalam Air Sisa Sintetik Basuhan Kereta Menggunakan Fiber Kapok: Kajian Skala-Kelompok)

Muhammad Shahrul Shafendy Ibrahim* and Nor Haslina Hashim

# Department of Civil Engineering Technology,

# Faculty of Engineering Technology,

# Universiti Tun Hussein Onn Malaysia, 86400 Batu Pahat, Johor, Malaysia

# *Corresponding author:  msshafendy2@gmail.com

Received: 16 April 2017; Accepted: 7 March 2018

Abstract

Kapok fiber (Ceiba pentandra) is a natural sorbent that exhibits excellent hydrophobic-oleophilic characteristics. The effects of dosage, and contact time were studied in a batch study. The initial and final concentration of the oil and grease and anionic surfactants in the synthetic car wash wastewater were evaluated to determine the removal efficiency of Kapok fiber. The results show excellent performance of Kapok fiber in removing oil and grease up to 100%, achieved using 0.1 g with 10 minutes contact time. Meanwhile, highest removal of anionic surfactants was up to 46%, achieved using 3.0 g of Kapok fiber with 10 minutes contact time. Overall, Kapok fiber showed great potential as an effective oil and grease, and anionic surfactants adsorbent.

# Keywords:  wastewater treatment, car wash wastewater, Kapok fiber, oil and grease, anionic surfactants

# Abstrak

Serat Kapok (Ceiba pentandra) adalah penyerap semulajadi yang mempamerkan ciri-ciri hidrofobik-oleofilik cemerlang. Kesan dos, dan masa tindak balas dikaji dalam kajian skala kelompok. Kepekatan awal dan akhir kehadiran minyak dan gris surfaktan anionik dalam air kumbahan sintetik disediakan telah dinilai untuk menentukan kecekapan serat Kapok. Keputusan menunjukkan prestasi yang sangat baik serat Kapok dalam mengeluarkan minyak dan gris dan surfaktan anionik. Penyingkiran minyak dan gris sehingga 100% telah dicapai dengan menggunakan 0.1 g dengan masa tindak balas selama 10 minit, manakala penyingkiran surfaktan anionik sehingga 46% telah dicapai dengan menggunakan 3.0 g serat Kapok dengan masa 10 minit kenalan. Secara keseluruhan, serat Kapok berpotensi tinggi sebagai minyak dan gris yang berkesan dan penjerap surfaktan anionic yang berkesan.

# Kata kunci:  rawatan air sisa, air sisa basuhan kereta, serat Kapok, minyak dan gris, surfaktan anionik

References

- Bhatti, Z. A., Mahmood, Q., Raja, I. A., Malik, A. H., Khan, M. S. and Wu D. (2011). Chemical oxidation of carwash industry wastewater as an effort to decrease water pollution. Physical Chemistry Earth, 36(9-11): 465-469.

- Shahbazi, R., Kasra-Kermanshahi, R., Gharavi, S., Moosavi- Nejad, Z. and Borzooee, F. (2013). Screening of SDS-degrading bacteria from car wash wastewater and study of the alkylsulfatase enzyme activity. Iranian Journal of Microbiology, 5(2): 153-158.

- Lau, W. J., Ismail, A. F. and Firdaus, S. (2013). Car wash industry in Malaysia: Treatment of car wash effluent using ultrafiltration and nanofiltration membranes. Separation Purification Technology, 104: 26-31.

- Jönsson, C., and Jönsson, A. S. (1995). The influence of degreasing agents used at car washes on the performance of ultrafiltration membranes. Desalination, 100(1-3): 115-123.

- Kwach, B. O. and Lalah, J. O. (2009). High concentrations of polycyclic aromatic hydrocarbons found in water and sediments of car wash and kisat areas of Winam Gulf, Lake Victoria-Kenya. Bulletin Environmental Contamination Toxicology, 83(5): 727-733.

- Wu, L., Ge, G. and Wan, J. (2009). Biodegradation of oil wastewater by free and immobilized Yarrowia Lipolytica W29. Journal of Environmental Science, 21(2): 237-242.

- Perkowski, J., Bzdon, S. A., Bulska and Jóźwiak, W. K. (2006). Decomposition of detergents present in car-wash sewage by titania photo-assisted oxidation. Polish Journal of Environmental Study, 15(3): 457-465.

- Aloui, F., Kchaou, S. and Sayadi, S. (2009). Physicochemical treatments of anionic surfactants wastewater: effect on aerobic biodegradability. Journal of Hazardous Material, 164(1): 353-359.

- Merta, J. and Stenius, P. (1999). Interactions between cationic starch and mixed anionic surfactants. Colloids Surfaces A Physicochem. Engineering Aspect, 149(1-3): 367-377.

- Nielsen, A. D. Borch, K. and Westh, P. (2000). Thermochemistry of the specific binding of C12 surfactants to bovine serum albumin. Life Science, 1479: 321-331.

- Zheng, Y., Wang, J., Zhu, Y. and Wang,  A. (2015). Research and application of kapok fiber as an absorbing material: A mini review. Journal of Environmental Science, 27: 21-32.

- Abdullah, M. A., Rahmah, A. U. and Man, Z. (2010). Physicochemical and sorption characteristics of Malaysian Ceiba pentandra (L.) Gaertn. as a natural oil sorbent. Journal of Hazardous Materials, 177 (1-3): 683-691.

- Rahmah, A. U. and Abdullah, M. A. (2011). Evaluation of Malaysian Ceiba pentandra (L.) Gaertn for oily water filtration using factorial design. Desalination, 266(1-3): 51-55.

- Hori, S., Flavier, K. and Kuga, M. E. (2000). Excellent oil Absorbent Kapok Ceiba pentandra (L.) Gaertn fiber: Fiber structure, chemical characteristics, and application. Japan Wood Resource Society, 46: 401-404.

- Lim, T. T. and Huang, X. (2007). Evaluation of Kapok (Ceiba pentandra (L.) Gaertn.) as a natural hollow hydrophobic–oleophilic fibrous sorbent for oil spill cleanup. Chemosphere, 66(5): 955-963.

- Adak, A., Bandyopadhyay, M. and Pal, A. (2005). Removal of anionic surfactant from wastewater by alumina: A case study. Colloids Surfaces A Physicochem. Engineering Aspect, 254(1-3): 165-171.

- APHA. (2005). Standard methods for the examination of water and wastewater. American Public Health Association ,Washington, D.C.

- Wang, J., Zheng, Y. and Wang, A. (2012). Effect of Kapok fiber treated with various solvents on oil absorbency. Industrial Crops Product, 40(1): 178-184.

- Rengasamy, R. S., Das, D. and Praba Karan, C. (2011). Study of oil sorption behavior of filled and structured fiber assemblies made from polypropylene, Kapok and Milkweed fibers. Journal of Hazardous Materials, 186(1): 526-532.

- Ismail, Z. (2013). Comparative study on raw and modified Kapok fibers as sorbent materials for oil sorption. Thesis Universiti Teknologi PETRONAS, Malaysia.

- Wang, J., Zheng, Y. and Wang, A. (2012). Superhydrophobic Kapok fiber oil-absorbent: Preparation and high oil absorbency. Chemical Engineering Journal, 213: 1-7.

- Zhang, R. and Somasundaran, P. (2006). Advances in adsorption of surfactants and their mixtures at solid/solution interfaces. Advance Colloid Interface Science, 123: 213-229.

- Stone, A. (2013). The theory of intermolecular forces. OUP Oxford.