Malaysian Journal of Analytical Sciences Vol 22 No 5 (2018): 906 - 913

MENGKUANG FIBER REINFORCED THERMOPLASTIC NATURAL RUBBER COMPOSITES: INFLUENCE OF RUBBER CONTENT ON MECHANICAL PROPERTIES AND MORPHOLOGY

# (Komposit Termoplastik Getah Asli Diperkuat Serabut Mengkuang: Pengaruh Kandungan Getah ke atas Sifat Mekanik dan Morfologi)

Wan Zarina Wan Mohamed1, 2, Azizah Baharum1, 3*, Ishak Ahmad1, 3, Ibrahim Abdullah4, Nurzam Ezdiani Zakaria1

### 1School of Chemical Sciences and Food Technology, Faculty of Sciences and Technology,

### Universiti Kebangsaan Malaysia, 43600 UKM Bangi Selangor, Malaysia

### 2Faculty of Engineering and Life Sciences,

### Universiti Selangor, 45600 Bestari Jaya Selangor, Malaysia

### 3Polymer Research Center, Faculty of Science and Technology,

### Universiti Kebangsaan Malaysia, 43600 UKM Bangi Selangor, Malaysia

### 4Academy Sciences of Malaysia, 50480 Kuala Lumpur, Malaysia

### *Corresponding email:  azeiss@ukm.edu.my

Received: 20 July 2017; Accepted: 28 April 2018

Abstract

This paper presents the influence of rubber on mengkuang (MK) reinforced thermoplastic composites as the rubber content appeared to increase at low fibre loading of 10% MK and high fibre loading of 30% MK. The MK fibre was blended with high density polyethylene (HDPE) and natural rubber (NR) through melt blending via internal mixer. The MK composites at 10% MK fibre loading exhibited higher tensile strength, tensile strain at break, and impact strength; but lower tensile modulus than MK composites at 30% fibre loading. Both fibre contents showed that the tensile strength and the tensile modulus decreased, while tensile strain at break and impact strength seemed to increase as the rubber content increased up to 40%. Field emission scanning electron microscopy (FESEM) micrograph was employed to observe the fibre dispersion, as well as physical interactions between the fibre and the matrix.  This study showed that the effects of MK fibre loading on mechanical properties and morphology were influenced by rubber content.

Keywords:  rubber, polymer composites, mengkuang fibre, mechanical properties, morphology

# Abstrak

Kertas kerja ini membentangkan pengaruh getah ke atas komposit termoplastik diperkuat serabut mengkuang (MK) dengan peningkatan kandungan getah pada muatan serabut rendah MK 10% dan muatan serabut tinggi MK 30%. Serabut MK telah diadun bersama polietilena berketumpatan tinggi (HDPE) dan getah asli (NR) melalui pengadunan lebur dengan pencampur dalaman. Komposit MK pada muatan serabut 10% menunjukkan kekuatan regangan, kekuatan terikan pada takat putus, dan kekuatan hentaman yang lebih tinggi; tetapi modulus regangan yang rendah berbanding komposit MK pada muatan serabut 30%. Kedua-dua muatan serabut menunjukkan kekuatan regangan dan modulus regangan menurun, sementara kekuatan terikan regangan takat putus dan kekuatan hentaman seperti meningkat dengan pertambahan kandungan getah sehingga 40%. Sebaran serabut MK dan interaksi fizikal antara serabut dan matrik telah diperhati menerusi mikroskop elektron imbasan pancaran medan (FESEM). Kajian telah menunjukkan kesan muatan serabut MK terhadap sifat mekanikal dan morfologi komposit mengkuang dipengaruhi oleh kandungan getah.

# Kata kunci:  getah, komposit polimer, serabut mengkuang, sifat mekanik, morfologi

References

- Saheb, N. D. and Jog, J. P. (1999). Natural fiber polymer composites: A review. Advance Polymer Technology, 18(4): 351-363.

- Joshi, S., Drzal, L., Mohanty, A. and Arora, S. (2004). Are natural fiber composites environmentally superior to glass fiber reinforced composites?. Composite Part A: Applied Science and Manufacturing, 35(3): 371-376.

- Alves, F. M. E., Pereira, T. V. C. and Gomes, O. D. F. M. (2013). The effect of fiber morphology on the tensile strength of natural fibers. Journal of Materials Research and Technology, 2(2): 149-157.

- Tezara, C., Siregar, J. P., Lim, H. Y., Fauzi, F. A., Yazdi, M. H., Moey, L. K. and Lim, J. W. (2016). Factors that affect the mechanical properties of kenaf fiber reinforced polymer: A review. Journal of Mechanical Engineering and Sciences, 10(2): 2159-2175.

- John, M. J., Varughese, K. T. and Thomas, S. (2008). Green composites from natural fibers and natural rubber: effect of fiber ratio on mechanical and swelling characteristics. Journal of Natural Fibers, 5(1): 47-60.

- Thakur, V. K., Thakur, M. K. and Gupta, R. K. (2014). Review: Raw natural fiber–based polymer composites. Internatinal Journal of Polymer Analysis and Characterization, 19(3): 256-271.

- Monteiro, S. N., Lopes, F. P. D., Ferreira, A. S. and Nascimento, D. C. O. (2009). Natural-fiber polymer-matrix composites: Cheaper, tougher, and environmentally friendly. Polymer-Matrix Composites, 61(1): 17-22.

- Fortea-Verdejo, M., Bumbaris, C.,  E., Burgstaller, C., Bismark, A. and Lee, K. Y. (2017). Plant fibre-reinforced polymers: Where do we stand in terms of tensile properties?. International Materials Reviews, 62(8): 441-464.

- Hassaini, L., Kaci, M., Touati, N., Pillin, S., Kervoelen, A. and Bruzaud, S. (2017). Valorization of olive husk flour as a filler for biocomposites based on poly(3-hydroxybutyrate-co-3-hydroxyvalerate): Effects of silane treatment. Polymer Testing, 59: 430-440.

- Puglia, D., Sarasini, F., Santulli, C. and Kenny, J. M. (2017). Manufacturing of natural fiber/agrowaste based polymer composites. Green Biocomposites, Springer: pp. 125–147.

- Preet Singh, J. I., Dhawan, V., Singh, S. and Jangid, K. (2017). Study of effect of surface treatment on mechanical properties of natural fiber reinforced composites. Material Today Proceeding, 4(2):2793-2799.

- Ahmad, S., Abdullah, I., Sulaiman, C. S. and Kohjiya, S. (1994). Natural rubber-hdpe blends with liquid natural-rubber as a compatibilizer. I. thermal and mechanical-properties. Journal of Applied Polymer Science, 51:1357-1363.

- Rozman, H. D., Tan, K. W., Kumar, R. N., Abubakar, A., Mohd Ishak, Z. A. and Ismail, H. (2000). The effect of lignin as a compatibilizer on the physical properties of coconut fiber- polypropylene composites. European Polymer Journal, 36: 1483-1494.

- Jamil, M. S., Ahmad, I. and Abdullah, I. (2006). Effects of rice husk filler on the mechanical and thermal properties of liquid natural rubber compatibilized high-density polyethylene/natural rubber blends. Journal of Polymer Research, 13(4):315-321.

- Zahari, W. Z. W., Badri, R. N. R. L., Ardyananta, H., Kurniawan, D. and Nor, F. M. (2015) Mechanical properties and water absorption behavior of polypropylene / ijuk fiber composite by using silane treatment. Procedia Manufacturing, 2: 573-578.

- Stelescu, M-D., Manaila, E., Craciun, G. and Dumitrascu, M. (2014). New green polymeric composites based on hemp and natural rubber processed by electron beam irradiation. The Scientific World Journal, 2014: 1-13.

- Chen, R. S., Ahmad, S. and Gan, S. (2016). Characterization of rice husk-incorporated recycled thermoplastic blend composites. BioResources, 11(4): 8470-8482.

- Ibrahim, A. and Dahlan, M. (1998). Thermoplastic natural rubber blends. Progress in Polymer Science, 23: 665-706.

- El-Shekeil, Y. A., Sapuan, S. M., Khalina, A., Zainudin, E. S. and Al-Shuja'a, O. M. (2012). Influence of fiber content on the mechanical and thermal properties of Kenaf fiber reinforced thermoplastic polyurethane composites. Journal of Thermal Analysis and Calorimetry, 109: 299-303.

- Syafri, R., Ahmad, I. and Abdullah, I. (2011). Effect of rice husk surface modification by LENR the on mechanical properties of NR/HDPE reinforced rice husk composite. Sains Malaysiana, 40(7): 749-756.