Malaysian Journal of Analytical Sciences Vol 22 No 5 (2018): 914 - 920

FABRICATION OF CELLULOSE MICROSPHERES FROM MODIFIED COTTON LINTER AND OIL PALM TRUNK FIBRE VIA EMULSION METHOD

(Fabrikasi Mikrosfera Selulosa daripada Linter Kapas dan Gentian Batang Kelapa Sawit Termodifikasi Melalui Kaedah Emulsi)

Balqis Az-Zahraa Norizan1, Nurul Shuhadah Mahadi1, Nurul Nazatulatika Mohd Nizam1, Sarani Zakaria1,

Muhammad Fauzi Daud 2, Sharifah Nabihah Syed Jaafar1*

1School of Applied Physics, Faculty of Science and Technology,

# Universiti Kebangsaan Malaysia, 43600 UKM Bangi, Selangor, Malaysia

2Institute of Medical Science Technology,

Universiti Kuala Lumpur Malaysia, 43000 Kajang, Selangor, Malaysia

*Corresponding author:  nabihah@ukm.edu.my

Received: 20 July 2017; Accepted: 28 April 2018

Abstract

In this study, cellulose microspheres from modified cotton linter (CL) and oil palm trunk fibre (OPTF) were fabricated by using simple emulsion method. The cellulose was obtained from the CL and OPTF through the alkaline pre-treatment and acid hydrolysis processes. The emulsion method was performed using polyvinyl alcohol (PVA) as an emulsifying agent. The characterization of the cellulose from CL and OPTF were analysed using Fourier transform infrared spectroscopy (FTIR) and X-ray diffraction (XRD), and the morphological characterizations of cellulose microspheres were later observed under optical microscopy (OM) and field emission-scanning electron microscopy (FE-SEM). Based on the results, FTIR spectra displayed the lignin and hemicellulose had removed after treatments, while XRD revealed that the crystallinity index of OPTF and CL was increased after the treatments.  The microspheres, formed  with  different  ranges  of  size between 80 to 150 µm under OM and FE-SEM, showed the formation of pores on the surface of the microspheres.

Keywords:  emulsification, lignin, porous, field emission scanning electron microscopy

Abstrak

Kajian ini dijalankan bagi menghasilkan mikrosfera selulosa daripada linter kapas (LK) dan gentian batang kelapa sawit (GBKS) melalui kaedah emulsi. Selulosa didapati daripada LK dan gentian GBKS selepas proses pra-rawatan alkali dan hidrolisis asid. Manakala, kaedah emulsi dijalankan dengan menggunakan polivinil alkohol (PVA) sebagai agen pengemulsi. Pencirian selulosa daripada LK dan GBKS akan dianalisa menggunakan analisis transformasi inframerah Fourier (FTIR) dan pembelauan sinar-X (XRD) dan pencirian morfologi bagi mikrosfera selulosa dijalankan oleh mikroskopi optik (OM) dan mikroskop elektron imbasan-pancaran medan (FE-SEM). Berdasarkan keputusan FTIR yang diperoleh, lignin dan hemiselulosa telah berjaya dibuang selepas rawatan, sementara itu, keputusan XRD menunjukkan terdapat peningkatan pada indeks kehabluran bagi GBKS dan LK selepas rawatan.  Mikrosfera yang terbentuk juga dapat diperhatikan melalui OM dengan saiz berjulat 80 hingga 150 µm dan FE-SEM pula menunjukkan penghasilan liang pada permukaan kedua-dua mikrosfera.

Kata kunci:  pengemulsi, lignin, berliang, mikroskop elektron imbasan pancaran medan

References

- Xiao, Q., Zhou, K., Chen, C., Jiang, M., Zhang, Y., Luo, H. and Zhang, D. (2016). Hollow and porous hydroxyapatite microspheres prepared with an O/W emulsion by spray freezing method. Materials Science & Engineering C, 69: 1068-1674.

- Yang, H., Xie, Y., Hao, G., Cai, W. and Guo, X. (2015). Preparation of porous alumina microspheres via n oil-in-water emulsion method accompanied by a sol–gel process. New Journal of Chemistry, 40: 589-595.

- Dong, S., Bortner, M. J. and Roman, M. (2016). Analysis of the sulfuric acid hydrolysis of wood pulp for cellulose nanocrystal production: a central composite design study. Industrial Crops and Products, 93: 76-87.

- Czaja, W. K., Young, D. J., Kawecki, M. and Jr., R. M. (2007). The future prospects of microbial cellulose in biomedical applications. Biomacromolecules, 8: 1-12.

- Kemala, T., Budianto, E. and Soegiyono, B. (2012). preparation and characterization of microspheres based on blend of poly(lactic acid) and poly(ε-caprolactone) with poly(vinyl alcohol) as emulsifier. Arabian Journal of Chemistry, 5: 103-108.

- Suhaily, S. S., Jawaid, M., Abdul Khalil, H., Mohamed, A. and Ibrahim, F. (2012). A review of oil palm biocomposites for furniture design and applications: potential and challenges. BioResources, 7(3): 4400-4423.

- Tang, Y., Shen, X., Zhang, J., Guo, D., Kong, F. and Zhang, N. (2015). Extraction of cellulose nano-crystals from old corrugated container fibre using phosphoric acid and enzymatic hydrolysis followed by sonication. Carbohydrate Polymers, 125: 360-366.

- Lamaming, J., Hashim, R., Sulaiman, O., Leh, C. P., Sugimoto, T. and Nordin, N. A. (2015). Cellulose nanocrystals isolated from oil palm trunk. Carbohydrate Polymers, 127: 202-208.

- Gan, S., Padzil, F. N. M., Zakaria, S., Chia, C. H., Jaafar, S. N. S. and Chen, R. S. (2015). Synthesis of liquid hot water cotton linter to prepare cellulose membrane using NaOH/Urea or LiOH/Urea. BioResources, 10: 2244-255.

- Lamaming, J., Hashim, R., Leh, C. P., Sulaiman, O., Sugimoto, T. and Nasir, M. (2015). Isolation and characterization of cellulose nanocrystals from parenchyma and vascular bundle of oil palm trunk (Elaeis Guineensis). Carbohydrate Polymers, 134: 534-540.

- Ramli, R., Junadi, N., Beg, M. D. and Yunus, R. M. (2015). Microcrystalline cellulose (MCC) from oil palm empty fruit bunch (EFB) fibre via simultaneous ultrasonic and alkali treatment. International Journal of Chemical, Nuclear, Materials and Metallurgical Engineering, 9: 8-11.

- Salim, B. and Sorya, N. (2015). Effects of chemical treatments on the structural, mechanical and morphological properties of poly(vinylchloride)/spartium junceum fibre composites. Cellulose Chemistry and Technology, 49: 375-385.

- Rhim, J.-W., Reddy, J. P. and Luo, X. (2014). Isolation of cellulose nanocrystals from onion skin and their utilization for the preparation of agar-based bio-nano composites films. Cellulose, 22: 407-420.

- Mohamad Haafiz, M., Hassan, A., Zakaria, Z. and Inuwa, I. (2014). Isolation and characterization of cellulose nanowhiskers from oil palm biomass microcrystalline cellulose. Carbohydrate Polymers, 103: 119-125.

- Nazir, M. S., Wahjoedi, B. A., Yussof, A. W. and Abdullah, M. A. (2013). Eco-friendly extraction and characterization of cellulose from oil palm empty fruit bunches. BioResources, 8: 2161-2172.

- Owolabi, A. F., Mohamad Haafiz, M., Hossain, M. S., Hussin, M. H. and Nurul Fazita, M. (2017). Influence of alkaline hydrogen peroxide pre-hydrolysis on the isolation of microcrystalline cellulose from oil palm fronds. International Journal of Biological Macromolecules, 95: 1228-1234.

- Lamaming, J., Hashim, R., Leh, C. P. and Sulaiman, O. (2017). Properties of cellulose nanocrystals from oil palm trunk isolated by total chlorine free method. Carbohydrate Polymers, 156: 409-416.

- Mi, Y., Li, J., Zhou, W., Zhang, R., Ma, G. and Su, Z. (2016). Improved stability of emulsions in preparation of uniform small-sized konjac glucomanna (KGM) microspheres with epoxy-based polymer membrane by premix membrane emulsification. Polymers, 8: 1-13.

- Parida, P., Mishra, S. C., Sahoo, S., Behera, A. and Nayak, B. P. (2016). Development and characterization of ethylcellulose based microspheres for sustained release of nifedipine. Journal of Pharmaceutical Analysis, 6: 341-344.

- Murakami, M., Matsumoto, A., Watanabe, C., Kurumado, Y. and Takama, M. (2015). Fabrication of porous ethyl cellulose microspheres based on the acetone-glycerin-water ternary system: Controlling porosity via the solvent-removal mode. Drug Discoveries & Therapeutics, 9: 303-309.

- Qutachi, O., Vetsch, J., Gill, D., Cox, H., Scurr, D. and Hofmann, S. (2014). Injectable and porous PLGA microspheres that form highly porous scaffolds at body temperature. Acta Biomaterialia, 10: 5090-5098.