Malaysian Journal of Analytical Sciences Vol 23 No 4 (2019): 572 - 579

# AN OPTICAL SENSOR BASED ON GRAPHENE QUANTUM DOTS FOR HYDROGEN PEROXIDE DETECTION

(Sensor Optik berasaskan Titik Kuantum Grafin untuk Pengesanan Hidrogen Peroksida)

Amiruddin Ashil Mastar1, Jaafar Abdullah1,2*, Nor Azah Yusof1,2, Yap Wing Fen1,3

1Department of Chemistry

2Institute of Advanced Technology

3Department of Physic, Faculty of Science

Universiti Putra Malaysia, 43400 UPM Serdang, Selangor, Malaysia

*Corresponding author:  jafar@upm.edu.my

Received: 19 August 2018; Accepted: 8 July 2019

Abstract

Graphene quantum dots (GQDs) is a zero-dimensional material of the carbon family and considered as a small cutting fragment from graphene sheet. It has unique electronic and optical properties due to electron confinement in the finite size of graphene cluster that leads to the opening of energy gap and quantization of electronic energy. In this study, biosensing based on GQDs in combination with enzyme (horseradish peroxidase, HRP) for the determination of hydrogen peroxide (H2O2) has been presented. The GQDs was used as an indicator reveals the fluorescence property of the system based on fluorescence quenching of GQDs which is induced from the enzymatic reaction. The presence of H2O2 quenches the fluorescence intensity of GQDs system which is proportional to the concentration of H2O2. Parameters optimization such as response time, enzyme concentrations, pH of buffer have been investigated. For linear calibration graph, it showed a linear dependence on the H2O2 concentration ranging from 1.0 to 100.0 μM with the detection limit of 1.0 μM.

Keywords:  quantum dots, fluorescence, hydrogen peroxide, quenching, sensor

Abstrak

Titik kuantum grafin (GQDs) adalah bahan dimensi-sifar keluarga karbon dan dianggap sebagai serpihan kecil dari lembaran grafin. Ia mempunyai ciri-ciri elektronik dan optik yang unik disebabkan oleh pengasingan elektron dalam saiz finit kelas grafin yang membawa kepada pembukaan jurang tenaga dan pengkuantuman tenaga elektronik. Dalam kajian ini, biopenderiaan berasaskan GQDs digabungkan dengan enzim (peroksidase horseradish, HRP) untuk penentuan hidrogen peroksida (H2O2) telah dibentangkan. GQDs digunakan sebagai penunjuk mempamerkan sifat pendarfluor sistem berasaskan pendarfluor pelindapkejutan GQD yang diaruhkan dari tindak balas enzim. Kehadiran H2O2 mengurangkan keamatan pendarfluor sistem GQD yang berkadaran dengan kepekatan H2O2. Pengoptimuman parameter seperti masa tindak balas, kepekatan enzim, pH penimbal telah dikaji. Bagi graf penentukuran linear, ia menunjukkan kebergantungan kelinearan terhadap kepekatan H2O2 di antara 1.0 hingga 100.0 μM dengan had pengesanan 1.0 μM.

Katakunci: titik kuantum, pendarfluor, hidrogen peroksida, pelindapkejutan, sensor

References

- Azmi, N. E., Ramli, N. I., Abdullah, J., Abdul Hamid, M. A., Sidek, H., Abd Rahman, S. and Yusof, N. A. (2015). A simple and sensitive fluorescence based biosensor for the determination of uric acid using H2O2-sensitive quantum dots/dual enzymes. Biosensors and Bioelectronics, 67: 129-133.

- Dong, C., Qian, H., Fang, N. and Ren, J. (2006). Study of fluorescence quenching and dialysis process of CdTe quantum dots, using ensemble techniques and fluorescence correlation spectroscopy. Journal of Physical Chemistry B, 110(23):11069-11075.

- He, S., Song, B., Li, D., Zhu, C., Qi, W., Wen, Y. and Fan, C. (2010). A graphene nanoprobe for rapid, sensitive, and multicolor fluorescent DNA analysis. Advanced Functional Materials, 20(3): 453-459.

- Ji, X., Zheng, J., Xu, J., Rastogi, V. K., Cheng, T. C., DeFrank, J. J. and Leblanc, R. M. (2005). (CdSe)ZnS quantum dots and organophosphorus hydrolase bioconjugate as biosensors for detection of paraoxon. Journal of Physical Chemistry B, 109(9): 3793-3799.

- Kim, K. E., Kim, T. G. and Sung, Y. M. (2012). Fluorescent cholesterol sensing using enzyme-modified CdSe/ZnS quantum dots. Journal of Nanoparticle Research, 14(1179): 1-9.

- Lu, C.-H., Yang, H.-H., Zhu, C.-L., Chen, X. and Chen, G.-N. (2009). A graphene platform for sensing biomolecules. Angewandte Chemie, 48(26): 4785-4787

- Ponomarenko, L. A., Schedin, F., Katsnelson, M. I., Yang, R., Hill, E. W., Novoselov, K. S. and Geim, A. K. (2008). Chaotic dirac billiard in graphene quantum dots. Science, 320(5874): 356-358.

- Razmi, H. and Mohammad-Rezaei, R. (2013). Graphene quantum dots as a new substrate for immobilization and direct electrochemistry of glucose oxidase: Application to sensitive glucose determination. Biosensors and Bioelectronics 41: 498-504.

- Shen, J., Zhu, Y., Yang, X., Zong, J., Zhang, J. and Li, C. (2012). One-pot hydrothermal synthesis of graphene quantum dots surface-passivated by polyethylene glycol and their photoelectric conversion under near-infrared light. New Journal of Chemistry 36: 97-101.

- Tang, J. and Marcus, R. A. (2006). Determination of energetics and kinetics from single-particle intermittency and ensemble-averaged fluorescence intensity decay of quantum dots. The Journal of Chemical Physics, 125 (044703): 1-8.

- Tetsuka, H., Asahi, R., Nagoya, A., Okamoto, K., Tajima, I., Ohta, R. and Okamoto, A. (2012). Optically tunable amino-functionalized graphene quantum dots. Advanced Materials, 24(39): 5333-5338.

- Wang, D., Wang, L., Dong, X., Shi, Z. and Jin, J. (2012). Chemically tailoring graphene oxides into fluorescent nanosheets for Fe3+ion detection. Carbon, 50(6): 2147-2154.

- Xie, R., Wang, Z., Zhou, W., Liu, Y., Fan, L., Li, Y. and Li, X. (2016). Graphene quantum dots as smart probes for biosensing. Analytical Methods, 8(20): 4001–4016.

- Zhuo, S., Shao, M. and Lee, S. T. (2012). Upconversion and downconversion fluorescent graphene quantum dots. Ultrasonic preparation and photocatalysis. ACS Nano, 6(2): 1059-1064.