Malaysian Journal of Analytical Sciences Vol 23 No 6 (2019): 914 - 925

# ANTIBACTERIAL PROPERTIES OF CHITOSAN EDIBLE FILMS INCORPORATED WITH MUSK LIME EXTRACTS FOR THE PRESERVATION OF SQUIDS

# (Sifat Antibakteria Filem Kitosan Boleh Dimakan Yang Ditambah Dengan Ekstrak

# Limau Kasturi Bagi Pengawetan Sotong)

# Choong Kah Wai1, Tee Yee Bond2, Nyam Kar Lin1, Pui Liew Phing1*

# 1Department of Food Science and Nutrition, Faculty of Applied Sciences,

# UCSI University, 56000 Cheras, Kuala Lumpur, Malaysia

# 2Centre for Pre-University Studies,

# Stella Maris International School,

# Lorong Setiabistari 2, Medan Damansara, 50490 Kuala Lumpur, Malaysia.

# *Corresponding author:  puilp@ucsiuniversity.edu.my

Received: 30 May 2019; Accepted: 3 November 2019

Abstract

# The chitosan (CH) films incorporated with different concentrations (1% to 5%) of musk lime extracts (MLE) were investigated for physical, mechanical, chemical, and antibacterial properties. Storage test on squids’ shelf-life was also conducted. The addition of MLE into CH film had increased the inhibition zones against gram-negative bacteria, Pseudomonas aeruginosa and Vibrio parahaemolyticus. It also reduced the moisture content, water solubility, tensile strength and elongation at break. Films with higher concentration of MLE had higher intensity in opacity and appeared more greenish. From the Fourier transforms infrared (FTIR) spectra, the addition of 4% and 5% of MLE in CH films shifted the -CH3 stretching at peak 2921 cm-1 and the signal of the hydrophilic representative zones (-OH and –NH stretch, amide II and carboxyl group) were slightly reduced at 3200 cm-1, 1570 cm-1 and 1400 cm-1, respectively. The FTIR results did not suggest any cross-linkage between the MLE and CH. At 4 °C storage condition, wrapping the squids with MLE incorporated films had prolonged their shelf-life from 5 days to 15 days compared to wrapping with neat CH film.

# Keywords:  edible film, shelf-life, antibacterial properties, chitosan, musk lime

# Abstrak

# Filem kitosan (CH) yang ditambah dengan ekstrak limau kasturi (MLE) dalam kepekatan yang berbeza (1% hingga 5%) telah disiasat untuk sifat fizikal, mekanikal, kimia, dan antibakteria. Ujian hayat makanan ke atas sotong juga dijalankan. Penambahan MLE ke dalam filem CH telah meningkatkan zon perencatan terhadap bakteria gram-negatif, Pseudomonas aeruginosa dan Vibrio parahaemolyticus. Ia juga mengurangkan kandungan kelembapan, keterlarutan air, kekuatan tegangan dan pemanjangan. Filem dengan kepekatan MLE yang lebih tinggi mempunyai intensiti yang lebih tinggi dalam kelegapan dan kelihatan lebih hijau. Spektrum inframerah transformasi Fourier (FTIR) menunjukan bahawa penambahan 4% dan 5% MLE menyebabkan peralihan regangan -CH3 di puncak 2921 cm-1 dan isyarat wakil zon hidrofilik (-OH dan -NH, amida II dan kumpulan karboksil) dikurangkan sedikit masing-masing pada 3200 cm-1, 1570 cm-1 dan 1400 cm-1. Keputusan FTIR tidak menunjukkan sebarang hubungan silang antara MLE dan CH. Pada suhu penyimpanan 4 °C, pembungkusan sotong dengan  filem yang ditambah dengan MLE didapati menambah jangka hayat sotong dari 5 hari kepada 15 hari, jika dibandingan dengan filem CH yang dibalut dengan kemas.

Kata kunci:  filem yang boleh dimakan,  jangka hayat, sifat antibakteria, kitosan, limau kasturi

References

- Robertson, G. L. (2005). Food packaging: principles and practice. CRC press.

- Giatrakou, V. I. and Savvaidis, I. N. (2012). Bioactive packaging technologies with chitosan as a natural preservative agent for extended shelf-life food products. In Modified atmosphere and active packaging technologies. CRC Press, Florida: pp. 708-753.

- Jouki, M., Yazdi, F. T., Mortazavi, S. A., Koocheki, A. and Khazaei, N. (2014). Effect of quince seed mucilage edible films incorporated with oregano or thyme essential oil on shelf life extension of refrigerated rainbow trout fillets. International Journal of Food Microbiology, 174: 88 - 97.

- Restuccia, D., Spizzirri, U. G., Parisi, O. I., Cirillo, G., Curcio, M., Iemma, F., Puoci, F., Vinci, G. and Picci, N. (2010). New EU regulation aspects and global market of active and intelligent packaging for food industry applications. Food Control, 21(11): 1425 - 1435.

- Embuscado, M. E. and Huber, K. C. (2008). Edible films and coatings: Why, what, and how. Springer, New York:  pp.1 - 25.

- Saremnezhad, S., Azizi, M. H., Barzegar, M., Abbasi, S. and Ahmadi, E. (2011). Properties of a new edible film made of faba bean protein isolate. Journal of Agricultural Science and Technology, 13(2): 181 - 192.

- Mastromatteo, M., Danza, A., Conte, A., Muratore, G. and Del Nobile, M. A. (2010). Shelf life of ready to use peeled shrimps as affected by thymol essential oil and modified atmosphere packaging. International Journal of Food Microbiology, 144(2): 250 - 256.

- Remya, S., Mohan, C. O., Bindu, J., Sivaraman, G. K., Venkateshwarlu, G. and Ravishankar, C. N. (2016). Effect of chitosan based active packaging film on the keeping quality of chilled stored barracuda fish. Journal of Food Science and Technology, 53(1): 685 - 693.

- Quintavalla, S. and Vicini, L. (2002). Antimicrobial food packaging in meat industry. Meat Science, 62(3): 373 - 380.

- Muppalla, S. R., Kanatt, S. R., Chawla, S. P. and Sharma, A. (2014). Carboxymethyl cellulose–polyvinyl alcohol films with clove oil for active packaging of ground chicken meat. Food Packaging and Shelf Life, 2(2): 51 - 58.

- Emiroğlu, Z. K., Yemiş, G. P., Coşkun, B. K. and Candoğan, K. (2010). Antimicrobial activity of soy edible films incorporated with thyme and oregano essential oils on fresh ground beef patties. Meat Science, 86 (2): 283 - 288.

- Lim, T. K. (2012). Citrus x microcarpa. Springer, Netherlands: pp. 865 - 870.

- Beh, L. K., Zakaria, Z., Beh, B. K., Ho, W. Y., Yeap, S. K. and Alitheen, N. B. M. (2012). Comparison of total phenolic content and antioxidant activities of freeze-dried commercial and fresh fruit juices. Journal of Medicinal Plants Research, 6(48): 5857 - 5862.

- Chen, H. C., Peng, L. W., Sheu, M. J., Lin, L. Y., Chiang, H. M., Wu, C. T., Wu, C.S. and Chen, Y. C. (2013). Effects of hot water treatment on the essential oils of calamondin. Journal of Food and Drug Analysis, 21(4): 363 - 368.

- Manaf, Y. N., Osman, A., Lai, O. M., Long, K. and Ghazali, H. M. (2008). Characterisation of musk lime (Citrusmicrocarpa) seed oil. Journal of the Science of Food and Agriculture, 88(4): 676 - 683.

- Paarup, T., Sanchez, J. A., Moral, A., Christensen, H., Bisgaard, M. and Gram, L. (2002). Sensory, chemical and bacteriological changes during storage of iced squid (Todaropsis eblanae). Journal of Applied Microbiology, 92(5): 941 - 950.

- Lapa-Guimarães, J., de Felício, P. E. and Guzmán, E. S. C. (2005). Chemical and microbial analyses of squid muscle (Loligo Plei) during storage in ice. Food Chemistry, 91(3): 477 - 483.

- Vaz-Pires, P., Seixas, P., Mota, M., Lapa-Guimarães, J., Pickova, J., Lindo, A. and Silva, T. (2008). Sensory, microbiological, physical and chemical properties of cuttlefish (Sepia Officinalis) and broadtail shortfin squid (Illex coindetii) stored in ice. LWT-Food Science and Technology, 41(9): 1655 - 1664.

- Weerakkody, N. S., Caffin, N., Turner, M. S. and Dykes, G. A. (2010). In vitro antimicrobial activity of less-utilized spice and herb extracts against selected food-borne bacteria. Food Control, 21(10): 1408 - 1414.

- Association of Analytical Chemists (1995). Official methods of analysis of AOAC international.

- Zaman, N. B. K., Lin, N. K. and Phing, P. L. (2018). Chitosan film incorporated with Garcinia Atroviridis for the packaging of indian mackerel (Rastrelliger kanagurta). Ciência e Agrotecnologia, 42(6): 666 - 675.

- Hoque, M. S., Benjakul, S. and Prodpran, T. (2011). Properties of film from cuttlefish (Sepia pharaonis) skin gelatin incorporated with cinnamon, clove and star anise extracts. Food Hydrocolloids, 25(5): 1085 - 1097.

- Velu, S., Abu Bakar, F., Mahyudin, N. A., Saari, N. and Zaman, M. Z. (2014). In vitro antimicrobial activity of musk lime, key lime and lemon extracts against food related pathogenic and spoilage bacteria. International Food Research Journal, 21(1): 379 - 386.

- Kumar, V., Sukumar, D. and Muruganantham, M. (2015). Microbial quality of frozen squid (Sepioteuthis lessoniana, Lesson 1830) treated with food grade commercial chemicals. Indian Journal of Animal Research, 49(5): 736 - 741.

- Tantasuttikul, A., Kijroongrojana, K. and Benjakul, S. (2011). Quality indices of squid (Photololigo duvaucelii) and cuttlefish (Sepia aculeata) stored in ice. Journal of Aquatic Food Product Technology, 20 (2): 129 - 147.

- Siripatrawan, U. and Harte, B. R. (2010). Physical properties and antioxidant activity of an active film from chitosan incorporated with green tea extract. Food Hydrocolloids, 24(8): 770 - 775.

- Rubilar, J. F., Cruz, R. M., Silva, H. D., Vicente, A. A., Khmelinskii, I. and Vieira, M. C. (2013). Physico-mechanical properties of chitosan films with carvacrol and grape seed extract. Journal of Food Engineering, 115(4): 466 - 474.

- Cano, A., Cháfer, M., Chiralt, A. and González-Martínez, C. (2016). Physical and antimicrobial properties of starch-PVA blend films as affected by the incorporation of natural antimicrobial agents. Foods, 5 (1): 3.

- Ojagh, S. M., Rezaei, M., Razavi, S. H. and Hosseini, S. M. H. (2010). Effect of chitosan coatings enriched with cinnamon oil on the quality of refrigerated rainbow trout. Food Chemistry, 120(1): 193 - 198.

- Gómez-Guillén, M. C., Ihl, M., Bifani, V., Silva, A. M. D. O. E. and Montero, P. (2007). Edible films made from tuna-fish gelatin with antioxidant extracts of two different murta ecotypes leaves (Ugni molinae Turcz). Food Hydrocolloids, 21(7): 1133 - 1143.

- Asif, M. (2014). Brief information related to potential therapeutic tendencies of citrus plants. International Journal of Biological Research, 2(2): 116 - 120.

- Hosseini, M. H., Razavi, S. H. and Mousavi, M. A. (2009). Antimicrobial, physical and mechanical properties of chitosan‐based films incorporated with thyme, clove and cinnamon essential oils. Journal of Food Processing and Preservation, 33(6): 727 - 743.

- Bourtoom, T. (2008). Edible films and coatings: characteristics and properties. International Food Research Journal, 15(3): 237 - 248.

- Pelissari, F. M., Grossmann, M. V., Yamashita, F. and Pineda, E. A. G. (2009). Antimicrobial, mechanical, and barrier properties of cassava starch− chitosan films incorporated with oregano essential oil. Journal of Agricultural and Food Chemistry, 57(16): 7499 - 7504.

- Pranoto, Y., Rakshit, S. K. and Salokhe, V. M. (2005). Enhancing antimicrobial activity of chitosan films by incorporating garlic oil, potassium sorbate and nisin. LWT-Food Science and Technology, 38(8): 859 - 865.

- Xuan, X. T., Fan, Y. F., Ling, J. G., Hu, Y. Q., Liu, D. H., Chen, S. G., Ye, X.Q. and Ding, T. (2017). Preservation of squid by slightly acidic electrolyzed water ice. Food Control, 73: 1483 - 1489.

- Xu, Y. X., Kim, K. M., Hanna, M. A. and Nag, D. (2005). Chitosan–starch composite film: Preparation and characterization. Industrial Crops and Products, 21(2): 185 - 192.

- Tongnuanchan, P., Benjakul, S. and Prodpran, T. (2012). Properties and antioxidant activity of fish skin gelatin film incorporated with citrus essential oils. Food Chemistry, 134(3): 1571 - 1579.

- Yuan, G., Lv, H., Yang, B., Chen, X. and Sun, H. (2015). Physical properties, antioxidant and antimicrobial activity of chitosan films containing carvacrol and pomegranate peel extract. Molecules, 20(6): 11034 - 11045.

- Allwin, S. J., Jeyasanta, K. I. and Patterson, J. (2015). Extraction of chitosan from white shrimp (Litopenaeus vannamei) processing waste and examination of its bioactive potentials. Advances in Biological Research, 9(6): 389 - 396.

- Chaiyakosa, S., Charernjiratragul, W., Umsakul, K. and Vuddhakul, V. (2007). Comparing the efficiency of chitosan with chlorine for reducing Vibrio parahaemolyticus in Shrimp. Food control, 18(9): 1031 - 1035.

- Kirbaşlar, F. G., Tavman, A., Dülger, B. and Türker, G. (2009). Antimicrobial activity of turkish citrus peel oils. Pakistan Journal of Botany, 41(6): 3207-3212.

- Musa, N., Wei, L. S., Seng, C. T., Wee, W. and Leong, L. K. (2008). Potential of edible plants as remedies of systemic bacterial disease infection in cultured fish. Global Journal of Pharmacology, 2(2): 31 - 36.

- Wang, Y. C., Chuang, Y. C. and Hsu, H. W. (2008). The flavonoid, carotenoid and pectin content in peels of citrus cultivated in Taiwan. Food Chemistry, 106(1): 277 - 284.

- Vandeputte, O. M., Kiendrebeogo, M., Rasamiravaka, T., Stevigny, C., Duez, P., Rajaonson, S., Diallo, B., Mol, A., Baucher, M. and El Jaziri, M. (2011). The flavanone naringenin reduces the production of quorum sensing-controlled virulence factors in Pseudomonas aeruginosa PAO1. Microbiology, 157(7): 2120 - 2132.

- Márquez‐Ríos, E., Morán‐Palacio, E. F., Lugo‐Sánchez, M. E., Ocano‐Higuera, V. M. and Pacheco‐Aguilar, R. (2007). Postmortem biochemical behavior of giant squid (Dosidicus gigas) mantle muscle stored in ice and its relation with quality parameters. Journal of Food Science, 72(7): 356 - 362.

- Wang, J. J., Lin, T., Li, J. B., Liao, C., Pan, Y. J. and Zhao, Y. (2014). Effect of acidic electrolyzed water ice on quality of shrimp in dark condition. Food Control, 35(1): 207 - 212.

- Tomac, A. and Yeannes, M. I. (2012). Gamma radiation effect on quality changes in vacuum‐packed squid (Illex argentinus) mantle rings during refrigerated (4 - 5° C) storage. International Journal of Food Science and Technology, 47(7): 1550 -1557.

- Zaragozá, P., Fuentes, A., Ruiz-Rico, M., Vivancos, J. L., Fernández-Segovia, I., Ros-Lis, J. V., Barat, J.M. and Martínez-Máñez, R. (2015). Development of a colorimetric sensor array for squid spoilage assessment. Food Chemistry, 175: 315 - 321.