# SYNTHESIS AND CHARACTERIZATION OF CATALYTIC POLYMER- CLAY FILM FOR TREATMENT OF 17α-ETHINYLESTRADIOL

# (Sintesis dan Pencirian Filem Polimer-Tanah Liat dengan Pemangkin untuk Rawatan

# 17α-Etinilestradiol)

# Nur Khairunnisa Nazri, Nabilah Ismail1*, Mohd Aidil Adhha Abdullah1, Fatimah Hashim1, Leonard James Wright2

# 1Faculty of Science and Marine Environment,

# Universiti Malaysia Terengganu, 21030 Kuala Nerus, Terengganu, Malaysia

2Centre of Green Chemical Sciences,

University of Auckland, 23 Symonds St, Private Bag 92019, Auckland, New Zealand

*Corresponding author:  nabilah.i@umt.edu.my

Received: 20 November 2019; Accepted: 5 April 2020; Published:  9 June 2020

Abstract

# Synthetic estrogen such as 17α-ethinylestradiol (EE2) is considered as one of the pharmaceuticals found in waterways worldwide usually due to human utilization and excretion into wastewater treatment system. In this study, catalytic polymer-clay film was used to treat EE2 in the contaminated water by oxidizing the pollutant. Polychloromethylstyrene was synthesized along with the clay cloisite to form films that can anchor catalyst Iron-tetra amido microcylic ligand (Fe-TAML). Fe-TAML works efficiently with hydrogen peroxide to activate the iron to higher oxidation state for a film performance. Polymer-clay was then casted, cured, cross-linked and functionalized to form a film that can bind the catalyst into it. Characterization of the films was done using Fourier Transform Infrared (FTIR) to determine the presence of the functional group; preliminary analysis of oxidation study was carried out using UV-Vis Spectroscopy. Furthermore, the toxicity of the oxidized solution of EE2 after undergoing oxidation with catalytic polymer-clay film was investigated using Acanthamoeba sp. to determine its toxicity towards the environment. The results of preliminary oxidation study showed the performance of film in oxidizing the contaminant and the result of toxicity study using MTT assay shows more than 70% of viability of Acanthamoeba sp. which indicated that the film was less toxic towards the environment. Hence, this film has high potential for solving the problems of contaminated water.

# Keywords:  ethinylestradiol, polychloromethylstyrene, Fe-TAML, cloisite, catalytic polymer-clay

# Abstrak

Estrogen sintetik yang dikenali sebagai 17α-etinilestradiol (EE2) adalah salah satu farmaseutikal yang terdapat dalam saluran air di seluruh dunia kebiasaannya disebabkan penggunaan oleh manusia dan perkumuhan ke dalam sistem rawatan air sisa. Dalam kajian ini, filem polimer-tanah liat pemangkin digunakan untuk merawat EE2 dalam air yang tercemar dengan menumpukan bahan pencemar dan mengoksida bahan tersebut. Poliklorometilsterina di sintesis bersama dengan tanah liat cloisite untuk membentuk filem-filem yang boleh melekatkan pemangkin ferum ligan tetra amido mikrosiklik (Fe-TAML). Fe-TAML berfungsi cekap dengan hidrogen peroksida untuk mengaktifkan ferum kepada keadaan pengoksidaan yang lebih tinggi untuk prestasi filem. Polimer-tanah liat kemudian diacuankan, dirawat, disilangkan dan difungsikan untuk membentuk sebuah filem yang boleh mengikat pemangkin kepadanya. Pencirian filem dilakukan dengan menggunakan spektroskopi inframerah transformasi Fourier (FTIR) untuk menentukan kehadiran  kumpulan berfungsi. Tambahan lagi, kajian ketoksikan EE2 yang teroksida setelah menjalani pengoksidaan dengan filem polimer-tanah liat pemangkin telah disiasat menggunakan Acanthamoeba sp. untuk menentukan ketoksikannya terhadap alam sekitar. Hasil kajian ketoksikan menggunakan pengujian MTT menunjukkan lebih dari 70% ia bertahan dan menujukkan filem tersebut kurang toksik terhadap alam sekitar. Oleh itu, filem ini mempunyai potensi yang tinggi untuk menyelesaikan masalah berkaitan air tercemar.

Kata kunci:  ethinillestradiol, poliklorometilsterina, Fe-TAML, cloisite, pemangkin polimer-tanah liat

Introduction

Ethinylestradiol (EE2), an artificial estrogen in oral contraceptives, can be found in inland waterways worldwide [1]. It mainly emerges in wastewater treatment system from human excretion [2] such as urine and through the disposal of wastes including pregnancy test [3-5]. To prevent pregnancy and stabilize menstrual cycle, most women use oral contraceptive. This is known as a huge contributor to synthetic EE2 in the environment [6]. Based on several studies, human estrogens namely estradiol (E2) and estrone (E1) as well as the artificial estrogen (EE2) are responsible for a significant part of the endocrine disrupting effects seen in the aquatic environment [7-9]. Compounds that adjust the endocrine system and because harmful effects are referred to as endocrine disrupting chemicals (EDCs) [10]. When EDCs pollute the aquatic environment, they will potentially disturb the endocrine system of animals by altering the natural balance of hormones [11]. EE2 seems to be more harmful as it has a longer half-life compared to other natural estrogen [12]. Moreover, EE2 has the possibility to accumulate in biota and sediment [13] where it has been shown that it is endocranially active [14]. The exposure effects of EE2 in wastewater treatment bring the feminization of male fish based on most research [15]. As stated by Jobling et al. [16] and Harris et al. [17], EE2 can reduce the reproductive success, leading to the feminization of wild male fish [18].

The method of using hydrogen peroxide with the presence of tetra amido microcyclic ligand (TAML) catalyst is one of the environmentally friendly, money saving and very effective way to help us overcome the unsuitable method of using ozone or activated carbon method to remove pharmaceutical ingredient from wastewater. Iron TAML are fully-functional, small molecule that imitate of peroxidase enzymes at nanomolar concentrations can decompose many micro pollutants. For example, in laboratory studies, TAML/peroxide has been shown to efficiently degrade the persistent drug sertraline via its oxidative metabolites [19], the recalcitrant pesticides trichlorophenol and pentachlorophenol [20], thiophosphate pesticides and many other micro pollutants [21]. TAML/peroxide has been reported to degrade a lot of pharmaceutical based on the preliminary studies on United Kingdom municipal wastewater [2].

The contraceptive pill hormone EE2 causes serious impacts on aquatic life [22]; therefore, this study investigates the effectiveness of TAML/peroxide and polymer-clay in removing EE2 and its biological effects. Preliminary studies at high pH (8-10) and high concentrations of hydrogen peroxide (4 mM, 136 ppm) indicate that the removal of EE2 and other estrogens (estradiol (E2), estrone (E1) all at 80 μM) with TAML (83 nM) is possible [23]. In addition, in vivo toxicity tests using embryonic zebrafish suggest that TAML was not overtly toxic to fish [24] while in vitro tests also showed that TAML did not show inherent endocrine disrupting activity [25].

Taken together, these studies set the stage for the current multidisciplinary, cross-sector study to investigate the removal of EE2 from laboratory waters and real wastewater, under more environmentally appropriate conditions. These include neutral pH, lower hydrogen peroxide concentrations and estrogen concentrations of more than a million-fold lower than previously tested, which are much more environmentally relevant and still ecotoxic to fish [2].

Organic-inorganic composite-based materials known as clay minerals have been widely used for water purification for decades. They have many

characteristics such as high surface area, easily to adsorb and unique chemical composition besides being small in size (nano). However, to make the clay effective in removing the micro pollutant from water, the developments of clay-polymer nanocomposite film have been introduced. The modified polymer or known as Cloisite has been use in this study. Cloisite 10A contains dimethyl, benzyl, hydrogenated tallow and quaternary ammonium and is used with polychloromethylstyrene. Several studies have reported enhanced performance and characteristic of polymeric films by adding clay-based nanomaterials into the film matrix [26-29]. The blending of polymer with clay improved the characteristic in term of optical [30-32], mechanical [33, 34] and barrier properties [35-37].

From this study, polymerization of chloromethyl styrene was used together with clay Cloisite 10A to treat the estrogen known as EE2. Catalyst Fe-TAML/H2O2 helps in the process of heterogeneous catalytic oxidation reaction. In addition, the toxicity studies using MTT assay have been conducted.

# Materials and Methods

4-vinylbenzyl chloride was purchase from Sigma Aldrich. N, N-dimethylhexadecylamine, 1,4-dioxane, 1,6-diaminohexane, diethanolamine, dimethyl-formamide and 17α-ethinylestradiol were purchased from Sigma Aldrich. Buffer solution were prepared by using sodium carbonate, sodium bicarbonate and 35% hydrogen peroxide from Merck.

# Polymerization of chloromethylstyrene with clay

# 30 mL of 0.5% NaOH was added to 30 mL chloromethylstyrene (CMS) in separating funnel to remove inhibitor from chloromethylstyrene. This step was repeated for another two times. After that, the CMS were washed by using deionized water for three times until the water turned neutral. This step was followed by adding potassium carbonate to remove excess water. An amount 4% (w/v) of cloisite clay from the volume of CMS were added into flat bottom flask containing CMS and was heated in an oil bath with temperature of under 85 oC with stirring speed of 150 rpm in nitrogen condition. The CMS was heated until completely viscous. After viscous, methyl ethyl ketone was dropped in the viscous solution and the mixture was dropped added slowly to the volume of 20 mL in the beaker that contained methanol to obtain the polymer flakes. The flakes were then filtered using Buchner funnel and dried for 10 minutes in the oven.

Casting, curing and functionalization of polymer clay film

# The flakes were dissolved in the dimethylformamide (DMF) and casted on the backing membrane (polypropylene) to obtain the film. After casted on the membrane and glass, the film was cured for 5 hours at the oven at 85 oC. Next, the film was heated for 5 hours at 85 oC in N, N-dimethylhexadecylamine in 1,4-dioxane with a ratio of (6:4). After functionalization, the polymer film was heated in 1,6-diaminohexane in 1,4-dioxane with ratio (6:4) for crosslinking the polymer. End capping step involved heating the polymer film with neat diethanolamine for 5 hours at 85 oC.

Anchoring of Fe-TAML

# The film was immersed in the aqueous Fe-TAML solution (20.0 mL, 50 μM, 1.0 μmole Fe-TAML) until all the absorbed. After that, the film was removed from the solution, washed and immersed on a wire support in fresh carbonate buffer solution (20.0 mL 0.01 M, pH 9.5) and stirred for 15 to 20 minutes. The procedure was repeated for three times. The measurement of amount of Fe-TAML that was not adsorbed from the original solution of Fe-TAML and the amounts that leached into solution after immersion in the buffer solution was measured. To measure this, dye orange II together with hydrogen peroxide were catalyzed by small amount of Fe-TAML and used as a standard condition.

Characterization using attenuated total reflectance-Fourier-transform infrared and scanning electron microscope

ATR-FTIR spectra of the samples were analyzed on a Nicolet 380 FT-IR. The samples were put on the stage to analyzed their functional group. Further, SEM JEOL JSM-5800 was used to analyze the morphology of the film’s surface.

Oxidation of EE2 using catalyzed polymer-clay film

The oxidation of EE2 was done in a beaker containing carbonate/bicarbonate buffer solution (8.5 mL, 0.01 M, pH 9.5). The EE2 solution (11.4 mL, 11.83 µM) was added followed by H2O2 solution (0.1 mL, 0.2 M) and buffer solution was added until the total volume of the solution became 20 mL. The solution was stirred at 750 rpm and the film was added to the solution. The ratio of H2O2:EE2:Fe-TAML was 200: 1.35: 40.5, while the resulting concentration for EE2 was 2 ppm (6.76 µM), H2O2 (1.0 mM). After 30 minutes, the film was removed, and 1 mg catalase was added to the solution to destroy the H2O2 and stirred for another 30 minutes. Peroxide test strip was used to confirm that all H2O2 has been destroyed. The solution was then passed through the hydrophilic-lipophilic cartridge from Waters Corporation. The solution was collected for the MTT assay study.

MTT (2 3-[4,5-dimethylthiazol-2-yl]-2,5 diphenyl tetrazolium bromide) assay of oxidize solution on Acanthamoeba sp.

Acanthamoeba sp. (environmental isolate) used in the experiment was isolated from Setiu Wetlands, Terengganu and used in this experiment. The trophozoites were maintained in axenic conditions in 4% protease-yeast-glucose medium and were subculture for a week. MTT assay by Mossman [38] was used in this study to determine the toxicity of oxidized solution by catalytic polymer-clay film on Acanthamoeba sp. The first step was subculturing the cell in new flask for 4 days. After 4 days, the cells were ready to be used for the experiment. To start the experiment, all cells and media were transferred to centrifuge tube to sediment the cell. After centrifugation for 15 minutes, the media was removed and replaced with new media. The cell and media contained in the centrifuge tube were transferred in a 96-well plate, a process called cell seeding. After that, the 96-well plate was kept in the oven at 30 oC for 24 hours. After 24 hours, the treatment process was done. The media were removed, while oxidized solutions with different concentrations were put in the 96-well plate. There were five replicates with seven concentrations. This process was carried out for 24 hours. After that, the solutions were removed and rinsed with PBS solution. MTT was transferred into the 96-well plate and after 4 hours, MTT was suspended while DMSO was dropped into the 96-well plate. The readings of viability of the cell were analyzed by micro plate reader instrument.

Results and Discussion

Fourier-transform infrared analysis

The FTIR spectrum of polymer-clay film the characteristic absorption peaks due to stretching vibration of C–H in the region 3000-2850 cm-1 region which showed alkane functional group, whereas the band around 1645 cm-1 was due to stretching vibration of C–C stretch for alkane (Figure 1). The band around 1463 cm-1 showed the stretching vibration of C–C in ring or known as aromatic, 1043 cm-1 band was due to C–N stretching of functional group aliphatic amine and 808 cm-1 band was due to C–Cl stretching vibration and functional group of alkyl halide. These bands showed the stretching from the polychloromethylstyrene-clay films that were functionalized with N, N-dimethylhexadecylamine and 1,4-dioxane, 1,6-diaminohexane with 1,4-dioxane and neat diethanolamine.

Scanning electron microscope

SEM was used to investigate the surface morphology of prepared sample. The polychloromethylstyrene was synthesized with clay Cloisite 10A and casted. The image of SEM (Figure 2) showed that the film has no hole after casting and functionalization which can anchor any catalyst into it for further use. Polymer-clay film was treated with a long chain tertiary amine which reacts with chloromethyl groups converting them into quaternary ammonium functions and followed by crosslinking the polymer chain; end capping the remaining unreacted chloromethyl group. Therefore, Fe-TAML can be anchor to the film.

Viscosity of polymer-clay

Viscosity is the internal friction of a fluid to resist flow. Meanwhile, shear stress is stress component applied tangentially and commonly recognized by sigma (σ) symbol. It is equal to the force vector (a vector has magnitude and direction) divided by the area of application and is expressed in the unit of force per unit

area (Pa). Shear rate is the velocity gradient established in a fluid as a result of an applied shear stress and expressed in unit of reciprocal seconds, s-1. Viscosity can be calculated as shear stress over shear rate. Based on the Figure 3, the shear stress increased as the shear rate increase. The viscosity of different polymers is

inconsistent and gives different results. Therefore, to ensure that we can produce the same viscosity of the film, this result can be referred.

Viscosity=Shear StressShear Rate		            (1)

Toxicity studies using MTT assay

MTT assay was conducted for studying the toxicity of the oxidize solution that was treated by the catalytic polymer-clay film. After the cells were treated with oxidized solution at varying concentrations for 24 hours at 30 oC in a 96-well plate, the medium in the plate was discarded. The plate was washed with PBS solution 3 times before loading the MTT solution. This was to ensure that the glucose content in the medium has been completely removed. The presence of glucose in the medium will reduce the efficiency of MTT reaction. MTT specific activity can be reduced by cells that extensively metabolized D-glucose. Cytotoxicity of oxidized solution on Acanthamoeba sp. was determined based on the percentage of viable Acanthamoeba sp. after exposure to oxidized solution for 24 hours at 30 oC. In general, the viability of Acanthamoeba sp. decreased with increasing concentrations of oxidized solution. This shows that the growth of the cells was affected once exposed to oxidized solution. However, the percentage of viability of Acanthamoeba sp. as illustrated in Figure 4 showed that more than 70%. This means that the oxidize solution was not highly toxic to the cell and environment.

Figure 1.  FTIR Spectrum of Polymer-Clay Films after functionalization

Figure 2.  SEM image of functionalized polymer-clay film

Figure 3.  Shear rate against shear stress graph

Figure 4.  Graph of percentage of viability of Acanthamoeba sp. from MTT assay

Conclusion

# The catalytic polymer-clay employed in this work in treating 17α-Ethinylestradiol has been successful. Characterization of the catalytic polymer-clay shows that the film contains functional group that helps the catalyst to oxidize EE2. The results have showed that the production of film does not give harmful effects towards the environment based on the result of toxicity study obtained. Therefore, EE2 can be treated using polymer and clay in the presence of catalyst.

# Acknowledgement

# The authors would like to acknowledge the Ministry of Education Malaysia for Fundamental Research Grant Scheme FRGS 59474 (FRGS/1/2017/ STG01/UMT/ 03/1) and Universiti Malaysia Terengganu for facilities and support.

References

- Johnson, A. C., Dumont, E., Williams, R. J., Oldenkamp, R., Cisowska, I. and Sumpter, J. P. (2013). Do concentrations of ethinylestradiol, estradiol, and diclofenac in European rivers exceed proposed EU environmental quality standards? Environmental Science & Technology, 47(21): 12297-12304.

- Mills, M. R., Arias-Salazar, K., Baynes, A., Shen, L. Q., Churchley, J., Beresford, N., Gayathri, C., Gil, R. R., Kanda, R., Jobling, S. and Collins, T. J. (2015). Removal of ecotoxicity of 17α-ethinylestradiol using TAML/peroxide water treatment. Scientific Reports, 5: 10511.

- Liu, Z. H., Lu, G. N., Yin, H., Dang, Z. and Rittmann, B. (2015). Removal of natural estrogens and their conjugates in municipal wastewater treatment plants: A critical review. Environmental Science & Technology, 49(9): 5288-5300.

- Kostich, M., Flick, R. and Martinson, J. (2013). Comparing predicted estrogen concentrations with measurements in US waters. Environmental Pollution, 178: 271-277.

- De Mes, T., Zeeman, G. and Lettinga, G. (2005). Occurrence and fate of estrone, 17β-estradiol and 17α-ethynylestradiol in STPs for domestic wastewater. Reviews in Environmental Science and Biotechnology, 4(4): 275.

- Lim, Y. L., Morad, N., Lalung, J., Chan, S. Y. and Bakar, S. A. A. (2016). Isolation and identification of 17α-ethinylestradiol-degrading bacterial strains from POME and cow dung. International Journal of Environmental Science and Development, 7(12): 881.

- Desbrow, C. E. J. R., Routledge, E. J., Brighty, G. C., Sumpter, J. P. and Waldock, M. (1998). Identification of estrogenic chemicals in STW effluent. 1. Chemical fractionation and in vitro biological screening. Environmental Science & Technology, 32(11): 1549-1558.

- Körner, W., Spengler, P., Bolz, U., Schuller, W., Hanf, V. and Metzger, J. W. (2001). Substances with estrogenic activity in effluents of sewage treatment plants in southwestern Germany. 2. biological analysis. Environmental Toxicology and Chemistry: An International Journal, 20(10): 2142-2151.

- Snyder, S. A., Villeneuve, D. L., Snyder, E. M. and Giesy, J. P. (2001). Identification and quantification of estrogen receptor agonists in wastewater effluents. Environmental Science & Technology, 35(18): 3620-3625.

- Hultman, M. T., Song, Y. and Tollefsen, K. E. (2015). 17α-ethinylestradiol (EE2) effect on global gene expression in primary rainbow trout (Oncorhynchus mykiss) hepatocytes. Aquatic Toxicology, 169: 90-104.

- Snyder, S. A., Westerhoff, P., Yoon, Y. and Sedlak, D. L. (2003). Pharmaceuticals, personal care products, and endocrine disruptors in water: Implications for the water industry. Environmental Engineering Science, 20(5): 449-469.

- Scala-Benuzzi, M. L., Takara, E. A., Alderete, M., Soler-Illia, G. J., Schneider, R. J., Raba, J. and Messina, G. A. (2018). Ethinylestradiol quantification in drinking water sources using a fluorescent paper based immunosensor. Microchemical Journal, 141: 287-293.

- De Wit, M., Keil, D., van der Ven, K., Vandamme, S., Witters, E. and De Coen, W. (2010). An integrated transcriptomic and proteomic approach characterizing estrogenic and metabolic effects of 17α-ethinylestradiol in zebrafish (Danio rerio). General and Comparative Endocrinology, 167(2): 190-201.

- Bhandari, R. K., Deem, S. L., Holliday, D. K., Jandegian, C. M., Kassotis, C. D., Nagel, S. C., Tillitt, D. E., vom Saal, F. S. and Rosenfeld, C. S. (2015). Effects of the environmental estrogenic contaminants bisphenol a and 17α-ethinylestradiol on sexual development and adult behaviors in aquatic wildlife species. General and Comparative Endocrinology, 214: 195-219.

- Caldwell, D. J., Mastrocco, F., Anderson, P. D., Länge, R. and Sumpter, J. P. (2012). Predicted‐no‐effect concentrations for the steroid estrogens estrone, 17β‐estradiol, estriol, and 17α‐ethinylestradiol. Environmental Toxicology and Chemistry, 31(6): 1396-1406.

- Jobling, S., Coey, S., Whitmore, J. G., Kime, D. E., Van Look, K. J. W., McAllister, B. G., Beresford, N., Henshaw, A. C., Brighty, G., Tyler, C. R. and Sumpter, J. P. (2002). Wild intersex roach (Rutilus rutilus) have reduced fertility. Biology of Reproduction, 67(2): 515-524.

- Harris, C. A., Hamilton, P. B., Runnalls, T. J., Vinciotti, V., Henshaw, A., Hodgson, D., Coe, T. S., Jobling, S., Tyler, C. R. and Sumpter, J. P. (2010). The consequences of feminization in breeding groups of wild fish. Environmental Health Perspectives, 119(3): 306-311.

- Jobling, S., Williams, R., Johnson, A., Taylor, A., Gross-Sorokin, M., Nolan, M., Tyler, C.R., van Aerle, R., Santos, E. and Brighty, G. (2005). Predicted exposures to steroid estrogens in UK rivers correlate with widespread sexual disruption in wild fish populations. Environmental Health Perspectives, 114 (Suppl 1): 32-39.

- Shen, L. Q., Beach, E. S., Xiang, Y., Tshudy, D. J., Khanina, N., Horwitz, C. P., Bier, M.E. and Collins, T. J. (2011). Rapid, biomimetic degradation in water of the persistent drug sertraline by TAML catalysts and hydrogen peroxide. Environmental Science & Technology, 45(18): 7882-7887.

- Gupta, S. S., Stadler, M., Noser, C. A., Ghosh, A., Steinhoff, B., Lenoir, D., Horwitz, C. P., Schramm, K.W. and Collins, T. J. (2002). Rapid total destruction of chlorophenols by activated hydrogen peroxide. Science, 296(5566): 326-328.

- Kundu, S., Chanda, A., Khetan, S. K., Ryabov, A. D. and Collins, T. J. (2013). TAML activator/peroxide-catalyzed facile oxidative degradation of the persistent explosives trinitrotoluene and trinitrobenzene in micellar solutions. Environmental Science & Technology, 47(10): 5319-5326.

- Länge, R., Hutchinson, T. H., Croudace, C. P., Siegmund, F., Schweinfurth, H., Hampe, P., Panter, G.H. and Sumpter, J. P. (2001). Effects of the synthetic estrogen 17α‐ethinylestradiol on the life‐cycle of the fathead minnow (Pimephales promelas). Environmental Toxicology and Chemistry: An International Journal, 20(6): 1216-1227.

- Shappell, N. W., Vrabel, M. A., Madsen, P. J., Harrington, G., Billey, L. O., Hakk, H., Larsen, G. L., Beach, E. S., Horwitz, C. P., Ro, K.  and Hunt, P. G. (2008). Destruction of estrogens using Fe-TAML/peroxide catalysis. Environmental Science & Technology, 42(4): 1296-1300.

- George, P. (1953). The chemical nature of the second hydrogen peroxide compound formed by cytochrome C peroxidase and horseradish peroxidase. Titration with reducing agents. Biochemical Journal, 54(2): 267.

- Ellis, W. C., Tran, C. T., Roy, R., Rusten, M., Fischer, A., Ryabov, A. D., Blumberg, B. and Collins, T. J. (2010). Designing green oxidation catalysts for purifying environmental waters. Journal of the American Chemical Society, 132(28): 9774-9781.

- Alum, A., Yoon, Y., Westerhoff, P. and Abbaszadegan, M. (2004). Oxidation of bisphenol A, 17β‐estradiol, and 17α‐ethynyl estradiol and byproduct estrogenicity. Environmental Toxicology: An International Journal, 19(3): 257-264.

- Balsiger, H. A., de la Torre, R., Lee, W.-Y. and Cox, M. B. (2010). A four-hour yeast bioassay for the direct measure of estrogenic activity in wastewater without sample extraction, concentration, or sterilization. Science of The Total Environment. 408(6): 1422-1429.

- Barr, W. J., Yi, T., Aga, D., Acevedo, O. and Harper, W. F. (2011). Using electronic theory to identify metabolites present in 17α-ethinylestradiol biotransformation pathways. Environmental Science & Technology, 46(2): 760-768.

- Boone, A. J., Chang, C. H., Greene, S. N., Herz, T. and Richards, N. G. J. (2003). Modeling the spin-dependent properties of open-shell Fe(III) - containing systems: towards a computational description of nitrile hydratase. Coordination Chemistry Reviews 238, 291-314.

- Alexandre, M. and Dubois, P. (2000). Polymer-layered silicate nanocomposites: preparation, properties and uses of a new class of materials. Materials Science and Engineering: Reports, 28(1-2): 1-63.

- Strawhecker, K. E. and Manias, E. (2000). Structure and properties of poly(vinyl alcohol)/Na+ montmorillonite nanocomposites. Chemistry of Materials, 12(10): 2943-2949.

- Koo, C. M., Ham, H. T., Choi, M. H., Kim, S. O. and Chung, I. J. (2003). Characteristics of polyvinylpyrrolidone-layered silicate nanocomposites prepared by attrition ball milling. Polymer, 44(3): 681-689.

- Giannelis, E. P. (1996). Polymer layered silicate nanocomposites. Advanced Materials, 8(1): 29-35.

- LeBaron, P. C., Wang, Z. and Pinnavaia, T. J. (1999). Polymer-layered silicate nanocomposites: An overview. Applied Clay Science, 15(1-2): 11-29.

- Messersmith, P. B. and Giannelis, E. P. (1995). Synthesis and barrier properties of poly (ε‐caprolactone) ‐layered silicate nanocomposites. Journal of Polymer Science Part A: Polymer Chemistry, 33(7): 1047-1057.

- Yano, K., Usuki, A. and Okada, A. (1997). Synthesis and properties of polyimide‐clay hybrid films. Journal of Polymer Science Part A: Polymer Chemistry, 35(11): 2289-2294.

- Ke, Z. and Yongping, B. (2005). Improve the gas barrier property of PET film with montmorillonite by in situ interlayer polymerization. Materials Letters, 59(27): 3348-3351.

- Mosmann, T. (1983). Rapid colorimetric assay for cellular growth and survival: application to proliferation and cytotoxicity assays. Journal of Immunological Methods, 65(1-2): 55-63.