Malaysian Journal of Analytical Sciences Vol 24 No 3 (2020): 436 - 448

GREEN SYNTHESIZED COPPER NANOPARTICLES FROM Blumea balsamifera LINN. LEAVES AND ITS BIOCIDAL ACTIVITIES AGAINST Bactrocera dorsalis (HENDEL)

(Sintesis Hijau Nanopartikel Kuprum dari Daun Blumea balsamifera Linn dan Aktiviti Biosida Melawan Bactrocera dorsalis (Hendel))

# Danila S. Paragas 1,2*, Kathlia D.C. Cruz1, and Elaida R. Fiegalan3

1School of Chemical, Biological and Materials Engineering and Sciences,

Mapua University, Intramuros, Manila, Philippines

# 2Department of Chemistry, College of Arts and Sciences,

# Central Luzon State University, Science City of Muñoz, Nueva Ecija, Philippines

# 3Department of Crop Protection, College of Agriculture,

# Central Luzon State University, Science City of Muñoz, Nueva Ecija, Philippines

# *Corresponding author:  danilaparagas1010@clsu.edu.ph

Received: 20 November 2019; Accepted: 16 April 2020; Published:  9 June 2020

Abstract

The biocidal components of sambong (Blumea balsamifera) leaves against oriental fruit fly, Bactrocera dorsalis (Hendel) (Diptera: Tephritidae), were extracted using four green solvents, namely rice wine, rice wash, apple cider vinegar, and distilled water employing hot infusion, maceration, fermentation, and Soxhlet methods. These extracts were used in the synthesis of copper nanoparticles (CuNPs). The suspensions of nanoparticles were centrifuged, and the aggregates were separated and dried. The dried aggregates and colloidal suspensions of copper nanoparticles were tested on male adult oriental fruit flies. Improvised olfactometer was used to determine the adulticidal activities of the nanoparticles. Both dried aggregates and colloidal suspensions had varying effects on the mortality rates of fruit flies, which ranged from 25-100% within 12 hours exposure. However, dried aggregates yielded higher mortality rates than those of the colloidal suspensions. The researchers concluded that sambong can be used in the preparation of nanoparticle-enhanced biocide either as suspension concentrate or dust or powder with suitable sorption material. Ultimately, sambong can be considered as an alternative in managing the oriental fruit fly.

# Keywords:  biocide, Blumea balsamifera, nanoparticle, nanosuspension, oriental fruit fly

# Abstrak

Komponen biosida bagi daun sambong (Blumea balsamifera) melawan lalat buat oriental, Bactrocera dorsalis (Hendel) (Diptera: Tephritidae), telah diekstrak menggunakan empat pelarut hijau iaitu wain beras, basuhan beras, cuka epal, dan air suling berdasarkan keadah infusi panas, maserasi, penapaian dan Soxhlet. Pengestrakan ini digunakan dalam sistesis nanopartikel kuprum (CuNPs). Nanopartikel terampai telah diempar, dan gumpalan telah diasing dan dikeringkan. Gumpalan kering dan ampaian koloid bagi nanopartikel kuprum telah diuji terhadap lalat buah oriental jantan dewasa. Olfactometer telah digunapakai dalam penentuan aktiviti pendewasaan lalat terhadap nanopartikel. Gumpalan kering dan ampaian koloid, keduanya menghasilkan kesan yang berbeza terhadap kadar kematian lalat buah, iaitu julat 25-100% dalam tempoh 12 jam pendedahan. Walau bagaimanapun, gumpalan kering menghasilkan kadar kematian yang lebih tinggi berbanding ampaian koloid. Penyelidik membuat kesimpulan bahawa sambong boleh diguna dalam penyediaan nanopartikel-yang diperkaya biosida sama ada ampaian pekat, debu atau serbuk dengan bahan jerapan yang sesuai. Sambong boleh dipertimbangkan sebagai alternatif dalam pengawalan lalat buat oriental.

# Kata kunci:  biosida, Blumea balsamifera, nanopartikel, nanoampaian, lalat buah oriental

References

- Sharpe, R. M. and Irvine, D. S. (2004). How strong is the evidence of a link between environmental chemicals and adverse effects on human reproductive health?. British Medical Journal, 328(7437): 447.

- Pingali, P. L. and Roger, P. A. (2012). Impact of pesticides on farmer health and the rice environment (Vol. 7). Springer Science & Business Media.

- Mahmood, I., Imadi, S. R., Shazadi, K., Gul, A. and Hakeem, K. R. (2016). Effects of pesticides on environment. In Plant, soil, and microbes. Springer: pp. 253-269.

- Tubbs, C. W. and McDonough, C. E. (2018). Reproductive impacts of endocrine-disrupting chemicals on wildlife species: implications for conservation of endangered species. Annual Review of Animal Biosciences, 6: 287-304.

- Ndakidemi, B., Mtei, K. and Ndakidemi, P. A. (2016). Impacts of synthetic and botanical pesticides on beneficial insects. Agricultural Sciences, 7(06): 364.

- Gupta, S. and Dikshit, A. K. (2010). Biopesticides: an ecofriendly approach for pest control. Journal of Biopesticides, 3(1): 186-188.

- Thakore, Y. (2006). The biopesticide market for global agricultural use. Industrial Biotechnology, 2(3):194-208.

- Lichtfouse, E. (2013). Sustainable agriculture reviews (Vol. 13). Springer Science & Business Media.

- Pang, Y., Wang, D., Fan, Z., Chen, X., Yu, F., Hu, X., and Yuan, L. (2014). Blumea balsamifera - A phytochemical and pharmacological review. Molecules, 19(7): 9453-9477.

- Yuan, N. N., Hou, H. Y., Wang, J., Chen, Y. Z. and Xie, P. B. (2012). The research status of chemical constituents and activities of Blumea DC. [J]. Guangzhou Chemical Industry, 24: 015.

- Nessa, F., Ismail, Z., Mohamed, N. and Haris, M. R. H. M. (2004). Free radical-scavenging activity of organic extracts and of pure flavonoids of Blumea balsamifera DC leaves. Food Chemistry, 88(2): 243-252.

- Pang, Y., Wang, D., Hu, X., Wang, H., Fu, W., Fan, Z. and Yu, F. (2014). Effect of volatile oil from Blumea balsamifera (L.) DC. leaves on wound healing in mice. Journal of Traditional Chinese Medicine, 34(6): 716-724.

- Sivapragasam, A. (2009). Biopesticides from Malaysian flora–resources for sustainable pest management. In Discovering opportunities, expanding the economic horizon. Proceedings of the National Conference on New Crops and Bioresources, Seremban, Malaysia, 15–17 December 2009: pp. 125-132.

- Glova III, F. and Ines, M. C. (1989). Evaluation of selected botanical pesticides against rice green leafhopper Nephotettix virescens. In Pest Control Council of the Philippines, Baguio City (Philippines), 9–12 May 1989.

- Ines, M. C. and Baga, L. P. N. (1990). Evaluation of botanical pesticides against Fusarium rot of garlic. In 21. Pest Control Council of the Philippines Annual Convention, Bacolod City (Philippines), 7–10 May 1990.

- Suharto, H. (2002). Golden apple snail, Pomacea canaliculata (Lamarck) in Indonesia. Los Banos, Laguna, SEAMEO Regional Center for Graduate Study and Research in Agriculture (SEARCA), Philippines, 69–73.

- Sebastian, L. S. (2003). Management options for the golden apple snail.  Access from http://issg.org/database/species/reference_files/pomcan/pest_management.pdf. [Access online 05 December 2017].

- Harne, S., Sharma, A., Dhaygude, M., Joglekar, S., Kodam, K. and Hudlikar, M. (2012). Novel route for rapid biosynthesis of copper nanoparticles using aqueous extract of Calotropis procera L. latex and their cytotoxicity on tumor cells. Colloids and Surfaces B: Biointerfaces, 95: 284-288.

- Abbott, W. S. (1978). A method of computing the effectiveness of an insecticide. Journal of the American Mosquito Control Association, 3(2):302-303.

- Cha, D. H., Adams, T., Werle, C. T., Sampson, B. J., Adamczyk, J. J., Jr., Rogg, H. and Landolt, P. J. (2014). A four-component synthetic attractant for Drosophila suzukii (Diptera: Drosophilidae) isolated from fermented bait headspace. Pest Management Science, 70: 324-331.

- Wilkinson, C. F. (1976). Insecticide biochemistry and physiology. Plenum Press.

- Griffitt, R. J., Weil, R., Hyndman, K. A., Denslow, N. D., Powers, K., Taylor, D. and Barber, D. S. (2007). Exposure to copper nanoparticles causes gill injury and acute lethality in zebrafish (Danio rerio). Environmental Science & Technology, 41(23): 8178-8186.

- Ragaei, M. and Sabry, A. K. H. (2014). Nanotechnology for insect pest control. International Journal of Science, Environment And Technology, 3(2): 528-545.

- Singh, A. K. (2015). Engineered nanoparticles: Structure, properties, and mechanisms of toxicity. Academic Press.